# Supplementary material

# Synthesis of Iron Oxide/Activated Hydrochar Composite from Residual Brewery Biomass for Remediation of Water Contaminated with Chlorophenol

Matías Kopp a, Pedro Anabalón a, Sebastián Rocha c, María Eugenia González b, Juan Miguel Romero-García d, Eulogio Castro d, and Mara Cea b, *

aDoctorate in Engineering Sciences with Specialization in Bioprocess, Chemical Engineering Department, Universidad de La Frontera, Francisco Salazar 01145, Temuco, Chile.

bChemical Engineering Department, Universidad de La Frontera, Francisco Salazar 01145, Temuco 4780000, Chile.

cSchool of Engineering, Faculty of Sciences, Engineering and Technology, Universidad Mayor, Chile

dDepartment of Chemical, Environmental and Materials Engineering; Biorefinery Research Institute(I3B), University of Jaén, Campus Las Lagunillas s/n, 23071, Jaén, Spain

* Corresponding author, E-mail: mara.cea@ufrontera.cl.

### S.1 Materials and methods

## Instrumental characterization of carbonous material

Various characterization techniques were employed to examine the properties of the materials. Fourier Transform Infrared Spectroscopy (FTIR) was conducted using a Cary 630 FTIR (Agilent Technologies, USA) to identify the chemical functional groups present on the surface of the materials. The scanning range for the samples was 4000-600 cm-1. The superficial area and pore structure were analyzed by performing N2 adsorption-desorption isotherms at 77 K using a Nova 1000e analyzer (Quantachrome Instruments, USA). Prior to the adsorption measurements, the samples were subjected to degassing at 180 °C for 16 hours. The morphological characteristics of the materials were examined using scanning electron microscopy (SEM) SU-3500 (Hitachi, Japan) at an acceleration voltage of 10 kV, and their elemental composition was determined using energy dispersive X-ray spectroscopy (EDS). The crystal structure of the synthesized iron oxide/activated hydrochar composites was investigated through X-ray diffraction (XRD) analysis. XRD measurements were performed using a SmartLab X-ray Diffractometer (Rigaku, Japan) with a Cu tube (λ = 1.54184 Å) and a sampling increment of 0.01° within the range of 5 to 55°. The chemical composition of the materials (CHNS) was determined using an elemental analyzer EA3000 (Eurovector, Italy), while the inorganic composition of the materials was analyzed by total reflection X-ray fluorescence (TXRF) in a Bruker S4 T-Star (Bruker, Germany) spectrometer. Analysis was carried out on 30 mm quartz discs with Mo-K excitation of 17.5 keV. To determine the ash content Thermogravimetric analysis (TGA) of materials was performed in a PerkinElmer STAR 6000 thermogravimetric balance under N2 atmosphere (50 mL/min) from 30 to 900 °C and a heating rate of 10 °C/min. Finally, the isoelectric point (pHIEP) of the samples was determined using a Zetasizer Nano ZS equipment (Malvern Instruments, Ltd.). For this measurement, suspensions containing 0.025 g (Ø = 10-20 µm) of solid in 20 mL of deionized water were used.

## 2-chlorophenol (2-CP) quantification

The aqueous concentrations of 2-CP underwent analysis using high-performance liquid chromatography (HPLC) instrument (Jasco, Japan) equipped with an analytical C18 reversed-phase (RP) column, Inertsil ODS-4, 5 µm, 250 x 4.6 mm (Gl Science, Japan). The mobile phase consisted in an isocratic elution using a mixture of acetonitrile and 1% phosphoric acid in a ratio of 1:1 (v/v), flowing at a rate of 1 mL/min, and an automatic injection of 20 µL, while the loop volume was 100 µL. During the analysis, the column temperature was maintained at 35 °C, while the analytical wavelength was set at 274 nm. For quantification, an external standard calibration plot was constructed within the range of experimental concentrations employed.