Supplementary information

Stachys tibetica derived silver nanoparticles: A robust multifunctional material for enhanced biological activity and photocatalytic properties

Naseer Ahmad Dar, Parvaiz A Dar, Mahpara qadir, and Wajaht A. Shaha*

aDepartment of Chemistry, University of Kashmir, Hazratbal, Srinagar, 190006, Jammu and Kashmir`, India,

*Corresponding Author: Prof. Syed Wajaht Amin Shah

Department of Chemistry, University of Kashmir, Hazratbal, Srinagar 190006, Jammu and Kashmir, India,

E-mail: doctorwajaht@gmail.com  Tel: +919419054484/ +917006191306

C K_ROI (5)                                                                          N K_ROI (3)

|  | O K_ROI (5) |
| --- | --- |

Cl K_ROI (10)

Ag l ROI (12)

S1. Elemental mapping images of Carbon,Nitrogen,Oxygen,Silver and chlorine.

| Element | Weight % | MDL | Atomic % | Net Int. | Error % | R | A | F |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C K | 34.7 | 0.59 | 67.7 | 168.8 | 11.3 | 0.8238 | 0.0888 | 1.0000 |  |
| N K | 0.7 | 0.74 | 1.2 | 3.3 | 64.2 | 0.8318 | 0.0423 | 1.0000 |  |
| O K | 10.6 | 0.55 | 15.5 | 77.2 | 12.8 | 0.8384 | 0.0518 | 1.0000 |  |
| Cl K | 8.9 | 0.10 | 5.9 | 722.1 | 3.7 | 0.8860 | 0.8087 | 1.0475 |  |
| Ag L | 45.1 | 0.23 | 9.8 | 1250.9 | 3.3 | 0.8931 | 0.8164 | 1.0036 |  |
| S2. EDAX results of AgNp and quantitave results. |  |  |  |  |  |  |  |  |  |  |

S3. Radical scavenging activity of AgNp , Plant extract and ascorbic acid(results presented as average of three readings)

| Sample | Concentration(µg/ml) | % inhibition |
| --- | --- | --- |
| 1.AgNp | 25 | 34.5 |
|  | 50 | 36.2 |
|  | 100 | 48.2 |
|  | 150 | 51.7 |
|  | 200 | 67.2 |
|  | 250 | 82.7 |
|  | 300 | 84.4 |
|  | 350 | 89.6 |
| 2.Plant Extract | 25 | 8 |
|  | 50 | 17.2 |
|  | 100 | 27.2 |
|  | 150 | 31 |
|  | 200 | 34.4 |
|  | 250 | 48.9 |
|  | 300 | 51.3 |
|  | 350 | 62 |
| 4. Ascorbic Acid | 25 | 32.4 |
|  | 50 | 44.6 |
|  | 100 | 62 |
|  | 150 | 63.7 |
|  | 200 | 68.4 |
|  | 250 | 70.6 |
|  | 300 | 72.4 |
|  | 350 | 75.8 |

S4: (a and b) represent MIC determination of E.Coli(G-) and S. Aeureus (G +) bacteria.

| S5. Antibacterial properties of AgNp(Stachys Tibetica) using Agar well diffusion method. |  |  |  |  |
| --- | --- | --- | --- | --- |
|  | Percentage(%) inhibition(Average+SD) |  |  |  |
|  | AgNp | Plant Extract | Positive control (Streptomycin) | Negative Control(DMSO) |
| Bacillus Cereus | 12.1±1 | 2±1 | 23.9±1 | 0±0 |
| Pseudomonas | 11.8±1 | 1±1 | 20.8±1 | 0±0 |
| Escherichia coli | 9.8±1 | 4±1 | 20.9±1 | 0±0 |
| S.Aeureus | 7.2±1 | 5±1 | 10.1±1 | 0±0 |

(a)  antibacterial activity of B. Cereus

(b)  antibacterial activity of Pseudomonas

(d)  antibacterial activity of E.Coli

(e)  antibacterial activity of S.Aeureus