Serial chemical crystallography for autonomous quantitative phase analysis in an electron microscope

Taimin Yanga,b,*, David Geoffrey Watermanc,d, Zheting Chua,  James Beilsten-Edmandse, Zhehao Huanga,f, Xiaodong Zoua

a Department of Materials and Environmental Chemistry (MMK), Stockholm University, Svante Arrhenius väg 16C, Stockholm, SE-10691, Sweden

b Department of Physics and Astronomy, University of California, Irvine, California 92697, United States

c STFC, Rutherford Appleton Laboratory, Didcot OX11 0FA, UK

d Research Complex at Harwell, Rutherford Appleton Laboratory, Didcot OX11 0FA, UK

e Diamond Light Source Ltd, Harwell Science and Innovation Campus, Didcot OX11 0DE, UK

f Electron Microscopy Center, School of Emergent Soft Matter, South China University of Technology, 510640 Guangzhou, China

* Corresponding email: taimin.yang@mmk.su.se

Table of Contents		  							               Page

1. Supplementary Methods	4

1.1 Sample preparation	4

1.2 Instruments	4

1.3 Software setup	5

2. Supplementary Text	5

2.1 Instructions for data collection	5

2.2 Instructions for data processing	8

Reference	33

List of Tables and Figures

Figure S 1. Graphical user interfaces for (a) preparing t-SerialED experiment (b) executing t-SerialED experiment	10

Figure S 2 Illustration of the hardware and software setup for t-SerialED	11

Figure S 3. Process for eucentric height prediction of the whole grid from measured eucentric heights at positions marked with ‘+’. The prediction plot shows the grid is curved and a photo of the loaded grid confirms the grid is indeed curved.	11

Figure S 4 Schematics for eucentric height determination	12

Figure S 5 Schematics of automatic crystal finding. The area selection procedure allows for both automatic selection and manual adjustment. The radius of the scan area needs to be input by the user and it will be divided into a number of patches according to the desired magnification for crystal searching. The stage will move to the center of patches and take images and identify crystals. It is possible to take all the crystals that appear on each image. It is also possible to add conditions to filter out ideal targets. For instance, collect those targets that are not aggregate or not close to the edge of the image.	12

Figure S 6. Flowchart of preparation and data acquisition of t-SerialED datasets. At low mag level, the magnification is set to 110. The target grid squares will be identified from the atlas. At medium mag level, eucentric height will be measured at several places and the rest will be predicted. At high mag level, the microscope is always operated in diffraction mode. When taking images, diffraction defocus will be applied to show a Ronchigram with the same length scale when the microscope is operated in SA 7500.	13

Figure S 7. Target picking for isolated particles and aggregated particles. Spread parameter is the minimum separation between the targets. For isolated particles	14

Figure S 8. Target picking for aggregated particles and large blocks.  (a) For aggregated particles, the density of the target spots depends on the user-defined beam size. If the beam hits two or three particles at the same time, the indexing algorithm in DIALS is still able to distinguish each set of lattices.  (b, c, d) For large blocks, the algorithm will identify the edge of a large block and put red target spots along the edge according to the user-defined density.	14

Figure S 9. Flowchart of data processing of t-SerialED datasets	15

Figure S 10. An example of the restrain.phil file	15

Figure S 11 Typical t-SerialED datasets that can be indexed: (a) one crystal (b) two crystals (c) three crystals (d) low resolution, one crystal	16

Figure S 12 Typical t-SerialED datasets that are not indexable during data processing: (a) blocked (b) amorphous or blank (c) polycrystalline.	16

Figure S 13 Reconstructed 3D reciprocal space of an individual tilt series for MOF-235. Space group can be determined by checking the systematic absence of reflections. Reciprocal space viewed along: (a). a*-axis (b). b*-axis (c). c*-axis. (d). (hh-2hl) plane sliced from 3D reciprocal space in red.	17

Figure S 14 Photos of the (a) tablet, (b) capsule and (c) pellet. (d) The overall morphology of the Fe Supplement sample. After crushed in mortar, the shapes of the ingredients are irregular.	17

Figure S 15 CC1/2 plot to show the data quality. (a) Glycine (b) L-ascorbic acid (c) Zn acetate (d) Saccharin (e) Mg acetate (f) L-glutamic acid	18

Figure S 16 3D reciprocal space reconstructed from an individual dataset from paracetamol	19

Figure S 17 Crystal packing of paracetamol, hydrogen bonding network in the crystal and electron static potential map for the molecule	19

Figure S 18 3D reciprocal space reconstructed from an individual dataset from ferrous glycine complex.	20

Figure S 19 Atomic arrangement of ferrous glycine complex viewed from different directions.	20

Figure S 20 Coordination environment of two independent Fe atoms	21

Figure S 21 Histogram of number of indexed reflections. (a) Paracetamol (b) Fe supplement. Horizontal label represents the number of indexed reflections while vertical label is the frequency.	21

Figure S 22 (a) Magnified Rietveld refinement results within 2θ range of 8° to 14°. (b) Simulated PXRD for 2θ range of 8° to 14°, demonstrating the peaks located at 10.9° and 13.4° are the strong peaks.	22

Figure S 23 Overview of t-SerialED data processing workflow.	22

Table S 1 Statistics from data acquisition for MOF-235 and the mixture. The unindexable datasets include typical amorphous ED patterns, blocked ED patterns and polycrystalline ED patterns.	23

Table S 2 Ingredient composition in paracetamol tablet and Fe supplement capsule. The unindexed datasets include typical amorphous ED patterns, blocked ED patterns and polycrystalline ED patterns.	24

Table S 3. Summary for acquisition time and accumulated dose for different collection frames. The overhead time is the extra time required when the detector is not acquiring frames, including the time for locating crystals, adjusting eucentric height, switching states, rotating the stage, moving the beam, and translating the stage.	25

Table S 4. Comparison of the throughput of t-SerialED with previously reported methods based on electron diffraction. Note that the speed calculation does not include the time for preparing the experiment.	25

Table S 5 Data processing statistics of MOF-235 using CrystFEL	26

Table S 6 Data processing statistics of MOF-235 using DIALS	26

Table S 7 Data refinement statistics for MOF-235 datasets processed by CrystFEL and DIALS. The Rint in the dataset processed by CrystFEL is unknown because CrystFEL outputs a merged SHELX HKL files.	27

Table S 8 Input composition and number of crystals identified in the mixture	28

Table S 9 Data processing statistics for the mixture	28

Table S 10 Structure refinement statistics for the mixture	29

Table S 11 Summary of the phase analysis results of the crystalline contents in paracetamol tablet and iron supplement capsule using t-SerialED and PXRD. All the ratios displayed in the table are calculated without considering the amorphous contents.	30

Table S 12 Data processing statistics for paracetamol	31

Table S 13 Data statistics of the refinement results of paracetamol	31

Table S 14 Comparison of data processing statistics of with different threshold for data selection of ferrous glycine datasets	32

Table S 15 Comparison of data refinement statistics of with different threshold for data selection of ferrous glycine complex	32

1. Supplementary Methods

1.1 Sample preparation

MOF synthesis: Terephthalic acid (98%, Thermo Scientific), iron (III) chloride hexahydrate (98%, Thermo Scientific), and dimethylformamide (DMF, 99.8%, VWR chemical). The MOF sample was prepared following a modified method of a previously described procedure1. Terephthalic acid (3 mmol) was dissolved in 15 mL of DMF. Thereafter, an equivalent amount of iron (III) chloride hexahydrate (3 mmol) was dissolved in the terephthalic acid/DMF solution. The solution was then transferred to a reactor (reactor volume: 15 mL) that was equipped with an ultrasonic generator probe (VCX150, Sonics & Materials, Inc.). The device was set to continuous mode. This experiment was performed at 60% of the maximum power for 2h. The phase analysis results are listed in Table S 1.

Complex Mixture: The compounds were carefully weighed by an analytical balance (VWR) and then crushed into fine powder by a mortar. The mixture was prepared as by mixing the following 6 compounds: glycine (99%, Sigma Aldrich), L-ascorbic acid (99%, VWR chemical), Zn acetate (98%, Sigma Aldrich), saccharin (99%, Merck), Mg acetate (98%, VWR chemical), L-glutamic acid (99%, Sigma Aldrich). The input weight is set to 50mg for each compound. Other properties and phase analysis results are listed in Table S 1 and Table S 8.

Pharmaceuticals: Paracetamol tablets (Alvedon, API: 500mg, total: 590mg), Fe supplements capsule (Niferex, API: 567mg, total: 703mg) were purchased from a local pharmacy. The total weight of the medicine was measured by an analytical balance. The weight of API is documented in the manual while the weight of non-API is unknown. The API and non-API contents are obtained from the Swedish Medical Products Agency, as shown in Table S 2.

1.2 Instruments

TEM: All the datasets were obtained on a Thermo Fisher Scientific (TFS) Themis-Z electron microscope operated at 300kV with a 4096 × 4096 pixels Gatan Oneview CMOS detector (15 × 15μm pixel size) and a 512 × 512 pixels ASI Medipix 3 hybrid pixel detector (55 × 55 μm pixel size). The microscope was operated in diffraction mode during the whole data acquisition process. A monochromator was used to adjust the electrons drawn from the Schottky type electron gun (X-FEG). The exposure time was set to 0.25s and 0.5s for each imaging frame and ED frame, respectively. During t-SerialED data collection, the tilt range of each crystal was from -36° to +36°. Within the tilt range, the number of still frames taken for each crystal at different angles was set to 7, 25 or 49 and the angle interval of neighboring frames was 12.0°, 3.0° and 1.5°, respectively. When collecting ED frames, the beam size was set to 900 nm and the total current of the beam is 2pA, leading to 0.15 e / Å2 s-1 in dose rate. When collecting search images, the beam diameter was set to 8000 nm and the total current is 5pA, resulting in a dose rate of 0.005 e / Å2 s-1. The accumulated dose is depending on the number of frames collected for each crystal, as listed in Table S 3. Collecting more frames for each crystal can obtain more reflections, increasing the accuracy in unit cell determination and the chance to successfully index a multicrystal dataset. However, a larger number of frames means higher dose and data acquisition time. Therefore, in all the experiments, we chose 25 frames per crystal to achieve relative accurate indexing and short data acquisition time. The total acquisition time per crystal was 20.5s including the overhead time. The overhead time includes crystal finding, adjusting eucentric height, switching modes, moving the beam, rotating the stage and translating the stage. As shown in Table S 4, compared with other existing methods, our approach reduces the overheads and makes sure more than 60% of the time and more than 99% of the total dose is spent on collecting ED patterns, making the method time-saving and dose-efficient.

For MIL-88 samples, the t-SerialED experiments were conducted under room temperature condition using a Fischione model 2020 tomography holder. For the other samples, the t-SerialED experiments were conducted under cryogenic temperature (95K) using a high-tilt cryo-transfer holder (Gatan, Model 932).

PXRD: PXRD patterns were recorded using a Bruker D8 Discover X-ray diffractometer (Bruker, UK), using Cu Kα radiation (λ = 1.54184 Å) in 40 kV and 40 mA conditions. Glass capillaries were used to load the sample. The diffractometer collected data from 5° to 60° (2θ) with a scanning speed of 0.2°/min (paracetamol) and 0.033°/min (Fe supplement) at room temperature using Debye-Scherrer geometry. The total data collection time was 5h (paracetamol) and 28h (Fe supplement). Rietveld refinement was performed to analyze the crystalline contents in the paracetamol tablets and iron supplement capsule.

1.3 Software setup

Instamatic: Instamatic is a Python package that is being developed with the aim to automate the collection of electron diffraction data. At the core is a Python library for transmission electron microscope experimental control for the microscopes and interfaces to the detectors. Workflows have been implemented for multiple TEM experiments, including calibration and execution of t-SerialED experiments. The graphical user interface of both calibration and execution of t-SerialED are shown in Figure S 1. The overall architect of the hardware and software is shown in Figure S 2. The software controls the microscope through FEI TEM scripting interface and TCP/IP protocol is used for transferring the command from the detector computer to the microscope computer. The source code of the Instamatic package is available at https://github.com/instamatic-dev/ilnstamatic. The hardware and software requirements for installation and running of Instamatic are described in the readme.md file (https://github.com/instamatic-dev/instamatic/blob/master/readme.md). Documentation of the Instamatic package is available at https://instamatic.readthedocs.io, where more details of the program, setting up Instamatic, examples of running Instamatic for data collection, API reference, etc., are presented.

edtools: Edtools is a python package of a collection of tools for automated processing of t-SerialED datasets. The source code of edtools is available at https://github.com/instamatic-dev/edtools. The requirements for installation and running edtools are given in the readme.md file (https://github.com/instamatic-dev/edtools/blob/master/README.md). Documentation of edtools package is available at https://edtools.readthedocs.io, where one can find more details of the program, installation of edtools, a demo of running edtools for automated processing of t-SerialED datasets, API reference, etc. For running edtools, the DIALS package for reduction of t-SerialED datasets is required. The DIALS package is available at https://github.com/dials/dials. The instruction for the installation of the DIALS package can be found at https://dials.github.io/installation.html.

2. Supplementary Text

2.1 Instructions for data collection

Calibration of t-SerialED experiment: Before executing the t-SerialED experiments, the following preparation steps should be taken:

- Set an appropriate camera length, which depends on the highest resolution at the edge of the detector. In our case, the camera length is set to 285 mm and highest resolution at the edge of the detector is 0.78 Å.

- Decide the beam size in viewing mode and diffraction mode. For instance, the diameter of the beam in viewing mode and diffraction mode is set to 8 μm and 900 nm, respectively.

- Find the optimal diffraction defocus to generate an ED pattern with sharp reflections. Then use this diffraction defocus as the zero-point.

- Set an appropriate diffraction defocus value in viewing mode to match the real space pixel size at certain magnification. For instance, the diffraction defocus is set to -19 um and it match the pixel size in SA mode at 7500×

- In diffraction mode, make sure the central spot of the diffraction pattern is located near the center of the detector

- Save the alignment result in the microscope so it can be used next time.

Target finding and eucentric height determination: The coordinates of the targets are determined using a multi-resolution approach (shown in Figure S 3) combined with an automated image analysis procedure, which can be adapted its parameters to the sample of interest:

- Take an image at the lowest magnification. The magnification is set so that a sufficiently large area is covered in one image and no obvious distortion at the edge of the image at the same time. In our case, we use magnification of 100×. Identify the centers of grid holes where the electron beam is not blocked by the copper grid.

- Select several centers located at the edge of the previous low mag image. Change the magnification to the medium magnification (i.e., 1150×). Use stage shift to move the grid so that the center of the first selected grid hole matches the center of the detector.

- The eucentric height of that position is determined from the shift of the image when the stage is tilted to different angles, as shown in Figure S 4. The detailed steps are described in a later section. Stage shift to the next selected grid until the eucentric heights for all selected grid holes are determined.

- Using a prediction algorithm to predict the eucentric height for the rest of the positions on the grid. The prediction results will be used as the coarse eucentric height.

- Then the microscope is switched to defocused diffraction mode, corresponding to high magnification (i.e., 7500×).

- The stage will be moved to the center position of the first grid hole and the fine eucentric height is determined using the same process in step 3. The user can define an area for data collection, which will be divided into a number of blocks depending on the predefined magnification, as shown in Figure S 5. Measurement of the fine eucentric height will only be performed on the first block. The difference between the fine eucentric height and the coarse eucentric height will be calculated and recorded. For the rest of the blocks, the predicted eucentric height is adjusted by the amount of difference.

- The positions of crystals in the image are automatically determined from the contrast in the image. The detailed steps are described in a later section. After all the datasets are collected for all the crystals within the image, the stage will move to the next position according to a designed pattern. The recorded difference will be applied to the coarse eucentric height and the fine eucentric height will be calculated accordingly.

- After the last block in the same grid hole is screened, the stage will be moved to the next grid hole. Step 6 and 7 will be repeated.

t-SerialED data collection: t-SerialED datasets are collected for all crystals within a Ronchigram at high magnification. For each t-SerialED datasets, the total number of frames can be an arbitrary number larger than 1. In our case, we use 7, 25 or 49 frames. The corresponding angle interval between frames is 12°, 3°, 1.5°. With the increase of frames, the sampling of the reciprocal space will be finer and more reflections can be used during geometry refinement. However, longer acquisition time is needed for each dataset. After balancing between efficiency and accuracy, most of the time, 25 frames are collected for each dataset. Figure S 6 demonstrates a flowchart for the data collection process. Below are the detailed procedures:

- The stage is moved to the position according to the designed pattern. The z-height will be adjusted to the measured or calculated fine eucentric height. The microscope will be switched to defocused imaging mode and an image at 0° will be acquired.

- The crystals in the image at 0° will be automatically identified. Then the microscope will be switched to diffraction mode. The electron beam will be moved to each identified crystal using beam shift and an ED pattern will be taken for each crystal.

- Then the quality of ED patterns will be checked using an automatic algorithm in order to check the quality of diffraction. Amorphous particles will not be selected.

- Next, the goniometer is rotated to a high angle. In our case, we set the tilt range to 72° and we start the tilt from -36°. The microscope will be switched to defocused diffraction mode and a Ronchigram will be taken after the tilting.

- The new Ronchigram will be compared with the Ronchigram taken at 0° and calculate the drift between two frames. The updated positions of identified crystals will be predicted based on the model of the grid and goniometer, as shown in section. The electron beam will be moved to each crystal using beam shift and an ED pattern will be acquired.

- Next, the goniometer will be rotated to the next angle. If the angle interval is set to below 10°, then no image will be acquired. The drift of the image compared with the last frame will be predicted and positions of the crystal will be calculated based on the grid and goniometer model. If the angle interval is larger than 10°, then the microscope will be set to defocused diffraction mode and an image of the crystals will be acquired. Then the positions of crystals will be updated accordingly and ED patterns for all crystals will be acquired.

- Do the same procedure in step 6 for the rest of the angles until the stage is rotated to the target angle (i.e. +36°).

Image analysis for target identification: Once a Ronchigram is taken in defocused diffraction mode, the coordinates of the targets are determined from the following image analysis procedure:

- Segment the image using a global thresholding algorithm. The threshold can be determined automatically using Li’s or Ostu’s method.

- A morphological closing operation with a structuring element of a typical minimum size of a single crystal is performed to exclude noise and features that are too small. Then a morphological dilation operation is performed.

- Crystals are often found within aggregates or thicker sample regions, which are registered as a single bright segment. A second round of thresholding and binarization can now be performed on each individual bright segment to locate individual crystals.

- For each segment, the beam position is selected using a k-means clustering approach. The number of clusters is determined by the size of the beam and the area of the segment. Multiple beam positions spaced by approximately the nano-beam diameter can be distributed over the segment using this approach, as shown in Figure S 7 and Figure S 8.

Automatic eucentric height measurement: The eucentric height measurement of a certain position on the grid can be calculated from Equation S 1 using the following procedures.

| defocus=shift÷2÷tanθ-cs*tanθ2 | Equation S 1 |
| --- | --- |

- Rotate the stage to angle -θ (i.e., -5°) and take an image 1

- Rotate the stage to angle +θ (i.e., +5°) and take an image 2

- Compare the shift between the image 1 and 2 and calculate the shift of the objects using cross correlation

- Calculate the defocus value using Equation 1 and move the z height by the calculated defocus value

- At low magnification, repeat steps 1-4 using a larger angle (i.e., 15°) in order to obtain a more accurate eucentric height. At high magnification, this step can be omitted.

2.2 Instructions for data processing

We built an automated data processing pipeline with edtools, which calls DIALS and PETS2. Before running edtools, make sure that all the t-SerialED datasets are put in one folder. A typical cycle of using edtools for processing t-SerialED datasets for phase analysis and structure determination goes through the following steps: 1) edtools.update_dials, 2) edtools.autoindex, 3) edtools.extract_dials_info, 4) edtools.find_cell, and 5) edtools.dials_to_CrystFEL. A step-by-step demonstration of processing t-SerialED datasets is shown as following:

2.2.1 Preparation of data processing

The direct output datasets are in MRC format. All the datasets are expected to be in the DIALS readable image format. In our case, we output SMV data format by specifying --write_smv True. The centers of diffraction patterns are aligned using cross-correlation. If the elliptical distortion is known, then it is also possible to specify the parameters of elliptical distortion and correct before the next step. For accurate unit cell indexing, PETS2 is needed and images in TIFF format are required. By specifying --write_tiff True, images in tiff format can be converted from MRC format.

Command: edtools.update_dials -cent True --write_smv True --write_tiff True --gain 7 --refine_center True --ellip_corr True

2.2.2 Automatic Indexing

For each dataset, edtools.autoindex_dials.exe will find the location of dials_process.bat file, in which dials.import, dials.find_spots and dials.index commands are included. A restrain file can be specified to specify the space group, unit cell, geometry refinement parameters and multi-lattice searching parameters, Figure S 10 is an example of the restrain file. The indexing algorithm from DIALS can not only index high-resolution single crystal datasets but also index high-resolution multi-crystal datasets. As resolution decreases and number of reflections decreases, the ability to resolve the number of multi-crystals in one dataset decreases. Figure S 11 shows typical datasets that are indexable. However, if there are too few reflections or the sample is polycrystalline, the indexing algorithm will fail (Figure S 12)

Command: edtools.autoindex_dials.exe --restrain True

2.2.3 Extract unit cell information

After all the datasets are indexed, edtools.extract_dials_info.exe is used to summarize the result and generate a list of datasets that fits the requirements. The requirements can be if the dataset only contains one lattice or the minimum number of indexed reflections or the percentage of indexed reflections. The purpose of the restraints is evaluation of the quality of indexing and checking if the indexing is reliable. To our experience, if the indexed reflections reach more than 100 and more than 30% of reflections are successfully indexed, then the indexing result is very reliable. The output of this command is a cells.yaml file.

command: edtools.extract_dials_info.exe -t_i 100 -t_p 0.3

2.2.4 Unit-cell-based clustering for phase analysis

After the creation of cells.yaml, it can be read by edtools.find_cells for unit cell clustering. The command will calculate the distance between the obtained unit cells and set up a threshold to cluster unit cells. After the command, it will summarize the result and calculate the mean value for each cluster. For each cluster, a yaml file will be created in which all the unit cells and corresponding datasets will be recorded.

command: edtools.find_cell.exe cells.yaml -c True

2.2.5 Data integration and merging

This command can convert SMV files into HDF5 files with metadata, which is required by diffracttem2 and CrystFEL3. Then diffracttem and CrystFEL can be used to further process the data. This command can also directly use dials.ssx_integrate to integrate all the datasets in cells.yaml and then merge all the frames as if they are individual crystals using xia2.ssx_reduce. The output of the command is a Shelx HKL file and a Shelx INS file, which can be input into Shelxt for structure solution.

command: edtools.dials_to_CrystFEL.exe cells.yaml --merge True --space_group Pnma -t 0.3 -d 0.9 --split True --integrate True

(a)

(b)

Figure S 1. Graphical user interfaces for (a) preparing t-SerialED experiment (b) executing t-SerialED experiment

Figure S 2 Illustration of the hardware and software setup for t-SerialED

Figure S 3. Process for eucentric height prediction of the whole grid from measured eucentric heights at positions marked with ‘+’. The prediction plot shows the grid is curved and a photo of the loaded grid confirms the grid is indeed curved.

Figure S 4 Schematics for eucentric height determination

Figure S 5 Schematics of automatic crystal finding. The area selection procedure allows for both automatic selection and manual adjustment. The radius of the scan area needs to be input by the user and it will be divided into a number of patches according to the desired magnification for crystal searching. The stage will move to the center of patches and take images and identify crystals. It is possible to take all the crystals that appear on each image. It is also possible to add conditions to filter out ideal targets. For instance, collect those targets that are not aggregate or not close to the edge of the image.

Figure S 6. Flowchart of preparation and data acquisition of t-SerialED datasets. At low mag level, the magnification is set to 110. The target grid squares will be identified from the atlas. At medium mag level, eucentric height will be measured at several places and the rest will be predicted. At high mag level, the microscope is always operated in diffraction mode. When taking images, diffraction defocus will be applied to show a Ronchigram with the same length scale when the microscope is operated in SA 7500.

Figure S 7. Target picking for isolated particles and aggregated particles. Spread parameter is the minimum separation between the targets. For isolated particles

(a)

(b)

(c)

(d)

Figure S 8. Target picking for aggregated particles and large blocks.  (a) For aggregated particles, the density of the target spots depends on the user-defined beam size. If the beam hits two or three particles at the same time, the indexing algorithm in DIALS is still able to distinguish each set of lattices.  (b, c, d) For large blocks, the algorithm will identify the edge of a large block and put red target spots along the edge according to the user-defined density.

Figure S 9. Flowchart of data processing of t-SerialED datasets

Figure S 10. An example of the restrain.phil file

(a)

(b)

(c)

(d)

Figure S 11 Typical t-SerialED datasets that can be indexed: (a) one crystal (b) two crystals (c) three crystals (d) low resolution, one crystal

(a)

(b)

(c)

Figure S 12 Typical t-SerialED datasets that are not indexable during data processing: (a) blocked (b) amorphous or blank (c) polycrystalline.

(a)

(b)

(c)

(d)

Figure S 13 Reconstructed 3D reciprocal space of an individual tilt series for MOF-235. Space group can be determined by checking the systematic absence of reflections. Reciprocal space viewed along: (a). a*-axis (b). b*-axis (c). c*-axis. (d). (hh-2hl) plane sliced from 3D reciprocal space in red.

(a)

(b)

(c)

(d)

Figure S 14 Photos of the (a) tablet, (b) capsule and (c) pellet. (d) The overall morphology of the Fe Supplement sample. After crushed in mortar, the shapes of the ingredients are irregular.

(a)

(b)

(c)

(d)

(e)

(f)

Figure S 15 CC1/2 plot to show the data quality. (a) Glycine (b) L-ascorbic acid (c) Zn acetate (d) Saccharin (e) Mg acetate (f) L-glutamic acid

(a)

(b)

(c)

(d)

Figure S 16 3D reciprocal space reconstructed from an individual dataset from paracetamol

(a)

(b)

(c)

Figure S 17 Crystal packing of paracetamol, hydrogen bonding network in the crystal and electron static potential map for the molecule

(a)

(b)

(c)

Figure S 18 3D reciprocal space reconstructed from an individual dataset from ferrous glycine complex.

(a)

(b)

(c)

Figure S 19 Atomic arrangement of ferrous glycine complex viewed from different directions.

(a)

(b)

Figure S 20 Coordination environment of two independent Fe atoms

Figure S 21 Histogram of number of indexed reflections. (a) Paracetamol (b) Fe supplement. Horizontal label represents the number of indexed reflections while vertical label is the frequency.

(a)

(b)

Figure S 22 (a) Magnified Rietveld refinement results within 2θ range of 8° to 14°. (b) Simulated PXRD for 2θ range of 8° to 14°, demonstrating the peaks located at 10.9° and 13.4° are the strong peaks.

Figure S 23 Overview of t-SerialED data processing workflow.

Table S 1 Statistics from data acquisition for MOF-235 and the mixture. The unindexable datasets include typical amorphous ED patterns, blocked ED patterns and polycrystalline ED patterns.

|  | MOF-235 | Mixture |
| --- | --- | --- |
| No. of datasets collected | 160 | 902 |
| Data collection time (h) | 1 | 6.5 |
| No. of unindexable datasets | 1 | 407 |
| No. of indexed datasets | 159 | 495 |

Table S 2 Ingredient composition in paracetamol tablet and Fe supplement capsule. The unindexed datasets include typical amorphous ED patterns, blocked ED patterns and polycrystalline ED patterns.

|  | Paracetamol tablet | Fe supplement capsule |
| --- | --- | --- |
| API compound | Paracetamol | Ferrous (II) glycine sulfate complex |
| API weight (mg) | 500 | 567 |
| Total weight (mg) | 590 | 703 |
| Density (API, g/cm3) | 1.29 | 1.98 |
| Density (tablet/capsule, g/cm3) * | 1.24 | 1.22 |
| Expected API weight ratio | 84.7% | 80.6% |
| Expected API volume ratio | 81.4% | 49.6% |
| Data collection time (h) | 1.7 | 3.8 |
| No. of datasets collected | 197 | 496 |
| No. of unindexed datasets | 33 | 288 |
| No. of indexed datasets | 164 | 216 |
| No. of datasets in API unit cells | 163 | 215 (207 form 1 + 8 form 2) |
| Measure API volume ratio (ED) | 82.8% | 43.4% |
| Non-API contents ** | Corn starch, pregelatinized starch (corn), povidone, potassium sorbate, talc, stearic acid, hypromellose, triacetin. | Ascorbic acid, microcrystalline cellulose, hypromellose, hydro-xypropylcellulose, methacrylic acid-ethyl acrylate copolymer (1:1) dispersion 30% (Eudragit L30 D-55) (contains methacrylic acid-ethyl acrylate copolymer (1:1), sodium lauryl sulfate, polysorbate 80), acetyl-triethyl citrate, talc |

* Measured using drainage method

** Composition was obtained from the datasheets from the official website of Swedish Medical Products Agency

Table S 3. Summary for acquisition time and accumulated dose for different collection frames. The overhead time is the extra time required when the detector is not acquiring frames, including the time for locating crystals, adjusting eucentric height, switching states, rotating the stage, moving the beam, and translating the stage.

|  | Time for ED frames (s) | Time for imaging frames (s) | Total overhead time (s) | Dose for imaging and overhead (e/ Å2) | Total time (s) | Accumulated dose (e/ Å2) |
| --- | --- | --- | --- | --- | --- | --- |
| 7 frames | 3.5 | 1.8 (7 images) | 2 | 0.019 | 7.3s | 0.544 |
| 25 frames | 12.5 | 3 (12 images) | 5 | 0.040 | 20.5 | 1.915 |
| 49 frames | 24.5 | 3 (12 images) | 9 | 0.060 | 36.5 | 3.735 |

Table S 4. Comparison of the throughput of t-SerialED with previously reported methods based on electron diffraction. Note that the speed calculation does not include the time for preparing the experiment.

| Method type | Microscope | Speed (s/crystal) | Crystal Picking | Average tilt angle (°) | References |
| --- | --- | --- | --- | --- | --- |
| t-SerialED (25 frames) | Themis-Z | 20.5 | Automatic | 72 | This work |
| SerialED | JEOL-2100 | 2 | Automatic | 0 | 4 |
| SerialED | FEI Tecnai | 1.36 | Automatic | 0 | 3 |
| SerialED | Themis-Z | 1.5 | Manual | 0 | 5 |
| SerialRED | JEOL-2100 | 60 | Automatic | 16 | 6 |
| SerialRED | JEOL-2100 | 67 | Automatic | 20 | 7 |
| SerialRED | Titan Krios | 748 | Manual | 80 | 8 |
| SerialRED | JEM-2100/ ARM300 | >150 | Manual | ~130 | 9 |
| SerialRED | Talos Arctica | >60 | Manual | 50 | 10 |

Table S 5 Data processing statistics of MOF-235 using CrystFEL

| d/A | nref | Possible | Completeness/% | Measured | Redundancy | Mean | CC | CCstar | Rsplit/% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 3.67 | 102 | 104 | 98.08 | 7533 | 73.9 | 4286.29 | 1 | 1 | 19.28 |
| 1.72 | 81 | 83 | 97.59 | 4272 | 52.7 | 7096.83 | 0.77 | 0.93 | 26.98 |
| 1.44 | 79 | 81 | 97.53 | 3422 | 43.3 | 4637.18 | 0.85 | 0.96 | 22.39 |
| 1.28 | 77 | 78 | 98.72 | 3103 | 40.3 | 2751.71 | 0.91 | 0.98 | 19.28 |
| 1.18 | 73 | 75 | 97.33 | 2577 | 35.3 | 2113.21 | 0.87 | 0.96 | 22.42 |
| 1.1 | 74 | 75 | 98.67 | 2389 | 32.3 | 1639.33 | 0.91 | 0.98 | 20.75 |
| 1.04 | 72 | 72 | 100 | 2123 | 29.5 | 1113.29 | 0.93 | 0.98 | 19.49 |
| 0.99 | 72 | 74 | 97.3 | 1828 | 25.4 | 959.93 | 0.76 | 0.93 | 27.76 |
| 0.95 | 74 | 75 | 98.67 | 1837 | 24.8 | 809.47 | 0.87 | 0.96 | 22.92 |
| 0.92 | 72 | 73 | 98.63 | 1595 | 22.2 | 681.9 | 0.86 | 0.96 | 20.86 |

Table S 6 Data processing statistics of MOF-235 using DIALS

|  | Overall | Low | High |
| --- | --- | --- | --- |
| High resolution limit | 0.90 | 2.44 | 0.90 |
| Low resolution limit | 18.36 | 18.36 | 0.92 |
| Completeness | 100.0 | 100.0 | 100.0 |
| Multiplicity | 133.9 | 223.6 | 64.5 |
| I/sigma | 7.9 | 23.1 | 1.5 |
| Rmerge | 1.061 | 1.619 | 1.186 |
| Rmeas | 1.064 | 1.624 | 1.194 |
| Rpim | 0.081 | 0.106 | 0.132 |
| Rsplit | 0.194 | 0.169 | 0.641 |
| CC half | 0.989 | 0.994 | 0.533 |
| Total observations | 107404 | 12967 | 2708 |
| Total unique | 802 | 58 | 42 |

Table S 7 Data refinement statistics for MOF-235 datasets processed by CrystFEL and DIALS. The Rint in the dataset processed by CrystFEL is unknown because CrystFEL outputs a merged SHELX HKL files.

|  | CrystFEL | DIALS |
| --- | --- | --- |
| Crystal system | hexagonal | hexagonal |
| Space group | P62c (190) | P62c (190) |
| a [Å] | 12.6200(18) | 12.6627(18) |
| b [Å] | 12.6200(18) | 12.6627(18) |
| c [Å] | 18.230(4) | 18.224(4) |
| α [°] | 90 | 90 |
| β [°] | 90 | 90 |
| γ [°] | 120 | 120 |
| 2θ range [°] | 0.12 to 1.25 (0.90 Å) | 0.10 to 1.26 (0.90 Å) |
| Index ranges | −16 ≤ h ≤ 16 −8 ≤ k ≤ 7 −23 ≤ l ≤ 24 | −14 ≤ h ≤ 14 −14 ≤ k ≤ 14 −20 ≤ l ≤ 20 |
| Independent reflections | 730 Rint = ? Rsigma = 0.1883 | 1283 Rint = 0.9977 Rsigma = 0.1268 |
| Completeness to θ = 0.630° | 99.9 % | 99.9 % |
| Data / Restraints / Parameters | 730/3/91 | 1283/55/88 |
| Goodness-of-fit | 1.214 | 1.237 |
| Final R indexes [I≥2σ(I)] | R1 = 0.1833 wR2 = 0.4139 | R1 = 0.1513 wR2 = 0.3610 |
| Final R indexes [all data] | R1 = 0.1916 wR2 = 0.4237 | R1 = 0.2013 wR2 = 0.3979 |

Table S 8 Input composition and number of crystals identified in the mixture

|  | Glycine | L-ascorbic | Zn acetate | Saccharin | Mg acetate | L-glutamic |
| --- | --- | --- | --- | --- | --- | --- |
| Density (g/cm3) | 1.61 | 1.65 | 1.74 | 0.828 | 1.45 | 1.46 |
| Mass (mg) | 50 | 50 | 50 | 50 | 50 | 50 |
| Volume (cm3) | 0.0311 | 0.0303 | 0.0289 | 0.0639 | 0.0345 | 0.0342 |
| Expected volume ratio (%) | 14.2 | 13.8 | 13.1 | 27.5 | 15.7 | 15.6 |
| No. crystals | 54 | 87 | 81 | 137 | 65 | 71 |
| Measured volume ratio (%) | 11.0 | 17.5 | 16.3 | 27.7 | 13.2 | 14.3 |

Table S 9 Data processing statistics for the mixture

|  | Glycine | L-ascorbic | Zn acetate | Saccharin | Mg acetate | L-glutamic |
| --- | --- | --- | --- | --- | --- | --- |
| Resolution (Å) | 11.96 - 0.95 | 16.71 - 0.95 | 6.97 - 0.95 | 11.34 - 0.95 | 11.68 - 0.95 | 17.21 - 0.95 |
| Multiplicity | 9.1 | 9.5 | 27.2 | 36.5 | 3.7 | 6.4 |
| Completeness | 97.52% | 99.69% | 89.33% | 99.94% | 89.43% | 98.79% |
| Mean I/σ(I) | 8.6 | 12.8 | 11.1 | 10.9 | 6.8 | 14.5 |
| Rmerge | 0.515 | 0.484 | 0.604 | 0.569 | 0.47 | 0.47 |
| Rmeas | 0.541 | 0.51 | 0.611 | 0.576 | 0.528 | 0.506 |
| Rpim | 0.149 | 0.151 | 0.08 | 0.086 | 0.223 | 0.178 |
| Rsplit | 0.212 | 0.153 | 0.198 | 0.095 | 0.355 | 0.155 |
| CC½ | 0.916 | 0.971 | 0.96 | 0.995 | 0.749 | 0.978 |

Table S 10 Structure refinement statistics for the mixture

|  | Glycine | L-ascorbic | Zn acetate | Saccharin | Mg acetate | L-glutamic |
| --- | --- | --- | --- | --- | --- | --- |
| Crystal system | monoclinic | monoclinic | monoclinic | monoclinic | monoclinic | orthorhombic |
| Space group | P21/n (14) | P21 (4) | C2/c (15) | P21/c (14) | P21/c (14) | P212121 (19) |
| a [Å] | 5.005(2) | 6.315(2) | 14.394(3) | 9.422(2) | 4.8084(4) | 5.091(2) |
| b [Å] | 11.964(2) | 6.448(2) | 5.330(2) | 6.809(2) | 11.9943(13) | 17.209(3) |
| c [Å] | 5.368(2) | 16.893(3) | 10.962(3) | 11.665(2) | 8.5548(8) | 6.930(2) |
| α [°] | 90.00(3) | 90.00(3) | 90 | 90.00(3) | 90 | 90.00(3) |
| β [°] | 111.83(3) | 99.01(3) | 99.88(2) | 103.53(3) | 95.355(7) | 90.00(3) |
| γ [°] | 90.00(3) | 90.00(3) | 90 | 90.00(3) | 90 | 90.00(3) |
| 2θ range [°] | 0.19 to 1.22 (0.93 Å) | 0.07 to 1.22 (0.93 Å) | 0.16 to 1.17 (0.96 Å) | 0.12 to 1.19 (0.95 Å) | 0.16 to 1.20 (0.94 Å) | 0.13 to 1.19 (0.95 Å) |
| Index ranges | −5 ≤ h ≤ 5 −12 ≤ k ≤ 12 −5 ≤ l ≤ 5 | −6 ≤ h ≤ 6 −6 ≤ k ≤ 6 −17 ≤ l ≤ 17 | −14 ≤ h ≤ 13 −5 ≤ k ≤ 5 −11 ≤ l ≤ 11 | −9 ≤ h ≤ 9 −7 ≤ k ≤ 7 −12 ≤ l ≤ 12 | −4 ≤ h ≤ 4 −12 ≤ k ≤ 12 −8 ≤ l ≤ 8 | −5 ≤ h ≤ 5 −18 ≤ k ≤ 17 −7 ≤ l ≤ 7 |
| Reflections collected | 5767 | 15474 | 11616 | 60945 | 3305 | 9277 |
| Independent reflections | 362 Rint = 0.5281 Rsig = 0.1747 | 1635 Rint = 0.5784 Rsig = 0.2014 | 427 Rint = 0.6088 Rsig = 0.2379 | 895 Rint = 0.5382 Rsig = 0.0761 | 542 Rint = 0.6925 Rsig = 0.3286 | 743 Rint = 0.7130 Rsig = 0.1956 |
| Completeness to θ = 0.609° | 99.5 % | 98.3 % | 88.6 % | 99.7 % | 94.8 % | 100.0 % |
| Data / Restraints / Parameters | 362/0/48 | 1635/1/234 | 427/0/52 | 895/18/110 | 542/0/62 | 743/0/46 |
| Goodness-of-fit | 0.813 | 0.743 | 1.932 | 3.376 | 1.025 | 1.111 |
| Final R indexes [I≥2σ(I)] | R1 = 0.2066 wR2 = 0.4878 | R1 = 0.1735 wR2 = 0.4105 | R1 = 0.2095 wR2 = 0.4476 | R1 = 0.1614 wR2 = 0.3449 | R1 = 0.3327 wR2 = 0.6709 | R1 = 0.2266 wR2 = 0.5168 |
| Final R indexes [all data] | R1 = 0.2421 wR2 = 0.5374 | R1 = 0.2175 wR2 = 0.4767 | R1 = 0.3256 wR2 = 0.5159 | R1 = 0.2104 wR2 = 0.3859 | R1 = 0.4102 wR2 = 0.7422 | R1 = 0.2702 wR2 = 0.5726 |

Table S 11 Summary of the phase analysis results of the crystalline contents in paracetamol tablet and iron supplement capsule using t-SerialED and PXRD. All the ratios displayed in the table are calculated without considering the amorphous contents.

|  | Paracetamol tablet | Iron supplement capsule |
| --- | --- | --- |
| No. of datasets in API unit cells | 163 | 215 (form 1: 207, form 2: 8) |
| No. of datasets in talc unit cells | 1 | 2 |
| Volume ratio of API (ED) | 99.4% | 99.0% (form 1: 95.4%, form 2: 3.6%) |
| Volume ratio of talc (ED) | 0.6% | 1.0% |
| Volume ratio of API (Xray) | 98.2% | 97.7% (form 1: 97.6%, form 2: 0.1%) |
| Volume ratio of talc (Xray) | 1.8% | 2.3% |

Table S 12 Data processing statistics for paracetamol

|  | Overall | Low | High |
| --- | --- | --- | --- |
| High resolution limit | 0.90 | 2.44 | 0.90 |
| Low resolution limit | 11.50 | 11.50 | 0.92 |
| Completeness | 100.0 | 100.0 | 100.0 |
| Multiplicity | 22.6 | 47.2 | 13.0 |
| I/sigma | 6.5 | 12.3 | 1.9 |
| Rmerge(I) | 0.978 | 1.935 | 1.200 |
| Rmeas(I) | 0.996 | 1.957 | 1.255 |
| Rpim(I) | 0.183 | 0.280 | 0.355 |
| Rsplit(I) | 0.283 | 0.158 | 0.631 |
| CC half | 0.942 | 0.974 | 0.751 |

Table S 13 Data statistics of the refinement results of paracetamol

| Crystal system | monoclinic |
| --- | --- |
| Space group (number) | P21/n (14) |
| a [Å] | 7.100 |
| b [Å] | 9.210 |
| c [Å] | 11.610 |
| α [°] | 90 |
| β [°] | 97.90 |
| γ [°] | 90 |
| 2θ range [°] | 0.16 to 1.29 (0.88 Å) |
| Index ranges | −7 ≤ h ≤ 7 −10 ≤ k ≤ 10 −12 ≤ l ≤ 12 |
| Reflections collected | 24365 |
| Independent reflections | 1070 Rint = 0.8518 Rsigma = 0.1728 |
| Completeness to θ = 0.6443° | 100.0 % |
| Data / Restraints / Parameters | 1070/0/104 |
| Goodness-of-fit on F2 | 0.981 |
| Final R indexes [I≥2σ(I)] | R1 = 0.1726 wR2 = 0.4187 |
| Final R indexes [all data] | R1 = 0.2165 wR2 = 0.4731 |

Table S 14 Comparison of data processing statistics of with different threshold for data selection of ferrous glycine datasets

| Threshold: 200 | Overall | Low | High |
| --- | --- | --- | --- |
| High resolution limit | 0.90 | 2.44 | 0.90 |
| Low resolution limit | 13.21 | 13.21 | 0.92 |
| Completeness | 100.0 | 100.0 | 100.0 |
| Multiplicity | 10.8 | 30.1 | 5.8 |
| I/sigma | 4.3 | 15.6 | 1.0 |
| Rmerge(I) | 0.858 | 0.896 | 1.042 |
| Rmeas(I) | 0.892 | 0.908 | 1.182 |
| Rpim(I) | 0.226 | 0.141 | 0.549 |
| Rsplit(I) | 0.334 | 0.268 | 0.456 |
| CC half | 0.757 | 0.607 | -0.016 |

| Threshold: 100 | Overall | Low | High |
| --- | --- | --- | --- |
| High resolution limit | 0.90 | 2.44 | 0.90 |
| Low resolution limit | 13.21 | 13.21 | 0.92 |
| Completeness | 100.0 | 100.0 | 100.0 |
| Multiplicity | 22.1 | 62.2 | 11.0 |
| I/sigma | 4.8 | 18.2 | 1.1 |
| Rmerge(I) | 0.775 | 0.855 | 1.359 |
| Rmeas(I) | 0.790 | 0.863 | 1.426 |
| Rpim(I) | 0.140 | 0.105 | 0.420 |
| Rsplit(I) | 0.284 | 0.244 | 0.728 |
| CC half | 0.752 | 0.543 | 0.685 |

Table S 15 Comparison of data refinement statistics of with different threshold for data selection of ferrous glycine complex

| Indexed spots threshold | 200 | 100 |
| --- | --- | --- |
| Crystal system | triclinic | triclinic |
| Space group (number) | P1 (2) | P1 (2) |
| a [Å] | 5.979(2) | 5.979(2) |
| b [Å] | 6.793(2) | 6.793(2) |
| c [Å] | 13.268(3) | 13.268(3) |
| α [°] | 85.49(3) | 85.49(3) |
| β [°] | 82.71(3) | 82.71(3) |
| γ [°] | 83.09(3) | 83.09(3) |
| 2θ range [°] | 0.09 to 1.26 (0.90 Å) | 0.09 to 1.26 (0.90 Å) |
| Reflections collected | 17290 | 34004 |
| Independent reflections | 1537 Rint = 0.7388 Rsigma = 0.3232 | 1538 Rint = 0.7776 Rsigma = 0.2630 |
| Completeness to θ = 0.630° | 99.1 % | 99.5 % |
| Data / Restraints / Parameters | 1537/4/158 | 1538/4/158 |
| Goodness-of-fit on F2 | 0.984 | 1.057 |
| Final R indexes [I≥2σ(I)] | R1 = 0.2137 wR2 = 0.4984 | R1 = 0.1704 wR2 = 0.4486 |
| Final R indexes [all data] | R1 = 0.2834 wR2 = 0.5529 | R1 = 0.2338 wR2 = 0.5109 |

Reference

1.	Lee, J. H., Ahn, Y. & Kwak, S.-Y. Facile Sonochemical Synthesis of Flexible Fe-Based Metal–Organic Frameworks and Their Efficient Removal of Organic Contaminants from Aqueous Solutions. ACS Omega 7, 23213–23222 (2022).

2.	Bücker, R., Hogan-Lamarre, P. & Miller, R. J. D. Serial Electron Diffraction Data Processing With diffractem and CrystFEL. Front. Mol. Biosci. 8, (2021).

3.	Bücker, R. et al. Serial protein crystallography in an electron microscope. Nat Commun 11, 996 (2020).

4.	Smeets, S., Zou, X. & Wan, W. Serial electron crystallography for structure determination and phase analysis of nanocrystalline materials. J Appl Cryst 51, 1262–1273 (2018).

5.	Hogan-Lamarre, P., Luo, Y., Bücker, R., Miller, R. J. D. & Zou, X. STEM SerialED: achieving high-resolution data for ab initio structure determination of beam-sensitive nanocrystalline materials. IUCrJ 11, 62–72 (2024).

6.	Wang, B., Zou, X. & Smeets, S. Automated serial rotation electron diffraction combined with cluster analysis: an efficient multi-crystal workflow for structure determination. IUCrJ 6, 854–867 (2019).

7.	Luo, Y. et al. High-throughput phase elucidation of polycrystalline materials using serial rotation electron diffraction. Nat. Chem. 15, 483–490 (2023).

8.	Lightowler, M. et al. Phase Identification and Discovery of an Elusive Polymorph of Drug-Polymer Inclusion Complex Using Automated 3D Electron Diffraction. Angewandte Chemie International Edition 63, e202317695 (2024).

9.	Takaba, K., Maki-Yonekura, S. & Yonekura, K. Collecting large datasets of rotational electron diffraction with ParallEM and SerialEM. Journal of Structural Biology 211, 107549 (2020).

10.	Unge, J., Lin, J., Weaver, S. J., Her, A. S. & Gonen, T. Autonomous MicroED data collection enables compositional analysis. (2023) doi:10.26434/chemrxiv-2023-8qvwg.