Supporting information

Polyimide nanofiber aerogel with hierarchical porosity: a novel platform in high-temperature oil absorption

Lidong Tiana*, Yi Zhang a, Yibin Liu a, Shan Zhangb*,

a College of Materials Science and Engineering, Xi’an University of Science and Technology, Xi’an, Shaanxi 710054, P. R. China.

b Institute of New Materials and Technology, Shaanxi Coal and Chemical Technology Institute Co.,Ltd., Xi’an, Shaanxi 710100, P. R. China.

E-mails: ldtian@xust.edu.cn (Lidong Tian); zhangshanzs33@163.com (Shang Zhang)

Figure S1 SEM images of PI nanofibers: (a) overall morphology and (b) single PI fiber morphology.

Figure S2 Density and porosity of PSF, PIF and PIF-a.

The density of the PSF, PIF and PIF-a were calculated from the following formula:

ρareogel=mV                        (1)

where m and V were the weight and volume of the aerogel or nanofibers, respectively.

The porosity was calculated using the following formula:

Porosity%=(1-ρareogelρa)×100          (2)

where ρareogel and ρa were the volumetric mass densities of the PI aerogel and synthesized PI or PS, respectively. ρa of synthesized PI is 1.37 g/cm3, ρa of PS is 1.06 g/cm3.

Table S1 Thermogravimetric data of PIF-a and PSF

| Sample | Tinitial (℃)a | T5% loss (℃)b | T10% loss (℃)c |
| --- | --- | --- | --- |
| PIF-a | 356 | 505 | 533 |
| PSF | 101 | 299 | 322 |

a the initial thermal decomposition temperature, measured by TGA in nitrogen.

b the 5% quality loss temperature, measured by TGA in nitrogen.

c the 10% quality loss temperature, measured by TGA in nitrogen.

Figure S3 (a) SEM image of PSF under room temperature, (b) SEM image of PSF under 150℃, (c) SEM image of PI nanofibers under room temperature, (d) SEM image of PI nanofibers under 150℃.

Table S2 Nitrogen physisorption characterization of PSF under different temperatures

| Sample | SSAa (m2 g-1) | TPVb (cm3 g-1) | Vmesoc (cm3 g-1) | Vmacrod (cm3 g-1) | APSe (nm) |
| --- | --- | --- | --- | --- | --- |
| PIF-a-150 | 36.25 | 0.09 | 0.07 | 0.02 | 31.2 |
| PIF-a-200 | 36.18 | 0.09 | 0.07 | 0.02 | 31.2 |
| PIF-a-250 | 36.21 | 0.09 | 0.07 | 0.02 | 31.2 |
| PIF-a-300 | 9.13 | 0.04 | 0.01 | 0.03 | 60.4 |

a Specific surface area (SSA) is calculated by the Brunauer-Emmett-Teller (BET) method.

b TPV means the total pore volume.

c Vmeso indicates the mesopore (2–50 nm) volume calculated by the BJH method.

d Vmacro indicates the macropore (>50 nm) volume calculated by the BJH method.

e APS indicates the adsorption average pore width calculated by the BET method (4V/A by BET).