Table 1

Transesterification reaction requirement for the production of Roselle biodiesel

| Description | Values |
| --- | --- |
| Oil quantity | 1000 ml |
| Methanol (1:3 molar ratio) | 280 ml |
| Sodium hydroxide (H2SO4) | 1.65 ml |
| Temperature | 60 - 75 °C |
| Time period | 60-70 min |
| RPM | 320 – 600 rpm |
| Biodiesel obtained | 830 ml |

Table 2

Free fatty acid composition of Roselle biodiesel

| Fatty Acid | Structure | Molecular Structure | Formula | Mol. wt | % (w/w) |
| --- | --- | --- | --- | --- | --- |
| Linoleic acid | 18:2 |  | C18H32O2 | 280.2512 | 38.18 |
| Palmitic acid | 16:0 |  | C16H32O2 | 257.2503 | 18.49 |
| Linolenic acid | 18:3 |  | C18H30O2 | 279.2235 | 2.08 |
| Oleic acid | 18:1 |  | C18H34O2 | 281.2667 | 33.32 |
| Lignoceric acid | 24:0 |  | C24H48O2 | 367.3543 | 1.11 |
| Stearic acid | 18:0 |  | C18H36O2 | 285.2624 | 4.08 |

Table 3

Important physical-chemical properties of diesel, Roselle and its blends

| Fuel | Testing method | B0 | LA20 | LA40 | LA60 | LA80 | LA100 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Density (@20° C) (kg/m3) | ASTM D4052 | 830 | 838.2 | 849.6 | 859.2 | 868.6 | 877 |
| Kinematic viscosity (@40° C) (mm2/s) | ASTM D445 | 2.9 | 3.24 | 3.5 | 4.25 | 4.85 | 5.64 |
| Heating value (MJ/ kg) | ASTM D4809 | 42.5 | 41.6 | 40.7 | 40.16 | 39.44 | 38.74 |
| Cetane number | ASTM D613 | 48 | 48.8 | 49.67 | 50.45 | 51.25 | 52.3 |
| Flash point (° C) | ASTM D93 | 50 | 75.2 | 94.4 | 116.7 | 135.2 | 159.2 |
| C% | ASTM D5291 | 86.14 | 84 | 83.09 | 81.52 | 80.10 | 78.71 |
| H% | ASTM D5291 | 13.86 | 13.49 | 13.12 | 12.75 | 12.29 | 12.12 |
| O% | ASTM D5291 | 0.004 | 2.25 | 4.02 | 5.71 | 7.54 | 9.23 |

Table 4

The detailed specification of test engine.

| Engine parameters | Specifications |
| --- | --- |
| Make | Legion Brothers, India |
| Engine type | Four stroke, CI engine. |
| Cooling | Water-cooled engine |
| Bore×Stroke | 80mm×110mm |
| No of cylinders | 1 |
| Compression ratio | 17.5 |
| Dynamometer | Eddy current dynamometer |
| Rated power@ 1500 rpm (k W) | 3.5 |
| Dynamometer | Eddy current dynamometer |
| Start of injection timing | 19 to 27° C bTDC |
| Connecting rod length | 235 mm |
| Exhaust gas analyzer | Testo-350 flue gas analyzer |

Table 5

Test matrix and acronyms used for diesel and Roselle fuel operation.

| Mode | Fuel used | Constant parameter |  | IT, ° CA bTDC | Load | Acronyms used |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | CR | Speed |  |  |  |
| Diesel | Diesel | 17.5 | 1500 rpm | 19 21 23 25 27 | 25%, 50%, 75%, 100% | B0 |
| Biodiesel + Diesel | 20% Roselle + 80% Diesel | 17.5 | 1500 rpm | 19 21 23 25 27 | 25%, 50%, 75%, 100% | LA20 |
| Biodiesel + Diesel | 40% Roselle + 60% Diesel | 17.5 | 1500 rpm | 19 21 23 25 27 | 25%, 50%, 75%, 100% | LA40 |
| Biodiesel + Diesel | 60% Roselle + 40% Diesel | 17.5 | 1500 rpm | 19 21 23 25 27 | 25%, 50%, 75%, 100% | LA60 |
| Biodiesel + Diesel | 80% Roselle + 20% Diesel | 17.5 | 1500 rpm | 19 21 23 25 27 | 25%, 50%, 75%, 100% | LA80 |
| Biodiesel | 100% Roselle | 17.5 | 1500 rpm | 19 21 23 25 27 | 25%, 50%, 75%, 100% | LA100 |

Table 6

Uncertainty analysis of test engine.

| S. No | Instrument | Percentage uncertainty |
| --- | --- | --- |
| 1 | Load indicator | ±0.2 |
| 2 | Speed sensor | ±1.0 |
| 3 | Temperature sensor | ±0.15 |
| 4 | Pressure sensor | ±0.5 |
| 5 | Crank angle encoder | ±0.2 |
| 6 | Smoke meter | ±1.0 |
| 7 | Eddy current dynamometer | ±0.15 |
| 8 | Fuel burette | ±1.0 |
| 9 | Manometer | ±1.0 |
| 10 | Test 350 gas analyser CO2 NOX | ± 1.0 ± 0.5 |

Table 7. ANN Settings used for modelling

| Parameter | Value | MATLAB function/syntax |
| --- | --- | --- |
| Hidden layer neurons (h) | 6 | - |
| Topology | 3-6-10 | fitnet(6) |
| Data division (in %) | 70%-15%-15% | dividerand |
| Data division (in data points) | 84-18-18 | - |
| Network type | feed-forward back-propagation | feedforwardnet(hiddenSizes,trainFcn) |
| Transfer function | Hyperbolic tangent sigmoid in hidden layer; linear in output layer. | tansig in hidden layer; purelin in output layer. |
| Training function | Levenberg Marquardt algorithm | net.trainFcn=’trainlm’; |
| Performance function | Mean square error | MSE |
| Learning function | Gradient descent with momentum weight and bias learning function | learngdm |