Supporting Information

Aqueous Asymmetric Pseudocapacitor Featuring High Areal Energy and Power Using Conjugated Polyelectrolytes and Ti3C2Tx MXene

Benjamin Rui Peng Yipab, Chaofan Chenc, Yan Jiangab, David Ohayonab, Guillermo C. Bazanab*, Xuehang Wangc*

a Departments of Chemistry and Chemical & Biomolecular Engineering, National University of Singapore, Singapore 119077.

b Institute for Functional Intelligent Materials, National University of Singapore, Singapore 117544

c Department of Radiation Science and Technology, Delft University of Technology, Delft 2629 JB, The Netherlands

* Corresponding Authors: Professor Guillermo C. Bazan (chmbgc@nus.edu.sg); Dr Xuehang Wang (x.wang-22@tudelft.nl)

Keywords: asymmetric pseudocapacitors, MXenes, conjugated polyelectrolytes, high-rate capability, high areal capacitance, large mass loading

Figure S1. Experimental thickness measurements from cross-sectional SEM and extrapolation to obtain the thicknesses that are used in this work for electrochemical characterization. a) For CPE-K and b) for Ti3C2Tx.

|  | C=N | C-S | C-C | C=C |
| --- | --- | --- | --- | --- |
| Pristine | 0.16 | 0.35 | 1.00 | 1.24 |
| Doped | 0.06 | 0.46 | 1.00 | 0.18 |
| Dedoped | 0.13 | 1.00 | 1.00 | 1.46 |

Figure S2. Peak fitting of XPS C 1s data with a table (right) of peak intensity ratios C=N : C-S : C-C : C=C normalized to C-C.

Figure S3. X-ray diffractogram of drop cast 1.0 mg cm-2 Ti3C2Tx on a silicon substrate.

Figure S4. Cross-sectional SEM of drop cast CPE-K and Ti3C2Tx on silicon substrates.

Figure S5. Cyclic voltammograms of drop cast CPE-K film at various mass loading. a) CV normalized to current density for 2.8, 5.6, 8.4, and 11.2 mg cm-2 at 10 mV s-1. CVs for CPE-K films at increasing scan rates from 5 – 10,000 mV s-1 for b) 2.8, c) 5.6 and d) 8.4 mg cm-2.

Figure S6. Electrochemical characterization of drop cast Ti3C2Tx film at various mass loading. a) CV from 5 to 10,000 mV s-1 of drop cast Ti3C2Tx at a mass loading of 0.96 mg cm-2. b) log current versus log scan rate for Ti3C2Tx films. c) Representative GCD trace of Ti3C2Tx at 0.96 mg cm-2 from 5 to 100 A g-1. d) Specific capacitance as a function of specific current for Ti3C2Tx films. e) Linear fit of Z’ versus ω-1/2 to obtain the Warburg coefficient, σ.  f) Nyquist plot of EIS data for Ti3C2Tx films. g) Cycling stability of Ti3C2Tx (1.9 mg cm-2). h) Areal capacitance as a function of scan rate of drop cast Ti3C2Tx compared to drop cast CPE-K showing comparable capacitance.

Figure S7. Mass balancing experiment to obtain optimum voltage window for Ti3C2Tx//CPE-K asymmetric pseudocapacitor.

Table S1. Coulombic efficiencies of Ti3C2Tx//CPE-K at different mass ratios and voltage windows.

| Ratio CPE-K :Ti3C2Tx | CPE-K Mass (ug) | Ti3C2Tx Mass (ug) | Potential window (V) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | 0.6 | 0.7 | 0.8 | 0.9 | 1.0 | 1.1 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 |
|  |  |  | Coulombic efficiency (%) |  |  |  |  |  |  |  |  |  |  |  |
| 4.0 | 200 | 50 | 98 | 98 | 98 | 97 | 97 | 96 | 97 | 97 | 95 | 92 | - | - |
| 3.5 | 200 | 57 | 98 | 98 | 97 | 97 | 97 | 97 | 97 | 97 | 97 | 95 | - | - |
| 3.0 | 200 | 67 | 99 | 98 | 98 | 98 | 98 | 97 | 97 | 98 | 98 | 97 | 90 | 84 |
| 2.5 | 200 | 80 | 99 | 98 | 98 | 98 | 98 | 97 | 97 | 97 | 93 | 84 | - | - |

Figure S8. Electrochemical characterization of high mass loading (15.1 mg cm-2) Ti3C2Tx//CPE-K. a) Cyclic voltammograms from 5 to 10,000 mV s-1. b) GCD trace at 0.5 – 10 A g-1. c) Areal capacitance (normalized to the area of one glassy carbon electrode) as a function of scan rate.

Figure S9. Further electrochemical characterization of CPE-K//Ti3C2Tx devices a) Cyclic voltammetry of CPE-K//Ti3C2Tx pouch cell from 5 – 10,000 mV s-1. b) Areal capacitance of pouch cell and solid-state device as a function of scan rate. c) Constant current charge/discharge trace of pouch cell and solid-state device. d) Cycling stability measurements of CPE-K//Ti3C2Tx pouch cell cycled repeatedly at 20 A g-1.

Figure S10. Photographs of the device-making process. a) Aqueous droplet of CPE-K on 1x1 cm graphite foil current collectors. b) Photograph of 7.7 mg cm-2 pouch cell beside a Singapore 10 cent coin. c) Ti3C2Tx (left) and CPE-K (right) film on graphite foils meant for solid-state devices. d) Electrodes sandwiched and clamped using two glass slides to apply pressure on the gel electrolyte during drying. Thicknesses of e) pouch cell and f) solid-state device.