Supplementary Information for

Direction-Specific Diffusion of CO2 Augmented by Polygonal Rifling in Chiral Hexagonal Boron Nitride Nanotubes.

Manh-Thuong Nguyen,a* David J. Heldebrant,a,b*, Jian Liua and Abhoyjit Bhownc

[a] Pacific Northwest National Laboratory, Richland, Washington 99352, United States

[b] Pacific Northwest National Laboratory, Richland, Washington 99352, United States

Washington State University, Pullman, Washington 99164, United States

[c] Electric Power Research Institute, Palo Alto, California 94304, United States

S1. Methods

S1.1. Systems

We considered the h-BN nanotubes (BNNTs) of indices (5,5), (6,4), (7,3), (9,0), and (7,4), as generated using the TubeGen server. 1

For binding energy screening, we used nanotubes/surfaces of which the chiral index and unit cell shown in Figure S1

Figure S1. The unit cell size and chiral index of hBNNTs used for binding energy calculations.

S1.2. Static density functional calculations for binding energies

The binding energy of a (confined) X (X=CO2, N2) molecule a hBNNT was calculated as

ΔE(X)=ECO2-hBNNT-EX-EhBNNT,

in which the energy E of each system was calculated at the density functional level 	provided in Materials and Methods (main text).

S1.3. Diffusion coefficient (D)

D of CO2 along the tube direction (z), Dz, was calculated from the mean square displacement (MSDz)

Dz=12limt→∞ddtMSDz(t),

MSDz(t)=|rzt-rz(0)|2,

in which rz is the z component of the centroid coordinate of a CO2 molecule and the <> notation indicates the ensemble average.

S1.4. Adsorption free energy

At 1 atm, the free energy of X in hBNNTs (X= CO2, N2) was approximated as

∆G0X≈∆E(X)- μT, p0,X,

in which ∆E is the calculated adsorption energy, and μT, p0,X is the chemical potential of molecule X at temperature T (T= room temperature in this study) and pressure p0 = 1 atm, as taken from NIST-JANAF Thermochemical Tables 2.

S2. Results

Figure S2. MSDz of CO2 in hBNNT from AIMD. The diffusion coefficient is calculated as the slope of the linear part from 4 to 6 ps.

Figure S3. MSDz of CO2 in hBNNTs from xTB-MD.

Figure S4. Radial distribution functions, g(r), of atom pairs, in which C and O are CO2 atoms and B and N are hBNNT atoms.

Figure S5.  Distribution of the OCO angle.

Figure S6. Angle ⍺ between the CO2 molecule (OO direction) and the tube direction (z), and its distribution.

Uncategorized References

1.	J. T. Frey and D. J. Doren Tw-i, http://turin.nss.udel.edu/research/tubegenonline.html),   University of Delaware, Newark DE, 2011. TubeGen 3.4 (web-interface, http://turin.nss.udel.edu/research/tubegenonline.html), J. T. Frey and D. J. Doren, University of Delaware, Newark DE, 2011.   [cited]Available from: TubeGen 3.4 (web-interface, http://turin.nss.udel.edu/research/tubegenonline.html), J. T. Frey and D. J. Doren, University of Delaware, Newark DE, 2011.

2.	NIST. NIST-JANAF Thermochemical Tables, 2024.