Supporting Information

Figure S1 The morphography of Al films after CV test with different LiFSI concentrations in electrolytes (a) 0, (b) 0.2M, (c) 0.4M (d) 0.6M

Figure S2 Galvanostatic charge–discharge curves at 1C with different electrolytes

Figure S3 Cycle performance at a 1C current density at 45°C

Table S1 Ion conductivity of electrolyte with different LiFSI at 25°C

| LiFSI content | 0 M | 0.2 M | 0.4 M | 0.6 M |
| --- | --- | --- | --- | --- |
| Conductivity (mS cm-1) | 8.01 | 8.09 | 8.31 | 8.48 |