Coffee husks activated carbon supported cobalt oxide-Zinc oxide nanocomposites for enhanced adsorption-photocatalytic degradation of methylene blue dye in water

Waktola Fite Dinka1, Melkamu Biyana Regasa2

1,2Department of Chemistry, College of Natural and Computational Sciences, Wollega University, Nekemte, Ethiopia

1Department of Chemistry, College of Natural and Computational Sciences, Dambi Dollo University, Dambi Dollo, Ethiopia

Figure 1 a) UV-Vis spectra and b) Energy band gap c) FT-IR spectra of AC prepared from coffee husk.

Figure 2. UV-Vis absorbance spectra of a) nanoparticle and binary nanocomposite and b) supported nanocomposite.

Figure 3. Tauc’s plot for optical band gap estimation for nanoparticle, binary nanocomposite and supported nanocomposite.

Figure 4. The FT-IR spectrum of ZnO/Co3O4/AC nanocomposite with three different atios (1:2:1, 1:2:2 and 1:2:4) were recorded to investigate their bonding properties.

Table 1 Optimization of different experimental parameters to prepare stable and efficient ZnO/Co3O4/AC photocatalyst.

| Parameter | Values | Maximum absorbance point |
| --- | --- | --- |
| Precursor mass ratio | ZnO:Co3O4:AC | 1:1:2 |
|  | 1:2:4 |  |
|  | 1:2:1 |  |
|  | 1:2:2 |  |
| Solution pH | 6 | 10 |
|  | 8 |  |
|  | 10 |  |
|  | 12 |  |
| Reaction temperature (oC) | 60 | 75 |
|  | 75 |  |
|  | 90 |  |
| Reaction time (hour) | 2 | 4 |