Supporting Information

Pressure-Induced Phase Transitions in Bilayer La3Ni2O7

Mingyu Xu1#, Greeshma C.  Jose 2#, Aya Rutherford3, Haozhe Wang1, Stephen Zhang4, Robert J. Cava4, Haidong Zhou3, Wenli Bi2*, Weiwei Xie1*

1Department of Chemistry, Michigan State University, East Lansing, MI, 48824, USA

2Department of Physics, University of Alabama at Birmingham, Birmingham, AL, 35294, USA

3Department of Physics and Astronomy, University of Tennessee, Knoxville, TN, 37996, USA

4Department of Chemistry, Princeton University, Princeton, NJ, 08540, USA

#contributed equally

Table SI. Crystal structure refinement data……………………………………………………...S2

Table SII. Atomic coordinates and isotropic displacement parameters…….................................S3

Fig. S1. Criterion of TDW and T’ based on the plots of dR/dT at different pressures……..… S4

Fig. S2. Normalized resistance (R(T)/R(150 K)) of La3Ni2O7-2222………………………...S5

Table SI. The crystal structure and refinement of La3Ni2O7 at room temperature K (Mo Kα radiation). Values in parentheses are estimated standard deviation from refinement.

| Chemical Formula | La3Ni2O7 |
| --- | --- |
| Formula Weight | 646.15 g/mol |
| Space Group | Cmcm |
| Unit Cell dimensions | a = 20.5510(13) Å b = 5.4508(4) Å c = 5.3975(4) Å |
| Volume | 604.62(7) Å3 |
| Z | 4 |
| Density (calculated) | 7.098 g/cm3 |
| Absorption coefficient | 26.849 mm−1 |
| F (000) | 1132 |
| 2θ range | 7.734 to 81.316° |
| Reflections collected | 4856 |
| Independent reflections | 1047 [Rint = 0.0701] |
| Refinement method | Full-matrix least-squares on F2 |
| Data/restraints/parameters | 1047/0/37 |
| Final R indices | R1 (I>2σ(I)) = 0.0460; wR2 (I > 2 σ(I)) = 0.1067 R1 (all) = 0.0862; wR2 (all) = 0.1261 |
| Largest diff. peak and hole | +7.82 e-/Å3 and -2.74 e-/Å3 |
| R. M. S. deviation from mean | 0.769 e-/Å3 |
| Goodness-of-fit on F2 | 0.997 |

Table SII. Atomic coordinates and equivalent isotropic atomic displacement parameters (Å2) of La3Ni2O7. (Ueq is defined as one-third of the trace of the orthogonalized Uij tensor.) Values in parentheses are estimated standard deviations from refinement.

| Atoms | Wyck. | x | y | z | Occ. | Ueq |
| --- | --- | --- | --- | --- | --- | --- |
| La1 | 4c | 0 | 0.75046(11) | 1/4 | 1 | 0.008(14) |
| La2 | 8g | 0.32020(2) | 0.25758(7) | 1/4 | 1 | 0.007(13) |
| Ni | 8g | 0.09594(5) | 0.25201(16) | 1/4 | 1 | 0.005(19) |
| O1 | 4c | 0 | 0.29120(15) | 1/4 | 1 | 0.008(15) |
| O2 | 8g | 0.20360(3) | 0.21760(12) | 1/4 | 1 | 0.012(13) |
| O3 | 8e | 0.39500(4) | 0 | 0 | 1 | 0.013(13) |
| O4 | 8e | 0.08990(3) | 0 | 0 | 1 | 0.012(14) |

Tables SI and SII show the results of the single-crystal XRD. The structure was solved and refined using the Bruker SHELXTL Software Package with the space group Cmcm, La3Ni2O7. The final anisotropic full-matrix least-squares refinement on F2 with 37 variables converged at R1 = 8.62%, for the observed data and wR2 = 12.61% for all data. The goodness-of-fit was 0.997. The largest peak in the final difference electron density synthesis was 7.82 e-/Å3, and the largest hole was -2.74 e-/Å3 with an RMS deviation of 0.769 e-/Å3. Based on the final model, the calculated density was 7.098 g/cm3 and F (000), 1132 e-.

Fig. S1. Criterion of TDW and T’ based on the plots of dR/dT at different pressures. Fig. S1a shows the criterion (onset and offset value) of TSDW using dR/dT in the temperature range from 80 K to 150 K. Fig. S1b gives the criterion of T’ based on dR/dT in the temperature range from 10 K to 100 K.

Fig. S1 shows the criteria for the determination of TSDW and T’. The values of TSDW and T’ are given by the mean values of onset and offset, and the transition width is given by the half value of the difference of onset and offset.

Fig. S2. Normalized resistance (R(T)/R(150 K)) of La3Ni2O7-2222 under the different magnetic fields (Fig. S2a) and T’-H phase diagram (Fig. S2b) at 15.9 GPa. Fig. S2a shows the normalized resistance as a function of temperature under the different magnetic fields at 15.9 GPa. (Inset) The derivative of resistance as a function of temperature. Fig. S2b shows the temperature-magnetic field (T-H) phase diagram. The black symbols show the T’ values, and the red star symbols present the onset values. The red solid line gives the linear fit of T’, and the red dashed line presents the straight line across the onset values.