Supplementary File

Figure S1: Variation in weight loss of carbon steel coupons (left side) and corrosion inhibition (right side) versus the testing time; [a] in pure water, [b] in formation water, [c] in diesel fuel and [d] in sulfuric acid.

| [a] |  |  |
| --- | --- | --- |
| [b] |  |  |
| [c] |  |  |
| [d] |  |  |

Figure S2: Variation in weight loss of carbon steel coupons (left side) and corrosion inhibition (right side) versus the testing time at different temperature; [a] in pure water, [b] in formation water, [c] in diesel fuel and [d] in sulfuric acid.

| [a] |  |  |
| --- | --- | --- |
| [b] |  |  |
| [c] |  |  |
| [d] |  |  |

Table 1. List of the utilized chemical reagents and their suppliers.

| No. | Name of chemical reagent | Source and purity |
| --- | --- | --- |
| 1 | Styrene monomer | Fisher Chemical (USA), 99.5% |
| 2 | Potassium persulfate (KOOSO4) | Solvay Chemicals (USA),98 % |
| 3 | Anionic – alkyl sulfonates surfactant | Zschimmer&Schwars (Germany) |
| 4 | Zinc chloride (ZnCl2) | Sigma-Aldrich (Germany), 99.99% |
| 5 | Tri-ethyl amine (C2H5)3N | Fisher Chemical (USA), 99.0% |