Table 1. Top Ten Hits from Additive Algorithm’s FTIR Trial for Positive Controls and Environmental Microplastic "C2. Blue Fiber" (Tol: 15, 10, and 5 1/cm) Blue: Predicted presence of CP in different forms [40][29][19]. Orange: Predicted presence of colorless additives.

| CP | CA-CP | HDPE-CP | LDPE-CP | PP-CP | PS-CP | PET-CP | PA-CP | PMMA-CP- | PVC-CP- | FLOPP-E |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Copper Phthalocyanine Blue (Hummel, 2002)(T:15) Copper Phthalocyanine Blue (Hummel, 2002)(T:10) Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:5) | Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:15) Copper Phthalocyanine Blue (Hummel, 2002)(T:10) Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:5) | Copper Phthalocyanine Blue (Hummel, 2002)(T:15) Copper Phthalocyanine Blue (Hummel, 2002)(T:10) Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:5) | Copper Phthalocyanine Blue (Hummel, 2002)(T:15) Copper Phthalocyanine Blue (Hummel, 2002)(T:10) Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:5) | Copper Phthalocyanine Blue (Hummel, 2002)(T:15) Copper Phthalocyanine Blue (Hummel, 2002)(T:10) Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:5) | Copper Phthalocyanine Blue (Hummel, 2002)(T:15) Copper Phthalocyanine Blue (Hummel, 2002)(T:10) Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:5) | Copper Phthalocyanine Blue (Hummel, 2002)(T:15) Copper Phthalocyanine Blue (Hummel, 2002)(T:10) Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:5) | Copper Phthalocyanine Blue (Hummel, 2002)(T:15) Copper Phthalocyanine Blue (Hummel, 2002)(T:10) Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:5) | Zinc Iron Chloride Brown (IRUG, n.d.)(T:15) Copper Phthalocyanine Blue (Hummel, 2002)(T:10) Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:5) | Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:15) Copper Phthalocyanine Blue (Hummel, 2002)(T:10) Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:5) | Fatty acid triglycerol ester [Realube SI] (No Color - Lubricant) (Hummel, 2002)(T:15) Sodium 2,4,5,7-tetrabromofluorescein Red (Hummel, 2002)(T:10) "GRABIT" of Dioxazine Purple - [CHSOS](T:5) |
| Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:15) Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:10) Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:5) | Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:15) Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:10) Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:5) | Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:15) Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:10) Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:5) | Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:15) Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:10) Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:5) | Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:15) Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:10) Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:5) | Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:15) Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:10) Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:5) | Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:15) Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:10) Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:5) | Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:15) Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:10) Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:5) | Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:15) Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:10) Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:5) | Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:15) Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:10) Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:5) | Antimony nickel titanium oxide yellow (Hummel, 2002)(T:15) Priplast 3142 - Azelaic Polyester (Plasticizer - No Color) (Hummel, 2002)(T:10) 2,9-dichloro-7,14-dioxo-5,7,12,14-tetrahydroquinolino[2,3-b]acridine (N/A, most likely Magenta/Red) (Hummel, 2002)(T:5) |
| Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:15) Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:10) Copper Phthalocyanine Blue (Hummel, 2002)(T:5) | Copper Phthalocyanine Blue (Hummel, 2002)(T:15) Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:10) Copper Phthalocyanine Blue (Hummel, 2002)(T:5) | Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:15) Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:10) Copper Phthalocyanine Blue (Hummel, 2002)(T:5) | Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:15) Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:10) Copper Phthalocyanine Blue (Hummel, 2002)(T:5) | Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:15) Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:10) Copper Phthalocyanine Blue (Hummel, 2002)(T:5) | Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:15) Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:10) Copper Phthalocyanine Blue (Hummel, 2002)(T:5) | Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:15) Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:10) Copper Phthalocyanine Blue (Hummel, 2002)(T:5) | Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:15) Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:10) Copper Phthalocyanine Blue (Hummel, 2002)(T:5) | Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:15) Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:10) Copper Phthalocyanine Blue (Hummel, 2002)(T:5) | Copper Phthalocyanine Blue (Hummel, 2002)(T:15) Copper phthalocyanine (beta form) Blue (Hummel, 2002)(T:10) Copper Phthalocyanine Blue (Hummel, 2002)(T:5) | Antimony Nickel Titanium Oxide Yellow (Hummel, 2002)(T:15) Sodium 4-chloro-3-toluidine-6-sulfonic acid -> 2-naphthol Red (Hummel, 2002)(T:10) Di-i-butylphthalate (No Color - Plasticizer) (Hummel, 2002)(T:5) |
| Zinc Iron Chloride Brown (IRUG, n.d.)(T:15) Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color)(T:10) Tributyltin oxide (Biocide - No Color) (Hummel, 2002)(T:5) | Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:15) Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:10) Benzenesulfonohydrazide (Blowing Agent - No Color) (Hummel, 2002)(T:5) | Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:15) Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:10) Benzenesulfonohydrazide (Blowing Agent - No Color) (Hummel, 2002)(T:5) | Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:15) Phthalocyanine, halogenated, metalfree [Heliogen Blau LG] Blue (Hummel, 2002)(T:10) Priplast 3142 - Azelaic Polyester (Plasticizer - No Color) (Hummel, 2002)(T:5) | Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:15) Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:10) Tributyltin oxide (Biocide - No Color) (Hummel, 2002)(T:5) | Zinc Iron Chloride Brown (IRUG, n.d.)(T:15) 2,4-xylyldiphenylphosphate (No Color - Plasticizer) (Hummel, 2022)(T:10) Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:5) | Zinc Iron Chloride Brown (IRUG, n.d.)(T:15) Phthalocyanine, halogenated, metalfree [Heliogen Blau LG] Blue (Hummel, 2002)(T:10) Benzenesulfonohydrazide (Blowing Agent - No Color) (Hummel, 2002)(T:5) | Zinc Iron Chloride Brown (IRUG, n.d.)(T:15) Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:10) 4-4-bis(1-amino-9,10-anthraquinonediyl) on calcium carbonate Red (Hummel, 2002)(T:5) | Copper phthalocyanine (alpha form) Blue (Hummel, 2002)(T:15) 2,4-xylyldiphenylphosphate (No Color - Plasticizer) (Hummel, 2022)(T:10) Aluminum Hydroxysilicate (Filler - No Color) (Hummel, 2002)(T:5) | PY 110 - Isoindolinone Yellow "GRABIT"(T:15) Phthalocyanine, halogenated, metalfree [Heliogen Blau LG] Blue (Hummel, 2002)(T:10) Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:5) | Pentaerythrol fatty ester [Loxiol EP 861] (No Color - Lubricant) (Hummel, 2002)(T:15) 2,2'-(2,5-thiophenediyl)-bis(5-t-butylbenzoxazole) (Whitening Agent - Yellow) (Hummel, 2002)(T:10) Di(C6-C10-aIkyl)phthalate (No Color - Plasticizer) (Hummel, 2002)(T:5) |
| Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color)(T:15) Tributyltin oxide (Biocide - No Color) (Hummel, 2002)(T:10) Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:5) | Triphenylphosphite (PVC-stabilizer - No Color) (Hummel, 2002)(T:15) 2,4-xylyldiphenylphosphate (No Color - Plasticizer) (Hummel, 2022)(T:10) Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:5) | Zinc Iron Chloride Brown (IRUG, n.d.)(T:15) Phthalocyanine, halogenated, metalfree [Heliogen Blau LG] Blue (Hummel, 2002)(T:10) Tributyltin oxide (Biocide - No Color) (Hummel, 2002)(T:5) | Zinc Iron Chloride Brown (IRUG, n.d.)(T:15) Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:10) Benzenesulfonohydrazide (Blowing Agent - No Color) (Hummel, 2002)(T:5) | Zinc Iron Chloride Brown (IRUG, n.d.)(T:15) Phthalocyanine, halogenated, metalfree [Heliogen Blau LG] Blue (Hummel, 2002)(T:10) Tributyltin oxide (Biocide - No Color) (Hummel, 2002)(T:5) | Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:15) Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:10) 2,4-xylyldiphenylphosphate (No Color - Plasticizer) (Hummel, 2022)(T:5) | Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:15) Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:10) Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:5) | Zinc dibenzyldithiocarbamate (Accelerator - No Color) (Hummel, 2002)(T:15) N-phenyl-2-naphthylamine (Antioxidant - Violet-Brown) (Hummel, 2002)(T:10) Nickel 3,5-di-t-butyl-4-hydroxybenzyl phosphonic acid monoethylester (Stabilizer - Yellow/Green) (Hummel, 2002)(T:5) | Copper Phthalocyanine Blue (Hummel, 2002)(T:15) Dibenzimidazolo( 1,2-e,1 ',2'-m)-4,9-diaza-3,8- pyrenequinone Orange (Hummel, 2002)(T:10) 2,2'-methylene-bis(6-t-butyl-4-methylphenol) (Reinforcing Resin - Red) (Hummel, 2002)(T:5) | Pyranthrone Orange (Hummel, 2002)(T:15) 2,2'-ethylene-bis(4,6-di-t-butylphenyl)fluorophosphite (Stabilizer/Antioxidant - White) (Hummel, 2002)(T:10) Copper hexadecachlorophthalocyanine Green (Hummel, 2002)(T:5) | Sulfur-containing Sodium-Aluminum Silicate Blue (Hummel, 2002)(T:15) 4-4-bis(1-amino-9,10-anthraquinonediyl) on calcium carbonate Red (Hummel, 2002)(T:10) Dimethylphthalate (No Color - Plasticizer) (Hummel, 2002)(T:5) |
| 7,9,12-tribromopyranthrone Orange (Hummel, 2002)(T:15) Phthalocyanine, halogenated, metalfree [Heliogen Blau LG] Blue (Hummel, 2002)(T:10) Trimethylolpropane Isostearate Adipate (Plasticizer - No Color) (Hummel, 2002)(T:5) | Pyranthrone Orange (Hummel, 2002)(T:15) Phthalocyanine, halogenated, metalfree [Heliogen Blau LG] Blue (Hummel, 2002)(T:10) Nickel 3,5-di-t-butyl-4-hydroxybenzyl phosphonic acid monoethylester (Stabilizer - Yellow/Green) (Hummel, 2002)(T:5) | 7,9,12-tribromopyranthrone Orange (Hummel, 2002)(T:15) Triheptyltrimellitate (No Color - Plasticizer) (Hummel, 2022)(T:10) Trimethylolpropane Isostearate Adipate (Plasticizer - No Color) (Hummel, 2002)(T:5) | 7,9,12-tribromopyranthrone Orange (Hummel, 2002)(T:15) Triheptyltrimellitate (No Color - Plasticizer) (Hummel, 2022)(T:10) Tributyltin oxide (Biocide - No Color) (Hummel, 2002)(T:5) | 7,9,12-tribromopyranthrone Orange (Hummel, 2002)(T:15) 2,4-xylyldiphenylphosphate (No Color - Plasticizer) (Hummel, 2022)(T:10) Priplast 3142 - Azelaic Polyester (Plasticizer - No Color) (Hummel, 2002)(T:5) | 2,4-xylyldiphenylphosphate (No Color - Plasticizer) (Hummel, 2022)(T:15) Triphenylphosphate (No Color - Plasticizer) (Hummel, 2022)(T:10) Tetrabenzylthiuramdisulfide (Accelerator - No Color) (Hummel, 2002)(T:5) | Phthalocyanine, halogenated, metalfree [Heliogen Blau LG] Blue (Hummel, 2002)(T:15) 2,4-xylyldiphenylphosphate (No Color - Plasticizer) (Hummel, 2022)(T:10) Trimethylolpropane Isostearate Adipate (Plasticizer - No Color) (Hummel, 2002)(T:5) | Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:15) N-butylbenzenesulfonamide (No Color - Plasticizer) (Hummel, 2022)(T:10) Priplast 3142 - Azelaic Polyester (Plasticizer - No Color) (Hummel, 2002)(T:5) | Tetraethylthiuramdisulfide (Accelerator - No Color) (Hummel, 2002)(T:15) Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:10) Dibenzimidazolo( 1,2-e,1 ',2'-m)-4,9-diaza-3,8- pyrenequinone Orange (Hummel, 2002)(T:5) | Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:15) Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:10) Barium zinc ester carboxylate [Swedstab 502] (PVC-stabilizer - No Color) (Hummel, 2002)(T:5) | Sodium 4-chloro-3-toluidine-6-sulfonic acid -> 2-naphthol Red (Hummel, 2002)(T:15) Indanthrone Blue (Hummel, 2002)(T:10) Dibutylphthalate (No Color - Plasticizer) (Hummel, 2002)(T:5) |
| Pyranthrone Orange (Hummel, 2002)(T:15) 2,4-xylyldiphenylphosphate (No Color - Plasticizer) (Hummel, 2022)(T:10) Nickel 3,5-di-t-butyl-4-hydroxybenzyl phosphonic acid monoethylester (Stabilizer - Yellow/Green) (Hummel, 2002)(T:5) | PY 110 - Isoindolinone Yellow "GRABIT"(T:15) Pyranthrone Orange (Hummel, 2002)(T:10) 2,4-xylyldiphenylphosphate (No Color - Plasticizer) (Hummel, 2022)(T:5) | Pyranthrone Orange (Hummel, 2002)(T:15) 2,4-xylyldiphenylphosphate (No Color - Plasticizer) (Hummel, 2022)(T:10) Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:5) | Pyranthrone Orange (Hummel, 2002)(T:15) Tributyltin oxide (Biocide - No Color) (Hummel, 2002)(T:10) Trimethylolpropane Isostearate Adipate (Plasticizer - No Color) (Hummel, 2002)(T:5) | Pyranthrone Orange (Hummel, 2002)(T:15) 4'-nitrophenyl(3-amino-4-methoxyphenyl)sulfonate -> 2-hydroxynaphthoic arylide-2- methylanilide Red (Hummel, 2002)(T:10) Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:5) | 7,9,12-tribromopyranthrone Orange (Hummel, 2002)(T:15) i-decyldiphenyl phosphite (PVC-stabilizer - No Color) (Hummel, 2002)(T:10) i-decyldiphenyl phosphite (PVC-stabilizer - No Color) (Hummel, 2002)(T:5) | PY 110 - Isoindolinone Yellow "GRABIT"(T:15) Epoxidized octanoic ester (Stabilizer - Light-Yellow) (Hummel, 2002)(T:10) Fatty acid ester + acid [Baerolub L-PO-1] (No Color - Lubricant) (Hummel, 2002)(T:5) | 3-chloroaniline -> 2-hydroxynaphthoic arylide-2-methoxyanilide Orange (Hummel, 2002)(T:15) Phthalocyanine, halogenated, metalfree [Heliogen Blau LG] Blue (Hummel, 2002)(T:10) Ni-dibutyldithiocarbamate (Antioxidant - Green) (Hummel, 2002)(T:5) | Triphenylphosphate (No Color - Plasticizer) (Hummel, 2022)(T:15) 2,2'-ethylene-bis(4,6-di-t-butylphenyl)fluorophosphite (Stabilizer/Antioxidant - White) (Hummel, 2002)(T:10) Priplast 3142 - Azelaic Polyester (Plasticizer - No Color) (Hummel, 2002)(T:5) | 7,9,12-tribromopyranthrone Orange (Hummel, 2002)(T:15) Triphenylphosphite (PVC-stabilizer - No Color) (Hummel, 2002)(T:10) Tributyltin oxide (Biocide - No Color) (Hummel, 2002)(T:5) | ox-Hydrocarbon Wax [Baerolub L-AX] (No Color - Lubricant) (Hummel, 2022)(T:15) tris(nonylphenyl)phosphite (Antioxidant - Yellow) (Hummel, 2002)(T:10) Dihexylphthalate (No Color - Plasticizer) (Hummel, 2002)(T:5) |
| 2,7-dibromoanthanthrone Red (Hummel, 2002)(T:15) 2,2'-ethylene-bis(4,6-di-t-butylphenyl)fluorophosphite (Stabilizer/Antioxidant - White) (Hummel, 2002)(T:10) Priplast 3142 - Azelaic Polyester (Plasticizer - No Color) (Hummel, 2002)(T:5) | 7,9,12-tribromopyranthrone Orange (Hummel, 2002)(T:15) 1,3-bis(t-butylperoxy-2-propyl)benzene (Crosslinking Agent - No Color) (Hummel, 2002)(T:10) Priplast 3142 - Azelaic Polyester (Plasticizer - No Color) (Hummel, 2002)(T:5) | PY 110 - Isoindolinone Yellow "GRABIT"(T:15) Tributyltin oxide (Biocide - No Color) (Hummel, 2002)(T:10) Priplast 3142 - Azelaic Polyester (Plasticizer - No Color) (Hummel, 2002)(T:5) | Phthalocyanine, halogenated, metalfree [Heliogen Blau LG] Blue (Hummel, 2002)(T:15) 7,9,12-tribromopyranthrone Orange (Hummel, 2002)(T:10) Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002)(T:5) | Aliphatic-aromatic polyester based on phthalic acid (Plastificator for rubber processing/Nitrile Rubber Additive - No Color) (Hummel, 2002)(T:15) Tributyltin oxide (Biocide - No Color) (Hummel, 2002)(T:10) 2,5-di-t-pentylhydroquinone (Antioxidant - Yellow to Grey-White) (Hummel, 2002)(T:5) | Triphenylphosphate (No Color - Plasticizer) (Hummel, 2022)(T:15) N-butylbenzenesulfonamide (No Color - Plasticizer) (Hummel, 2022)(T:10) Benzenesulfonohydrazide (Blowing Agent - No Color) (Hummel, 2002)(T:5) | 7,9,12-tribromopyranthrone Orange (Hummel, 2002)(T:15) Triheptyltrimellitate (No Color - Plasticizer) (Hummel, 2022)(T:10) N-butylbenzenesulfonamide (No Color - Plasticizer) (Hummel, 2022)(T:5) | 2,2'-ethylene-bis(4,6-di-t-butylphenyl)fluorophosphite (Stabilizer/Antioxidant - White) (Hummel, 2002)(T:15) Ni-dibutyldithiocarbamate (Antioxidant - Green) (Hummel, 2002)(T:10) Tetrabenzylthiuramdisulfide (Accelerator - No Color) (Hummel, 2002)(T:5) | i-decyldiphenyl phosphite (PVC-stabilizer - No Color) (Hummel, 2002)(T:15) Triheptyltrimellitate (No Color - Plasticizer) (Hummel, 2022)(T:10) Trimethylolpropane Isostearate Adipate (Plasticizer - No Color) (Hummel, 2002)(T:5) | 1,3-bis(t-butylperoxy-2-propyl)benzene (Crosslinking Agent - No Color) (Hummel, 2002)(T:15) Epoxidized octanoic ester (Stabilizer - Light-Yellow) (Hummel, 2002)(T:10) Trimethylolpropane Isostearate Adipate (Plasticizer - No Color) (Hummel, 2002)(T:5) | Priplast 3142 - Azelaic Polyester (Plasticizer - No Color) (Hummel, 2002)(T:15) 2-trifluoromethylaniline -> 5-N-acetoacetylamino-benzimidazolone Yellow (Hummel, 2002)(T:10) 1,8-bis(thiophenyl)-9,10-anthraquinone Yellow (Hummel, 2002)(T:5) |
| PY 110 - Isoindolinone Yellow "GRABIT"(T:15) 7,9,12-tribromopyranthrone Orange (Hummel, 2002)(T:10) Benzenesulfonohydrazide (Blowing Agent - No Color) (Hummel, 2002)(T:5) | Tris(nonylphenyl)phosphite (Stabilizer - No Color) (Hummel, 2002)(T:15) 7,9,12-tribromopyranthrone Orange (Hummel, 2002)(T:10) Barium zinc ester carboxylate [Swedstab 502] (PVC-stabilizer - No Color) (Hummel, 2002)(T:5) | Phthalocyanine, halogenated, metalfree [Heliogen Blau LG] Blue (Hummel, 2002)(T:15) 7,9,12-tribromopyranthrone Orange (Hummel, 2002)(T:10) N-butylbenzenesulfonamide (No Color - Plasticizer) (Hummel, 2022)(T:5) | PY 110 - Isoindolinone Yellow "GRABIT"(T:15) N-butylbenzenesulfonamide (No Color - Plasticizer) (Hummel, 2022)(T:10) N-butylbenzenesulfonamide (No Color - Plasticizer) (Hummel, 2022)(T:5) | Triphenylphosphate (No Color - Plasticizer) (Hummel, 2022)(T:15) 2,5-di-t-pentylhydroquinone (Antioxidant - Yellow to Grey-White) (Hummel, 2002)(T:10) Barium zinc ester carboxylate [Swedstab 502] (PVC-stabilizer - No Color) (Hummel, 2002)(T:5) | PY 110 - Isoindolinone Yellow "GRABIT"(T:15) i-decyldiphenylphosphate (No Color - Plasticizer) (Hummel, 2022)(T:10) Tributyltin oxide (Biocide - No Color) (Hummel, 2002)(T:5) | Pyranthrone Orange (Hummel, 2002)(T:15) i-alkylepoxystearate (Plasticizer - No Color) (Hummel, 2002)(T:10) Tributyltin oxide (Biocide - No Color) (Hummel, 2002)(T:5) | Tetrabenzylthiuramdisulfide (Accelerator - No Color) (Hummel, 2002)(T:15) 2,2'-ethylene-bis(4,6-di-t-butylphenyl)fluorophosphite (Stabilizer/Antioxidant - White) (Hummel, 2002)(T:10) Pentadecanesulfonic acid phenol/Crestol esters [Mesamoll] (No Color - Plasticizer) (Hummel, 2022)(T:5) | 5,5' -dichloro-7,7' -dimethylthioindigo Purple (Hummel, 2002)(T:15) Phthalocyanine, halogenated, metalfree [Heliogen Blau LG] Blue (Hummel, 2002)(T:10) 1,3-bis(t-butylperoxy-2-propyl)benzene (Crosslinking Agent - No Color) (Hummel, 2002)(T:5) | Phthalocyanine, halogenated, metalfree [Heliogen Blau LG] Blue (Hummel, 2002)(T:15) 2,4-xylyldiphenylphosphate (No Color - Plasticizer) (Hummel, 2022)(T:10) 1,3-bis(t-butylperoxy-2-propyl)benzene (Crosslinking Agent - No Color) (Hummel, 2002)(T:5) | N-butylbenzenesulfonamide (No Color - Plasticizer) (Hummel, 2022)(T:15) Phthalocyanine, halogenated, metalfree [Heliogen Blau LG] Blue (Hummel, 2002)(T:10) Zinc benzothiazolemercaptide (Vulcanization Accelerator - No Color) (Hummel, 2002)(T:5) |
| Triphenylphosphate (No Color - Plasticizer) (Hummel, 2022)(T:15) N-phenyl-2-naphthylamine (Antioxidant - Violet-Brown) (Hummel, 2002)(T:10) 2,7-dibromoanthanthrone Red (Hummel, 2002)(T:5) | Aliphatic-aromatic polyester based on phthalic acid (Plastificator for rubber processing/Nitrile Rubber Additive - No Color) (Hummel, 2002)(T:15) "2,2'-ethylene-bis(4,6-di-t-butylphenyl)fluorophosphite (Stabilizer/Antioxidant - White) (Hummel, 2002)"(T:10) Tributyltin oxide (Biocide - No Color) (Hummel, 2002)(T:5) | N,N-dimethylethanolamine (Curing agent/activator - No Color) (Hummel, 2002)(T:15) N-butylbenzenesulfonamide (No Color - Plasticizer) (Hummel, 2022)(T:10) Phthalocyanine, halogenated, metalfree [Heliogen Blau LG] Blue (Hummel, 2002)(T:5) | N,N-dimethylethanolamine (Curing agent/activator - No Color) (Hummel, 2002)(T:15) N-phenyl-2-naphthylamine (Antioxidant - Violet-Brown) (Hummel, 2002)"(T:10) Cadmium Sulfide/Cadmium Selenide w/ Barium Sulfate Red (Hummel, 2002)(T:5) | 4'-nitrophenyl(3-amino-4-methoxyphenyl)sulfonate -> 2-hydroxynaphthoic arylide-2- methylanilide Red (Hummel, 2002)(T:15) Vulkanol FH - Polyether w/ Ester and Alcoholic Groups (Plasticizer - No Color) (Hummel, 2002)(T:10) N-butylbenzenesulfonamide (No Color - Plasticizer) (Hummel, 2022)(T:5) | Dipropylphthalate (No Color - Plasticizer) (Hummel, 2002)(T:15) 7,9,12-tribromopyranthrone Orange (Hummel, 2002)(T:10) Tributyltin oxide (Biocide - No Color) (Hummel, 2002)(T:5) | 2,7-dibromoanthanthrone Red (Hummel, 2002)(T:15) Epoxidized soybean oil (PVC-Costabilizer - No Color) (Hummel, 2002)(T:10) 1,3-bis(t-butylperoxy-2-propyl)benzene (Crosslinking Agent - No Color) (Hummel, 2002)(T:5) | N-phenyl-2-naphthylamine (Antioxidant - Violet-Brown) (Hummel, 2002)(T:15) Zinc N-butyldithiocarbamate (Accelerator - Light Grey) (Hummel, 2002)(T:10) Benzenesulfonohydrazide (Blowing Agent - No Color) (Hummel, 2002)(T:5) | 4,4'-methylene-bis(2,6-di-t-butylphenol) (2) (Antioxidant - Yellow) (Hummel, 2002)(T:15) 1,3-bis(t-butylperoxy-2-propyl)benzene (Crosslinking Agent - No Color) (Hummel, 2002)(T:10) 2,5-di-t-pentylhydroquinone (Antioxidant - Yellow to Grey-White) (Hummel, 2002)(T:5) | 2,7-dibromoanthanthrone Red (Hummel, 2002)(T:15) Copper hexadecachlorophthalocyanine Green (Hummel, 2002)(T:10) Benzenesulfonohydrazide (Blowing Agent - No Color) (Hummel, 2002)(T:5) | Tri(C6-C8-alkyl)trimellitate (No Color - Plasticizer) (Hummel, 2022)(T:15) 6,14-dichloro-1,9-dibromopyranthrone Red (Hummel, 2002)(T:10) tris(nonylphenyl)phosphite (Antioxidant - Yellow) (Hummel, 2002)(T:5) |

Table 2. Top Ten Hits from Additive Algorithm’s Raman Trial for Positive Controls and Environmental Microplastic "Polyester 12. Red Fiber" (Tol: 15, 10, and 5 1/cm). Red: Predicted presence of pyrroles [41][30][31][32][33][34][35][36][37][38][39]. Green: Predicted presence of quinones.

| DPP | CA + DPP | HDPE + DPP | LDPE + DPP | PP + DPP | PS + DPP | PET + DPP | PA + DPP | PMMA + DPP | PVC + DPP | SLOPP-E Entry |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PO73 (Pyrrole) Muscovite - Colorless - KAl2(AlSi3O10)(F,OH)2 (Mineral) PR88 (Thioindigo) | PR67 (Azo) PR254 (Pyrrole) PR270 (Pyrrole) | PY154 (Azo) Muscovite - Colorless - KAl2(AlSi3O10)(F,OH)2 (Mineral) PR88 (Thioindigo) | PO73 (Pyrrole) Muscovite - Colorless - KAl2(AlSi3O10)(F,OH)2 (Mineral) PR88 (Thioindigo) | PR40 (Azo) Muscovite - Colorless - KAl2(AlSi3O10)(F,OH)2 (Mineral) PR88 (Thioindigo) | Muscovite - Colorless - KAl2(AlSi3O10)(F,OH)2 (Mineral) PR264 (Pyrrole) PR270 (Pyrrole) | PR270 (Pyrrole) PR270 (Pyrrole) PR270 (Pyrrole) | PY5(Azo) PR270(Pyrrole) PR270(Pyrrole) | PR270 (Pyrrole) PR270 (Pyrrole) PR88 (Pyrrole) | PR254 (Pyrrole) PR254 (Pyrrole) PR270 (Pyrrole) | PR176 (Azo) PG8 (Metal Naphthoquinone) PG12 (Naphthoquinone) |
| PR270 (Pyrrole) PR270 (Pyrrole) Muscovite - Colorless - KAl2(AlSi3O10)(F,OH)2 (Mineral) | PR51 (Azo) PR67 (Azo) PR255 (Pyrrole) | PR254 (Pyrrole) PR270 (Pyrrole) Muscovite - Colorless - KAl2(AlSi3O10)(F,OH)2 (Mineral) | PR254 (Pyrrole) PR254 (Pyrrole) Muscovite - Colorless - KAl2(AlSi3O10)(F,OH)2 (Mineral) | PR67 (Azo) PR270 (Pyrrole) Muscovite - Colorless - KAl2(AlSi3O10)(F,OH)2 (Mineral) | PR51 (Azo) PR270 (Pyrrole) PR255 (Pyrrole) | PY100 (Azo) PR255 (Pyrrole) PR255 (Pyrrole) | PO73 (Pyrrole) PR254 (Pyrrole) PR255 (Pyrrole) | PR254 (Pyrrole) PR51 (Pyrrole) Muscovite - Colorless - KAl2(AlSi3O10)(F,OH)2 (Mineral) | PO73 (Pyrrole) PR270 (Pyrrole) Muscovite - Colorless - KAl2(AlSi3O10)(F,OH)2 (Mineral) | PR184 (Azo) PR4 (Azo) PG8 (Metal Naphthoquinone) |
| PR254 (Pyrrole) PR254 (Pyrrole) PR270 (Pyrrole) | PO46 (Azo) PR51 (Azo) PR62 (Double Azo) | PR270 (Pyrrole) PR254 (Pyrrole) PR270 (Pyrrole) | PR264 (Pyrrole) PR264 (Pyrrole) PR270 (Pyrrole) | PY4 (Azo) PR254 (Pyrrole) PR270 (Pyrrole) | PR264 (Pyrrole) PR255 (Pyrrole) Muscovite - Colorless - KAl2(AlSi3O10)(F,OH)2 (Mineral) | PR255 (Pyrrole) PR51 (Pyrrole) Muscovite - Colorless - KAl2(AlSi3O10)(F,OH)2 (Mineral) | PR270 (Pyrrole) PR264 (Pyrrole) PR254 (Pyrrole) | PO73 (Pyrrole) PR255 (Pyrrole) PR270 (Pyrrole) | PR270 (Pyrrole) PR51 (Azo) PR255 (Pyrrole) | PR12 (Azo) PY5(Azo) PY213 (Azo) |
| PR51 (Azo) PR255 (Pyrrole) PR255 (Pyrrole) | PR254 (Pyrrole) PR270 (Pyrrole) PR251 (Azo) | PBr42 (Double Azo) PR67 (Azo) PR255 (Pyrrole) | PR270 (Pyrrole) PR270 (Pyrrole) PR255 (Pyrrole) | PR51 (Azo) PR62 (Double Azo) PR255 (Pyrrole) | PY147 (Anthraquinone) PR51 (Azo) PY50 (Azo) | PO17 (Azo) PR254 (Pyrrole) PR251 (Azo) | PR254 (Pyrrole) PY16 (Double Azo) PR172 (Xanthene) | PR51 (Azo) PR254 (Pyrrole) PR255 (Pyrrole) | PO17 (Azo) PR264 (Pyrrole) PR51 (Azo) | PY153 (Dioxime Nickel Complex) PO61 (Azo) PR4 (Azo) |
| PR255 (Pyrrole) PR51 (Azo) PR172 (Xanthene) | PY4 (Azo) PR62(Double Azo) PO71 (Pyrrole) | PR264 (Pyrrole) PR264 (Pyrrole) PO31 (Double Azo) | PR255 (Pyrrole) PR255 (Pyrrole) PR264 (Pyrrole) | PO73 (Pyrrole) PBr42 (Double Azo) PR251 (Azo) | PR251 (Azo) PR254 (Pyrrole) PR251 (Azo) | PR264 (Pyrrole) PY100 (Azo) PO71 (Pyrrole) | PY154 (Azo) PR255 (Pyrrole) PR264(Pyrrole) | PY120 (Azo) PR67 (Azo) PR172 (Xanthene) | PR255 (Pyrrole) PR255 (Pyrrole) PY75 (Azo) | PR162 (Azo) PY213 (Azo) PR146 (Azo) |
| PR264 (Pyrrole) PR264 (Pyrrole) PR254 (Pyrrole) | PO73 (Pyrrole) PO73 (Pyrrole) PY17 (Double Azo) | PO73 (Pyrrole) PR255 (Pyrrole) PY116 (Azo) | PY154 (Azo) PY153 (Dioxime Nickel Complex) PO71 (Pyrrole) | PR58_4 (Azo) PR67 (Azo) PR85 (Anthraquinone) | PY50 (Azo) PR62 (Double Azo) PO71 (Pyrrole) | PO46 (Azo) PR264 (Pyrrole) PR264 (Pyrrole) | PR264(Pyrrole) PO73 (Pyyrole) PR251 (Azo) | PR67 (Azo) PR264 (Pyrrole) PR251 (Azo) | PY194 (Azo) PO73 (Pyrrole) PO31 (Double Azo) | PO74 (Azo) PY3 (Azo) PR213 (Azo) |
| PR120 (Azo) PO73 (Pyrrole) PR251 (Azo) | PR58_4 (Azo) PR264 (Pyrrole) PR67 (Azo) | PR58_4 (Azo) PBr42 (Double Azo) PY75 (Azo) | PY5 (Azo) PO73 (Pyrrole) PR254 (Pyrrole) | PR58 (Azo) PR51 (Azo) PY209_1 (Azo Metal Salt) | PY5 (Azo) PY212 (Anthraquinone-Azo) PY209_1 (Azo Metal Salt) | PO73 (Pyrrole) PR168 (Anthraquinone) PR49_1 (Azo) | PY16 (Double Azo) PR51 (Azo) PY5 (Azo) | PO46 (Azo) PY153 (Dioxime Nickel Complex) PO31 (Double Azo) | PR58_4 (Azo) PO17 (Azo) PR172(Xanthene) | PR245 (Azo) PR245 (Azo) PR184 (Azo) |
| PY100 (Azo) PR62 (Double Azo) PO71 (Pyrrole) | PR58 (Azo) PY16 (Double Azo) PR85 (Anthraquinone) | PR58 (Azo) PR51 (Single Azo) PO62 (Single azo) | PV13 (Azo) PR51 (Azo) PR172 (Xanthene) | PR270 (Pyrrole) PR255 (Pyrrole) PO31 (Double Azo) | PR255 (Pyrrole) PR251 (Azo) PR254 (Pyrrole) | PY147 (Anthraquinone) PY212 (Anthraquinone-Azo) PR49 (Azo) | PO2 (Azo) PY5 (Azo) PO31 (Double Azo) | PR37 (Double Azo) PR62 (Double Azo) PR168 (Anthraquinone) | PR58 (Azo) PR62 (Double Azo) PR185 (Azo) | PR8 (Azo) PR8 (Azo) PY77 (Double Azo) |
| PO71 (Pyrrole) PR67 (Azo) PO13 (Double Azo) | PY206 (Azo) PR255 (Pyrrole) PR51 (Azo) | PR245 (Pyrrole) PY153 (Dioxime Nickel Complex) PBk1 (Azine) | PR67 (Azo) PY212 (Anthraquinone-Azo) PY154 (Azo) | PR60_1 (Azo) PR99 (Azo) PR172 (Xanthene) | PO73 (Pyrrole) PY50 (Azo) PR62 (Double Azo) | PY154 (Azo) PR62 (Double Azo) PY209_1 (Azo Metal Salt) | PY80 (Double Azo - due to being a Diarylide) PY152 (Double Azo) PR51 (Azo) | PO2 (Azo) PO73 (Pyrrole) PY212 (Anthraquinone-Azo) | PO71 (Pyrrole) PY111 (Azo) PR264 (Pyrrole) | PR208 (Azo) PY82 (Azo) PR64 (Azo) |
| PR58_4 (Azo) PY212 (Anthraquinone-Azo) PO31 (Double Azo) | PY194 (Azo) PY4 (Azo) PR60 (Azo) | PR40 (Azo) PO73 (Pyrrole) PR251 (Azo) | PR37 (Double Azo) PY77 (Double Azo) PO31 (Double Azo) | PY5 (Azo) PO73 (Pyrrole) PR168 (Anthraquinone) | PR67 (Azo) PY62 (Azo) PR173 (Xanthene) | PR254 (Pyrrole) PO13 (Double Azo) PO68 (Heterocycle) | PY120 (Azo) PR99 (Azo) PY75 (Azo) | PY206 (Azo) PR99 (Azo) PBk1 (Azine) | PR264 (Pyrrole) PO71 (Pyrrole) PV23 (Dioxazine) | PR258 (Azo) PR12 (Azo) PR268 (Azo) |

Table 3. Extended Additive Algorithm Study of Randomly Selected Samples of Each Color in FLOPP-E Database [19]

[29].

| Sample Name | Best Match | Tol (1/cm) | Pos. | Score |
| --- | --- | --- | --- | --- |
| C1_BlackFiber | N-(dichlorofluoromethylthio)phthalimide (Biocide - No Color) | 10 | 9 | 0.001912 |
| C4_GreenFiber | Viridian Green | 5 | 3 | 0.02551 |
| C6_RedFiber | 4-nitroaniline -> 2-naphthol Red | 5 | 8 | 0.000609 |
| C10_GreyFiber | Titanium Dioxide White (Hummel, 2002) | 5 | 4 | 0.006378 |
| C11_PinkFiber | 6,6' -dichloro-4,4' -dimethylthioindigo Pink | 15 | 7 | 0.005058 |
| C12_OrangeFiber | 3-chloroaniline -> 2-hydroxynaphthoic arylide-2-methoxyanilide Orange (Hummel, 2002) | 5 | 6 | 0.000566 |
| PE10_BlueFragment | Barium Permanganate and Barium Sulfate Blue (Hummel, 2002) | 15 | 6 | 0.032653 |
| PE11_GreenFragment | Viridian Green (Hummel, 2002) | 15 | 7 | 0.005434 |
| PE12_WhiteFilm | Benzenesulfonohydrazide (Blowing Agent - No Color) (Hummel, 2002) | 5 | 2 | 0.011338 |
| PE20_YellowFragment | Antimony nickel titanium oxide yellow (Hummel, 2002) | 5 | 4 | 0.011338 |
| PE23_PurpleFilm | Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002) | 5 | 9 | 0.000643 |
| PE31_OrangeFragment | 7,9,12-tribromopyranthrone Orange (Hummel, 2002) | 10 | 9 | 0.001146 |
| PE33_BrownFragment | Dicumylperoxide (Crosslinker - No Color) (Hummel, 2002) | 5 | 1 | 0.01666 |
| PE35_BlackFragment | Benzenesulfonohydrazide (Blowing Agent - No Color) (Hummel, 2002) | 5 | 1 | 0.05102 |
| PE38_GreyFragment | Benzenesulfonohydrazide (Blowing Agent - No Color) (Hummel, 2002) | 5 | 4 | 0.000556 |
| PE40_ClearFragment | Benzenesulfonohydrazide (Blowing Agent - No Color) (Hummel, 2002) | 5 | 2 | 0.05102 |
| PE46_PinkFragment | 6,6' -dichloro-4,4' -dimethylthioindigo Pink (Hummel, 2002) | 15 | 7 | 0.003354 |
| PE47_RedFragment | 6,14-dichloro-1,9-dibromopyranthrone Red (Hummel, 2002) | 10 | 8 | 0.001633 |
| PET5_BlueFragment | 2-mercaptobenzothiazole + tetramethylthiuramdisulfide (Vulcanization Accelerator - No Color) (Hummel, 2002) | 5 | 7 | 0.000493 |
| PET9_YellowFiberBundle | Antimony nickel titanium oxide yellow (Hummel, 2002) | 5 | 3 | 0.004082 |
| PET10_PurpleFiberBundle | 2-mercaptobenzothiazole + tetramethylthiuramdisulfide (Vulcanization Accelerator - No Color) (Hummel, 2002) | 5 | 3 | 0.000567 |
| PET16_RedFilm | 4-nitro-2-toluidine -> 2-hydroxynaphthoic arylide-2-methylanilide Red (Hummel, 2002) | 5 | 4 | 0.000424 |
| PET17_ OrangeFilm | N,N'-dicyclohexyl-2-benzothiazolesulfanemide (Accelerator - No Color) (Hummel, 2002) | 5 | 3 | 0.000548 |
| PET18_BlackFiber | N,N'-dicyclohexyl-2-benzothiazolesulfanemide (Accelerator - No Color) (Hummel, 2002)" | 5 | 10 | 0.000396 |
| PET19_GreenFiber | Copper hexabromodecachlorophthalocyanine Green (2) (Hummel, 2002) | 5 | 4 | 0.011338 |
| PET21_ClearFragment | N,N-dimethylethanolamine (Curing agent/activator - No Color) (Hummel, 2002) | 5 | 1 | 0.02551 |
| PMMA1_OrangeFragment | Benzenesulfonohydrazide (Blowing Agent - No Color) (Hummel, 2002) | 5 | 5 | 0.000715 |
| PMMA2_RedFiber | Aromatic-aliphatic sulfonamide (Vulcanization Retarder - No Color) (Hummel, 2002) | 5 | 8 | 0.000438 |
| PP10_YellowFragment | Antimony nickel titanium oxide yellow (Hummel, 2002) | 5 | 4 | 0.012755 |
| PP12_WhiteFragment | Titanium Dioxide White (Hummel, 2002) | 10 | 8 | 0.006378 |
| PP18_GreyFragment | Titanium Dioxide White (Hummel, 2002) | 15 | 7 | 0.005434 |
| PP29_GreenFragment | 16,17 -dimethoxyviolanthrone Green (Hummel, 2002) | 5 | 6 | 0.000531 |
| PP31_PurpleFragment | Phenoxazine Purple (Hummel, 2002) | 5 | 9 | 0.000494 |
| PP34_BrownFilm | 2,5-dichloroaniline -> 2-hydroxynaphthoic arylide-2,5-dimethoxyanilide Brown (Hummel, 2002) | 15 | 6 | 0.003559 |
| PP35_ClearFilm | N-(dichlorofluoromethylthio)phthalimide (Biocide - No Color) (Hummel, 2002) | 5 | 9 | 0.000512 |
| PP49_BlackFragment | N-(cyclohexylthio)phthalimide (Vulcanization Retarder - No Color) (Hummel, 2002) | 5 | 9 | 0.000419 |
| PP53_BlueFragment | Thioindigo Blue (Hummel, 2002) | 5 | 1 | 0.006378 |
| PP54_RedFragment | 2,7-dibromoanthanthrone Red (Hummel, 2002) | 5 | 5 | 0.000403 |
| PP62_OrangeFiber | 3-chloroaniline -> 2-hydroxynaphthoic arylide-2-methoxyanilide Orange (Hummel, 2002) | 5 | 10 | 0.000491 |
| PS3_BlueFoam | t-butylcumylperoxide (Crosslinking - No Color) (Hummel, 2002) | 5 | 3 | 0.001155 |
| PS6_WhiteFoam | Hydroquinone (Antioxidant - No Color) (Hummel, 2002) | 5 | 4 | 0.02551 |
| PS11_ClearSphere | N-nitrosodiphenylamine (Vulcanization Retarder - N/A) (Hummel, 2002) | 5 | 4 | 0.000889 |
| PS12_OrangeFoam | Zinc dibenzyldithiocarbamate (Accelerator - No Color) (Hummel, 2002) | 5 | 6 | 0.000558 |
| PVC2_BlueFragment | 4-amino-2,5-diethoxybenzanilide -> 2-hydroxynaphthoic arylide-2-methylanilide Blue (Hummel, 2002) | 5 | 8 | 0.000539 |
| PVC3_OrangeFoam | Calcium aniline -> 2-naphthol-6-sulfonic acid Orange (Hummel, 2002) | 5 | 7 | 0.00069 |
| PVC6_ClearFilm | Zinc diethyldithiocarbamate (Vulcanization Accelerator - No Color) (Hummel, 2002) | 5 | 8 | 0.000933 |
| PVC7_GreenFilm | Viridian Green (Hummel, 2002) | 5 | 4 | 0.02551 |
| PVC8_GreyFragment | N,N'-diphenyl-p-phenylendiamine (Antioxidant - Dark-Grey) (Hummel, 2002) | 10 | 8 | 0.00116 |
| PVC9_WhiteFragment | Titanium Dioxide White (Hummel, 2002) | 5 | 9 | 0.006378 |

Table 4. Extended Additive Algorithm Study of Randomly Selected Samples of Each Color in SLOPP-E Database [30][31].

| Sample Name | Best Match | Family | Tol. | Pos. | Score |
| --- | --- | --- | --- | --- | --- |
| CelluloseAcetate1_ClearFilm | Muscovite | Mineral [KAl2(AlSi3)O10(OH,F)2] | 15 | 1 | 0.0018891 |
| CelluloseAcetate3_PinkFiber | PR31 | Azo [C31H23N5O6] | 5 | 1 | 0.0005537 |
| DyedCellulose1_RedFiber | PR40 | Azo [C18H14N2Na2O8S2] | 5 | 1 | 0.0003403 |
| DyedCellulose3_GreenFiber | PG10 | Azo [C15H10ClN3O2] | 5 | 4 | 0.000306 |
| DyedCellulose4_YellowFiber | PY109 | Isoindolinone [C23H8Cl8N4O2] | 5 | 4 | 0.0007045 |
| Polyethylene20_BlueFilm | PB16 | Phthalocyanine [C32H18N8] | 5 | 4 | 0.000527 |
| Polyethylene8_LightBlueFilm | PB3 | Triarylmethane [C25H28ClN2] | 10 | 10 | 0.0006359 |
| Polyethylene18_GreenFragment | PG12 | Naphthoquinone [C10H7NO5S] | 10 | 8 | 0.0008685 |
| Polyethylene19_WhiteFragment | Quartz | Mineral [SiO2] | 5 | 7 | 0.0005033 |
| Polypropylene6_ClearFragment | Muscovite | Mineral [KAl2(AlSi3)O10(OH,F)2] | 10 | 7 | 0.0014142 |
| Polypropylene8_YellowFragment | PY154 | Azo [C18H14F3N5O3] | 5 | 2 | 0.0003434 |
| Polypropylene10_BrownFiber | PBr25 | Azo [C24H15Cl2N5O3] | 10 | 2 | 0.0014345 |
| Polypropylene13_PinkFiber | PR204 | Unknown (Pos. Polycyclic) | 5 | 1 | 0.0007635 |
| Polypropylene16_WhiteFragment | Muscovite | Mineral [KAl2(AlSi3)O10(OH,F)2] | 5 | 9 | 0.000668 |
| Polypropylene17_PurpleFiber | Indigo_3 | Unknown | 10 | 7 | 0.0007176 |
| Polypropylene20_OrangeFragment | PO2 | Azo [C16H11N3O3] | 10 | 5 | 0.0013371 |
| Polystyrene1_YellowFragment | PY104 | Azo [C16H12N2O7S2] | 5 | 3 | 0.0004198 |
| Polystyrene8_BlueFoam | PB16 | Phthalocyanine [C32H18N8] | 5 | 5 | 0.0006147 |
| Polystyrene4_WhiteFilm | Muscovite | Mineral [KAl2(AlSi3)O10(OH,F)2] | 5 | 2 | 0.000535 |
| Polyester2_RedFiber | PR123 | Perylene [C40H26N2O6] | 5 | 1 | 0.0007595 |
| Polyester7_PinkFiber | PR210 | Azo [C25H20N4O4] | 5 | 2 | 0.0007758 |
| Polyester9_PurpleFiber | PV2 | Xanthene [C30H36N2O3] | 5 | 2 | 0.0003527 |
| Polyester11_BlueFiber | PB3 | Triarylmethane [C25H28ClN2] | 5 | 6 | 0.000316 |
| Polyamide1_BlueFragment | PB3 | Triarylmethane [C25H28ClN2] | 5 | 6 | 0.0004808 |
| Polyamide2_PinkFiber | PR54 | Azo [C20H14N2O4S] | 5 | 1 | 0.0006617 |
| PolyvinylChloride3_BlueFragment | PB15 | Phthalocyanine [C32H16CuN8] | 5 | 1 | 0.0006882 |
| PolyvinylChloride4_OrangeFoam | PO43 | Amino ketone [C26H12N4O2] | 5 | 3 | 0.0005555 |