Supporting information

Unveiling the Mechanisms of Biopolymer and Bioenzyme Sand Stabilization: A Chemical and Microstructural Approach

Geethu Thomas1,*, Ripsa Rani Nayak2, Navneet Kumar Gupta2,*, Gali Madhavi Latha1,2

1Department of Civil Engineering, Indian Institute of Science, Bengaluru, India - 560012

2Centre for Sustainable Technologies, Indian Institute of Science, Bengaluru, India- 560012

E-mail: GT:  toms88geethu@gmail.com (ORCID: 0000-0002-4039-2606), NKG: nkgupta@iisc.ac.in (ORCID: 0000-0002-4204-4680)

Number of pages: 20

Number of figures: 12

Number of tables: 5

Table of content

| Figure S1. BET analysis of untreated sand.……………………………………………….….. | S4 |
| --- | --- |
| Figure S2. BET analysis of Sand with 15% Kaolin………………………………………….. | S5 |
| Figure S3. BET analysis of Sand + 15% Kaolin treated with TerraZyme…………………… | S6 |
| Figure S4. BET analysis of Sand + 15% Kaolin treated with Xanthan gum………………... | S7 |
| Figure S5. EDS data of sand and treated soils………………………………………………. | S8 |
| Figure S6. XPS survey of TerraZyme and Xanthan gum treated soils………………………. | S9 |
| Figure S7. C 1s narrow scan XPS spectra of soil-additive combinations…………………… | S10 |
| Figure S8. Si 2p narrow scan XPS spectra of soil-additive combinations…………………... | S11 |
| Figure S9. O 1s narrow scan XPS spectra of soil-additive combinations…………………… | S12 |
| Table S1. Chemical composition of soil-additive combinations obtained from XPS………... | S13 |
| Table S2. XPS analysis of O 1s binding states of different soil-additives combinations…….. | S14 |
| Table S3. XPS analysis of C 1s binding states of different soil-additives combinations…….. | S15 |
| Table S4. XPS analysis of Al 2p binding states of different soil-additives combinations…… | S16 |
| Table S5. XPS analysis of Si 2p binding states of different soil-additives combinations……. | S17 |
| Figure S10. Functionalities groups (Si 2p) versus peak deviatoric stress for treated soils…... | S18 |
| Figure S11. Functionalities groups (O 1s) versus peak deviatoric stress for treated soils…… | S19 |
| Figure S12. Functionalities groups (C 1s) versus peak deviatoric stress for treated soils…… | S20 |

Figure S1. BET analysis of untreated sand.

Figure S2. BET analysis of Sand with 15% Kaolin.

Figure S3. BET analysis of Sand + 15% Kaolin treated with TerraZyme.

Figure S4. BET analysis of Sand + 15% Kaolin treated with Xanthan gum

Figure S5. EDS data of sand and treated soils.

Figure S6. XPS survey of TerraZyme and Xanthan gum treated soils.

Figure S7. C 1s narrow scan XPS spectra of soil-additive combinations

Figure S8. Si 2p narrow scan XPS spectra of soil-additive combinations

Figure S9. O 1s narrow scan XPS spectra of soil-additive combinations

Table S1. Chemical composition of soil-additive combinations obtained from XPS.

| Soil-additive combinations | Atom (%) |  |  |  |
| --- | --- | --- | --- | --- |
|  | Al | Si | O | C |  |
| Sand | 5.12 | 25.49 | 10.78 | 58.62 |  |
| Sand + 15% Kaolin | 12.46 | 25.6 | 13.44 | 48.5 |  |
| Sand + 15% Kaolin + TD | 11.97 | 25.98 | 6.18 | 55.87 |  |
| Sand + 15% Kaolin + XG | 10.93 | 24.4 | 8.52 | 56.15 |  |

Table S2. XPS analysis of O 1s binding states of different soil-additives combinations.

|  |  | O 1s binding states (atom %) |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Soil-additive combinations | Al2O3 |  | SiO2 | C=O | C-O |
|  | 531.1 eV |  | 532.8 eV | 532 eV | 533 eV |
| Sand | 1.83254 |  | 18.46613 | 12.9697 | 25.55037 |
| Sand + 15% Kaolin | 4.41277 |  | 21.10364 | 9.16345 | 13.83785 |
| Sand + 15% Kaolin + TD | 1.20732 |  | 42.05443 | 6.15924 | 6.6448 |
| Sand + 15% Kaolin + XG | 2.90256 |  | 32.42175 | 11.50793 | 9.43299 |

Table S3. XPS analysis of C 1s binding states of different soil-additives combinations.

|  |  | C 1s binding states (atom %) |  |  |
| --- | --- | --- | --- | --- |
| Soil-additive combinations | C-C |  | C-O-C | O-C=O |
|  | 284.8eV |  | 286 eV | 288.5 eV |
| Sand | 6.56601 |  | 2.71629 | 2.03979 |
| Sand + 15% Kaolin | 7.60381 |  | 5.219 | 0.87956 |
| Sand + 15% Kaolin + TD | 3.58599 |  | 2.14 | 0.52561 |
| Sand + 15% Kaolin + XG | 3.77398 |  | 3.76893 | 1.00401 |

Table S4. XPS analysis of Al 2p binding states of different soil-additives combinations.

|  | Al 2p binding states (atom %) |  |  |
| --- | --- | --- | --- |
| Soil-additive combinations | Aluminosilicate | Al (OH)3 | Al oxide |
|  | 74.282 eV | 74.403 eV | 75.61 eV |
| Sand | 1.22033 | 2.2566 | 0.20199 |
| Sand + 15% Kaolin | 1.74407 | 2.72015 | 7.99582 |
| Sand + 15% Kaolin + TD | 1.29504 | 3.50757 | 7.9504 |
| Sand + 15% Kaolin + XG | 1.75294 | 2.95579 | 6.24506 |

Table S5. XPS analysis of Si 2p binding states of different soil-additives combinations.

| Soil-additive combinations | Si 2p binding states (atom %) |  |
| --- | --- | --- |
|  | Aluminosilicate | SiO2 |
|  | 102.7 eV | 103.5 eV |
| Sand | 3.74817 | 22.0925 |
| Sand + 15% Kaolin | 6.13578 | 19.86433 |
| Sand + 15% Kaolin + TD | 6.34802 | 20.0701 |
| Sand + 15% Kaolin + XG | 4.89075 | 19.64925 |

Figure S10. Functionalities groups (Si 2p) versus peak deviatoric stress for treated soils.

Figure S11. Functionalities groups (O 1s) versus peak deviatoric stress for treated soils.

Figure S12. Functionalities groups (C 1s) versus peak deviatoric stress for treated soils.