- Supplementary Information

- 1. Influence of passive core thickness on threshold current densities of QCLs fabricated from the PIC wafer

A deviation in the passive core thickness was observed during the fabrication of the two-color PICs. SEM images confirmed that the passive waveguide core layer was approximately 1330 nm thick, 6.5% above the target thickness of 1250 nm. While this issue can easily be controlled for in the future growths, the unexpected change in the passive waveguide core thickness led to the unpredicted increase in the threshold current densities Jth of the DFB QCLs processed from the PIC wafer used for our current work. As a result, only one of the two lasers on the PIC achieved CW operation at room temperature.

The threshold current density of a semiconductor laser is inversely proportional to the to the modal overlap Γ 28:

Jth=αm+αwΓg.						(1S)

Here αm is the mirror losses, αw is the waveguide losses, and g the differential gain coefficient. Although the 5-mm- long, 10-µm-wide ridge-waveguide reference devices situated directly on top of the unetched passive waveguide layer (as shown in Fig. 4 of the main text) had low threshold current densities, the 7-8 µm wide DFB devices with sidewall corrugation integrated with the passive components exhibited increased threshold current densities due to mode leakage from the QCL core into the passive waveguide core and resultant decrease in the value of Γ. This prevented CW operation of the 7.3 µm DFB QCLs in the PIC at room temperature.

To investigate the effect of ridge width on the devices’ performance, we characterized more reference devices of the length equal to that of the lasers reported in Fig. 4 of the main text (5 mm, to keep αm constant) but with reduced ridge widths of 8 µm and 6 µm. Figure 1S (a,b) shows the light-current characteristics for the 5-mm-long Fabry-Perot ridge-waveguide lasers with the ridge widths of 10 µm, 8 µm, and 6 µm. The data is shown for devices processed from the 6.25 m QCL sections of the PIC wafer and devices processed from the 7.3 m QCL sections of the PIC wafer. A significant increase in threshold current density was observed for the devices with 8 µm ridge widths. Devices 6 µm ridge widths did not achieve lasing. These experimental findings are confirmed by COMSOL simulations of the

Figure 1S. Influence of the passive core thickness on threshold current densities of the PIC lasers. (a,b) Light-output-current characteristics of 5 mm long ridge-waveguide QCLs with different ridge widths of 10 µm (dotted lines), 8 µm (solid lines), and 6 µm (dashed lines) processed from the two-color PIC wafer. Results for the 6.25 µm QCL (a), and for the 7.3 µm QCL (b) are shown. (c,d) Simulated overlap factors for the QCLs of different ridge widths processed from the PIC wafer. The data is shown for the case of the passive waveguide core thickness being the target 1250 nm (squares) and the actual 1330 nm thickness (triangles). Panel (c) shows the results for the =6.25 µm QCLs, panel (d) shows the results for the =7.3 µm QCLs.

modal overlap of the fundamental TM00 mode with the QCL active region. The data is shown in Fig. 1S (c,d) as a function of devices’ ridge widths for the case of both the target thickness and the 6.5% higher thickness of the passive waveguide core. The results indicate up to factor of two decrease in the laser mode overlap with the QCL active region.  We thus expect that the PIC laser performance can improved considerably by maintaining the accurate control of the passive waveguide core thickness.