Photoelectrochemical immunosensor for chloramphenicol detection based on cation exchange reaction-mediacted photocurrent enhancement of ZnIn2S4/TiO2/Ti3C2 MXene coupled with controlled-release strategy

Mengqin Zhenga,#, Huizi Linb,#, Suhua Lia, Shuoying Huanga, Jiangwei Huanga, Wenqiang Laia, Dianping Tangc, Youxiu Lina,*

a Key Laboratory of Modern Analytical Science and Separation Technology of Fujian Province, Key Laboratory of Pollution Monitoring and Control of Fujian Province, College of Chemistry, Chemical Engineering and Environment, Minnan Normal University, Zhangzhou 363000, People’s Republic of China

b Department of Neonatology, Fujian Children's Hospital (Fujian Branch of Shanghai Children's Medical Center), College of Clinical Medicine for Obstetrics & Gynecology and Pediatrics, Fujian Medical University, Fuzhou 350108, People’s Republic of China

c Key Laboratory of Analysis and Detection for Food Safety (MOE & Fujian Province), Institute of Nanomedicine and Nanobiosensing, Department of Chemistry, Fuzhou University, Fuzhou 350108, People’s Republic of China

*Corresponding author: Youxiu Lin, E-mail: youxiu90@163.com

### Materials and reagents

Titanium aluminide (Ti3AlC2, ≥ 99%) was supplied by Xinxi Technology; Lithium fluoride (LiF), Sodium hydrogen phosphate (Na2HPO4), monosodium phosphate (NaH2PO4) , dipotassium phosphate (K2HPO4), sodium chloride (NaCl), potassium chloride (KCl), potassium nitrate(KNO3), glutaraldehyde, hydrochloric acid (HCl) and anhydrous ethanol (C2H5OH) were purchased from Shanghai Aladdin Biochemical Technology Co., Ltd; Sodium fluoroborate (NaBF4), Indium(III) chloride tetrahydrate (InCl3·4H2O), inc chloride dihydrat (ZnCl2·2H2O) were purchased from Shanghai Macklin; Thioacetamide (TAA), copper oxide nanoparticles (CuO NPs, 50 nm in diameter), Penicillin (PG), oxytetracycline (OTC), tetracycline (TCN), chloramphenicol (CAP), ciprofloxacin (CIP), chloramphenicol monoclonal antibody (mAb), bovine serum albumin (BSA) were purchased from Sigma Aldrich. All chemicals and reagents required for the experiments are of analytical grade and do not require purification before use. Deionized water was obtained from a Millipore water-purification system (18.2 MΩ·cm, Milli-Q, Germany).

### Instruments and equipment

All photoelectrochemical measurements were performed with CHI 660E electrochemical workstation (Chenhua, Shanghai, China). The surface morphology of the sample was obtained from scanning electron microscopy (SEM, Tescan Mira4, USA). UV-vis spectra were obtained on a Shimadzu UV 3600 Plus spectrometer (Japan). X-ray diffraction (XRD) patterns were obtained by using D8 focus diffractometer (Bruker AXS, Germany). X-ray photoelectron spectra (XPS) were elucidated using an ESCALAB 250 electron energy spectrometer (Thermo Fisher Scientific K-Alpha, USA)