Luminescence “on-off-on” sensing of acute myocardial infarction biomarker miRNA-208a based on copper nanoclusters-MoS2 FRET system

Suzhen Zhang 1, Danling Mei 1, Hongming Fang 2, Quanwei Li 4, Xiumei Zhou 1, Xueqin Zhao 1*, Zhencang Zheng 3*, Biao Huang 1*

1 College of Life Sciences and Medicine, Zhejiang Sci-Tech University, Hangzhou 310018, China; suzhenzhang2022@163.com (S.Z.); 2719119394@qq.com (D.M.); zhouxiumei824@163.com (X.Z.)

2 Xiaoshan Hospital, Hangzhou Normal University, Hangzhou 311200, China; 3295988078@qq.com

3 Department of Critical Care Medicine, Taizhou Central Hospital, (Taizhou University Hospital), Taizhou, Zhejiang 318000, China; zhengzc2023@163.com

4 Beijing Institute of Hepatology, You'an Hospital, Capital Medical University, Beijing 100069, China; quanweili@mail.ccmu.edu.cn

* Correspondence:: zhaoxueqin@zstu.edu.cn(X.Z.); zhengzc2023@163.com(Z.Z.); huangbiao@zstu.edu.cn (B.H.)

Table S1. Recovery of the assay of miRNA-208a in 10% human serum.

| Sample | Added (nM) | Found (nM) (n=3) | Recovery (%) | RSD (%) |
| --- | --- | --- | --- | --- |
| 1 | 2.5 | 2.45 | 98.13 | 1.0 |
| 2 | 5 | 4.93 | 98.67 | 0.5 |
| 3 | 10 | 9.97 | 99.73 | 3.0 |
| 4 | 15 | 14.70 | 97.98 | 2.2 |
| 5 | 20 | 20.24 | 101.20 | 1.3 |

Table S2. The sequences of the cDNA probe and miRNA-208a

| Nucleic acid | Sequence (5’-3’) |
| --- | --- |
| cDNA Probe | TATTCTGCTCGTTTTTCGAACA |
| miRNA-208a | AUAAGACGAGCAAAAAGCUUGU |

Table S3. Mismatch sequence for specific detection

| Nucleic acid | Sequence (5’-3’) |
| --- | --- |
| Single base mismatch sequence | AUAACACGAGCAAAAAGCUUGU |
| Double base mismatch sequence | AUUACACGAGCAAAAAGCUUGU |
| Mismatched sequence | UAGCUUAUCAGACUGAUGUUGA |

Figure S1. Optimization conditions for synthesis PEI-CuNCs.

Figure S2. FTIR of CuNCs.

Figure S3. Storage stability of CuNCs.

Figure S4. Optimization of the CuNCs-cDNA-MoS2 sensing strategy. (a) Fluorescence spectra of the CuNCs−DNA with the concentrations of 3.9-500 μg mL-1. (b) Fluorescence spectra of the CuNCs-cDNA-MoS2 prepared 20 μg mL-1 of CuNCs-cDNA and MoS2 with the concentrations from 1 to 28 μg mL-1. (c) △F as a function of different concentrations of MoS2 (△F=F-F0) nanosheets after introducing the target miRNA-208a. (d) FL of CuNCs-cDNA-MoS2 with time in the absent or present of the target miR-208a.