# Supplementary Information

Interface Engineering to Regulate Oxidation Dynamics of Supported Nanoparticles

Shiyuan Chen1, 3, Kai Zhang1, 3, Yuhui Chen1, Bo Shao1, Chaobin Zeng2, Wentao Yuan1, Hangsheng Yang1, Zhongkang Han1*, Ying Jiang1*, Ze Zhang1 & Yong Wang1*

1Center of Electron Microscopy and State Key Laboratory of Silicon and Advanced Semiconductor Materials, School of Materials Science and Engineering, Zhejiang University, Hangzhou, 310027, China.

2Hitachi High-Technologies (Shanghai) Co., Ltd, Shanghai, 201203, China.

3These authors contributed equally.

Correspondence Email: hanzk@zju.edu.cn; yjiang0209@zju.edu.cn; yongwang@zju.edu.cn;

Movie. S1 and S2

Supplementary Table 1. The structure and interplanar spacing of Pd, PdO and Pd2O

| Pd (cubic) | PdO (tetragonal) | Pd2O (cubic) |
| --- | --- | --- |
| dPd(111)=2.2457 Å - dPd(200)=1.9449 Å | - dPdO(100)=3.0200 Å - dPdO(002)=2.6550 Å | - dPd2O(110)=3.0264 Å - dPd2O(111)=2.4711 Å |
| - dPd(220)=1.3752 Å | - dPdO(101)=2.6251 Å | - dPd2O(200)=2.1400 Å |
|  | - dPdO(110)=2.1354 Å |  |
|  | - dPdO(102)=1.9940 Å |  |

Supplementary Table 2. The epitaxial mismatch between PdO low-index surfaces and CeO2 (111) surface (all surface periodicities are unified into orthometric modeling; mismatch=(1-dsmaller/dbigger)×100%)

| Mismatch | CeO2 (111) d1=3.88 Å | CeO2 (111) d2=6.72 Å |
| --- | --- | --- |
| d1-PdO(001)=3.10 Å d2-PdO(001)=3.10 Å d1-PdO(100)=3.10 Å d2-PdO(100)=5.41 Å d1-PdO(110)=5.41 Å d2-PdO(110)=4.39 Å d1-PdO(111)=4.39 Å d2-PdO(111)=5.83 Å d3-PdO(111)=4.11 Å d4-PdO(111)=6.23 Å d1-PdO(101)=6.23 Å | 20.1% 20.1% 20.1% 28.3% 28.3% 11.6% 11.6% 33.4% 5.60% 37.7% 37.7% | 53.9% 53.9% 53.9% 19.5% 19.5% 34.7% 34.7% 13.2% 38.8% 7.29% 7.29% |
| d2-PdO(101)=3.10 Å | 20.1% | 53.9% |

Supplementary Table 3. The cohesive interfacial energy in different interface system (all surface periodicities are unified into orthometric modeling; slab 1 is the substrate and slab 2 is the loaded layer)

| Slab 1 | Slab 2 | interfacial energy (eV/Å2) |
| --- | --- | --- |
| CeO2(100) CeO2(100) R45° CeO2(100) CeO2(100) R45° CeO2(100) CeO2(100) R45° CeO2(100) CeO2(100) CeO2(100)-Full O CeO2(100)-Full O MgO(100) R45° | Pd(100) Pd(100) Pd(110) Pd(110) Pd(111) Pd(111) PdO(001) PdO(101) PdO(001) PdO(101) Ni(110) | -0.076522187 -0.071297688 -0.093608573 -0.079873112 -0.077324574 -0.051109087 -0.050358646 -0.032735456 -0.081015621 -0.082257015 -0.024840681 |
| MgO(100) R45° | Ni(111) | 0.007129554 |
| MgO(100) | NiO(110) | -0.009193551 |
| MgO(100) R45° | NiO(110) | -0.057884956 |
| MgO(100) | NiO(111)-Full O | -0.026952707 |
| MgO(100) | NiO(111)-Half O | -0.059671761 |
| MgO(100) R45° | NiO(111)-Full O | -0.050957064 |
| MgO(100) R45° | NiO(111)-Half O | -0.008853368 |
| CeO2(111) | Pd(100) | -0.063080309 |
| CeO2(111) R90° | Pd(100) | -0.064084722 |
| CeO2(111) | Pd(110) | -0.059539828 |
| CeO2(111) | Pd(111) | -0.058672059 |
| CeO2(111) R90° | Pd(111) | -0.059734565 |
| CeO2(111) R90° | PdO(100) | -0.048950027 |
| CeO2(111) | PdO(001)-Full O | -0.062319055 |
| CeO2(111) | PdO(001)-Half O | -0.064252301 |
| CeO2(111) | PdO(001)-Full O R45° | -0.049157622 |
| CeO2(111) | PdO(001)-Half O R45° | -0.079168143 |
| CeO2(111) | PdO(101) | -0.04501318 |
| CeO2(111) R90° | PdO(101) | -0.071266919 |
| CeO2(100) | PdO(100) | -0.129666628 |
| MgO(100) | NiO(100) | -0.13385027 |
| CeO2(100) | Ru(001) | -0.1344277654 |
| CeO2(100) R45° | Ru(001) | -0.1250518085 |
| CeO2(100) | Ru(100) | -0.1501181809 |
| CeO2(100) R45° | Ru(100) | -0.1318406539 |
| CeO2(100) | Ru(110) | -0.1514797351 |
| CeO2(100) | RuO2(100) | -0.0592805540 |
| CeO2(100) R45° | RuO2(100) | -0.0923283196 |
| CeO2(100) | RuO2(101) | -0.0779633336 |
| CeO2(100) R45° | RuO2(101) | -0.0852717032 |

Supplementary Figure 1.  Morphology and structure of Pd/CeO2(100) and Pd/CeO2(111) catalysts. Low- a, c and high- b, d magnification HAADF-STEM images of Pd/CeO2(100) and Pd/CeO2(111) catalysts.

Supplementary Figure 2. In situ oxidation of Pd/CeO2(100), labeled as P2, in 5 Pa oxygen with increasing temperatures.

Supplementary Figure 3. In situ oxidation of Pd/CeO2(100), labeled as P3, in 5 Pa oxygen with increasing temperatures.

Supplementary Figure 4. Crystallographic relationships between Pd and PdO. a-c HAADF-ESTEM images of the intermediate states during the oxidation of the first NP (P1), second NP (P2) and third NP (P3). a’-c’ FFT patterns obtained from the dashed red squares in (a-c) showing the rotation angles between the Pd(-111) and PdO(10-1) reflections. Blue circles correspond to the Pd patterns and pink to the PdO patterns.

Supplementary Figure 5. Crystallographic relationships between Pd, PdO and CeO2 in the first nanoparticle (P1). a-b HAADF-ESTEM images of the intermediate and final states during the oxidation of P1. a’-b’ FFT patterns obtained from the dashed red squares in a-b showing the rotation angles between the Pd(-111) and CeO2(100), as well as PdO(10-1) and CeO2(100) reflections. Blue circles correspond to the Pd patterns, pink to the PdO patterns, and green to the CeO2 patterns.

Supplementary Figure 6. The optimized model of calculating binding energy in PdO/CeO2 (100) structure. a Model of PdO/CeO2(100) heterojunction structure. b-c Model of isolated CeO2 and PdO slab (grey balls: Pd atoms; yellow green balls: Ce atoms; red balls: O atoms; blue dashed line square: crystal period).

Supplementary Figure 7. Diffusion route and the energy barrier of oxygen in PdO/CeO2 heterojunction structure. a Diffusion route of O oxygen in heterojunction structure in zone axis of CeO2 [001] (grey balls: Pd atoms; red balls: O atoms; yellow green balls: Ce atoms; orange balls: O atoms at the start of diffusion; blue balls: O atoms at the end of diffusion). b-c The energy barrier of O diffusion in heterojunction structure with different directions (b: vertical diffusion; c: horizontal diffusion; x-axis: the start layer of oxygen atoms).

Supplementary Figure 8. Model of bulk PdO. a-b The projected image of the model in two zone axes (grey balls: Pd atoms; red balls: O atoms; dashed blue circles and blue arrow: the position of diffused oxygen atoms and the direction).

Supplementary Figure 9. Model of pure Pd (111) surface. a The top view of Pd (111) surface model (grey balls: Pd atoms; lattice in different colors: lattice in different crystal period); b the side view of Pd (111) surface model (silver balls: Pd atoms; orange dashed-lined rectangle: crystal period of the model).

Supplementary Figure 10. The model of Pd (111) surface with adsorbed O atoms and their corresponding calculated energy data (grey balls: Pd atoms; red balls: O atoms; red balls with dashed blue circles: selected O atoms which diffused deeper).

Supplementary Figure 11. The curve of calculated average adsorption energy of oxygen and corresponding energy barrier of oxygen diffusion changed with coverage of oxygen on Pd (111) surface. a Average adsorption energy of oxygen atom. b Diffusion energy barrier of oxygen on the Pd (111) with different oxygen coverage (dashed reference line: diffusion energy barrier in PdO bulk, average vertical and horizonal diffusion energy barrier in PdO/CeO2 (100) heterostructure).