Appendix

Table A-1 Segment designs used in the trials. Segments for trial A, C and D were supplied by Andritz and segments used in trial B were supplied by Valmet. R refers to the rotor-side and S to the stator-side.
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Table A-2 Refining conditions.
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Trial Barwidth Edge length BarwidthEdge length

mm km/rev mm km/rev

A 58TC425/426 1.5 287 - - -

B

R: SWPS258F37/M37 

S: SWP5258E72/M72

3.5 139

R: SWP5258D61/M61 

S: SWP5258D61/M61 

2.2 214

C 58TC425/426 1.5 287 58TC425/426 1.5 287

D 72TA203/204 1.6 414 - - -

Primary Secondary

Type Type


image2.png
Production  Motor
Trial rate  load  °¢ SE
bdih MW kwh/bdt  3/m
163 13 77 045
163 17 97 o062
170 14 8 100
BPrimHigh  17.0 17 106 132
BSeclow  17.0 14 81 064
BSecHigh 165 17 101 084
c 153 14 160 049
o 151 27 176 086





