SUPPLEMENTARY DATA

Equation of State for Solid Argon Valid for Temperatures up to 760 K and Pressures up to 6300 MPa

Xiong Xiaoa, Sakimsan Sriskandarubanb, Helen E. Maynard-Caselyc, Monika Tholb, Peter Falloona, Roland Spanb, Eric F. Mayad*

a Fluid Science and Resources Division, School of Engineering, University of Western Australia, 35 Stirling Hwy, Crawley 6009, Perth, Australia

b Thermodynamics, Faculty of Mechanical Engineering, Ruhr-Universität Bochum, Universitätsstraße 150, 44801, Bochum, Germany

c Australian Nuclear Science and Technology Organisation, Lucas Heights 2234, New South Wales, Australia

d Future Energy Exports Cooperative Research Centre, 35 Stirling Highway, Crawley, WA, 6009, Australia

e-mail (corresponding author): eric.may@uwa.edu.au

Table S1. Optimized parameter values for the solid argon equation of state.

| Parameter | Value |
| --- | --- |
| c1/MPa | 2897 |
| c2/MPa | 8000 |
| c3/MPa | 941 |
| θD,0/K | 100 |
| γD,0 | 1 |
| qD | 1 |
| b1 | 1 |
| b2 | 1 |
| b3 | 1 |
| Sm(g, Tt, pt) /(J mol–1 K–1) | 131.15 |

Figure S1. Comparison of variable temperature D2O data from this experimental set up, with the values determined by Fortes [1].

Figure S2. Temperature-dependent evolution of the (111) and (002) diffraction peaks for solid argon as measured by neutron scattering.

The (111) and (002) peaks correspond to specific crystallographic planes in the face-centered cubic (FCC) structure of solid argon, with (111) representing a dense plane cutting through all three axes and (002) indicating planes perpendicular to the z-axis. Changes in the intensity and width of these peaks above 66 K indicate the onset of strain in the crystal lattice due to crystallite growth at higher temperatures.

# References

[1]	A.D. Fortes, Acta Cryst. B 74 (2018) 196-216.