Supporting information

Preparation of CeZrO2 with mixed alcohol/water solvents: as highly active catalysts for the synthesis of dimethyl carbonate from CO2 and methanol

YaningWang, Guisheng Qi*, Yujing Guo, Ning Li, Jingting He, Qiang Guo, Youzhi Liu

Email address: zbdxqgs@126.com

Shanxi Province Key Laboratory of Chemical Process Intensification, School of Chemistry and

Chemical Engineering, North University of China, Taiyuan 030051,PR China

1. Solvent properties

Table S1. Physical and chemical properties of the solvents used in the experiment

| Solvent | Water | Ethanol | Ethylene glycol | Glycerol | n-butanol |
| --- | --- | --- | --- | --- | --- |
| Molecular formula | H2O | C2H6O | C2H6O2 | C3H8O3 | C4H10O |
| Molecular weight | 18.02 | 46.07 | 78.07 | 92.09 | 74.12 |
| Dielectric constant (ε) | 78.3 | 24.5 | 41.1 | 46.5 | 17.1 |
| Density/(g·cm3),25℃ | 0.997 | 0.7893 | 1.11 | 1.261 | 0.81 |
| Viscosity/(mPa·s) ,25℃ | 0.8903 | 0.5525 | 22.8 | 1.499 | 2.05 |
| Surface tension/(mM·m-1) | 71.81 | 22.10 | 48.4 | 61.9 | 26.0 |

2. particle size distribution

Fig. S1. pore size distribution curves CZ-W (a), CZ-EA (b), CZ-EG (c), CZ-GLY(d), CZ-BA (e), particle size distribution after reaction of CZ-BA (f).