SUPPORTING INFORMATION

Enhanced Photocatalytic Performance of Non-stoichiometric WO3-x Nanocrystals Via Near-Infrared Localized Surface Plasmon Resonance

Mohsen Zafari, Fatemeh Shariatmadar Tehrani*

Faculty of Physics, Semnan University, POBOX:35195-363, Semnan, Iran

* f_tehrani@semnan.ac.ir

Table of Contents

1.	Images of WO3-x Nanocrystals	2

2.	EDX analysis	2

3.	Free Carrier Density Calculations	4

3.1	The Mie-Gans theory	4

4.	Deconvoluted PL spectra of WO3-x Nanocrystals 	6

5.	photocatalytic degradation of Methylene Blue	8

# Images of WO3-x Nanocrystals

Figure S1. Images of samples synthesized by acidification method (i.e.W3, W3N, W1.5, and W1.5N) and their calcined samples - 400°C for 2 h - (i.e.W3C, W3NC, W1.5C, and W1.5NC)

# EDX analysis

Table S1. Elemental composition of the samples based on EDX analysis.

| Sample | O (at%) | W (at%) | Calculated Composition |
| --- | --- | --- | --- |
| W3 | 65.6 | 27.2 | W27O65 (~WO2.41) |
| W3N | 70.8 | 24.6 | W25O71 (~WO2.87) |
| W1.5 | 70.7 | 25.1 | W25O71 (~WO2.82) |
| W1.5N | 69.9 | 23.7 | W24O70 (~WO2.95) |
| W3C | 57.2 | 32.5 | W32O57 (~WO1.76) |
| W3NC | 71.8 | 24.9 | W25O72 (~WO2.88) |
| W1.5C | 68.4 | 26.9 | W27O68 (~WO2.54) |
| W1.5NC | 68.9 | 25.8 | W25O69 (~WO2.67) |

Figure S2. EDX spectra of WO3-x nanocrystals.

# Free Carrier Density Calculations

## The Mie-Gans theory

We simulated the absorption spectrum of nanocrystals  using Equation 1, the parameters defined in Equations 2-7, and the assumptions noted in the work of Manthiram et al [1]. The calculated stoichiometry of WO3-x nanocrystals shows a higher oxygen deficiency than predicted from XRD analysis (see Tables 1 and S2). This could explain the unprecedentedly high free carrier density of our synthesized nanocrystals. We should also mention that the calculated oxygen deficiency showed a lower percentage of oxygen vacancies than the EDX analysis in most cases. This difference may be due to the aspect ratio of WO3-x calculated from FESEM images (see Tables S1 and S2).

Table S2. LSPR peak, γ, ωp, and free carrier density of WO3-x nanocrystals calculated from predict the LSPR spectrum by using the Mie-Gans theory.

| Sample | λLSPR(nm) | γ (eV) | ωp (eV) | Ne (cm-3) | Oxygen Deficiency (%) | Calculated Composition |
| --- | --- | --- | --- | --- | --- | --- |
| W3 | --- | -- | -- | -- | -- | -- |
| W3N | --- | -- | -- | -- | -- | -- |
| W1.5 | 1246 | 1.08 | 2.55 | 5.62 ×1021 | 5.01 | WO2.85 |
| W1.5N | 1213 | 1.23 | 2.77 | 6.67 ×1021 | 5.95 | WO2.82 |
| W3C | 1899 | 2.21 | 4.00 | 1.38 ×1022 | 12.35 | WO2.63 |
| W3NC | 1769 | 2.70 | 4.84 | 2.03 ×1022 | 18.07 | WO2.46 |
| W1.5C | 1771 | 1.86 | 3.44 | 1.03 ×1022 | 9.15 | WO2.73 |
| W1.5NC | 1728 | 2.01 | 3.69 | 1.18 ×1022 | 10.55 | WO2.68 |

Figure S3. Histograms of WO3-x nanocrystals (length and width).

Table S3. Aspect ratio calculated for WO3-x nanocrystals.

| Sample | length | Width |  | Aspect ratio (R) |
| --- | --- | --- | --- | --- |
| W3 | 628.78 | 104.52 | nm | 6.02 |
| W3N | 0.3484 | 0.0953 | µm | 3.66 |
| W1.5 | 200.81 | 49.89 | nm | 4.03 |
| W1.5N | 1.0305 | 0.7081 | µm | 1.46 |
| W3C | 638.10 | 68.59 | nm | 9.30 |
| W3NC | 0.7303 | 0.0896 | µm | 8.82 |
| W1.5C | 178.32 | 40.29 | nm | 4.43 |
| W1.5NC | 179.79 | 67.50 | nm | 2.66 |

# Deconvoluted PL spectra of WO3-x Nanocrystals

Figure S4. Deconvoluted PL spectra of (a) W3, (b) W3C, (c) W3N, (d) W3NC, (e) W1.5, (f) W1.5C, (g) W1.5N, and (h) W1.5NC.

# photocatalytic degradation of Methylene Blue

Table S4. The degradation efficiencies and apparent rate constants of the photocatalysts.

| Photocatalyst | Light source | Reaction time (min) | Rate constant k (min-1) | degradation (%) | reference |
| --- | --- | --- | --- | --- | --- |
| WO3 | 300-W Xenon | 240 | 0.00286 | 40.5 | [2] |
| Au-WO3 |  |  | 0.01150 | 68.0 |  |
| WS2 monolayer | 15-W visible-light | 120 | 0.01716 | ∼80.0 | [3] |
| WO3⋅H2O | 300-W Xenon | 30 | 0.00056 | ∼12.9 | [4] |
| WO3/TiO2 | 9-W visible-light | 120 | 0.00197 | 27.0 | [5] |
|  | 9-W UV-light |  | 0.01800 | 90.0 |  |
| WO3/SiO2 | 65-W visible-light | 120 | 0.01300 | 91.0 | [6] |
| WO3 | 300-W Xenon | 90 | 0.00130 | 15.4 | [7] |
| WR1(WO3 + 10 mg GO) |  |  | 0.00280 | 31.4 |  |
| WR2(WO3 + 20 mg GO) |  |  | 0.00410 | 46.4 |  |
| WR3(WO3 + 30 mg GO) |  |  | 0.00730 | 82.2 |  |
| WO3 nanorod (WR) | 50-W tungsten | 60 | 0.00550 | 13.4 | [8] |
| WO3 | 72-W halogen | 420 | 0.00250 | ∼98.0 | [9] |
| W3 | 100-W Xenon | 125 | 0.00196 | 19.0 | This work |
| W3N |  |  | 0.00439 | 38.0 |  |
| W1.5 |  |  | 0.00592 | 49.8 |  |
| W1.5N |  |  | 0.00809 | 60.3 |  |
| W3C |  |  | 0.00288 | 28.8 |  |
| W3NC |  |  | 0.00501 | 42.8 |  |
| W1.5C |  |  | 0.00882 | 64.4 |  |
| W1.5NC |  |  | 0.01228 | 75.7 |  |

Reference:

[1]	Manthiram K, Alivisatos AP. Tunable Localized Surface Plasmon Resonances in Tungsten Oxide Nanocrystals. J Am Chem Soc 2012;134:3995–8. https://doi.org/10.1021/ja211363w.

[2]	Yang X, Fu H, Wang W, Xiong S, Han D, Deng Z, et al. Enhanced solar light photocatalytic performance based on a novel Au-WO3@TiO2 ternary core–shell nanostructures. Appl Surf Sci 2020;505:144631. https://doi.org/10.1016/j.apsusc.2019.144631.

[3]	Thakur D, Sharma M, Vaish R, Balakrishnan V. WS 2 Monolayer for Piezo–Phototronic Dye Degradation and Bacterial Disinfection. ACS Appl Nano Mater 2021;4:7879–87. https://doi.org/10.1021/acsanm.1c01202.

[4]	Tang J, Meng R, Xue Y, Zhang S, Li Q. Fabrication of a novel Ag3PO4/WO3·H2O composite with enhanced visible light photocatalytic performance for the degradation of methylene blue and oxytetracycline. Inorg Chem Commun 2021;132:108792. https://doi.org/10.1016/j.inoche.2021.108792.

[5]	Yang L, Si Z, Weng D, Yao Y. Synthesis, characterization and photocatalytic activity of porous WO3/TiO2 hollow microspheres. Appl Surf Sci 2014;313:470–8. https://doi.org/10.1016/j.apsusc.2014.05.230.

[6]	Sharma S, Basu S. Highly reusable visible light active hierarchical porous WO3/SiO2 monolith in centimeter length scale for enhanced photocatalytic degradation of toxic pollutants. Sep Purif Technol 2020;231:115916. https://doi.org/10.1016/j.seppur.2019.115916.

[7]	Ramar V, Balasubramanian K. Reduced Graphene Oxide/WO 3 Nanorod Composites for Photocatalytic Degradation of Methylene Blue under Sunlight Irradiation. ACS Appl Nano Mater 2021;4:5512–21. https://doi.org/10.1021/acsanm.1c00863.

[8]	Joice MRS, David TM, Wilson P. WO 3 Nanorods Supported on Mesoporous TiO 2 Nanotubes as One-Dimensional Nanocomposites for Rapid Degradation of Methylene Blue under Visible Light Irradiation. J Phys Chem C 2019;123:27448–64. https://doi.org/10.1021/acs.jpcc.9b05647.

[9]	DePuccio DP, Botella P, O’Rourke B, Landry CC. Degradation of Methylene Blue Using Porous WO 3 , SiO 2 –WO 3 , and Their Au-Loaded Analogs: Adsorption and Photocatalytic Studies. ACS Appl Mater Interfaces 2015;7:1987–96. https://doi.org/10.1021/am507806a.