Supplementary Material

USE OF IONIC LIQUID IN DIFFERENT ROUTES FOR OBTAINING NANOCELLULOSE FROM YERBA MATE RESIDUES

Marcos Aurélio Dahlem Júnior¹, Vinícius Demétrio da Silva², Henri Stephan Schrekker², André Luis Catto³, Jean-Manuel Raimundo4, Ruth Marlene Campomanes Santana¹

¹PPGE3M, School of Engineering, Federal University of Rio Grande do Sul, Porto Alegre, RS, Brazil

²Laboratory of Technological Processes and Catalysis, Institute of Chemistry, Federal University of Rio Grande do Sul, Porto Alegre, RS, Brazil

³Center of Exact and Technological Sciences, University of Taquari Valley - UNIVATES, Lajeado, RS, Brazil

4Aix-Marseille Université, CNRS, CINaM, 13009 Marseille, France

(marcosdahlem@gmail.com*; viniciusdemetrio@gmail.com; henri.schrekker@ufrgs.br; andrecatto@terra.com.br; jean-manuel.raimundo@univ-amu.fr; ruth.santana@ufrgs.br)

XRD data manipulations

Using the Peak Analyzer of the OriginLab® software, it was possible to estimate the amorphous base and the baseline (background). The type of peak used was Gaussian. XRD data manipulations performed with the OriginLab® software version 8.5.1 are succinctly described in the text below.

After plot your curves in OriginLab® software, goes to Analysis > Peaks and Baseline > Peak Analyzer: now you can Integrate Peaks; Create Baseline; Subtract Baseline or Find Peaks. After that, it will be possible to obtain the peak area using estimated amorphous base as reference and total peak area using background base as reference. Figure S1 shows some examples in each step and Equation 1 how the crystallinity index (CI) was calculated.

Figure S1. (A) Normal XDR plot without smooth, (B) after adding background and amorphous base (estimated), (C) peak area using amorphous base as reference and (D) total peak area using background base as reference.

CI= ƩAcƩAtotal x 100 					                                          (1)

Where CI is the crystallinity index, ƩAc is the area of ​​the diffraction peak related to the crystal plane and ƩAtotal refers to the total area.