Supplemental information

TITLE: “Multiple effects of modified biochar in saline-alkali soil: reducing salinity, providing nutrition, and promoting root colonization by beneficial bacteria”

AUTHORS:

Jiyuan Wanga

Muhammad Riazb

Saba Babara

Zeinab El-Desoukia

Yuxuan Lia

Xiangling Wanga

Xiaoyang Xiaa

Cuncang Jianga*

a“Microelement Research Center, College of Resources and Environment, Huazhong Agricultural University, Wuhan, Hubei, 430070, P.R. China”

b“College of Resources and Environment, Zhongkai University of Agriculture and Engineering, Guangzhou, 510225, P.R. China”

*Corresponding author (jcc2000@mail.hzau.edu.cn)

List of Contents

Text S1 The characterization methods of biochar samples.

Text S2 The methods for analyzing the soil basic chemical properties.

Table S1 The basic properties of the experimental soil.

Table S2 The soil basic chemical properties under different treatments.

Fig. S1 The available Fe content of biochar samples.

Fig. S2 The bacterial community traits in 15-30 cm depth of soils with the addition of different biochar samples. (a) Shannon index of bacterial community in 15-30 cm depth of soil. (b) The relative abundance of soil bacteria at the phylum level. (c) The relative abundance of soil bacteria at the genus level. (d) Redundancy analysis (RDA) based on genus level. (e) The two-factor network analysis based on genus level.

Fig. S3 The phylogenetic tree of endophytic bacteria on genus level.

Fig. S4 The standardized relative abundances of microbial functions predicted by Functional Annotation of Prokaryotic Taxa (FAPROTAX) analysis.

Text S1 The characterization methods of biochar samples

The pH of biochar samples was measured in a 1:5 (w/v) suspension using a pH meter. The total carbon (C) and nitrogen (N) content were determined by an element analyzer (Vario EL cube, Elemental Instruments Co., Germany). A flame spectrophotometer was used to measure the potassium (K) and sodium (Na) content of biochar samples. And an inductively coupled plasma mass spectrometer (ICP-MS) was employed to test the calcium (Ca), magnesium (Mg), and iron (Fe) content of biochar. The surface structure of biochar samples was characterized using a scanning electron microscopy (SEM; S-4800, Hitachi Ltd., Japan). Fourier transform infrared spectroscopy (FTIR; Nicolet IS50, Thermo Scientific, USA) was used to determine the surface functional groups of samples. X-ray diffraction (XRD; D8 ADVANCE, Bruker Co., USA) was employed to test the crystal phase composition of samples, and the specific instrument parameters was as follows: tube current, 40 mA; tube voltage, 40 kV; Cu target wavelength, 1.54 Å; Co target wavelength, 1.79 Å; scanning speed, 10° min-1; scanning range (2θ), 5°-90°.

Text S2 The methods for analyzing the soil basic chemical properties

The soil organic matter content was measured with the K2Cr2O7-volumetric method. Soil pH was determined in a 1:2.5 (w/v) suspension by using a pH meter (FE20, Shanghai Mettler Toledo Co., China). Soil EC was tested in a 1:5 (w/v) suspension using a conductivity meter. Soil NH4+-N and NO3--N were extracted with 2 mol L-1 KCl and measured using a flow analyzer (AA3, SEAL Co., Germany). Soil available phosphorus (AP) and available potassium (AK) were extracted with NaHCO3 and CH3COONH4, then measured by ultraviolet spectrophotometry (TU-1810, Beijing Persee General Instrument Co., Ltd., China) and flame photometer (FP6410, Shanghai Jingqi Instrument Co., Ltd., China), respectively.

Table S1 The basic properties of the experimental soil

| Parameters | pH | SOM (g·kg-1) | EC (dS·m-1) | AN (mg·kg-1) | AP (mg kg-1) | AK (mg kg-1) | Mechanical composition (%) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  | Clay | Silt | Sand |
| Values | 9.64 | 3.10 | 4.96 | 18.67 | 12.34 | 261.67 | 32.49 | 4.06 | 63.45 |

Note: SOM, soil organic matters; EC, electrical conductivity; AN, available nitrogen; AP, available phosphorus; AK, available potassium

Table S2 The soil basic chemical properties under different treatments

| Soil depth | Treatments | NH4+-N (mg·kg-1) | NO3--N (mg·kg-1) | Available P (mg·kg-1) | Available K (mg·kg-1) | Exchangeable Na (g kg-1) | Exchangeable Ca (g kg-1) | Exchangeable Mg (g kg-1) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0-15 cm | CK | 15.77±0.93bc | 2.92±0.79d | 16.49±0.34d | 377.33±6.03d | 3.48±0.20a | 2.62±0.09c | 0.24±0.01b |
|  | PBC | 13.33±2.26c | 5.83±2.10c | 17.70±0.55c | 565.33±11.93a | 2.97±0.13b | 2.85±0.07b | 0.26±0.01ab |
|  | HBC | 17.12±2.49b | 15.30±0.88ab | 18.27±0.34c | 431.78±9.19c | 3.11±0.12b | 2.95±0.09ab | 0.26±0.01a |
|  | FBC | 19.33±0.85a | 17.14±0.32a | 22.27±0.87a | 431.67±12.66c | 2.57±0.23c | 2.95±0.07ab | 0.27±0.01a |
|  | HFBC | 18.56±1.53ab | 14.35±1.37b | 19.54±0.64b | 459.67±4.73b | 3.20±0.05ab | 3.03±0.08a | 0.26±0.02a |
| 15-30 cm | CK | 36.25±1.19a | 168.21±24.84c | 19.84±0.46d | 417.00±15.62c | 6.63±0.08a | 2.95±0.07b | 0.25±0.01a |
|  | PBC | 34.86±2.49a | 706.61±55.96b | 22.89±0.34c | 597.67±14.57a | 5.20±0.32c | 3.09±0.09a | 0.24±0.01ab |
|  | HBC | 36.26±2.84a | 700.13±48.96b | 24.00±0.85b | 449.67±3.79b | 5.20±0.43c | 3.20±0.02a | 0.25±0.01a |
|  | FBC | 27.69±2.29b | 909.84±76.08a | 26.31±0.68a | 461.00±3.61b | 5.18±0.13c | 3.14±0.06a | 0.24±0.01ab |
|  | HFBC | 16.54±1.74c | 779.74±36.69b | 25.46±0.44a | 467.19±7.96a | 5.99±0.09b | 3.23±0.09a | 0.23±0.01b |

Note: Values followed by a different lowercase letter indicated significant differences according to Duncan's test (p < 0.05).

Fig. S1 The available Fe content of biochar samples (Means ± S.E., n = 3).

Fig. S2 The bacterial community traits in 15-30 cm depth of soils with the addition of different biochar samples. (a) Shannon index of bacterial community in 15-30 cm depth of soil. (b) The relative abundance of soil bacteria at the phylum level. (c) The relative abundance of soil bacteria at the genus level. (d) Redundancy analysis (RDA) based on genus level. (e) The two-factor network analysis based on genus level.

Fig. S3 The phylogenetic tree of endophytic bacteria on genus level.

Fig. S4 The standardized relative abundances of microbial functions predicted by Functional Annotation of Prokaryotic Taxa (FAPROTAX) analysis.