Supporting information

Fig. S1 EDX spectrum of Co@NC-800 catalyst.

Fig. S2. The wide-range XPS spectrum of Co@NC-T samples.

Fig. S3. XRD spectra of different cobalt content of Co@NC-800 catalysts

Fig. S4. XRD spectra of fresh and reused Co@NC-800 catalyst.

Table S1

Elemental analysis results of catalyst under different pyrolysis temperature.

| Sample | N (wt. %) | C (wt. %) | H (wt. %) |
| --- | --- | --- | --- |
| Co@NC-700 | 9.15 | 81.30 | 1.04 |
| Co@NC-800 | 8.19 | 82.34 | 1.74 |
| Co@NC-900 | 7.17 | 85.00 | 0.55 |

Table S2

The Co content of Co@NC-T catalysts.

| Sample | Co |
| --- | --- |
| Co@NC-700 | 0.69 |
| Co@NC-800 | 0.96 |
| Co@NC-900 | 0.54 |
| 1Co@NC-800 | 0.46 |
| 2Co@NC-800 | 0.59 |

Table S3

Structure parameters of Co@NC-T catalysts.

| Catalyst | Surface area | Pore size | Pore volume |
| --- | --- | --- | --- |
| Co@NC | 209.06 | 1.96 | 0.10 |
| Co@NC-800 | 268.19 | 1.78 | 0.12 |