Fig. S1 Characterization by X-ray diffraction (XRD) pattern of iron NPs obtained from borohydride reduction of FeBr2 5X10-3M in water/isopropanol solution. A. XRD diffraction pattern if iron NPs, B. Crystal structure (BCC)and characterization of metallic iron NPs (JCPDS#00-0696), c. Characterization of oxidizes phase of iron NPs lepidocrocite: FeO (OH) (JCPDS #044-4015)

Fig.S2 XPS binding energies of boron by products in iron NPs synthesize by NaBH4. Reduction in isopropanol/water solution. Peaks are related to boron binding energies a. Na2B4O2, b. FeB

TABLE 1 S2: XPS chemical analysis and surface atomic score levels of boron by, oxygen and iron determined In  iron NPs

| Surface Atomic Score Levels % |  |  |  |
| --- | --- | --- | --- |
| WASHING SOLUTIONS | BORON | OXYGEN | IRON |
| Clorophorm 13 49 19.1 |  |  |  |
| Acetone 11 60 23.06 |  |  |  |
| Hexane 6 72 17.95 |  |  |  |
| Toluene 5 69 17.48 |  |  |  |
| Isopropanol 22 42 14.23 |  |  |  |
| **Isopropanol/water 14 51 13.77 |  |  |  |
| Toluene/methanol 5 38 19.66 |  |  |  |
| Acetone/methanol 5 42 19.75 |  |  |  |
| Clophorm/methanol 23 19.63 14.11 |  |  |  |
| hexane/methanol 2 38 16.56 |  |  |  |

**solution use in all synthesis process, to dilute FeBr2, H2AuCl4 3[H2O] and NaBH4.