Supplementary Material

Investigation of Structural, Electronic, and Optical Properties of Er-Doped KNN System Based on First-Principles Calculations

Journal of Electroceramics

Zhichao Gong1 · Haojie Yue1 · Kailing Fang1 · Kun Guo1,* · Bing Xie1 · Zhiyong Liu1 · Pu Mao1 ·

Jinshan Lu1 · Kui Yao2 · Francis Eng Hock Tay3

1School of Power and Energy,

Nanchang Hangkong University, Nanchang 330063, China

2Institute of Materials Research and Engineering,

A*STAR (Agency for Science, Technology and Research),

2 Fusionopolis Way, 138634, Singapore,

3Department of Mechanical Engineering, National University of Singapore,

9 Engineering Drive 1, 117575, Singapore

*Corresponding Author: guokun@nchu.edu.cn

Table S1 Calculated formation energies (eV).

|  | E (Er→Nb) (×104) | E(KNN) (×104) | mNb (×103) | mEr (×103) | Ef |
| --- | --- | --- | --- | --- | --- |
| Er replacing Nb | -35656.35262 | -32220.08175 | -1656.574512 | -5091.890618 | -0.9547657 |

Fig. S1 The charge density distribution on (100) plane: (a, d) Pure KNN, (b) Er substituted K atom, (e) Er substituted Na atom, (c-g) Pure KNN, K-bit, Na-bit B-bit plane.

Table S2 Mulliken Populations

The pure KNN structure:

Atomic Populations (Mulliken)

-----------------------------

Species          Ion Spin      s      p      d      f     Total  Charge(e)   Spin(hbar/2)

=======================================================================

O               1   up:     0.91   2.43   0.00   0.00   3.34    -0.68        0.00

1   dn:     0.91   2.43   0.00   0.00   3.34

O               2   up:     0.91   2.43   0.00   0.00   3.34    -0.69        0.00

2   dn:     0.91   2.43   0.00   0.00   3.34

O               3   up:     0.92   2.42   0.00   0.00   3.34    -0.68        0.00

3   dn:     0.92   2.42   0.00   0.00   3.34

O               4   up:     0.92   2.43   0.00   0.00   3.34    -0.69       -0.00

4   dn:     0.92   2.43   0.00   0.00   3.34

O               5   up:     0.91   2.43   0.00   0.00   3.34    -0.68        0.00

5   dn:     0.91   2.43   0.00   0.00   3.34

O               6   up:     0.91   2.43   0.00   0.00   3.34    -0.69        0.00

6   dn:     0.91   2.43   0.00   0.00   3.34

O               7   up:     0.92   2.42   0.00   0.00   3.34    -0.68        0.00

7   dn:     0.92   2.42   0.00   0.00   3.34

O               8   up:     0.92   2.43   0.00   0.00   3.34    -0.69       -0.00

8   dn:     0.92   2.43   0.00   0.00   3.34

O               9   up:     0.91   2.43   0.00   0.00   3.34    -0.68        0.00

9   dn:     0.91   2.43   0.00   0.00   3.34

O              10   up:     0.91   2.43   0.00   0.00   3.34    -0.69        0.00

10   dn:     0.91   2.43   0.00   0.00   3.34

O              11   up:     0.92   2.42   0.00   0.00   3.34    -0.68        0.00

11   dn:     0.92   2.42   0.00   0.00   3.34

O              12   up:     0.92   2.43   0.00   0.00   3.34    -0.69       -0.00

12   dn:     0.92   2.43   0.00   0.00   3.34

O              13   up:     0.91   2.43   0.00   0.00   3.34    -0.68        0.00

13   dn:     0.91   2.43   0.00   0.00   3.34

O              14   up:     0.91   2.43   0.00   0.00   3.34    -0.69        0.00

14   dn:     0.91   2.43   0.00   0.00   3.34

O              15   up:     0.92   2.42   0.00   0.00   3.34    -0.68        0.00

15   dn:     0.92   2.42   0.00   0.00   3.34

O              16   up:     0.92   2.43   0.00   0.00   3.34    -0.69       -0.00

16   dn:     0.92   2.43   0.00   0.00   3.34

O              17   up:     0.91   2.44   0.00   0.00   3.35    -0.70        0.00

17   dn:     0.91   2.44   0.00   0.00   3.35

O              18   up:     0.91   2.45   0.00   0.00   3.36    -0.71       -0.00

18   dn:     0.91   2.45   0.00   0.00   3.36

O              19   up:     0.91   2.44   0.00   0.00   3.35    -0.70       -0.00

19   dn:     0.91   2.44   0.00   0.00   3.35

O              20   up:     0.91   2.44   0.00   0.00   3.35    -0.70       -0.00

20   dn:     0.91   2.44   0.00   0.00   3.35

O              21   up:     0.91   2.44   0.00   0.00   3.35    -0.70       -0.00

21   dn:     0.91   2.44   0.00   0.00   3.35

O              22   up:     0.91   2.44   0.00   0.00   3.36    -0.71       -0.00

22   dn:     0.91   2.44   0.00   0.00   3.36

O              23   up:     0.91   2.44   0.00   0.00   3.36    -0.71       -0.00

23   dn:     0.91   2.44   0.00   0.00   3.36

O              24   up:     0.91   2.44   0.00   0.00   3.36    -0.71       -0.00

24   dn:     0.91   2.44   0.00   0.00   3.36

Na              1   up:     0.97   2.93   0.00   0.00   3.90     1.20       -0.00

1   dn:     0.97   2.93   0.00   0.00   3.90

Na              2   up:     0.96   2.93   0.00   0.00   3.88     1.23        0.00

2   dn:     0.96   2.93   0.00   0.00   3.88

Na              3   up:     0.97   2.94   0.00   0.00   3.90     1.19        0.00

3   dn:     0.97   2.94   0.00   0.00   3.90

Na              4   up:     0.97   2.94   0.00   0.00   3.90     1.19        0.00

4   dn:     0.97   2.94   0.00   0.00   3.90

K               1   up:     0.88   2.75   0.10   0.00   3.74     1.52        0.00

1   dn:     0.88   2.75   0.10   0.00   3.74

K               2   up:     0.86   2.76   0.10   0.00   3.72     1.56        0.00

2   dn:     0.86   2.76   0.10   0.00   3.72

K               3   up:     0.86   2.76   0.10   0.00   3.72     1.56        0.00

3   dn:     0.86   2.76   0.10   0.00   3.72

K               4   up:     0.87   2.76   0.10   0.00   3.73     1.54        0.00

4   dn:     0.87   2.76   0.10   0.00   3.73

Nb              1   up:     1.21   3.43   1.51   0.00   6.15     0.70       -0.00

1   dn:     1.21   3.43   1.51   0.00   6.15

Nb              2   up:     1.21   3.43   1.51   0.00   6.15     0.70       -0.00

2   dn:     1.21   3.43   1.51   0.00   6.15

Nb              3   up:     1.21   3.43   1.51   0.00   6.15     0.70       -0.00

3   dn:     1.21   3.43   1.51   0.00   6.15

Nb              4   up:     1.21   3.43   1.51   0.00   6.15     0.70       -0.00

4   dn:     1.21   3.43   1.51   0.00   6.15

Nb              5   up:     1.21   3.42   1.51   0.00   6.14     0.72        0.00

5   dn:     1.21   3.42   1.51   0.00   6.14

Nb              6   up:     1.21   3.44   1.51   0.00   6.16     0.68       -0.00

6   dn:     1.21   3.44   1.51   0.00   6.16

Nb              7   up:     1.21   3.42   1.51   0.00   6.14     0.72        0.00

7   dn:     1.21   3.42   1.51   0.00   6.14

Nb              8   up:     1.21   3.44   1.51   0.00   6.16     0.68       -0.00

8   dn:     1.21   3.44   1.51   0.00   6.16

=========================================================================================

Bond                   Population        Spin       Length (A)

================================================================================

O 13 -- Nb 7                   0.86        -0.00          1.86575

O 1  -- Nb 5                   0.86        -0.00          1.86575

O 9  -- Nb 5                   0.86        -0.00          1.86575

O 5  -- Nb 7                   0.86        -0.00          1.86575

O 14 -- Nb 4                   0.86        -0.00          1.86655

O 2  -- Nb 1                   0.86        -0.00          1.86655

O 10 -- Nb 3                   0.86        -0.00          1.86655

O 6  -- Nb 2                   0.86        -0.00          1.86655

O 11 -- Nb 3                   0.92        -0.00          1.87505

O 7  -- Nb 2                   0.92        -0.00          1.87505

O 15 -- Nb 4                   0.92        -0.00          1.87505

O 3  -- Nb 1                   0.92        -0.00          1.87505

O 16 -- Nb 8                   0.92        -0.00          1.87695

O 4  -- Nb 6                   0.92        -0.00          1.87695

O 12 -- Nb 6                   0.92        -0.00          1.87695

O 8  -- Nb 8                   0.92        -0.00          1.87695

O 22 -- Nb 6                   0.68        -0.00          1.98552

O 22 -- Nb 8                   0.68        -0.00          1.98552

O 21 -- Nb 7                   0.69        -0.00          1.98660

O 21 -- Nb 5                   0.69        -0.00          1.98660

O 24 -- Nb 3                   0.67         0.00          1.98948

O 24 -- Nb 2                   0.67         0.00          1.98948

O 23 -- Nb 4                   0.67         0.00          1.98948

O 23 -- Nb 1                   0.67         0.00          1.98948

O 20 -- Nb 3                   0.72         0.00          2.00285

O 20 -- Nb 2                   0.72         0.00          2.00285

O 19 -- Nb 4                   0.72         0.00          2.00285

O 19 -- Nb 1                   0.72         0.00          2.00285

O 17 -- Nb 7                   0.73        -0.00          2.00414

O 17 -- Nb 5                   0.73        -0.00          2.00414

O 18 -- Nb 8                   0.71         0.00          2.00883

O 18 -- Nb 6                   0.71         0.00          2.00883

O 13 -- Nb 2                   0.47         0.00          2.18676

O 1  -- Nb 3                   0.47         0.00          2.18676

O 9  -- Nb 1                   0.47         0.00          2.18676

O 5  -- Nb 4                   0.47         0.00          2.18676

O 10 -- Nb 6                   0.47        -0.00          2.18830

O 6  -- Nb 8                   0.47        -0.00          2.18830

O 14 -- Nb 8                   0.47        -0.00          2.18830

O 2  -- Nb 6                   0.47        -0.00          2.18830

O 15 -- Nb 7                   0.47        -0.00          2.22972

O 11 -- Nb 5                   0.47        -0.00          2.22972

O 7  -- Nb 7                   0.47        -0.00          2.22972

O 3  -- Nb 5                   0.47        -0.00          2.22972

O 12 -- Nb 3                   0.47        -0.00          2.23348

O 8  -- Nb 2                   0.47        -0.00          2.23348

O 16 -- Nb 4                   0.47        -0.00          2.23348

O 4  -- Nb 1                   0.47        -0.00          2.23348

O 22 -- Na 2                  -0.07        -0.00          2.48239

O 23 -- Na 3                  -0.08        -0.00          2.48958

O 24 -- Na 4                  -0.08        -0.00          2.48958

O 18 -- Na 1                  -0.07        -0.00          2.51914

O 9  -- Na 3                  -0.09        -0.00          2.63156

O 5  -- Na 3                  -0.09        -0.00          2.63156

O 13 -- Na 4                  -0.09        -0.00          2.63156

O 1  -- Na 4                  -0.09        -0.00          2.63156

O 10 -- Na 1                  -0.08        -0.00          2.65013

O 6  -- Na 1                  -0.08        -0.00          2.65013

O 14 -- Na 1                  -0.08        -0.00          2.65013

O 2  -- Na 1                  -0.08        -0.00          2.65013

O 14 -- Na 2                  -0.09         0.00          2.66362

O 10 -- Na 2                  -0.09         0.00          2.66362

O 6  -- Na 2                  -0.09         0.00          2.66362

O 2  -- Na 2                  -0.09         0.00          2.66362

O 12 -- Na 4                  -0.07        -0.00          2.67337

O 16 -- Na 3                  -0.07        -0.00          2.67337

O 8  -- Na 4                  -0.07        -0.00          2.67337

O 4  -- Na 3                  -0.07        -0.00          2.67337

O 21 -- K 4                   -0.23         0.00          2.72162

O 20 -- K 3                   -0.18        -0.00          2.73328

O 19 -- K 2                   -0.18        -0.00          2.73328

O 17 -- K 1                   -0.20         0.00          2.74869

O 13 -- O 24                  -0.03        -0.00          2.77859

O 9  -- O 23                  -0.03        -0.00          2.77859

O 5  -- O 23                  -0.03        -0.00          2.77859

O 1  -- O 24                  -0.03        -0.00          2.77859

O 15 -- K 4                   -0.18        -0.00          2.78971

O 11 -- K 4                   -0.18        -0.00          2.78971

O 7  -- K 4                   -0.18        -0.00          2.78971

O 3  -- K 4                   -0.18        -0.00          2.78971

O 12 -- K 3                   -0.16         0.00          2.79724

O 8  -- K 3                   -0.16         0.00          2.79724

O 16 -- K 2                   -0.16         0.00          2.79724

O 4  -- K 2                   -0.16         0.00          2.79724

O 10 -- O 22                  -0.03         0.00          2.79835

O 6  -- O 22                  -0.03         0.00          2.79835

O 14 -- O 22                  -0.03         0.00          2.79835

O 2  -- O 22                  -0.03         0.00          2.79835

O 13 -- K 3                   -0.22        -0.00          2.80038

O 9  -- K 2                   -0.22        -0.00          2.80038

O 5  -- K 2                   -0.22        -0.00          2.80038

O 1  -- K 3                   -0.22        -0.00          2.80038

O 6  -- O 14                  -0.03        -0.00          2.80582

O 2  -- O 10                  -0.03        -0.00          2.80582

O 15 -- K 1                   -0.20        -0.00          2.81678

O 11 -- K 1                   -0.20        -0.00          2.81678

O 7  -- K 1                   -0.20        -0.00          2.81678

O 3  -- K 1                   -0.20        -0.00          2.81678

O 16 -- O 23                  -0.03         0.00          2.82195

O 12 -- O 24                  -0.03         0.00          2.82195

O 4  -- O 23                  -0.03         0.00          2.82195

O 8  -- O 24                  -0.03         0.00          2.82195

O 10 -- O 18                  -0.03        -0.00          2.82351

O 6  -- O 18                  -0.03        -0.00          2.82351

O 14 -- O 18                  -0.03        -0.00          2.82351

O 2  -- O 18                  -0.03        -0.00          2.82351

O 9  -- O 21                  -0.02         0.00          2.82383

O 1  -- O 21                  -0.02         0.00          2.82383

O 13 -- O 21                  -0.02         0.00          2.82383

O 5  -- O 21                  -0.02         0.00          2.82383

O 5  -- O 13                  -0.02        -0.00          2.82847

O 1  -- O 9                   -0.02        -0.00          2.82847

O 21 -- Na 4                  -0.12        -0.00          2.82886

O 21 -- Na 3                  -0.12        -0.00          2.82886

O 11 -- O 21                  -0.03         0.00          2.83418

O 7  -- O 21                  -0.03         0.00          2.83418

O 15 -- O 21                  -0.03         0.00          2.83418

O 3  -- O 21                  -0.03         0.00          2.83418

O 14 -- O 19                  -0.02        -0.00          2.83453

O 2  -- O 19                  -0.02        -0.00          2.83453

O 10 -- O 20                  -0.02        -0.00          2.83453

O 6  -- O 20                  -0.02        -0.00          2.83453

O 14 -- O 15                  -0.01        -0.00          2.83900

O 2  -- O 3                   -0.01        -0.00          2.83900

O 10 -- O 11                  -0.01        -0.00          2.83900

O 6  -- O 7                   -0.01        -0.00          2.83900

O 16 -- O 22                  -0.02        -0.00          2.84171

O 8  -- O 22                  -0.02        -0.00          2.84171

O 12 -- O 22                  -0.02        -0.00          2.84171

O 4  -- O 22                  -0.02        -0.00          2.84171

O 14 -- O 23                  -0.02         0.00          2.84331

O 2  -- O 23                  -0.02         0.00          2.84331

O 10 -- O 24                  -0.02         0.00          2.84331

O 6  -- O 24                  -0.02         0.00          2.84331

O 24 -- Na 2                  -0.11         0.00          2.84391

O 23 -- Na 2                  -0.11         0.00          2.84391

O 13 -- O 20                  -0.03        -0.00          2.84421

O 9  -- O 19                  -0.03        -0.00          2.84421

O 5  -- O 19                  -0.03        -0.00          2.84421

O 1  -- O 20                  -0.03        -0.00          2.84421

O 8  -- O 16                  -0.01        -0.00          2.85067

O 4  -- O 12                  -0.01        -0.00          2.85067

O 11 -- O 24                  -0.02         0.00          2.85409

O 7  -- O 24                  -0.02         0.00          2.85409

O 15 -- O 23                  -0.02         0.00          2.85409

O 3  -- O 23                  -0.02         0.00          2.85409

O 15 -- O 19                  -0.02         0.00          2.85468

O 11 -- O 20                  -0.02         0.00          2.85468

O 7  -- O 20                  -0.02         0.00          2.85468

O 3  -- O 19                  -0.02         0.00          2.85468

O 13 -- O 17                  -0.02         0.00          2.85650

O 9  -- O 17                  -0.02         0.00          2.85650

O 5  -- O 17                  -0.02         0.00          2.85650

O 1  -- O 17                  -0.02         0.00          2.85650

O 17 -- K 3                   -0.22         0.00          2.85982

O 17 -- K 2                   -0.22         0.00          2.85982

O 6  -- O 13                  -0.02        -0.00          2.86033

O 5  -- O 14                  -0.02        -0.00          2.86033

O 2  -- O 9                   -0.02        -0.00          2.86033

O 1  -- O 10                  -0.02        -0.00          2.86033

O 20 -- Na 1                  -0.09        -0.00          2.86114

O 19 -- Na 1                  -0.09        -0.00          2.86114

O 15 -- O 17                  -0.03         0.00          2.86738

O 11 -- O 17                  -0.03         0.00          2.86738

O 7  -- O 17                  -0.03         0.00          2.86738

O 3  -- O 17                  -0.03         0.00          2.86738

O 16 -- O 18                  -0.02        -0.00          2.86755

O 12 -- O 18                  -0.02        -0.00          2.86755

O 8  -- O 18                  -0.02        -0.00          2.86755

O 4  -- O 18                  -0.02        -0.00          2.86755

O 18 -- K 3                   -0.18        -0.00          2.87322

O 18 -- K 2                   -0.18        -0.00          2.87322

O 16 -- O 19                  -0.02         0.00          2.88217

O 12 -- O 20                  -0.02         0.00          2.88217

O 8  -- O 20                  -0.02         0.00          2.88217

O 4  -- O 19                  -0.02         0.00          2.88217

O 9  -- O 11                  -0.02        -0.00          2.88246

O 5  -- O 7                   -0.02        -0.00          2.88246

O 13 -- O 15                  -0.02        -0.00          2.88246

O 1  -- O 3                   -0.02        -0.00          2.88246

O 5  -- O 16                  -0.03         0.00          2.88530

O 4  -- O 9                   -0.03         0.00          2.88530

O 8  -- O 13                  -0.03         0.00          2.88530

O 1  -- O 12                  -0.03         0.00          2.88530

O 11 -- K 2                   -0.19         0.00          2.88734

O 7  -- K 2                   -0.19         0.00          2.88734

O 15 -- K 3                   -0.19         0.00          2.88734

O 3  -- K 3                   -0.19         0.00          2.88734

O 20 -- K 1                   -0.23        -0.00          2.89162

O 19 -- K 1                   -0.23        -0.00          2.89162

O 16 -- K 4                   -0.17        -0.00          2.89581

O 8  -- K 4                   -0.17        -0.00          2.89581

O 12 -- K 4                   -0.17        -0.00          2.89581

O 4  -- K 4                   -0.17        -0.00          2.89581

O 6  -- O 16                  -0.02        -0.00          2.90070

O 4  -- O 10                  -0.02        -0.00          2.90070

O 8  -- O 14                  -0.02        -0.00          2.90070

O 2  -- O 12                  -0.02        -0.00          2.90070

O 24 -- K 4                   -0.25        -0.00          2.91158

O 23 -- K 4                   -0.25        -0.00          2.91158

O 15 -- O 16                  -0.02        -0.00          2.92585

O 11 -- O 12                  -0.02        -0.00          2.92585

O 7  -- O 8                   -0.02        -0.00          2.92585

O 3  -- O 4                   -0.02        -0.00          2.92585

O 10 -- K 2                   -0.22        -0.00          2.94176

O 6  -- K 2                   -0.22        -0.00          2.94176

O 14 -- K 3                   -0.22        -0.00          2.94176

O 2  -- K 3                   -0.22        -0.00          2.94176

O 12 -- K 1                   -0.21        -0.00          2.94680

O 8  -- K 1                   -0.21        -0.00          2.94680

O 16 -- K 1                   -0.21        -0.00          2.94680

O 4  -- K 1                   -0.21        -0.00          2.94680

O 22 -- Na 4                  -0.10        -0.00          2.95455

O 22 -- Na 3                  -0.10        -0.00          2.95455

O 15 -- Na 4                  -0.08        -0.00          2.96490

O 3  -- Na 4                  -0.08        -0.00          2.96490

O 11 -- Na 3                  -0.08        -0.00          2.96490

O 7  -- Na 3                  -0.08        -0.00          2.96490

O 7  -- O 15                  -0.02         0.00          2.96646

O 3  -- O 11                  -0.02         0.00          2.96646

O 1  -- Na 2                  -0.09         0.00          2.98691

O 13 -- Na 2                  -0.09         0.00          2.98691

O 9  -- Na 2                  -0.09         0.00          2.98691

O 5  -- Na 2                  -0.09         0.00          2.98691

Er substituted the K-site structure of KNN：

Atomic Populations (Mulliken)

-----------------------------

Species          Ion Spin      s      p      d      f     Total  Charge(e)   Spin(hbar/2)

=========================================================================================

O               1   up:     0.91   2.44   0.00   0.00   3.35    -0.71       -0.00

1   dn:     0.91   2.44   0.00   0.00   3.35

O               2   up:     0.91   2.44   0.00   0.00   3.35    -0.70       -0.00

2   dn:     0.91   2.44   0.00   0.00   3.35

O               3   up:     0.91   2.44   0.00   0.00   3.35    -0.70       -0.00

3   dn:     0.91   2.44   0.00   0.00   3.35

O               4   up:     0.91   2.44   0.00   0.00   3.35    -0.71       -0.00

4   dn:     0.91   2.44   0.00   0.00   3.36

O               5   up:     0.91   2.44   0.00   0.00   3.35    -0.71       -0.00

5   dn:     0.91   2.44   0.00   0.00   3.35

O               6   up:     0.91   2.44   0.00   0.00   3.35    -0.71       -0.00

6   dn:     0.91   2.44   0.00   0.00   3.35

O               7   up:     0.91   2.44   0.00   0.00   3.35    -0.70       -0.00

7   dn:     0.91   2.44   0.00   0.00   3.35

O               8   up:     0.91   2.44   0.00   0.00   3.35    -0.70       -0.00

8   dn:     0.91   2.44   0.00   0.00   3.35

O               9   up:     0.91   2.44   0.00   0.00   3.35    -0.71       -0.00

9   dn:     0.91   2.44   0.00   0.00   3.35

O              10   up:     0.91   2.44   0.00   0.00   3.35    -0.70       -0.00

10   dn:     0.91   2.44   0.00   0.00   3.35

O              11   up:     0.91   2.44   0.00   0.00   3.35    -0.70       -0.00

11   dn:     0.91   2.44   0.00   0.00   3.35

O              12   up:     0.91   2.44   0.00   0.00   3.35    -0.71       -0.00

12   dn:     0.91   2.44   0.00   0.00   3.36

O              13   up:     0.91   2.44   0.00   0.00   3.35    -0.71       -0.00

13   dn:     0.91   2.44   0.00   0.00   3.35

O              14   up:     0.91   2.44   0.00   0.00   3.35    -0.71       -0.00

14   dn:     0.91   2.44   0.00   0.00   3.35

O              15   up:     0.91   2.44   0.00   0.00   3.35    -0.70       -0.00

15   dn:     0.91   2.44   0.00   0.00   3.35

O              16   up:     0.91   2.44   0.00   0.00   3.35    -0.70       -0.00

16   dn:     0.91   2.44   0.00   0.00   3.35

O              17   up:     0.91   2.44   0.00   0.00   3.35    -0.71       -0.00

17   dn:     0.91   2.44   0.00   0.00   3.35

O              18   up:     0.91   2.44   0.00   0.00   3.36    -0.72       -0.00

18   dn:     0.91   2.45   0.00   0.00   3.36

O              19   up:     0.91   2.44   0.00   0.00   3.36    -0.71       -0.00

19   dn:     0.91   2.45   0.00   0.00   3.36

O              20   up:     0.91   2.44   0.00   0.00   3.35    -0.71       -0.00

20   dn:     0.91   2.44   0.00   0.00   3.35

O              21   up:     0.91   2.44   0.00   0.00   3.35    -0.70       -0.00

21   dn:     0.91   2.44   0.00   0.00   3.35

O              22   up:     0.91   2.44   0.00   0.00   3.35    -0.70       -0.00

22   dn:     0.91   2.44   0.00   0.00   3.35

O              23   up:     0.91   2.44   0.00   0.00   3.35    -0.70       -0.00

23   dn:     0.91   2.44   0.00   0.00   3.35

O              24   up:     0.91   2.44   0.00   0.00   3.36    -0.71       -0.00

24   dn:     0.91   2.44   0.00   0.00   3.36

Na              1   up:     0.96   2.91   0.00   0.00   3.87     1.26       -0.00

1   dn:     0.96   2.91   0.00   0.00   3.87

Na              2   up:     0.95   2.93   0.00   0.00   3.88     1.23       -0.00

2   dn:     0.95   2.93   0.00   0.00   3.88

Na              3   up:     0.96   2.91   0.00   0.00   3.87     1.27       -0.00

3   dn:     0.96   2.91   0.00   0.00   3.87

Na              4   up:     0.97   2.93   0.00   0.00   3.90     1.21        0.00

4   dn:     0.97   2.93   0.00   0.00   3.89

K               1   up:     0.87   2.70   0.09   0.00   3.66     1.68        0.00

1   dn:     0.87   2.70   0.09   0.00   3.66

K               2   up:     0.86   2.75   0.10   0.00   3.71     1.59        0.00

2   dn:     0.86   2.75   0.10   0.00   3.71

K               3   up:     0.86   2.75   0.10   0.00   3.70     1.60        0.00

3   dn:     0.86   2.75   0.10   0.00   3.70

Nb              1   up:     1.22   3.41   1.52   0.00   6.14     0.72       -0.00

1   dn:     1.22   3.41   1.52   0.00   6.14

Nb              2   up:     1.22   3.42   1.52   0.00   6.16     0.68        0.00

2   dn:     1.22   3.42   1.52   0.00   6.16

Nb              3   up:     1.22   3.41   1.52   0.00   6.15     0.70        0.00

3   dn:     1.22   3.41   1.52   0.00   6.15

Nb              4   up:     1.22   3.41   1.52   0.00   6.15     0.70        0.00

4   dn:     1.22   3.41   1.52   0.00   6.15

Nb              5   up:     1.22   3.41   1.52   0.00   6.14     0.72       -0.00

5   dn:     1.22   3.41   1.52   0.00   6.14

Nb              6   up:     1.22   3.42   1.52   0.00   6.16     0.68        0.00

6   dn:     1.22   3.42   1.52   0.00   6.16

Nb              7   up:     1.22   3.41   1.52   0.00   6.15     0.70        0.00

7   dn:     1.22   3.41   1.52   0.00   6.15

Nb              8   up:     1.22   3.41   1.52   0.00   6.15     0.70        0.00

8   dn:     1.22   3.41   1.52   0.00   6.15

Er              1   up:     1.05   3.04   0.32   7.00  11.42     1.50        2.34

1   dn:     1.05   3.04   0.31   4.67   9.08

=========================================================================================

Bond                   Population        Spin       Length (A)

================================================================================

O 10 -- Nb 5                   0.71         0.00          1.97090

O 2  -- Nb 1                   0.71         0.00          1.97090

O 14 -- Nb 6                   0.66        -0.00          1.97568

O 6  -- Nb 2                   0.66        -0.00          1.97568

O 9  -- Nb 7                   0.72         0.00          1.97802

O 1  -- Nb 3                   0.72         0.00          1.97802

O 13 -- Nb 3                   0.63        -0.00          1.97946

O 5  -- Nb 7                   0.63        -0.00          1.97946

O 11 -- Nb 5                   0.78         0.00          1.98289

O 3  -- Nb 1                   0.78         0.00          1.98289

O 23 -- Nb 5                   0.69         0.00          1.98365

O 23 -- Nb 1                   0.69         0.00          1.98365

O 15 -- Nb 6                   0.71        -0.00          1.98732

O 7  -- Nb 2                   0.71        -0.00          1.98732

O 16 -- Nb 4                   0.77         0.00          1.98805

O 8  -- Nb 8                   0.77         0.00          1.98805

O 22 -- Nb 4                   0.69         0.00          1.99239

O 22 -- Nb 8                   0.69         0.00          1.99239

O 21 -- Nb 3                   0.69         0.00          1.99862

O 21 -- Nb 7                   0.69         0.00          1.99862

O 24 -- Nb 2                   0.69         0.00          2.00544

O 24 -- Nb 6                   0.69         0.00          2.00544

O 10 -- Nb 8                   0.67         0.00          2.00611

O 2  -- Nb 4                   0.67         0.00          2.00611

O 12 -- Nb 8                   0.67        -0.00          2.00932

O 4  -- Nb 4                   0.67        -0.00          2.00932

O 20 -- Nb 6                   0.68        -0.00          2.01729

O 20 -- Nb 2                   0.68        -0.00          2.01729

O 17 -- Nb 7                   0.67        -0.00          2.02118

O 17 -- Nb 3                   0.67        -0.00          2.02118

O 14 -- Nb 4                   0.61        -0.00          2.02139

O 6  -- Nb 8                   0.61        -0.00          2.02139

O 9  -- Nb 2                   0.66         0.00          2.02634

O 1  -- Nb 6                   0.66         0.00          2.02634

O 18 -- Nb 8                   0.65        -0.00          2.02890

O 18 -- Nb 4                   0.65        -0.00          2.02890

O 13 -- Nb 1                   0.57        -0.00          2.03043

O 5  -- Nb 5                   0.57        -0.00          2.03043

O 15 -- Nb 3                   0.65         0.00          2.03368

O 7  -- Nb 7                   0.65         0.00          2.03368

O 19 -- Nb 5                   0.63        -0.00          2.03720

O 19 -- Nb 1                   0.63        -0.00          2.03720

O 12 -- Nb 5                   0.63        -0.00          2.04269

O 4  -- Nb 1                   0.63        -0.00          2.04269

O 16 -- Nb 6                   0.70         0.00          2.04456

O 8  -- Nb 2                   0.70         0.00          2.04456

O 11 -- Nb 7                   0.70         0.00          2.04722

O 3  -- Nb 3                   0.70         0.00          2.04722

O 19 -- Er 1                   0.08         0.00          2.53867

O 24 -- Na 4                  -0.06        -0.00          2.61214

O 13 -- Er 1                   0.06         0.00          2.61986

O 5  -- Er 1                   0.06         0.00          2.61986

O 12 -- Er 1                   0.05         0.00          2.64111

O 4  -- Er 1                   0.05         0.00          2.64111

O 18 -- Er 1                   0.07         0.00          2.65891

O 24 -- Na 2                  -0.09        -0.00          2.68512

O 9  -- Na 1                  -0.08         0.00          2.72521

O 1  -- Na 1                  -0.08         0.00          2.72521

O 14 -- Na 3                  -0.10        -0.00          2.72660

O 6  -- Na 3                  -0.10        -0.00          2.72660

O 5  -- O 12                  -0.04        -0.00          2.73287

O 4  -- O 13                  -0.04        -0.00          2.73287

O 13 -- O 19                  -0.04        -0.00          2.73905

O 5  -- O 19                  -0.04        -0.00          2.73905

O 13 -- O 17                  -0.04        -0.00          2.75235

O 5  -- O 17                  -0.04        -0.00          2.75235

O 18 -- Na 1                  -0.08        -0.00          2.75268

O 6  -- O 12                  -0.04        -0.00          2.75582

O 4  -- O 14                  -0.04        -0.00          2.75582

O 17 -- K 1                   -0.23        -0.00          2.75743

O 13 -- O 15                  -0.04        -0.00          2.76007

O 5  -- O 7                   -0.04        -0.00          2.76007

O 12 -- O 18                  -0.04        -0.00          2.76465

O 4  -- O 18                  -0.04        -0.00          2.76465

O 12 -- O 19                  -0.04        -0.00          2.76584

O 4  -- O 19                  -0.04        -0.00          2.76584

O 10 -- Na 1                  -0.08         0.00          2.76680

O 2  -- Na 1                  -0.08         0.00          2.76680

O 16 -- Na 4                  -0.08        -0.00          2.77171

O 8  -- Na 4                  -0.08        -0.00          2.77171

O 15 -- Na 3                  -0.10        -0.00          2.77503

O 7  -- Na 3                  -0.10        -0.00          2.77503

O 14 -- Na 2                  -0.12        -0.00          2.77510

O 6  -- Na 2                  -0.12        -0.00          2.77510

O 21 -- Na 2                  -0.07        -0.00          2.77519

O 14 -- O 15                  -0.03        -0.00          2.77572

O 6  -- O 7                   -0.03        -0.00          2.77572

O 15 -- K 3                   -0.18        -0.00          2.78186

O 7  -- K 3                   -0.18        -0.00          2.78186

O 16 -- K 2                   -0.15        -0.00          2.78451

O 8  -- K 2                   -0.15        -0.00          2.78451

O 20 -- Na 1                  -0.09         0.00          2.78548

O 14 -- O 18                  -0.03        -0.00          2.78678

O 6  -- O 18                  -0.03        -0.00          2.78678

O 14 -- O 20                  -0.03        -0.00          2.79211

O 6  -- O 20                  -0.03        -0.00          2.79211

O 9  -- Na 2                  -0.10        -0.00          2.79597

O 1  -- Na 2                  -0.10        -0.00          2.79597

O 22 -- Na 2                  -0.10         0.00          2.80814

O 23 -- Na 3                  -0.09         0.00          2.81000

O 15 -- O 20                  -0.03        -0.00          2.81306

O 7  -- O 20                  -0.03        -0.00          2.81306

O 10 -- Na 2                  -0.08         0.00          2.81382

O 2  -- Na 2                  -0.08         0.00          2.81382

O 22 -- Na 4                  -0.09         0.00          2.81626

O 15 -- O 17                  -0.03        -0.00          2.81866

O 7  -- O 17                  -0.03        -0.00          2.81866

O 21 -- Na 4                  -0.09        -0.00          2.81970

O 11 -- K 2                   -0.18        -0.00          2.82011

O 3  -- K 2                   -0.18        -0.00          2.82011

O 17 -- Er 1                   0.03         0.00          2.82296

O 11 -- Na 4                  -0.06        -0.00          2.82345

O 3  -- Na 4                  -0.06        -0.00          2.82345

O 9  -- O 24                  -0.03         0.00          2.82393

O 1  -- O 24                  -0.03         0.00          2.82393

O 14 -- O 24                  -0.03         0.00          2.82495

O 6  -- O 24                  -0.03         0.00          2.82495

O 9  -- O 21                  -0.03         0.00          2.82547

O 1  -- O 21                  -0.03         0.00          2.82547

O 14 -- O 22                  -0.03         0.00          2.82989

O 6  -- O 22                  -0.03         0.00          2.82989

O 6  -- O 10                  -0.03         0.00          2.83176

O 2  -- O 14                  -0.03         0.00          2.83176

O 11 -- K 3                   -0.18        -0.00          2.83201

O 3  -- K 3                   -0.18        -0.00          2.83201

O 6  -- O 9                   -0.03        -0.00          2.83451

O 1  -- O 14                  -0.03        -0.00          2.83451

O 16 -- O 22                  -0.03         0.00          2.83481

O 8  -- O 22                  -0.03         0.00          2.83481

O 21 -- Na 3                  -0.10        -0.00          2.83785

O 9  -- K 2                   -0.23        -0.00          2.83856

O 1  -- K 2                   -0.23        -0.00          2.83856

O 10 -- O 22                  -0.03         0.00          2.84181

O 2  -- O 22                  -0.03         0.00          2.84181

O 13 -- Na 3                  -0.12        -0.00          2.84201

O 5  -- Na 3                  -0.12        -0.00          2.84201

O 19 -- K 1                   -0.26        -0.00          2.84282

O 22 -- K 3                   -0.23        -0.00          2.84373

O 10 -- O 23                  -0.02         0.00          2.84383

O 2  -- O 23                  -0.02         0.00          2.84383

O 13 -- O 23                  -0.02         0.00          2.84689

O 5  -- O 23                  -0.02         0.00          2.84689

O 20 -- K 1                   -0.25        -0.00          2.84937

O 5  -- O 9                   -0.02         0.00          2.84958

O 1  -- O 13                  -0.02         0.00          2.84958

O 16 -- O 24                  -0.03        -0.00          2.85076

O 8  -- O 24                  -0.03        -0.00          2.85076

O 12 -- K 1                   -0.26        -0.00          2.85099

O 4  -- K 1                   -0.26        -0.00          2.85099

O 13 -- O 21                  -0.02         0.00          2.85362

O 5  -- O 21                  -0.02         0.00          2.85362

O 10 -- O 11                  -0.02         0.00          2.85409

O 2  -- O 3                   -0.02         0.00          2.85409

O 5  -- O 10                  -0.02         0.00          2.85505

O 2  -- O 13                  -0.02         0.00          2.85505

O 15 -- O 21                  -0.02         0.00          2.85612

O 7  -- O 21                  -0.02         0.00          2.85612

O 9  -- O 17                  -0.02         0.00          2.85649

O 1  -- O 17                  -0.02         0.00          2.85649

O 11 -- O 23                  -0.02         0.00          2.85907

O 3  -- O 23                  -0.02         0.00          2.85907

O 15 -- O 24                  -0.02         0.00          2.86116

O 7  -- O 24                  -0.02         0.00          2.86116

O 8  -- O 10                  -0.02        -0.00          2.86136

O 2  -- O 16                  -0.02        -0.00          2.86136

O 16 -- K 1                   -0.20        -0.00          2.86244

O 8  -- K 1                   -0.20        -0.00          2.86244

O 15 -- K 1                   -0.28        -0.00          2.86321

O 7  -- K 1                   -0.28        -0.00          2.86321

O 10 -- O 19                  -0.02         0.00          2.86407

O 2  -- O 19                  -0.02         0.00          2.86407

O 12 -- Na 3                  -0.11        -0.00          2.86439

O 4  -- Na 3                  -0.11        -0.00          2.86439

O 9  -- O 20                  -0.02         0.00          2.86613

O 1  -- O 20                  -0.02         0.00          2.86613

O 11 -- O 21                  -0.02         0.00          2.86638

O 3  -- O 21                  -0.02         0.00          2.86638

O 9  -- O 11                  -0.02         0.00          2.86869

O 1  -- O 3                   -0.02         0.00          2.86869

O 10 -- O 18                  -0.02         0.00          2.86869

O 2  -- O 18                  -0.02         0.00          2.86869

O 8  -- O 9                   -0.02        -0.00          2.87072

O 1  -- O 16                  -0.02        -0.00          2.87072

O 9  -- Na 4                  -0.12        -0.00          2.87388

O 1  -- Na 4                  -0.12        -0.00          2.87388

O 19 -- Na 1                  -0.10        -0.00          2.87412

O 12 -- O 23                  -0.02         0.00          2.87432

O 4  -- O 23                  -0.02         0.00          2.87432

O 22 -- Na 3                  -0.11         0.00          2.87550

O 24 -- K 3                   -0.24        -0.00          2.87832

O 15 -- O 16                  -0.02        -0.00          2.88132

O 7  -- O 8                   -0.02        -0.00          2.88132

O 12 -- O 22                  -0.02         0.00          2.88171

O 4  -- O 22                  -0.02         0.00          2.88171

O 23 -- Na 2                  -0.08        -0.00          2.88207

O 17 -- K 2                   -0.22        -0.00          2.88649

O 7  -- O 11                  -0.02         0.00          2.88754

O 3  -- O 15                  -0.02         0.00          2.88754

O 24 -- Na 3                  -0.12         0.00          2.88911

O 13 -- Na 1                  -0.13        -0.00          2.88992

O 5  -- Na 1                  -0.13        -0.00          2.88992

O 8  -- O 12                  -0.02         0.00          2.89587

O 4  -- O 16                  -0.02         0.00          2.89587

O 14 -- Na 1                  -0.15        -0.00          2.89872

O 6  -- Na 1                  -0.15        -0.00          2.89872

O 11 -- O 12                  -0.02         0.00          2.89917

O 3  -- O 4                   -0.02         0.00          2.89917

O 11 -- K 1                   -0.21        -0.00          2.90083

O 3  -- K 1                   -0.21        -0.00          2.90083

O 16 -- O 18                  -0.02         0.00          2.90282

O 8  -- O 18                  -0.02         0.00          2.90282

O 11 -- O 17                  -0.02         0.00          2.90419

O 3  -- O 17                  -0.02         0.00          2.90419

O 20 -- Er 1                   0.03         0.00          2.90428

O 11 -- O 19                  -0.02         0.00          2.90595

O 3  -- O 19                  -0.02         0.00          2.90595

O 23 -- K 3                   -0.25         0.00          2.90609

O 16 -- O 20                  -0.02         0.00          2.90699

O 8  -- O 20                  -0.02         0.00          2.90699

O 14 -- Er 1                  -0.01         0.00          2.90995

O 6  -- Er 1                  -0.01         0.00          2.90995

O 10 -- K 2                   -0.25         0.00          2.91440

O 2  -- K 2                   -0.25         0.00          2.91440

O 12 -- K 3                   -0.19        -0.00          2.91468

O 4  -- K 3                   -0.19        -0.00          2.91468

O 17 -- Na 1                  -0.11        -0.00          2.91476

O 16 -- K 3                   -0.20        -0.00          2.91499

O 8  -- K 3                   -0.20        -0.00          2.91499

O 19 -- K 2                   -0.19        -0.00          2.91505

O 21 -- K 3                   -0.27        -0.00          2.92337

O 18 -- K 1                   -0.26        -0.00          2.92806

O 20 -- K 2                   -0.23        -0.00          2.98754

O 10 -- Na 4                  -0.10        -0.00          2.99286

O 2  -- Na 4                  -0.10        -0.00          2.99286

================================================================================

Er substituted the Na-site structure of KNN：

Atomic Populations (Mulliken)

-----------------------------

Species          Ion Spin      s      p      d      f     Total  Charge(e)   Spin(hbar/2)

=========================================================================================

O               1   up:     0.91   2.44   0.00   0.00   3.35    -0.70       -0.01

1   dn:     0.91   2.44   0.00   0.00   3.35

O               2   up:     0.91   2.44   0.00   0.00   3.35    -0.71       -0.01

2   dn:     0.91   2.44   0.00   0.00   3.36

O               3   up:     0.91   2.43   0.00   0.00   3.35    -0.70       -0.01

3   dn:     0.91   2.44   0.00   0.00   3.35

O               4   up:     0.91   2.43   0.00   0.00   3.35    -0.70       -0.01

4   dn:     0.91   2.44   0.00   0.00   3.35

O               5   up:     0.91   2.44   0.00   0.00   3.35    -0.70       -0.01

5   dn:     0.91   2.44   0.00   0.00   3.35

O               6   up:     0.91   2.44   0.00   0.00   3.35    -0.71       -0.01

6   dn:     0.91   2.44   0.00   0.00   3.36

O               7   up:     0.91   2.43   0.00   0.00   3.35    -0.70       -0.01

7   dn:     0.91   2.44   0.00   0.00   3.35

O               8   up:     0.91   2.43   0.00   0.00   3.35    -0.70       -0.01

8   dn:     0.91   2.44   0.00   0.00   3.35

O               9   up:     0.91   2.44   0.00   0.00   3.35    -0.70       -0.01

9   dn:     0.91   2.44   0.00   0.00   3.35

O              10   up:     0.91   2.44   0.00   0.00   3.35    -0.71       -0.01

10   dn:     0.91   2.44   0.00   0.00   3.36

O              11   up:     0.91   2.43   0.00   0.00   3.35    -0.70       -0.01

11   dn:     0.91   2.44   0.00   0.00   3.35

O              12   up:     0.91   2.43   0.00   0.00   3.35    -0.70       -0.01

12   dn:     0.91   2.44   0.00   0.00   3.35

O              13   up:     0.91   2.44   0.00   0.00   3.35    -0.70       -0.01

13   dn:     0.91   2.44   0.00   0.00   3.35

O              14   up:     0.91   2.44   0.00   0.00   3.35    -0.71       -0.01

14   dn:     0.91   2.44   0.00   0.00   3.36

O              15   up:     0.91   2.43   0.00   0.00   3.35    -0.70       -0.01

15   dn:     0.91   2.44   0.00   0.00   3.35

O              16   up:     0.91   2.43   0.00   0.00   3.35    -0.70       -0.01

16   dn:     0.91   2.44   0.00   0.00   3.35

O              17   up:     0.91   2.44   0.00   0.00   3.35    -0.70       -0.00

17   dn:     0.91   2.44   0.00   0.00   3.35

O              18   up:     0.91   2.43   0.00   0.00   3.34    -0.69       -0.01

18   dn:     0.91   2.44   0.00   0.00   3.35

O              19   up:     0.91   2.43   0.00   0.00   3.35    -0.70       -0.01

19   dn:     0.91   2.44   0.00   0.00   3.35

O              20   up:     0.91   2.43   0.00   0.00   3.35    -0.70       -0.01

20   dn:     0.91   2.44   0.00   0.00   3.35

O              21   up:     0.91   2.44   0.00   0.00   3.35    -0.70       -0.01

21   dn:     0.91   2.44   0.00   0.00   3.35

O              22   up:     0.91   2.44   0.00   0.00   3.35    -0.71       -0.01

22   dn:     0.91   2.45   0.00   0.00   3.36

O              23   up:     0.91   2.44   0.00   0.00   3.35    -0.71       -0.01

23   dn:     0.91   2.44   0.00   0.00   3.36

O              24   up:     0.91   2.44   0.00   0.00   3.35    -0.71       -0.01

24   dn:     0.91   2.44   0.00   0.00   3.36

Na              1   up:     0.96   2.92   0.00   0.00   3.88     1.24       -0.00

1   dn:     0.97   2.92   0.00   0.00   3.88

Na              2   up:     0.96   2.91   0.00   0.00   3.88     1.24       -0.00

2   dn:     0.97   2.92   0.00   0.00   3.88

Na              3   up:     0.96   2.91   0.00   0.00   3.88     1.24       -0.00

3   dn:     0.97   2.92   0.00   0.00   3.88

K               1   up:     0.88   2.75   0.10   0.00   3.73     1.53       -0.00

1   dn:     0.89   2.75   0.10   0.00   3.73

K               2   up:     0.86   2.74   0.10   0.00   3.70     1.60       -0.00

2   dn:     0.86   2.74   0.10   0.00   3.70

K               3   up:     0.86   2.74   0.10   0.00   3.70     1.60       -0.00

3   dn:     0.86   2.74   0.10   0.00   3.70

K               4   up:     0.86   2.74   0.10   0.00   3.69     1.61       -0.00

4   dn:     0.86   2.74   0.10   0.00   3.70

Nb              1   up:     1.22   3.43   1.53   0.00   6.18     0.67        0.03

1   dn:     1.22   3.43   1.50   0.00   6.15

Nb              2   up:     1.22   3.43   1.53   0.00   6.18     0.67        0.03

2   dn:     1.22   3.43   1.50   0.00   6.15

Nb              3   up:     1.22   3.43   1.53   0.00   6.18     0.67        0.03

3   dn:     1.22   3.43   1.50   0.00   6.15

Nb              4   up:     1.22   3.43   1.53   0.00   6.18     0.67        0.03

4   dn:     1.22   3.43   1.50   0.00   6.15

Nb              5   up:     1.22   3.43   1.53   0.00   6.18     0.66        0.03

5   dn:     1.22   3.43   1.51   0.00   6.16

Nb              6   up:     1.22   3.43   1.53   0.00   6.18     0.67        0.04

6   dn:     1.22   3.42   1.50   0.00   6.15

Nb              7   up:     1.22   3.43   1.53   0.00   6.18     0.66        0.03

7   dn:     1.22   3.43   1.51   0.00   6.16

Nb              8   up:     1.22   3.43   1.53   0.00   6.18     0.67        0.04

8   dn:     1.22   3.42   1.50   0.00   6.15

Er              1   up:     1.04   3.02   0.29   7.00  11.36     1.46        2.17

1   dn:     1.04   3.03   0.28   4.83   9.19

=========================================================================================

Bond                   Population        Spin       Length (A)

================================================================================

O 21 -- Nb 5                   0.65         0.00          2.00003

O 21 -- Nb 7                   0.65         0.00          2.00003

O 18 -- Nb 8                   0.74         0.00          2.00207

O 18 -- Nb 6                   0.74         0.00          2.00207

O 13 -- Nb 7                   0.66         0.00          2.00217

O 9  -- Nb 5                   0.66         0.00          2.00217

O 5  -- Nb 7                   0.66         0.00          2.00217

O 1  -- Nb 5                   0.66         0.00          2.00217

O 16 -- Nb 8                   0.74         0.00          2.00472

O 12 -- Nb 6                   0.74         0.00          2.00472

O 8  -- Nb 8                   0.74         0.00          2.00472

O 4  -- Nb 6                   0.74         0.00          2.00472

O 23 -- Nb 1                   0.65         0.00          2.00703

O 24 -- Nb 3                   0.65         0.00          2.00703

O 24 -- Nb 2                   0.65         0.00          2.00703

O 23 -- Nb 4                   0.65         0.00          2.00703

O 13 -- Nb 2                   0.65         0.00          2.00757

O 1  -- Nb 3                   0.65         0.00          2.00757

O 9  -- Nb 1                   0.65         0.00          2.00757

O 5  -- Nb 4                   0.65         0.00          2.00757

O 14 -- Nb 4                   0.64         0.00          2.00789

O 10 -- Nb 3                   0.64         0.00          2.00789

O 6  -- Nb 2                   0.64         0.00          2.00789

O 2  -- Nb 1                   0.64         0.00          2.00789

O 15 -- Nb 4                   0.74         0.00          2.00906

O 11 -- Nb 3                   0.74         0.00          2.00906

O 7  -- Nb 2                   0.74         0.00          2.00906

O 3  -- Nb 1                   0.74         0.00          2.00906

O 20 -- Nb 3                   0.74         0.00          2.01029

O 20 -- Nb 2                   0.74         0.00          2.01029

O 19 -- Nb 4                   0.74         0.00          2.01029

O 19 -- Nb 1                   0.74         0.00          2.01029

O 14 -- Nb 8                   0.63         0.00          2.01319

O 2  -- Nb 6                   0.63         0.00          2.01319

O 10 -- Nb 6                   0.63         0.00          2.01319

O 6  -- Nb 8                   0.63         0.00          2.01319

O 16 -- Nb 4                   0.73         0.00          2.01484

O 4  -- Nb 1                   0.73         0.00          2.01484

O 12 -- Nb 3                   0.73         0.00          2.01484

O 8  -- Nb 2                   0.73         0.00          2.01484

O 22 -- Nb 6                   0.63         0.00          2.01602

O 22 -- Nb 8                   0.63         0.00          2.01602

O 17 -- Nb 7                   0.73         0.00          2.01676

O 17 -- Nb 5                   0.73         0.00          2.01676

O 15 -- Nb 7                   0.73         0.00          2.01885

O 11 -- Nb 5                   0.73         0.00          2.01885

O 7  -- Nb 7                   0.73         0.00          2.01885

O 3  -- Nb 5                   0.73         0.00          2.01885

O 22 -- Er 1                   0.03         0.00          2.63311

O 10 -- Er 1                   0.03         0.00          2.67324

O 2  -- Er 1                   0.03         0.00          2.67324

O 14 -- Er 1                   0.03         0.00          2.67324

O 6  -- Er 1                   0.03         0.00          2.67324

O 17 -- Na 1                  -0.08        -0.00          2.68325

O 10 -- O 22                  -0.04        -0.00          2.74146

O 2  -- O 22                  -0.04        -0.00          2.74146

O 14 -- O 22                  -0.04        -0.00          2.74146

O 6  -- O 22                  -0.04        -0.00          2.74146

O 10 -- O 24                  -0.04        -0.00          2.75058

O 6  -- O 24                  -0.04        -0.00          2.75058

O 2  -- O 23                  -0.04        -0.00          2.75058

O 14 -- O 23                  -0.04        -0.00          2.75058

O 6  -- O 13                  -0.04        -0.00          2.75233

O 5  -- O 14                  -0.04        -0.00          2.75233

O 2  -- O 9                   -0.04        -0.00          2.75233

O 1  -- O 10                  -0.04        -0.00          2.75233

O 6  -- O 14                  -0.04        -0.00          2.75295

O 2  -- O 10                  -0.04        -0.00          2.75295

O 13 -- O 24                  -0.04        -0.00          2.75735

O 9  -- O 23                  -0.04        -0.00          2.75735

O 1  -- O 24                  -0.04        -0.00          2.75735

O 5  -- O 23                  -0.04        -0.00          2.75735

O 5  -- O 13                  -0.04        -0.00          2.76394

O 1  -- O 9                   -0.04        -0.00          2.76394

O 9  -- O 21                  -0.04        -0.00          2.76397

O 1  -- O 21                  -0.04        -0.00          2.76397

O 13 -- O 21                  -0.04        -0.00          2.76397

O 5  -- O 21                  -0.04        -0.00          2.76397

O 24 -- Er 1                   0.01         0.00          2.77597

O 23 -- Er 1                   0.01         0.00          2.77597

O 11 -- Na 2                  -0.08        -0.00          2.77886

O 15 -- Na 3                  -0.08        -0.00          2.77886

O 3  -- Na 3                  -0.08        -0.00          2.77886

O 7  -- Na 2                  -0.08        -0.00          2.77886

O 20 -- Na 1                  -0.08        -0.00          2.78694

O 19 -- Na 1                  -0.08        -0.00          2.78694

O 13 -- Na 1                  -0.12        -0.00          2.79610

O 9  -- Na 1                  -0.12        -0.00          2.79610

O 5  -- Na 1                  -0.12        -0.00          2.79610

O 1  -- Na 1                  -0.12        -0.00          2.79610

O 21 -- Na 3                  -0.12        -0.00          2.80712

O 21 -- Na 2                  -0.12        -0.00          2.80712

O 9  -- Na 2                  -0.11        -0.00          2.82380

O 13 -- Na 3                  -0.11        -0.00          2.82380

O 5  -- Na 2                  -0.11        -0.00          2.82380

O 1  -- Na 3                  -0.11        -0.00          2.82380

O 9  -- Er 1                   0.00         0.00          2.82453

O 1  -- Er 1                   0.00         0.00          2.82453

O 13 -- Er 1                   0.00         0.00          2.82453

O 5  -- Er 1                   0.00         0.00          2.82453

O 16 -- K 2                   -0.19        -0.00          2.82719

O 12 -- K 3                   -0.19        -0.00          2.82719

O 8  -- K 3                   -0.19        -0.00          2.82719

O 4  -- K 2                   -0.19        -0.00          2.82719

O 20 -- K 2                   -0.19        -0.00          2.82828

O 19 -- K 3                   -0.19        -0.00          2.82828

O 24 -- Na 3                  -0.11        -0.00          2.83178

O 23 -- Na 2                  -0.11        -0.00          2.83178

O 15 -- K 3                   -0.19        -0.00          2.83298

O 11 -- K 2                   -0.19        -0.00          2.83298

O 7  -- K 2                   -0.19        -0.00          2.83298

O 3  -- K 3                   -0.19        -0.00          2.83298

O 17 -- K 3                   -0.19        -0.00          2.83920

O 17 -- K 2                   -0.19        -0.00          2.83920

O 4  -- Na 2                  -0.08        -0.00          2.83923

O 12 -- Na 3                  -0.08        -0.00          2.83923

O 8  -- Na 3                  -0.08        -0.00          2.83923

O 16 -- Na 2                  -0.08        -0.00          2.83923

O 12 -- K 4                   -0.19        -0.00          2.84001

O 4  -- K 4                   -0.19        -0.00          2.84001

O 16 -- K 4                   -0.19        -0.00          2.84001

O 8  -- K 4                   -0.19        -0.00          2.84001

O 10 -- Na 2                  -0.11        -0.00          2.84410

O 14 -- Na 3                  -0.11        -0.00          2.84410

O 6  -- Na 2                  -0.11        -0.00          2.84410

O 2  -- Na 3                  -0.11        -0.00          2.84410

O 24 -- Na 2                  -0.12        -0.00          2.84502

O 23 -- Na 3                  -0.12        -0.00          2.84502

O 20 -- K 3                   -0.19        -0.00          2.84745

O 19 -- K 2                   -0.19        -0.00          2.84745

O 18 -- K 3                   -0.19        -0.00          2.84999

O 18 -- K 2                   -0.19        -0.00          2.84999

O 13 -- O 17                  -0.02        -0.00          2.85384

O 9  -- O 17                  -0.02        -0.00          2.85384

O 5  -- O 17                  -0.02        -0.00          2.85384

O 1  -- O 17                  -0.02        -0.00          2.85384

O 13 -- O 20                  -0.02        -0.00          2.85722

O 9  -- O 19                  -0.02        -0.00          2.85722

O 5  -- O 19                  -0.02        -0.00          2.85722

O 1  -- O 20                  -0.02        -0.00          2.85722

O 13 -- O 15                  -0.02        -0.00          2.85782

O 9  -- O 11                  -0.02        -0.00          2.85782

O 5  -- O 7                   -0.02        -0.00          2.85782

O 1  -- O 3                   -0.02        -0.00          2.85782

O 11 -- O 21                  -0.02        -0.00          2.85976

O 3  -- O 21                  -0.02        -0.00          2.85976

O 15 -- O 21                  -0.02        -0.00          2.85976

O 7  -- O 21                  -0.02        -0.00          2.85976

O 11 -- K 4                   -0.19        -0.00          2.86074

O 3  -- K 4                   -0.19        -0.00          2.86074

O 15 -- K 4                   -0.19        -0.00          2.86074

O 7  -- K 4                   -0.19        -0.00          2.86074

O 3  -- O 23                  -0.02        -0.00          2.86305

O 15 -- O 23                  -0.02        -0.00          2.86305

O 11 -- O 24                  -0.02        -0.00          2.86305

O 7  -- O 24                  -0.02        -0.00          2.86305

O 8  -- O 14                  -0.02        -0.00          2.86332

O 6  -- O 16                  -0.02        -0.00          2.86332

O 4  -- O 10                  -0.02        -0.00          2.86332

O 2  -- O 12                  -0.02        -0.00          2.86332

O 17 -- K 1                   -0.23        -0.00          2.86471

O 15 -- K 1                   -0.23        -0.00          2.86511

O 11 -- K 1                   -0.23        -0.00          2.86511

O 7  -- K 1                   -0.23        -0.00          2.86511

O 3  -- K 1                   -0.23        -0.00          2.86511

O 10 -- O 11                  -0.02        -0.00          2.86707

O 6  -- O 7                   -0.02        -0.00          2.86707

O 14 -- O 15                  -0.02        -0.00          2.86707

O 2  -- O 3                   -0.02        -0.00          2.86707

O 14 -- O 19                  -0.02        -0.00          2.86732

O 10 -- O 20                  -0.02        -0.00          2.86732

O 6  -- O 20                  -0.02        -0.00          2.86732

O 2  -- O 19                  -0.02        -0.00          2.86732

O 8  -- O 13                  -0.02        -0.00          2.86764

O 5  -- O 16                  -0.02        -0.00          2.86764

O 4  -- O 9                   -0.02        -0.00          2.86764

O 1  -- O 12                  -0.02        -0.00          2.86764

O 4  -- O 23                  -0.02        -0.00          2.86829

O 16 -- O 23                  -0.02        -0.00          2.86829

O 12 -- O 24                  -0.02        -0.00          2.86829

O 8  -- O 24                  -0.02        -0.00          2.86829

O 14 -- O 18                  -0.02        -0.00          2.86903

O 10 -- O 18                  -0.02        -0.00          2.86903

O 6  -- O 18                  -0.02        -0.00          2.86903

O 2  -- O 18                  -0.02        -0.00          2.86903

O 18 -- Na 1                  -0.07        -0.00          2.87084

O 12 -- O 22                  -0.02        -0.00          2.87352

O 4  -- O 22                  -0.02        -0.00          2.87352

O 16 -- O 22                  -0.02        -0.00          2.87352

O 8  -- O 22                  -0.02        -0.00          2.87352

O 16 -- O 18                  -0.02        -0.00          2.87424

O 12 -- O 18                  -0.02        -0.00          2.87424

O 8  -- O 18                  -0.02        -0.00          2.87424

O 4  -- O 18                  -0.02        -0.00          2.87424

O 16 -- K 1                   -0.23        -0.00          2.87735

O 12 -- K 1                   -0.23        -0.00          2.87735

O 8  -- K 1                   -0.23        -0.00          2.87735

O 4  -- K 1                   -0.23        -0.00          2.87735

O 15 -- O 16                  -0.02        -0.00          2.87843

O 11 -- O 12                  -0.02        -0.00          2.87843

O 7  -- O 8                   -0.02        -0.00          2.87843

O 3  -- O 4                   -0.02        -0.00          2.87843

O 8  -- O 16                  -0.02        -0.00          2.87886

O 4  -- O 12                  -0.02        -0.00          2.87886

O 16 -- O 19                  -0.02        -0.00          2.87995

O 12 -- O 20                  -0.02        -0.00          2.87995

O 8  -- O 20                  -0.02        -0.00          2.87995

O 4  -- O 19                  -0.02        -0.00          2.87995

O 15 -- O 19                  -0.02        -0.00          2.88031

O 11 -- O 20                  -0.02        -0.00          2.88031

O 7  -- O 20                  -0.02        -0.00          2.88031

O 3  -- O 19                  -0.02        -0.00          2.88031

O 22 -- Na 3                  -0.11        -0.00          2.88269

O 22 -- Na 2                  -0.11        -0.00          2.88269

O 22 -- K 4                   -0.24        -0.00          2.88324

O 15 -- O 17                  -0.02        -0.00          2.88717

O 11 -- O 17                  -0.02        -0.00          2.88717

O 7  -- O 17                  -0.02        -0.00          2.88717

O 3  -- O 17                  -0.02        -0.00          2.88717

O 7  -- O 15                  -0.02        -0.00          2.89148

O 3  -- O 11                  -0.02        -0.00          2.89148

O 21 -- Er 1                  -0.00         0.00          2.89466

O 20 -- K 1                   -0.23        -0.00          2.90311

O 19 -- K 1                   -0.23        -0.00          2.90311

O 14 -- Na 1                  -0.12        -0.00          2.90477

O 10 -- Na 1                  -0.12        -0.00          2.90477

O 6  -- Na 1                  -0.12        -0.00          2.90477

O 2  -- Na 1                  -0.12        -0.00          2.90477

O 23 -- K 4                   -0.24        -0.00          2.91547

O 24 -- K 4                   -0.24        -0.00          2.91547

O 13 -- K 3                   -0.25        -0.00          2.91838

O 9  -- K 2                   -0.25        -0.00          2.91838

O 5  -- K 2                   -0.25        -0.00          2.91838

O 1  -- K 3                   -0.25        -0.00          2.91838

O 18 -- K 1                   -0.24        -0.00          2.93020

O 21 -- K 4                   -0.24        -0.00          2.93798

O 14 -- K 3                   -0.25        -0.00          2.94787

O 10 -- K 2                   -0.25        -0.00          2.94787

O 6  -- K 2                   -0.25        -0.00          2.94787

O 2  -- K 3                   -0.25        -0.00          2.94787

================================================================================