Supporting Information

Functionalization of Cellulosic Materials via a Bifunctional Azetidinium Coupler

Yue Sua, Ayodele Fatonab, Erin A.S. Doherty,c Richard J. Riehle,c Sachin Borkar,c Robert H. Peltonb and Jose M. Moran-Mirabala,d,e,*

a Department of Chemistry and Chemical Biology, Macmaster University, 1280 Main St. West, Hamilton, ON L8S 4M1, Canada

b Department of Chemical Engineering, McMaster University, 1280 Main St. West, Hamilton, ON L8S 4L7, Canada

c Solenis LLC, 2475 Pinnacle Drive, Wilmington, Delaware, United States of America, 19803

d Centre for Advanced Light Microscopy, McMaster University, 1280 Main St. West, Hamilton, ON L8S 4L7, Canada

e Brockhouse Institute for Materials Research, McMaster University, 1280 Main St. West, Hamilton, ON L8S 4L7, Canada

Figure S1. 1H NMR spectra of bifunctional azetidinium coupler (top), AZE-C12 (middle), and AZE-C18 (bottom).

(a)

(b)

Figure S2. Electrospray ionization mass spectra of (a) AZE-alkyne and (b) AZE-azide derivatives.

Figure S3. DLS of (a) CMC; (b) CMC-AZE-C12; (c) CMC-AZE-C18; (d) CMC-AZE-alkyne; and (e) CMC-AZE-azide polymers. Distributions are representative recordings from n = 3 independently prepared samples.

Figure S4. Dry (blue) and wet strength (purple) of paper sheets made from pulp fibres onto which CMC, CMC-AZE-C12, CMC-AZE-C18, CMC-AZE-alkyne, or CMC-AZE-azide were adsorbed. Numbers presented are means and standard deviations from n = 3 replicate sheets prepared independently.

Figure S5. Calibration curve for FAM-5-azide.

Figure S6. Fluorescence microscopy images of CMC-alkyne modified paper sheets reacted with FAM-azide