Graphical Abstract

Fig 1:- Steps Involved in Biochar Synthesis

Fig 2. The SEM analysis of (2A) BC control (2B) Au-NPs/BC-350. The presence of Au-NPs is seen in the image

Fig 3. XRD analysis of the Biochar sample.

Table 1. EDS analysis of the Au-NPs/BC nanocomposites

| Element | Weight% | Atomic% |  |
| --- | --- | --- | --- |
| C | 34.75 | 47.21 |  |
| O | 49.74 | 50.73 |  |
| K | 2.30 | 0.96 |  |
| Au | 13.22 | 1.09 |  |
| Totals | 100.00 |  |  |