Table 1 Results of geotechnical test and Simples statistics

| Sample collection site | Number Samples | Nature | Depth (m) | LL (%) | PI (%) | Fines (˂80µm) | MDD (g/cm3) | OMC (%) | CBR 95% OPM (%) | AASHTO |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Essos (Z1) | (N=10) | Clayey soils | 1.00 | 56 | 12 | 36 | 1.876 | 7.6 | 17 | A-7-5 (1) |
|  |  | Clayey soils | 1.00 | 57 | 11 | 70 | 1.881 | 15.2 | 16 | A-7-5 (10) |
|  |  | Clayey soils | 1 .00 | 54 | 16 | 82 | 1.854 | 19.3 | 18 | A-7-5 (13) |
|  |  | Clayey soils | 1.00 | 57 | 13 | 76 | 1.744 | 20.7 | 18 | A-7-5 (12) |
|  |  | Clayey soils | 1.00 | 51 | 17 | 63 | 1.802 | 11.9 | 16 | A-7-5 (10) |
|  |  | Clayey soils | 1.00 | 56 | 12 | 67 | 1.982 | 15.5 | 18 | A-7-5 (10) |
|  |  | Clayey soils | 1.00 | 48 | 18 | 72 | 1.783 | 12.9 | 15 | A-7-5 (12) |
|  |  | Clayey soils | 1.00 | 55 | 14 | 71 | 1.815 | 14.3 | 16 | A-7-5 (11) |
|  |  | Clayey soils | 1.00 | 51 | 16 | 70 | 1.998 | 12.5 | 20 | A-7-5 (11) |
|  |  | Clayey soils | 1.00 | 50 | 15 | 54 | 2.096 | 16.9 | 29 | A-7-5 (7) |
| Mendong (Z2) | (N=2) | Clayey soils | 1.00 | 72 | 33 | 73 | 1.795 | 20.3 | 13 | A-7-5 (19) |
|  |  | Silty or clayey gravel and sand | 1.00 | 57 | 26 | 27 | 1.930 | 16.8 | 22 | A-2-7 (2) |
| Eloumdem (Z3) | (N=8) | Clayey soils | 1.00 | 71 | 27 | 75 | 1.620 | 22.2 | 19 | A-7-5(18) |
|  |  | Clayey soils | 1.00 | 79 | 28 | 74 | 1.630 | 21.5 | 14 | A-7-5(19) |
|  |  | Clayey soils | 1.00 | 78 | 25 | 80 | 1.600 | 23.2 | 18 | A-7-5(18) |
|  |  | Clayey soils | 1.00 | 79 | 29 | 75 | 1.620 | 21.6 | 15 | A-7-5(19) |
|  |  | Clayey soils | 1.00 | 71 | 26 | 75 | 1.620 | 22.2 | 19 | A-7-5(19) |
|  |  | Clayey soils | 1.00 | 71 | 27 | 75 | 1.620 | 22.2 | 19 | A-7-5(19) |
|  |  | Clayey soils | 1.00 | 78 | 25 | 80 | 1.600 | 24.3 | 18 | A-7-5(18) |
|  |  | Clayey soils | 1.00 | 34 | 16 | 58 | 1.812 | 17.6 | 13 | A-6(7) |
| Minkan (Z4) | (N=2) | Clayey soils | 1.00 | 71 | 26 | 69 | 1.631 | 25.3 | 18 | A-7-5(12) |
|  |  | Clayey soils | 1.00 | 71 | 18 | 72 | 1.700 | 25.7 | 18 | A-7-5(9) |
| Olémbé (Z5) | (N=7) | Clayey soils | 1.00 | 54 | 17 | 67 | 1.636 | 21.2 | 25 | A-7-5 (12) |
|  |  | Clayey soils | 1.50 | 54 | 19 | 61 | 1.570 | 25.5 | 15 | A-7-5 (14) |
|  |  | Clayey soils | 1.65 | 75 | 30 | 70 | 1.580 | 24.4 | 14 | A-7-6 (18) |
|  |  | Clayey soils | 1.50 | 80 | 39 | 85 | 1.600 | 23.4 | 16 | A-7-6 (20) |
|  |  | Clayey soils | 1.60 | 80 | 39 | 85 | 1.580 | 23.5 | 15 | A-7-6 (20) |
|  |  | Clayey soils | 1.45 | 78 | 39 | 80 | 1.600 | 22.4 | 21 | A-7-6 (20) |
|  |  | Clayey soils | 1.50 | 54 | 20 | 80 | 1.590 | 22.2 | 17 | A-7-6 (20) |
| Nkol-Bisson (Z6) | (N=6) | Clayey soils | 1.00 | 71 | 34 | 73 | 1.690 | 19.3 | 21 | A-7-5(19) |
|  |  | Clayey soils | 1.00 | 71 | 30 | 71 | 1.650 | 21.5 | 23 | A-7-5(19) |
|  |  | Clayey soils | 1.00 | 70 | 35 | 71 | 1.677 | 22.0 | 21 | A-7-5(19) |
|  |  | Clayey soils | 1.00 | 71 | 32 | 74 | 1.670 | 20.5 | 14 | A-7-5(20) |
|  |  | Clayey soils | 1.00 | 70 | 28 | 70 | 1.705 | 19.5 | 12 | A-7-5(18) |
|  |  | Clayey soils | 1.00 | 75 | 32 | 75 | 1,690 | 19.5 | 13 | A-7-5(18) |
| Nfandena (Z7) | (N=4) | Clayey soils | 0.40 | 71 | 33 | 69 | 1.698 | 21.5 | 20 | A-7-5(11) |
|  |  | Clayey soils | 0.40 | 71 | 32 | 72 | 1.700 | 22.0 | 19 | A-7-5(12) |
|  |  | Silty or clayey gravel and sand | 0.80 | 58 | 18 | 21 | 2.000 | 13.0 | 37 | A-2-7(2) |
|  |  | Silty or clayey gravel and sand | 0.80 | 58 | 19 | 14 | 2.000 | 13.2 | 36 | A-2-7(2) |
| Mont-Fébé (Z8) | (N=2) | Silty or clayey gravel and sand | 0.80 | 50 | 21 | 16 | 2.084 | 16.2 | 41 | A-2-7 (1) |
|  |  | Silty or clayey gravel and sand | 0.80 | 48 | 28 | 12 | 2.092 | 15.2 | 53 | A-2-7 (1) |
| Nsimalen (Z9) | (N=4) | Clayey soils | 1.00 | 55 | 16 | 63 | 1.879 | 18.1 | 17 | A-7-5 (10) |
|  |  | Clayey soils | 1.00 | 49 | 14 | 46 | 1.876 | 15.6 | 20 | A-7-5 (4) |
|  |  | Clayey soils | 1.00 | 50 | 16 | 73 | 1.798 | 16.0 | 15 | A-7-5 (12) |
|  |  | Clayey soils | 1.00 | 57 | 18 | 60 | 1.888 | 16.6 | 21 | A-7-5 (10) |
| Minimum |  |  |  | 34 | 11 | 12 | 1.570 | 7.6 | 12 |  |
| Maximum |  |  |  | 80 | 39 | 85 | 2.096 | 25.7 | 53 |  |
| Average |  |  |  | 62.9 | 23.5 | 64.5 | 1.761 | 19.2 | 20 |  |
| Standard deviation |  |  |  | 11.6 | 8.2 | 19.1 | 0.157 | 4.2 | 8 |  |
| Coefficient of variation |  |  |  | 18.4 | 34.7 | 29.5 | 8.915 | 22.1 | 39 |  |

AL: Atterberg Limits; LL: Liquidity limit; PI: Plasticity Index; CBR: California Bearring Ratio; AASHTO: American Association of State Highway and Transportation Officials. Soil Classification System (from AASHTO M145 or ASTM D3282 [6]).