Supplementary Information for

Crystal structure of anthracen-9-yl(3,6-dimethoxynaphthalen-2-yl)methanone:

Decisive factors for formation of two-fold helical molecular assemblies in three directions affording chiral crystal

Kun Li1, Hiroaki Iitsuka1, Takehiro Tsumuki1, Keiichi Noguchi2, Noriyuki Yonezawa1, Akiko Okamoto1*

1Department of Organic and Polymer Materials Chemistry, Tokyo University of Agriculture and Technology, 2-24-16 Nakamachi, Koganei, Tokyo, 184–8588, Japan.

2 Instrumentation Analysis Center, Tokyo University of Agriculture and Technology, 2-24-16, Nakamachi, Koganei, Tokyo 184-8588, Japan

Corresponding author E-mail: aokamoto@cc.tuat.ac.jp

Table of Contents

1. Compound Data                                                         S-3

1H, 13C NMR, and IR Spectra

2. X-ray Diffraction Analysis                                                S-7

3. Hirshfeld surface analysis                                                 S-12

Hirshfeld surface mapped over dnorm and two-dimensional fingerprint plots

4. References                                                             S-15

- Compound Data

Spectral data of anthracen-9-yl(3,6-dimethoxynaphthalen-2-yl)methanone

Figure S-1. 1H NMR spectra of anthracen-9-yl(3,6-dimethoxynaphthalen-2-yl)methanone (300 MHz, in CDCl3; -0.5~10.5 ppm).

Figure S-2. 1H NMR spectra of anthracene-9-yl(3,6-dimethoxynaphthalen-2-yl)methanone (300 MHz, in CDCl3; 6.8~8.8 ppm).

Figure S-3. 13C NMR spectra of anthracene-9-yl(3,6-dimethoxynaphthalen-2-yl)methanone (75 MHz, in CDCl3; -0.5~200.5 ppm).

(equivalent interval)

(Standard)

Model name

Serial number

Affiliation

Organization

Analysis date

Update

Data type

Horizontal axis

Vertical axis

Start

End

Data interval

Number of data

Intensity

Wavenumber

Intensity

Wavenumber

Measurement date

Illuminant

Detector

Scan

Resolution

Zero filling

Apodization

Gain

Aperture

Scan speed

Filter

Model name

Serial number

Figure S-4. IR spectra of anthracen-9-yl(3,6-dimethoxynaphthalen-2-yl)methanone.

- X-ray Diffraction Analysis.

For the crystal structure determination, the single crystal of the title compound was used for data collection on a four circle Rigaku RAXIS RAPID diffractometer (equipped with a two-dimensional area IP detector).  The graphite-monochromated CuKa radiation (l = 1.54187 Å) was used for data collection. The lattice parameters were determined by the least-squares methods on the basis of all reflections with F2 > 2s(F2).  Crystal data, data collection, and structure refinement details are summarized in Table S-1.  The data collection and cell refinement were performed using RAPID-AUTO software [1].  The data reduction was performed using CrystalStructure [2].  The structures were solved by direct methods using SIR2011[3] and refined by a full-matrix least-squares procedure using the program SHELXL-2014 [4].  All H atoms were found in a difference map and were subsequently refined as riding atoms, C–H = 0.95 (aromatic), and 0.98 (methyl) Å, with Uiso(H) = 1.2Ueq (C). 　Crystallographic data have been deposited at the Cambridge Crystallographic Data Centre, and can be obtained free of charge on application to CCDC, 12 Union Road, Cambridge CB21EZ, UK (fax: (+44) 1223-336-033; email: deposit@ccdc.cam.ac.uk).

Crystal data for title compound: C27H20O3, , FW = 392.43, Orthorhombic, P212121, a = 8.2094(2) Å, b = 9.8435(2) Å, c = 25.3131(5)Å, V = 2045.53(8) Å3, T = 193 K, Z = 4, Dcalcd = 1.274 g cm-3, R1 = 0.037, wR2 = 0.117, GOF = 0.99. CCDC XXXXX.

Table S-2. Crystal data and details of the structure refinement for the title compound and

the homologous compounds.

|  | I (Bz) (Kato et al., 2011)[5] | II (Nap) (Okamoto et al., 2016)[6] | III (Anth) |
| --- | --- | --- | --- |
| Crystal data |  |  |  |
| Chemical formula | C19H16O3 | C23H18O3 | C27H20O3 |
| Mr | 292.32 | 342.37 | 392.43 |
| Crystal system, space group | Monoclinic, P21/c | Monoclinic, P21/c | Orthorhombic, P212121 |
| a, b, c (Å) | 8.7186(2), 20.4650(4), 8.5675 (2) | 8.8585(2), 22.1886(5), 9.10165(19) | 8.2094(2), 9.8435(2), 25.3131(5) |
| b (˚) | 102.475 (1) | 104.139 (1) | 90 |
| V (Å3) | 1492.57(6) | 1734.80 (7) | 2045.53 (8) |
| Z | 4 | 4 | 4 |
| m (mm-1) | 0.71 | 0.69 | 0.66 |
| Crystal size (mm) | 0.60 x 0.50 x 0.20 | 0.60 x 0.30 x 0.10 | 0.50 x 0.50 x 0.30 |
| Data collection |  |  |  |
| Tmin, Tmax | 0.677, 0.872 | 0.682, 0.934 | 0.735, 0.828 |
| No. of measured, independent and observed [I > 2s(I)] reflections | 26682, 2735, 2509 | 30270, 3173, 2587 | 11732, 3705, 3430 |
| Rint | 0.044 | 0.054 | 0.022 |
| (sin q/l)max (Å-1) | 0.602 | 0.602 | 0.602 |
| Refinement |  |  |  |
| R[F2 > 2s(F2)], wR(F2), S | 0.034, 0.098, 1.06 | 0.041, 0.113, 1.09 | 0.037, 0.117, 0.99 |
| No. of reflections | 2735 | 3173 | 3705 |
| No. of parameters | 202 | 238 | 273 |
| Δρmax, Δρmin (eÅ-3) | 0.23, -0.17 | 0.17, -0.15 | 0.20, -0.17 |

Table S-2. Geometric parameters for title compound: Bond lengths (Å)

Table S-3. Geometric parameters for title compound: Bond angles (˚).

Table S-4. Geometric parameters for title compound: Torsion angles (˚).

- Hirshfeld surface analysis [7-9]

Figure S-5. Hirshfeld surface of title compound III (Anth) mapped over dnorm (top) and two-dimensional fingerprint plots (bottom): (a) layered full plot and those delineated into (b) H...H, (c) H...C/C...H, (d) H...O/O...H, (e) C...O/O...C, (f) C...C, and (g) O...O contacts.

Figure S-6. Hirshfeld surface of homologous compound I (Bz) mapped over dnorm (top) and two-dimensional fingerprint plots (bottom): (a) layered full plot and those delineated into (b) H...H, (c) H...C/C...H, (d) H...O/O...H, (e) C... C, (f) C...O/O...C, and (g) O...O contacts.

Figure S-7. Hirshfeld surface of homologous compound II (Nap) mapped over dnorm (top) and two-dimensional fingerprint plots (bottom): (a) layered full plot and those delineated into (b) H...H, (c) H...C/C...H, (d) H...O/O...H, (e) C...O/O...C, (f) O...O, and (e) C...C contacts.

- References

[1] Rigaku. In: Rigaku Corporation; Tokyo, Japan, 1998.

[2] Rigaku. CrystalStructure; Rigaku Corporation: Tokyo, Japan, 2010.

[3] Burla MC, Caliandro R,  Camalli M, Carrozzini B, Cascarano GL, De Caro L, Giacovazzo C, Polidori G, Siliqi D, Spagna R (2007) J Appl Cryst 40:609-613.

[4] Sheldrick GM (2015) Acta Cryst A71: 3-8.

[5] Kato, Y., Takeuchi, R., Muto, T., Okamoto, A. & Yonezawa, N. (2011). Acta Cryst. E67, o668.

[6] Okamoto, A., Tsumuki, T. Sasagawa, K., Siqingaowa & Yonezawa, N. (2016). Eur. Chem. Bull. 5(6), 211-220.

[7] Spackman, M. A. & Jayatilaka, D. (2009). CrystEngComm, 11, 19-32.

[8] McKinnon, J. J., Jayatilaka, D. & Spackman, M. A. (2007). Chem. Commun., 3814-3816.

[9] Turner, M. J., McKinnon, J. J., Wolff, S. K., Grimwood, D. J., Spackman, P.R., Jayatilaka, D. & Spackman, M. A. CrystalExplorer17. University of Western Australia. http://hirsh-feldsurface.net 2017. Available from: http://hirsh-feldsurface.net