List of Tables

Table 1. Electroplating conditions for the Zn-Ni alloy on AISI 1020 steel.

| Bath composition | Value |
| --- | --- |
| ZnCl2 | 0.1 mol.L-1 (source of Zn) |
| NiCl2.6H2O | 0.1, 0.2 and 0.3 mol.L-1 (source of Ni) |
| KCl | 2.8 mol.L-1 (increase conductivity) |
| H3BO3 | 0.32 mol.L-1 (buffer solution) |
| Operational parameters |  |
| Current density | 80.0 mA/cm² |
| Temperature | 25°C |
| pH | 4.7-5.0 |
| Deposition time. | 45.0 min. |

Table 2.Chemical composition (wt.%) for base metal and electroplated alloys - Zn-Ni by EDS analysis.

| elments | Zn | Ni | C | O | Fe | Mo | Cr | Co |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| BM |  |  |  |  |  |  |  |  |
| wt.% | 0.01 | 0.01 | 5.48 | 1.96 | 90.6 | 0.89 | 0.38 | 0.69 |
| NiCl2.6H2O (mol. L-1) |  |  |  |  |  |  |  |  |
| 0.1 | 72.37 | 11.32 | 11.28 | 2.99 | 0.76 | 0.37 | 0.36 | 0.03 |
| 0.2 | 65.49 | 17.27 | 11.77 | 4.08 | 0.67 | 0.51 | 0.22 | 0.01 |
| 0.3 | 64.46 | 19.54 | 12.33 | 1.79 | 1.10 | 0.52 | 0.25 | 0.01 |

Table 3. Deposition efficiency obtained for different NiCl2.6H2O concentration  in the electroplating bath.

| NiCl2.6H2O(mol.L-1) | Ni (wt.%) | Edep (%) |
| --- | --- | --- |
| 0.1 | 11.32 | 48.50 |
| 0.2 | 17.27 | 65.96 |
| 0.3 | 19.54 | 72.20 |

Table 4. The electrochemical parameters of corrosion tests conducted in a 3.5% NaCl solution are presented for base metal samples without and with a Zn-Ni coating.

|  | Ecorr (mV) | Icorr (µA) | Rp (Ω) | CR (mmpy) |
| --- | --- | --- | --- | --- |
| BM | -962.89 | 183.70 | 52.70 | 0.68 |
| BM/Zn-Nix [x-wt.%] |  |  |  |  |
| 11.32 | -953.88 | 147.42 | 57.30 | 0.60 |
| 17.27 | -889.14 | 92.32 | 108.00 | 0.36 |
| 19.54 | -736.59 | 69.05 | 145.00 | 0.26 |

Table 5. Values obtained for the amount of hydrogen adsorbed on the deposits during electrodeposition.

| Ni (wt.%) | α x 106 | β (s-1) x104 | QHads(C/cm2) |  | QHads/F(mol/cm2) x107 |
| --- | --- | --- | --- | --- | --- |
| 11.32 | 9.95 | -4.49 | 0.022 | 2.28 |  |
| 17.27 | 14.42 | -1.96 | 0.073 | 7.56 |  |
| 19.54 | 26.36 | -1.66 | 0.158 | 16.37 |  |

Faraday Constant,  F=96,485.33 C.

Table 6. Estimation of the break-through time  (tb), apparent diffusivity (Dapp), Permeability (P) and Solubility (S) parameters.

|  | tb(s) | Dapp x105 (cm²/s) | P x1010 (mol/cm2.s) | S x 108 (mol/cm³) |
| --- | --- | --- | --- | --- |
| BM | 5 | 15.40 | 3.28 | 2.13 |
| BM/Zn-Nix (x-wt.%) |  |  |  |  |
| 11.32 | 17 | 4.53 | 3.63 | 8.02 |
| 17.27 | 36 | 2.14 | 1.25 | 5.85 |
| 19.54 | 129 | 0.15 | 2.74 | 45.8 |