Multifunctional Cellulose-Based Adsorbent from Waste Wood Wool for Heavy Metal Removal and Bacterial Disinfection: Insights into Adsorption Behavior, and DFT Calculations

Table S1. Adsorption isotherm models and their parameter values

| Metal Ion |  | Langmuir Model |  |  | Freundlich Model |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Pb(II) | Adsorbent | qmax (mg/g) | R2 | kf |  | 1/n | R2 |  |
|  | CU | 89.22 | 0.9998 | 75.1882 |  | 1.00245 | 0.9966 |  |
|  | CU-MBT | 185.18 | 0.9995 | 291.5076 |  | 0.95343 | 0.9930 |  |
| Cd(II) | CU | 103.09 | 0.9981 | 59.4169 |  | 0.64021 | 0.9713 |  |
|  | CU-MBT | 178.57 | 0.9997 | 353.0693 |  | 0.18697 | 0.78706 |  |
| HHHJJKHg(II) | CU | 80.64 | 0.9974 | 429.0619 |  | 1.02516 | 0.9887 |  |
|  | CU-MBT | 140.84 | 0.9980 | 55.2471 |  | 0.78890 | 0.9618 |  |

Fig S1. (a-f) Recyclability study for  CU and CU-MBT

Table S2. Effect of common anions on adsorption of Hg(II), Pb(II), and Cd(II) ions

| Coexisting ions | Coexisting ions concentration (mg/l) |  |  | Amount adsorbed (mg/g) |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Pb(II) | Cd(II) |  | Hg(II) |
| Sulphate | 10 | 9.1 | 11.42 |  | 9.02 |
|  | 30 | 9.31 | 11.21 |  | 9.26 |
|  | 50 | 9.43 | 11.32 |  | 9.21 |
| Phosphate | 2 | 9.11 | 11.43 |  | 9.23 |
|  | 5 | 9.14 | 11.42 |  | 9.34 |
|  | 10 | 9.02 | 11.53 |  | 9.26 |
| Bicarbonate | 50 | 9.26 | 11.42 |  | 9.31 |
|  | 100 | 9.34 | 11.53 |  | 9.26 |
|  | 200 | 9.42 | 11.45 |  | 9.14 |
| Nitrate | 10 | 9.31 | 11.48 |  | 9.26 |
|  | 30 | 9.44 | 11.46 |  | 9.21 |
| Silicate | 10 | 9.26 | 11.58 |  | 9.41 |
|  | 20 | 9.41 | 11.49 |  | 9.26 |
|  | 50 | 9.62 | 11.35 |  | 9.47 |
| Chloride | 100 | 9.22 | 11.15 |  | 9.26 |
|  | 200 | 9.34 | 11.26 |  | 9.42 |
|  | 300 | 9.49 | 11.51 |  | 9.46 |
| Arsenate | 0.2 | 9.37 | 11.28 |  | 9.28 |
|  | 0.5 | 9.46 | 11.47 |  | 9.04 |
|  | 1 | 9.58 | 11.21 |  | 9.26 |

Fig. S2.  Antibacterial activity of CU and CU-MBT against a) E.coli b) S. aureus

Table S3. Zone of inhibition of CU and CU-MBT against S. aureus and E.coli

| Concentration (ppm) | E. coli |  | S. aureus |  |
| --- | --- | --- | --- | --- |
|  | CU | CU-MBT | CU | CU-MBT |
| 10 | 1.32 ± 0.11 | 2.5 ± 0.2 | 0.45 ± 0.01 | 2.22 ± 0.15 |
| 50 | 1.51 ± 0.2 | 3.4 ± 0.2 | 0.54 ± 0.02 | 2.65 ± 0.05 |
| 100 | 1.61 ± 0.15 | 4.5± 0.2 | 0.92 ± 0.01 | 3.62 ± 0.20 |

Fig. S3.  Zone of inhibition against a) E.coli b) S. aureus

Table S4. Application of CU-MBT to Hg(II), Pb(II), and Cd(II). contaminated real water

| Parameters | Before Adsorption | After Adsorption |
| --- | --- | --- |
| pH | 7.9 | 7.01 |
| TDS | 1498mg/l | 1301mg/l |
| Alkali | 500 mg/l | 428 mg/l |
| Cadmium | 2.05 ppm | 0.051 ppm |
| Lead | 2.11 ppm | 0.03 ppm |
| Mercury | 2.12 ppm | 0.056 ppm |
| Manganese | 2.01 ppm | 0.101 ppm |
| Zinc | 2.05 ppm | 0.212 ppm |
| Iron | 2.89 ppm | 2.721 ppm |
| Copper | 2.02 ppm | 0.056 ppm |
| Nickel | 2.01 ppm | 0.121 ppm |

Table S5: Energetic parameters, FMOs and Global reactivity descriptors of cellulose and cellulose-MBT

| Parameters | CU | CU- MBT |
| --- | --- | --- |
| Total Energy (keV) | -35.306 keV | -65.806 keV |
| Dipole Moment (debye) | 5.0397 | 2.9892 |
| HOMO (eV) | -7.3954 | -0.25875 |
| LUMO (eV) | -0.7749 | -0.07154 |
| Energy gap (eV) | 6.6205 | 5.0940 |
| Electron affinity(A) (eV) | 0.7749 | 1.9466 |
| Ionization Potential (I) (eV) | 7.3954 | 7.0406 |
| Electronegativity ( χ) (eV) | 4.0852 | 4.4936 |
| Chemical potential(µ)(eV) | -4.0852 | -4.4936 |
| Chemical hardness (Ƞ) (eV) | 3.3102 | 2.5469 |
| Chemical Softness (S) (eV-1) | 0.1511 | 0.1963 |
| Global Electrophilicity index (ω) (eV) | 2.5208 | 3.9639 |