Supporting Information for

A Method for Recycling the Pd Catalyst at Molar ppm Level

Shohei Masuu,a Misaki Goto,s Saki Miyamoto,a Tomoya Kiguchi,a Tsutomu Shinagawa,b Yoshimasa Matsumura,a Osamu Shimomuraa and Atsushi Ohtaka,a,*

aDepartment of Applied Chemistry, Faculty of Engineering, Osaka Institute of Technology, 5-16-1 Ohmiya, Asahi, Osaka 535-8585, Japan. bElectronic Materials Research Division, Morinomiya Center, Osaka Research Institute of Industrial Science and Technology (ORIST), 1-6-50 Morinomiya, Joto, Osaka, 536-8553, Japan.

General comments

1H NMR spectra in CDCl3 were recorded with a 400 MHz NMR spectrometer (ECZ400S, JEOL Ltd.) using tetramethylsilane (δ = 0) as an internal standard. Inductively coupled plasma optical emission spectrometry (ICP-OES) was performed using iCAP-7400 (Thermo Fisher Scientific Inc.). Field Emission Scanning electron microscope (FE-SEM) images of the deposits on the FTO substrates were obtained using an electron microscope (JEOL JSM-7800F, JSM-6700F) with an acceleration voltage of 5.0 kV.

Typical procedures for the Hiyama coupling reaction with mol ppm level of Pd loading.

Trimethoxyphenylsilane (148 mg, 0.75 mmol), 4-bromotoluene (85.5 mg, 0.5 mmol), potassium fluoride (87.1 mg, 1.5 mmol), propylene glycol (1 mL), and 1.0 mmol/L of THF solution of Pd(OAc)2 (10 μL, 2 mol ppm relative to 4-bromotoluene) were added to a screw-capped vial (no. 02, Maruemu Co., Osaka, Japan) with stir bar. After stirring vigorously (1350 rpm) at 100 °C for 1 h under air, the vial was immersed in water (∼20 °C) for about 10 min to cool the reaction mixture to room temperature. The recovered stir bar was washed with H2O (1.0 mL × 3) and diethyl ether (1.0 mL × 3), then dried in vacuo, and reused. The aqueous solution was extracted five times with diethyl ether. The combined organic extracts were dried over anhydrous MgSO4 and evaporation of the solvent afforded the desired product. Characterization of the product was established by comparison of their 1H NMR spectra with those of authentic samples.

Scheme S1. Hiyama coupling reaction with various Pd loading.

Typical procedures for the Suzuki coupling reaction with mol ppm level of Pd loading..

4-Methylphenylboronic acid (102 mg, 0.75 mmol), bromobenzene (78.5 mg, 0.5 mmol), 1.5 mol/L aqueous KOH solution (1 mL), and 1.0 mmol/L of THF solution of Pd(OAc)2 (10 μL, 2 mol ppm relative to bromobenzene) were added to a screw-capped vial (no. 02, Maruemu Co., Osaka, Japan) with stir bar. After stirring vigorously (1350 rpm) at 90 °C for 1 h under air, the vial was immersed in water (∼20 °C) for about 10 min to cool the reaction mixture to room temperature. The recovered stir bar was washed with H2O (1.0 mL × 3) and diethyl ether (1.0 mL × 3), then dried in vacuo, and reused. The aqueous solution was extracted five times with diethyl ether. The combined organic extracts were dried over anhydrous MgSO4 and evaporation of the solvent afforded the desired product. Characterization of the product was established by comparison of their 1H NMR spectra with those of authentic samples.

Scheme S2. Suzuki coupling reaction with various Pd loading.