Supplementary data

A Novel Nanomedicine for Osteosarcoma Treatment: Triggering Ferroptosis through GSH Depletion and Inhibition for Enhanced Synergistic PDT/PTT Therapy

Tangbing Xua,b,1 ，Qiming Maa,1，Chi Zhanga,b,1，Xiaoyan Hec，Qian Wange，Yunfeng Wua,b，Kunpeng Qina,b，Faxue Liaoa,b，Ping Zhoua,b，Pengfei Xua,b，Jialai Yangf,b,Junjun Yanga,b,Jun Changa,b,***,Lei Qiaod,**,Yong Hua,*

aDepartment of Orthopaedics, The First Affiliated Hospital of Anhui Medical University,Hefei 230022,China

bAnhui Public Health Clinical Center,Heifei 230012,China

cSchool of Life Sciences Anhui Medical University Hefei 230032, China

dDepartment of Polymer Science and Engineering University of Science and Technology of China Hefei 230026, China

eDepartment of Respiratory and Critical Care Medicine, The First Affiliated Hospital of Anhui Medical University, Hefei 230022, Anhui, China

fDepartment of emergency, The First Affiliated Hospital of Anhui Medical University, Hefei 230022, Anhui, China

Keywords:carrier-free nanomedicine,osteosarcoma,ferroptosis,PDT/PTTTherapy,

reactive oxygen species

* Corresponding author.

** Corresponding author.

***Corresponding author.

- mail addresses: changjun_2008@hotmail.com（J. Chang），Leiqiao@mail.ustc.edu.cn（L. Qiao），

- hy.in163@163.com（Y. Hu）

1 These authors contributed equally to this work.

Experimental data

Materials

Sorafenib and Copper sulfate pentahydrate (CuSO4.5H2O) were purchased from Shanghai Macklin Biochemical Co., Ltd. IR780 iodide was purchased from Guangzhou baiyun Biochemical Co.,dimethyl sulfoxide (DMSO) was purchased from Sigma−Aldrich (Beijing, China). (GSH) Colorimetric Assay Kit was supplied from Elabscience Biotechnology Co., Ltd.Reactive Oxygen Species Assay Kit and Calcein/PI Cell Viability/Cytotoxicity Assay Kit  were supplied  Beyotime Biotechnology (Shanghai, China).BODIPY™581/591(C11-BODIPY)was supplied from ThermoFisher Scientific.Phosphatebuffered saline (PBS), fetal bovine serum (FBS),  penicillin−streptomycin, trypsin ,and dulbecco's modified eagle's medium (DMEM), were purchased from Biological Industries Inc. The antibody of GAPDH was supplied from Cell Signaling Technology Inc. Anti- Glutathione Peroxidase 4 antibody and SLC7A11/xCT Polyclonal antibody were supplied from Wuhan sanying Biotechnology Co., Ltd.All other reagents were obtained from commercial suppliers and used as received.

Depletion of GSH

Different amounts of Cu2+ (0, 1, 2, 4, 8, 12, 16, and 32 µg mL-1)were added to the solution containing GSH (0.2 mM) and co-incubation for 30 min.Next, 25 µL of 5, 5’-dithiobis-2-nitrobenoic acid (DTNB) was added. An microplate reader was used to measure full absorption spectrums of different samples.The GSH was incubated with  CSIR (the concentration of Cu2+ was 20µg mL-1) for different time (0, 10, 20, 30, 40, 50, and 60 min) to detect the consumption of GSH .

Cellular uptake of CSIR
To investigate the cellular uptake,K7M2 cells were cultured in 6-well plates at a density of 1×105 cells per well overnight and then incubated with the different treatments including ‘PBS’, ‘free Cu2+’, ‘free SRF’, ‘free IR780’, ‘free Cu2+ +IR780’, ‘free SRF+IR780’, ‘free Cu2++SRF+IR780’and CSIR for 6 h. After three more washes with PBS, the cells were analysed by flow cytometry.Next, laser scanning confocal microscopy (CLSM, Zeiss LSM800) was used to visualize the cellular uptake of the nanomedicine.

K7M2 cells were plated overnight in 35- mm mattek culture dishes. The cell culture media were replaced with fresh media containing ‘free Cu2+ + SRF+ IR780’ and CSIR (IR780 concentration was 10 μg/mL). After incubation for 12 h, the cells were washed with PBS for 3 times and the cells nuclei were stained with Hoechst 33342 (10 μg/mL) for 10 min. Finally, intracellular IR780 (λex = 780 nm, λem =820 nm) and cells nuclei (λex = 346 nm, λem =460 nm) were imaged using CLSM.

Western blot analysis

K7M2 cells were seeded in a 6 cm petri dish containing 2 mL DMEM medium, with 2 ×105 cells per well and incubated at 37 °C for 24 h.the medium was replaced by fresh medium including ‘PBS’, ‘free Cu2+’, ‘free SRF’, ‘free IR780’, ‘free Cu2+ +IR780’, ‘free SRF+IR780’, ‘free Cu2++SRF+IR780’and CSIR (the concentration of Cu2+,SRF and IR780 were 20 μg mL-1, 10 μg mL-1, and 10 μg mL-1, respectively).After incubation for 12 h, the cells were exposed to laser irradiation (1.2 W cm-2) for 5 min. After 4 h incubation, cells were collected for protein extraction for western blotting.The total protein extracts were subjected to SDS-PAGE. After electrophoresis, the proteins were transferred to poly (vinylidene  fluoride) (PVDF) membranes (Millipore). To prevent non - specific binding, the sections were blocked  TBST (Trisbuffered saline with Tween-20) containing 5% milk for 1 h to prevent non - specific binding.Primary antibodies were incubated overnight at 4°C overnight and secondary antibodies at RT for one hour.The expressions of proteins were visualized using a chemiluminescence imaging analysis system (Tanon 5200, China).

Immunohistochemical analysis

the tumor sections were fixed in 4% paraformaldehyde for 20 min at room temperature ,and then a 5 mm thickness was cut off the samples after embedding them in paraffin.After washing in phosphate-buffered saline (PBS) with 0.05% Tween 20 (PBST), the sections were blocked with 2% bovine serum albumin (BSA, Sigma) and 0.1% Tween 20 for 1.5 h at 37 °C.Following incubation with primary antibody for 2h at 37°C in humidified chamber and then incubated with secondary antibody for 1h at 37°C in dark.Finally, the samples were analyzed with microscopy system.

Fig.S1  a) Energy-dispersive X-ray spectroscopy (EDS) of CSIR. b) XPS full spectrum

Fig.S2 XPS deconvoluted C1sa) spectra, F1s b), Cl2p c),I3d d), Cu2p3 e)and CuLMM f)spectra of CSIR

Fig.S3 a)CLSM and b)FCM analysis of red florescence in K7M2 cells after incubated with“PBS”,“Cu2++SRF+IR780” and “CSIR” for 6 h, respectively. Scale bar: 10 µm.

Fig.S4  a)Differential differences of the five genes enriched in the ferroptosis pathway. b)The 10 genes with the most obvious differences in the difference analysis.

Fig.S5  Weight–curve changes in mice following various treatments.

Fig.S6  H&E staining of the major organs include heart, liver, spleen, lung, and

kidney of different groups at 12th day post-treatment. Scale bars: 100 µm.

Fig.S7 a) The hemolysis ratio induced by CSIR with different concentration.

b) The images H2O, NaCl, and CSIR at the concentration of 25-100 μg mL-1before and after incubation with erythrocyte. c) Erythrocyte morphology was observed by inverted fluorescence microscope after incubation with different preparations for 6 h. Scale bar: 20 µm. Data were displayed as the mean ± SD (n = 3).