Adsorption and dehydration reaction of ethanol to ethylene on isomorphous B, Al, and Ga substitution of H-ZSM-5 zeolite: An embedded ONIOM study

Nattida Maeboonruan1, Bundet Boekfa1,2*, Thana Maihom1, Piti Treesukol1, Kanokwan Kongpatpanich3, Supawadee Namuangruk4, Michael Probst5 and Jumras Limtrakul3

1Department of Chemistry, Faculty of Liberal Arts and Science, Kasetsart University Kamphaeng Saen Campus, Nakhon Pathom 73140, Thailand
    2  Center for Advanced Studies in Nanotechnology for Chemical, Food and Agricultural Industries, Kasetsart University Institute for Advanced Studies, Kasetsart University, 
Bangkok 10900, Thailand
3School of Molecular Science and Engineering, Vidyasirimedhi Institute of Science and Technology (VISTEC), Rayong 21210, Thailand.

4National Nanotechnology Center (NANOTEC), National Science and Technology Development Agency, Pathum Thani 12120, Thailand

5Institute of Ion Physics and Applied Physics, University of Innsbruck, Innsbruck 6020, Austria

*e-mail: bundet.b@ku.ac.th

# Supporting information

1. H-[B]-ZSM-5, H-[Al]-ZSM-5 and H-[Ga]-ZSM-5  zeolites

| (a) | (b) | (c) |
| --- | --- | --- |

Figure S1: Optimized structures of (a) B-ZSM-5, (b) Al-ZSM-5 and (c) Ga-ZSM-5 zeolites determined by the ONIOM (5T:34T) scheme. The 5T cluster (ball-stick) is treated at the MP2/6-31G(d,p) level of theory, whereas 34T cluster is treated with the M06-2X/6-31G(d,p) density functional. Distances are given in Å.

Table S1: Selected structural parameters for the H-ZSM-5 zeolites isomorphously substituted with B, Al and Ga. The geometries are optimized with ONIOM 5T:34T MP2/6-31G (d,p):M06-2X/6-31G(d,p) scheme.

|  | B-ZSM-5 | Al-ZSM-5 | Ga-ZSM-5 |
| --- | --- | --- | --- |
| Distance (Å) |  |  |  |
| Si1-O1 | 1.65 | 1.66 | 1.66 |
| (B,Al,Ga)Hz | 2.34 | 2.36 | 2.42 |
| (B,Al,Ga)-O1 | 1.94 | 1.83 | 1.91 |
| (B,Al,Ga)-Oavg | 1.54 | 1.72 | 1.79 |
| O1-Hz | 0.97 | 0.97 | 0.97 |
| Angle (o) |  |  |  |
| Si1-O1-Hz | 115.88 | 116.64 | 117.36 |
| Si1-O1-(B,Al,Ga) | 138.57 | 130.35 | 129.72 |
| (B,Al,Ga)-O1-Hz | 102.03 | 111.21 | 110.01 |

2. Adsorption of ethanol on H-[B]-ZSM-5, H-[Al]-ZSM-5 and H-[Ga]-ZSM-5  zeolites

2.1 Optimized structures of the  adsorption complexes

| (a) | (b) | (c) |
| --- | --- | --- |

Figure S2: Optimized structures after adsorption of ethanol: (a) one hydrogen bonded (side on, AD-B-1A), (b) doubly hydrogen bonded (end at zigzag chanel, AD-B-1B) and (c) one hydrogen bonded (end at intersection region, AD-B-1C) on B-ZSM-5 zeolites from ONIOM 5T:34T MP2/6-31G(d,p):M06-2X/6-31G(d,p) calculations. Distances are in Å.

Table S2: Selected Data for the optimized structural parameters for the adsorption of ethanol on B-ZSM-5 zeolite. One hydrogen bonded (side on, AD-B-1A), doubly hydrogen bound (end at zigzag chanel, AD-B-1B) and one hydrogen bonded (end at intersection region, AD-B-1C) from ONIOM 5T:34T MP2/6-31G (d,p):M06-2X/6-31G(d,p) calculations.

|  | AD-B-1A |  | AD-B-1B |  | AD-B-1C |
| --- | --- | --- | --- | --- | --- |
| Distance (Å) |  |  |  |  |  |
| Si1-O1 | 1.66 |  | 1.67 |  | 1.67 |
| BHz | 2.29 |  | 2.27 |  | 2.27 |
| B-O1 | 1.77 |  | 1.73 |  | 1.75 |
| B-Oavg | 1.51 |  | 1.50 |  | 1.51 |
| O1-Hz | 1.02 |  | 1.03 |  | 1.02 |
| HzO | 1.58 |  | 1.55 |  | 1.58 |
| Angle (o) |  |  |  |  |  |
| Si1-O1-B | 137.31 |  | 137.38 |  | 136.90 |
| Si1-Hz-O | 123.26 |  | 139.60 |  | 141.78 |
| B-Hz-O | 144.68 |  | 131.77 |  | 125.50 |
| O1-Hz-O | 167.11 |  | 177.70 |  | 170.48 |
| (a) |  | (b) |  | (c) |  |  |

Figure S3: Optimized structures for the adsorption of ethanol (a) one hydrogen bonded (side on, AD-Al-1A), (b) doubly hydrogen bound (end at zigzag chanel, AD-Al-1B) and (c) one hydrogen bonded (end at intersection region, AD-Al-1C) on Al-ZSM-5 zeolites with ONIOM 5T:34T MP2/6-31G(d,p):M06-2X/6-31G(d,p). Distances are given in Å.

Table S3: Selected Data for the optimized structural parameters for the adsorption of ethanol on Al-ZSM-5 zeolite namely: one hydrogen bonded (side on, AD-Al-1A), double hydrogen bonded (end at zigzag chanel, AD-Al-1B) and one hydrogen bonded (end at intersection region, AD-Al-1C) calculated using the ONIOM 5T:34T MP2/6-31G (d,p):M06-2X/6-31G(d,p) scheme.

|  | AD-Al-1A |  | AD-Al-1B |  | AD-Al-1C |
| --- | --- | --- | --- | --- | --- |
| Distance (Å) |  |  |  |  |  |
| Si1-O1 | 1.64 |  | 1.64 |  | 1.59 |
| AlHz | 2.44 |  | 2.44 |  | 2.88 |
| Al-O1 | 1.80 |  | 1.79 |  | 1.73 |
| Al-Oavg | 1.72 |  | 1.72 |  | 1.72 |
| O1-Hz | 1.07 |  | 1.09 |  | 1.68 |
| HzO | 1.42 |  | 1.36 |  | 1.00 |
| Angle (o) |  |  |  |  |  |
| Si1-O1-Al | 127.57 |  | 127.54 |  | 128.19 |
| Si1-Hz-O | 132.26 |  | 151.91 |  | 170.86 |
| Al-Hz-O | 144.27 |  | 126.53 |  | 107.22 |
| O1-Hz-O | 173.23 |  | 169.01 |  | 139.92 |
| (a) |  | (b) |  | (c) |  |

Figure S4: Optimized structures for the adsorption of ethanol (a) one hydrogen bonded (side on, AD-Ga-1A), (b) double hydrogen bonded (end at zigzag chanel, AD-Ga-1B) and (c) one hydrogen bonded (end at intersection region, AD-Ga-1C) on Ga-ZSM-5 zeolites with ONIOM 5T:34T MP2/6-31G(d,p):M06-2X/6-31G(d,p). Distances are in Å.

Table S4: Selected Data for the optimized structural parameters for the adsorption of ethanol on Ga-ZSM-5 zeolite: one hydrogen bond (side on, AD-Ga-1A), doubly hydrogen bound (end at zigzag chanel, AD-Ga-1B) and one hydrogen bonded (end at intersection region, AD-Ga-1C) obtained from ONIOM 5T:34T MP2/6-31G (d,p):M06-2X/6-31G(d,p) calculations.

|  | AD-Ga-1A | AD-Ga-1B | AD-Ga-1C |
| --- | --- | --- | --- |
| Distance (Å) |  |  |  |
| Si1-O1 | 1.63 | 1.63 | 1.60 |
| GaHz | 2.50 | 2.51 | 2.61 |
| Ga-O1 | 1.87 | 1.85 | 1.81 |
| Ga-Oavg | 1.78 | 1.78 | 1.78 |
| O1-Hz | 1.08 | 1.12 | 1.44 |
| HzO | 1.39 | 1.30 | 1.05 |
| Angle (o) |  |  |  |
| Si1-O1-Ga | 127.01 | 125.83 | 126.16 |
| Si1-Hz-O | 132.28 | 153.18 | 166.79 |
| Ga-Hz-O | 143.49 | 126.43 | 115.38 |
| O1-Hz-O | 172.74 | 169.34 | 157.01 |

2.2 Adsorption energies

Table S5: Adsorption energies of ethanol on the H-[B]-ZSM-5 zeolit: one hydrogen bond (side on, AD-B-1A), doubly hydrogen bound (end at zigzag chanel, AD-B-1B) and one hydrogen bond (end at intersection region, AD-B-1C) ) obtained from ONIOM 5T:34T MP2/6-31G (d,p):M06-2X/6-31G(d,p) calculations. Energies are given in kcal/mol.

|  | AD-B-1A | AD-B-1B | AD-B-1C |
| --- | --- | --- | --- |
| ONIOM (MP2:M06-2X) a | -20.4 | -23.6 | -22.9 |
| MP2 b | -14.5 | -16.5 | -16.7 |
| Framework c | -5.9 | -7.1 | -6.2 |
| ONIOM (MP2:M06-2X) d | -17.2 | -20.0 | -19.2 |
| MP2 e | -12.5 | -13.9 | -13.7 |
| Framework c | -4.7 | -6.1 | -5.5 |
| Embedded ONIOM f | -19.0 | -23.1 | -21.6 |
| MP2 g | -14.9 | -16.7 | -15.8 |
| Framework c | -4.1 | -6.4 | -5.8 |

a ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T:34T

b MP2/6-31G(d,p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T//5T:34T

c EONIOM – Ehigh level

d ONIOM(MP2/6-311+G(2df,2p):M06-2X/6-311+G(2df,2p))//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T:34T

e MP2/6-311+G(2df,2p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T//5T:34T

f ONIOM(MP2/6-311+G(2df,2p):M06-2X/6-311+G(2df,2p))//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) with charge model 5T:34T

g MP2/6-311+G(2df,2p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) with charge model 5T//5T:34T

Table S6: Adsorption energies of ethanol on the H-[Al]-ZSM-5 zeolite namely: one hydrogen bond (side on, AD-Al-1A), double hydrogen bonded (end at  zigzag chanel, AD-Al-1B) and one hydrogen bonded (end at intersection region, AD-Al-1C) ) obtained from ONIOM 5T:34T MP2/6-31G (d,p):M06-2X/6-31G(d,p) calculations. Energies are given in kcal/mol.

|  | AD-Al-1A | AD-Al-1B | AD-Al-1C |
| --- | --- | --- | --- |
| ONIOM (MP2:M06-2X) a | -24.3 | -30.0 | -30.4 |
| MP2 b | -16.4 | -22.2 | -19.6 |
| Framework c | -7.9 | -7.8 | -10.8 |
| ONIOM (MP2:M06-2X) d | -21.3 | -26.0 | -25.7 |
| MP2 e | -14.7 | -19.3 | -16.8 |
| Framework c | -6.6 | -6.7 | -8.9 |
| Embedded ONIOM f | -23.3 | -29.8 | -28.1 |
| MP2 g | -17.1 | -22.2 | -18.9 |
| Framework c | -6.2 | -7.6 | -9.2 |

a ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T:34T

b MP2/6-31G(d,p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T//5T:34T

c EONIOM – Ehigh level

d ONIOM(MP2/6-311+G(2df,2p):M06-2X/6-311+G(2df,2p))//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T:34T

e MP2/6-311+G(2df,2p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T//5T:34T

f ONIOM(MP2/6-311+G(2df,2p):M06-2X/6-311+G(2df,2p))//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) with charge model 5T:34T

g MP2/6-311+G(2df,2p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) with charge model 5T//5T:34T

Table S7: Adsorption energies of ethanol on the H-[Ga]-ZSM-5 zeolite: one hydrogen bond (side on, AD-GaAl-1A), doubly hydrogen bound (end at  zigzag chanel, AD-Ga-1B) and one hydrogen bonded (end at intersection region, AD-Ga-1C) ) obtained from ONIOM 5T:34T MP2/6-31G (d,p):M06-2X/6-31G(d,p) calculations. Energies are given in kcal/mol.

|  | AD-Ga-1A | AD-Ga-1B | AD-Ga-1C |
| --- | --- | --- | --- |
| ONIOM (MP2:M06-2X) a | -26.4 | -31.8 | -33.0 |
| MP2 b | -18.0 | -23.3 | -24.4 |
| Framework c | -8.4 | -8.5 | -8.6 |
| ONIOM (MP2:M06-2X) d | -20.9 | -25.7 | -25.1 |
| MP2 e | -14.2 | -18.6 | -18.0 |
| Framework c | -6.7 | -7.1 | -7.1 |
| Embedded ONIOM f | -23.2 | -29.4 | -27.7 |
| MP2 g | -16.8 | -21.6 | -20.2 |
| Framework c | -6.4 | -7.8 | -7.5 |

a ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T:34T

b MP2/6-31G(d,p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T//5T:34T

c EONIOM – Ehigh level

d ONIOM(MP2/6-311+G(2df,2p):M06-2X/6-311+G(2df,2p))//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T:34T

e MP2/6-311+G(2df,2p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T//5T:34T

f ONIOM(MP2/6-311+G(2df,2p):M06-2X/6-311+G(2df,2p))//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) with charge model 5T:34T

g MP2/6-311+G(2df,2p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) with charge model 5T//5T:34T

3. Adsorptions of ethylene on H-[B]-ZSM-5, H-[Al]-ZSM-5 and H-[Ga]-ZSM-5  zeolites

| (a) | (b) | (c) |
| --- | --- | --- |

Figure S5: Optimized structures of ethylene adsorption on (a) B-ZSM-5, (b) Al-ZSM-5 and (c) Ga-ZSM-5 zeolites ) obtained from ONIOM 5T:34T MP2/6-31G (d,p):M06-2X/6-31G(d,p) calculations. Distances are given in Å.

Table S8: Selected Data for the optimized structural parameters for the adsorption of ethylene on the H-ZSM-5 zeolites isomorphously substituted with B, Al and Ga from ONIOM 5T:34T MP2/6-31G (d,p):M06-2X/6-31G(d,p) calculations.

|  | B-ZSM-5 | Al-ZSM-5 | Ga-ZSM-5 |
| --- | --- | --- | --- |
| Distance (Å) |  |  |  |
| Si1-O1 | 1.66 | 1.66 | 1.65 |
| (B,Al,Ga)Hz | 2.33 | 2.41 | 2.46 |
| (B,Al,Ga)-O1 | 1.85 | 1.82 | 1.89 |
| (B,Al,Ga)-Oavg | 1.52 | 1.72 | 1.78 |
| O1-Hz | 0.98 | 0.99 | 0.99 |
| HzC1 | 2.31 | 2.16 | 2.13 |
| HzC2 | 2.37 | 2.20 | 2.16 |
| C1-C2 | 1.34 | 1.34 | 1.34 |
| Angle (o) |  |  |  |
| Si1-O1-(B,Al,Ga) | 138.26 | 129.37 | 128.75 |
| Si1-Hz-C2 | 127.28 | 133.97 | 136.49 |
| (B,Al,Ga)-Hz-C2 | 136.37 | 136.17 | 134.57 |
| O1-Hz-C2 | 158.36 | 159.57 | 159.12 |

Table S9: Adsorption energies of ethylene on the H-[B]-ZSM-5, H-[Al]-ZSM-5 and H-[Ga]-ZSM-5 zeolites from ONIOM 5T:34T MP2/6-31G (d,p):M06-2X/6-31G(d,p) calculations. Energies are given in kcal/mol.

|  | B-ZSM-5 | Al-ZSM-5 | Ga-ZSM-5 |
| --- | --- | --- | --- |
| ONIOM (MP2:M06-2X) a | -10.7 | -13.2 | -14.3 |
| MP2 b | -6.7 | -8.9 | -9.9 |
| Framework c | -4.0 | -4.3 | -4.4 |
| ONIOM (MP2:M06-2X) d | -10.2 | -12.9 | -12.8 |
| MP2 e | -6.4 | -8.9 | -9.0 |
| Framework c | -3.7 | -4.0 | -3.8 |
| Embedded ONIOM f | -11.6 | -14.7 | -14.5 |
| MP2 g | -7.6 | -10.2 | -10.3 |
| Framework c | -4.0 | -4.5 | -4.2 |

a ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T:34T

b MP2/6-31G(d,p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T//5T:34T

c EONIOM – Ehigh level

d ONIOM(MP2/6-311+G(2df,2p):M06-2X/6-311+G(2df,2p))//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T:34T

e MP2/6-311+G(2df,2p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T//5T:34T

f ONIOM(MP2/6-311+G(2df,2p):M06-2X/6-311+G(2df,2p))//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) with charge model 5T:34T

g MP2/6-311+G(2df,2p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) with charge model 5T//5T:34T

4. Dehydration reactions of ethanol to ethylene on H-[B]-ZSM-5, H-[Al]-ZSM-5 and H-[Ga]-ZSM-5 zeolites

4.1 H-[B]-ZSM-5 zeolite

| AD-B-1C | TS1-B |
| --- | --- |
| IN1-B | IN2-B |
| TS2-B | PR-B |

Figure S6: Structures in the stepwise mechanism obtained from ONIOM 5T:34T MP2/6-31G (d,p):M06-2X/6-31G(d,p) calculations. Distances are given in Å.

Table S10	Selected structural parameters and energies for the stepwise mechanism on the H-[B]-ZSM-5 zeolites.

|  | AD-B-1C | TS1-B | IN1-B | IN2-B | TS2-B | PR-B |
| --- | --- | --- | --- | --- | --- | --- |
| Distance (Å) |  |  |  |  |  |  |
| Si1-O1 | 1.67 | 1.60 | 1.61 | 1.62 | 1.63 | 1.66 |
| Si2-O2 | 1.62 | 1.64 | 1.67 | 1.67 | 1.64 | 1.62 |
| B-Hz | 2.27 | 4.94 | 6.28 | - | - | - |
| B-O1 | 1.75 | 1.48 | 1.40 | 1.40 | 1.52 | 1.85 |
| B-O2 | 1.44 | 1.56 | 2.00 | 2.01 | 1.54 | 1.42 |
| Hz-O | 1.58 | 0.97 | 0.96 | - | - | - |
| O1-Hz | 1.02 | 3.85 | 5.25 | - | - | - |
| O1-H | 3.71 | 2.83 | 4.01 | 4.01 | 1.57 | 0.99 |
| C1-C2 | 1.51 | 1.48 | 1.51 | 1.51 | 1.40 | 1.34 |
| C1-O2 | 3.48 | 2.21 | 1.48 | 1.48 | 2.25 | 3.59 |
| C1-O | 1.45 | 2.10 | 4.84 | - | - | - |
| C2-H | 1.09 | 1.09 | 1.09 | 1.09 | 1.19 | 2.31 |
| Angle (o) |  |  |  |  |  |  |
| Si1-O1-B | 136.90 | 145.07 | 135.50 | 153.52 | 140.71 | 138.26 |
| Si2-O2-B | 145.23 | 138.00 | 134.01 | 133.96 | 140.82 | 143.25 |

Table S11: Relative energies of ethylene on the H-[B]-ZSM-5 zeolites from ONIOM 5T:34T MP2/6-31G (d,p):M06-2X/6-31G(d,p) calculations. Energies are given in kcal/mol. Total Activation energy are in parenthesis.

|  | AD-B-1C | TS1-B | IN1-B | IN2-B | TS2-B | PR-B |
| --- | --- | --- | --- | --- | --- | --- |
| ONIOM a | -22.9 | 20.3 | -11.4 | 0.0 | 42.6 | 9.4 |
|  |  | (43.2) |  |  | (42.6) |  |
| MP2 b | -16.7 | 36.0 | 0.8 | 1.3 | 45.7 | 13.4 |
|  |  | (52.7) |  |  | (44.4) |  |
| Framework c | -6.3 | -15.7 | -12.2 | -0.4 | -3.1 | -4.0 |
| ONIOM d | -19.2 | 23.8 | -8.5 | -0.4 | 40.2 | 5.2 |
|  |  | (43.0) |  |  | (40.6) |  |
| MP2 b | -13.7 | 35.6 | -1.0 | -0.4 | 43.4 | 8.9 |
|  |  | (49.3) |  |  | (43.8) |  |
| Framework c | -5.5 | -11.8 | -7.4 | 0.0 | -3.2 | -3.7 |
| Embedded ONIOM f | -21.6 | 20.7 | -11.8 | -2.8 | 36.1 | 3.8 |
|  |  | (42.3) |  |  | (38.9) |  |
| MP2 g | -15.8 | 30.0 | -2.1 | -1.0 | 38.7 | 7.7 |
|  |  | (45.8) |  |  | (39.7) |  |
| Framework c | -5.9 | -9.3 | -9.7 | -1.8 | -2.6 | -4.0 |

a ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T:34T

b MP2/6-31G(d,p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T//5T:34T

c EONIOM – Ehigh level

d ONIOM(MP2/6-311+G(2df,2p):M06-2X/6-311+G(2df,2p))//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T:34T

e MP2/6-311+G(2df,2p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T//5T:34T

f ONIOM(MP2/6-311+G(2df,2p):M06-2X/6-311+G(2df,2p))//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) with charge model 5T:34T

g MP2/6-311+G(2df,2p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) with charge model 5T//5T:34T

| AD-B-1A | TSc-B |
| --- | --- |
| INc-B | PRc-B |

Figure S7: Structures in the concerted mechanism obtained from ONIOM 5T:34T MP2/6-31G (d,p):M06-2X/6-31G(d,p) calculations. Distances are given in Å

Table S12 Selected structural parameters and energies for the concerted mechanism on the H-[B]-ZSM-5 zeolites.

|  | AD-B-1A | TSc-B | INc-B | PRc-B |
| --- | --- | --- | --- | --- |
| Distance (Å) |  |  |  |  |
| Si1-O1 | 1.66 | 1.62 | 1.61 | 1.62 |
| Si2-O2 | 1.62 | 1.67 | 1.66 | 1.65 |
| B-Hz | 2.29 | 3.05 | 3.52 | - |
| B-O1 | 1.77 | 1.46 | 1.40 | 1.41 |
| B-O2 | 1.42 | 1.60 | 1.98 | 1.97 |
| Hz-O | 1.58 | 0.97 | 0.97 | - |
| O1-Hz | 1.02 | 2.38 | 3.47 | - |
| O2-H | 2.82 | 1.32 | 0.97 | 0.98 |
| C1-C2 | 1.51 | 1.39 | 1.34 | 1.34 |
| C1-O | 1.45 | 2.11 | 3.38 | - |
| C2-H | 1.09 | 1.34 | 2.91 | 2.64 |
| Angle (o) |  |  |  |  |
| Si1-O1-B | 137.31 | 140.43 | 133.87 | 133.22 |
| Si2-O2-B | 146.74 | 140.18 | 141.80 | 141.39 |

Table S13 Relative energies of ethylene on the H-[B]-ZSM-5 zeolites from ONIOM 5T:34T MP2/6-31G (d,p):M06-2X/6-31G(d,p) calculations. Energies are given in kcal/mol. Total Activation energy are in parenthesis.

|  | AD-B-1A | TSc-B | INc-B | PRc-B |
| --- | --- | --- | --- | --- |
| ONIOM a | -20.4 | 33.3 | 0.0 | 9.6 |
|  |  | (53.7) |  |  |
| MP2 b | -14.5 | 38.2 | 11.4 | 15.5 |
|  |  | (52.7) |  |  |
| Framework c | -5.8 | -4.9 | -11.4 | -5.9 |
| ONIOM d | -17.2 | 35.0 | 0.6 | 5.9 |
|  |  | (52.2) |  |  |
| MP2 b | -12.5 | 38.1 | 8.5 | 11.1 |
|  |  | (50.6) |  |  |
| Framework c | -4.8 | -3.1 | -7.9 | -5.2 |
| Embedded ONIOM f | -19.0 | 29.5 | -4.4 | 4.9 |
|  |  | (48.5) |  |  |
| MP2 g | -14.9 | 33.5 | 6.7 | 11.8 |
|  |  | (48.4) |  |  |
| Framework c | -4.1 | -4.0 | -11.1 | -6.9 |

a ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T:34T

b MP2/6-31G(d,p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T//5T:34T

c EONIOM – Ehigh level

d ONIOM(MP2/6-311+G(2df,2p):M06-2X/6-311+G(2df,2p))//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T:34T

e MP2/6-311+G(2df,2p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T//5T:34T

f ONIOM(MP2/6-311+G(2df,2p):M06-2X/6-311+G(2df,2p))//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) with charge model 5T:34T

g MP2/6-311+G(2df,2p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) with charge model 5T//5T:34T

4.2 Dehydration reaction of ethanol to ethylene on H-[Al]-ZSM-5 zeolite

| AD-Al-1C | TS1-Al |
| --- | --- |
| IN1-Al | IN2-Al |
| TS2-Al | PR-Al |

Figure S8 	Structures occurring in the stepwise mechanism. obtained from ONIOM 5T:34T MP2/6-31G (d,p):M06-2X/6-31G(d,p) calculations. Distances are given in Å

Table S14: Selected structural parameters and energies for the stepwise mechanism on the H-[Al]-ZSM-5 zeolites.

|  | AD-Al-1C | TS1-Al | IN1-Al | IN2-Al | TS2-Al | PR-Al |
| --- | --- | --- | --- | --- | --- | --- |
| Distance (Å) |  |  |  |  |  |  |
| Si1-O1 | 1.59 | 1.57 | 1.57 | 1.59 | 1.60 | 1.66 |
| Si2-O2 | 1.61 | 1.60 | 1.67 | 1.68 | 1.60 | 1.59 |
| Al-Hz | 2.88 | 4.85 | 5.91 | - | - | - |
| Al-O1 | 1.73 | 1.71 | 1.68 | 1.69 | 1.73 | 1.82 |
| Al-O2 | 1.76 | 1.75 | 1.84 | 1.83 | 1.74 | 1.69 |
| Hz-O | 1.00 | 0.97 | 0.97 | - | - | - |
| O1-Hz | 1.68 | 3.48 | 4.78 | - | - | - |
| O1-H | 3.92 | 3.35 | 3.14 | 4.05 | 1.57 | 0.99 |
| C1-C2 | 1.51 | 1.48 | 1.50 | 1.51 | 1.40 | 1.34 |
| C1-O2 | 3.29 | 2.18 | 1.53 | 1.52 | 2.28 | 3.47 |
| C1-O | 1.47 | 2.10 | 3.41 | - | - | - |
| C2-H | 1.09 | 1.09 | 1.09 | 1.09 | 1.19 | 2.16 |
| Angle (o) |  |  |  |  |  |  |
| Si1-O1-Al | 128.19 | 131.90 | 134.29 | 128.34 | 128.99 | 129.37 |
| Si2-O2-Al | 133.67 | 129.27 | 124.19 | 127.84 | 132.47 | 133.76 |

Table S15 Relative energies of ethylene on the H-[Al]-ZSM-5 zeolites from ONIOM 5T:34T MP2/6-31G (d,p):M06-2X/6-31G(d,p) calculations. Energies are given in kcal/mol. Total Activation energy are in parenthesis.

|  | AD-Al-1C | TS1-Al | IN1-Al | IN2-Al | TS2-Al | PR-Al |
| --- | --- | --- | --- | --- | --- | --- |
| ONIOM a | -30.4 | 11.9 | -10.0 | 2.0 | 34.9 | 6.9 |
|  |  | (42.3) |  |  | (32.9) |  |
| MP2 b | -19.6 | 29.7 | 0.9 | 2.1 | 42.1 | 11.2 |
|  |  | (49.3) |  |  | (40.0) |  |
| Framework c | -10.8 | -17.8 | -10.9 | -0.1 | -7.2 | -4.3 |
| ONIOM d | -25.7 | 15.4 | -5.7 | 1.1 | 32.5 | 2.4 |
|  |  | (41.1) |  |  | (31.4) |  |
| MP2 b | -16.8 | 29.5 | 0.3 | 0.0 | 37.6 | 6.4 |
|  |  | (46.3) |  |  | (37.6) |  |
| Framework c | -8.9 | -14.1 | -5.9 | 1.1 | -5.1 | -4.0 |
| Embedded ONIOM f | -28.1 | 11.9 | -7.5 | -2.2 | 28.5 | 0.7 |
|  |  | (40.0) |  |  | (30.7) |  |
| MP2 g | -18.9 | 24.5 | 0.0 | -1.4 | 33.6 | 5.1 |
|  |  | (43.4) |  |  | (35.0) |  |
| Framework c | -9.2 | -12.6 | -7.5 | -0.8 | -5.1 | -4.4 |

a ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T:34T

b MP2/6-31G(d,p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T//5T:34T

c EONIOM – Ehigh level

d ONIOM(MP2/6-311+G(2df,2p):M06-2X/6-311+G(2df,2p))//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T:34T

e MP2/6-311+G(2df,2p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T//5T:34T

f ONIOM(MP2/6-311+G(2df,2p):M06-2X/6-311+G(2df,2p))//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) with charge model 5T:34T

g MP2/6-311+G(2df,2p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) with charge model 5T//5T:34T

| AD-Al-1A | TSc-Al |
| --- | --- |
| INc-Al | PRc-Al |

Figure S9 The concerted mechanism of ethanol to ethylene on the Al-ZSM-5 zeolites with 
ONIOM 5T:34T MP2/6-31G(d,p):M06-2X/6-31G(d,p). Distances are in Å.

Table S16: Selected structural parameters and energies for the stepwise mechanism on the H-[Al]-ZSM-5 zeolites.

|  | AD-Al-1A | TSc-Al | INc-Al | PRc-Al |
| --- | --- | --- | --- | --- |
| Distance (Å) |  |  |  |  |
| Si1-O1 | 1.64 | 1.59 | 1.59 | 1.59 |
| Si2-O2 | 1.58 | 1.63 | 1.67 | 1.66 |
| Al-Hz | 2.44 | 3.02 | 3.43 | - |
| Al-O1 | 1.80 | 1.70 | 1.68 | 1.69 |
| Al-O2 | 1.69 | 1.77 | 1.83 | 1.83 |
| Hz-O | 1.42 | 0.97 | 0.97 | - |
| O1-Hz | 1.07 | 2.24 | 3.62 | - |
| O2-H | 2.83 | 1.33 | 0.99 | 0.99 |
| C1-C2 | 1.51 | 1.38 | 1.34 | 1.34 |
| C1-O | 1.46 | 2.22 | 4.26 | - |
| C2-H | 1.09 | 1..32 | 2.45 | 2.37 |
| Angle (o) |  |  |  |  |
| Si1-O1-Al | 127.57 | 128.28 | 126.16 | 127.69 |
| Si2-O2-Al | 136.29 | 132.34 | 133.73 | 132.88 |

Table S17 Relative energies of ethylene on the H-[Al]-ZSM-5 zeolites from ONIOM 5T:34T MP2/6-31G (d,p):M06-2X/6-31G(d,p) calculations. Energies are given in kcal/mol. Total Activation energy are in parenthesis.

|  | AD-Al-1A | TSc-Al | INc-Al | PRc-1A |
| --- | --- | --- | --- | --- |
| ONIOM a | -24.3 | 24.8 | 0.2 | 9.7 |
|  |  | (49.1) |  |  |
| MP2 b | -16.4 | 31.1 | 8.8 | 15.3 |
|  |  | (47.5) |  |  |
| Framework c | -8.0 | -6.3 | -8.5 | -5.6 |
| ONIOM d | -21.3 | 26.3 | 1.8 | 6.2 |
|  |  | (47.6) |  |  |
| MP2 b | -14.7 | 30.3 | 6.5 | 10.6 |
|  |  | (45.0) |  |  |
| Framework c | -6.6 | -4.0 | -4.7 | -4.3 |
| Embedded ONIOM f | -23.3 | 19.3 | -4.4 | 5.1 |
|  |  | (42.6) |  |  |
| MP2 g | -17.1 | 25.3 | 4.3 | 11.2 |
|  |  | (42.4) |  |  |
| Framework c | -6.2 | -6.0 | -8.7 | -6.2 |

a ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T:34T

b MP2/6-31G(d,p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T//5T:34T

c EONIOM – Ehigh level

d ONIOM(MP2/6-311+G(2df,2p):M06-2X/6-311+G(2df,2p))//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T:34T

e MP2/6-311+G(2df,2p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T//5T:34T

f ONIOM(MP2/6-311+G(2df,2p):M06-2X/6-311+G(2df,2p))//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) with charge model 5T:34T

g MP2/6-311+G(2df,2p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) with charge model 5T//5T:34T

4.3 The dehydration reaction of ethanol to ethylene on H-[Ga]-ZSM-5 zeolite

| AD-Ga-1C | TS1-Ga |
| --- | --- |
| IN1-Ga | IN2-Ga |
| TS2-Ga | PR-Ga |

Figure S10 The optimized structures of ethanol to ethylene on the Ga-ZSM-5 zeolites with 
ONIOM 5T:34T MP2/6-31G(d,p):M06-2X/6-31G(d,p). Distances are in Å.

Table S18: Selected structural parameters and energies for the stepwise mechanism on the H-[Ga]-ZSM-5 zeolites.

|  | AD-Ga-1C | TS1-Ga | IN1-Ga | IN2-Ga | TS2-Ga | PR-Ga |
| --- | --- | --- | --- | --- | --- | --- |
| Distance (Å) |  |  |  |  |  |  |
| Si1-O1 | 1.60 | 1.56 | 1.56 | 1.57 | 1.59 | 1.65 |
| Si2-O2 | 1.59 | 1.60 | 1.67 | 1.67 | 1.59 | 1.58 |
| Ga-Hz | 2.61 | 4.90 | 5.95 | - | - | - |
| Ga-O1 | 1.81 | 1.78 | 1.74 | 1.74 | 1.80 | 1.89 |
| Ga-O2 | 1.80 | 1.82 | 1.91 | 1.91 | 1.81 | 1.75 |
| Hz-O | 1.05 | 0.97 | 0.97 | - | - | - |
| O1-Hz | 1.44 | 3.47 | 4.73 | - | - | - |
| O1-H | 3.11 | 2.88 | 2.99 | 3.97 | 1.55 | 0.99 |
| C1-C2 | 1.51 | 1.48 | 1.50 | 1.51 | 1.40 | 1.34 |
| C1-O2 | 3.27 | 2.15 | 1.53 | 1.52 | 2.27 | 3.31 |
| C1-O | 1.49 | 2.10 | 3.40 | - | - | - |
| C2-H | 1.09 | 1.09 | 1.09 | 1.09 | 1.19 | 2.13 |
| Angle (o) |  |  |  |  |  |  |
| Si1-O1-Ga | 126.16 | 127.88 | 128.78 | 123.57 | 126.01 | 128.75 |
| Si2-O2-Ga | 132.09 | 127.84 | 124.06 | 127.3 | 129.69 | 128.20 |

Table S19 Relative energies of ethylene on the H-[Ga]-ZSM-5 zeolites from ONIOM 5T:34T MP2/6-31G (d,p):M06-2X/6-31G(d,p) calculations. Energies are given in kcal/mol. Total Activation energy are in parenthesis.

|  | AD-Ga-1C | TS1-Ga | IN1-Ga | IN2-Ga |  | TS2-Ga | PR-Ga |
| --- | --- | --- | --- | --- | --- | --- | --- |
| ONIOM a | -33.0 | 9.3 | -11.8 |  | 0.8 | 31.9 | 5.8 |
|  |  | (42.3) |  |  |  | (31.1) |  |
| MP2 b | -24.4 | 26.8 | -0.3 |  | 1.5 | 39.0 | 10.2 |
|  |  | (51.2) |  |  |  | (37.5) |  |
| Framework c | -8.6 | -17.5 | -11.6 |  | -0.7 | -7.1 | -4.3 |
| ONIOM d | -25.1 | 16.5 | -5.2 |  | 3.1 | 33.4 | 2.5 |
|  |  | (41.6) |  |  |  | (30.3) |  |
| MP2 b | -18.0 | 29.5 | 1.4 |  | 1.9 | 38.2 | 6.3 |
|  |  | (47.5) |  |  |  | (36.3) |  |
| Framework c | -7.1 | -13.0 | -6.6 |  | 1.2 | -4.8 | -3.8 |
| Embedded ONIOM f | -27.7 | 13.4 | -6.0 |  | 0.4 | 29.5 | 0.9 |
|  |  | (41.1) |  |  |  | (29.1) |  |
| MP2 g | -20.2 | 24.8 | 1.8 |  | 0.8 | 34.3 | 5.1 |
|  |  | (45.0) |  |  |  | (33.5) |  |
| Framework c | -7.5 | -11.4 | -7.8 |  | -0.4 | -4.8 | -4.2 |

a ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T:34T

b MP2/6-31G(d,p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T//5T:34T

c EONIOM – Ehigh level

d ONIOM(MP2/6-311+G(2df,2p):M06-2X/6-311+G(2df,2p))//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T:34T

e MP2/6-311+G(2df,2p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T//5T:34T

f ONIOM(MP2/6-311+G(2df,2p):M06-2X/6-311+G(2df,2p))//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) with charge model 5T:34T

g MP2/6-311+G(2df,2p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) with charge model 5T//5T:34T

| AD-Ga-1A | TSc-Ga |
| --- | --- |
| INc-Ga | PRc-Ga |

Figure S11 The concerted mechanism of ethanol to ethylene on the Ga-ZSM-5 zeolites with 
ONIOM 5T:34T MP2/6-31G(d,p):M06-2X/6-31G(d,p). Distances are in Å.

Table S20: Selected structural parameters and energies for the stepwise mechanism on the H-[Ga]-ZSM-5 zeolites.

|  | AD-Ga-1A | TSc-Ga | INc-Ga | PRc-Ga |
| --- | --- | --- | --- | --- |
| Distance (Å) |  |  |  |  |
| Si1-O1 | 1.63 | 1.58 | 1.58 | 1.57 |
| Si2-O2 | 1.57 | 1.62 | 1.67 | 1.65 |
| Ga-Hz | 2.50 | 2.91 | 3.45 | - |
| Ga-O1 | 1.87 | 1.76 | 1.74 | 1.74 |
| Ga-O2 | 1.75 | 1.83 | 1.91 | 1.91 |
| Hz-O | 1.39 | 0.97 | 0.97 | - |
| O1-Hz | 1.08 | 2.09 | 3.71 | - |
| O2-H | 2.88 | 1.33 | 0.99 | 0.99 |
| C1-C2 | 1.51 | 1.38 | 1.34 | 1.34 |
| C1-O | 1.46 | 2.33 | 4.28 | - |
| C2-H | 1.09 | 1.32 | 2.40 | 2.20 |
| Angle (o) |  |  |  |  |
| Si1-O1-Ga | 127.01 | 123.68 | 120.72 | 122.75 |
| Si2-O2-Ga | 130.31 | 130.93 | 134.04 | 133.58 |

Table S21 Relative energies of ethylene on the H-[Ga]-ZSM-5 zeolites from ONIOM 5T:34T MP2/6-31G (d,p):M06-2X/6-31G(d,p) calculations. Energies are given in kcal/mol. Total Activation energy are in parenthesis.

|  | AD-Ga-1A | TSc-Ga | INc-Ga | PRc-Ga |
| --- | --- | --- | --- | --- |
| ONIOM a | -26.4 | 21.5 | -0.5 | 10.0 |
|  |  | (47.9) |  |  |
| MP2 b | -18.0 | 27.2 | 7.9 | 14.7 |
|  |  | (45.2) |  |  |
| Framework c | -8.4 | -5.7 | -8.4 | -4.7 |
| ONIOM d | -20.9 | 27.0 | 3.5 | 8.5 |
|  |  | (47.9) |  |  |
| MP2 b | -14.2 | 30.3 | 7.6 | 11.6 |
|  |  | (44.5) |  |  |
| Framework c | -6.8 | -3.3 | -4.0 | -3.1 |
| Embedded ONIOM f | -23.2 | 20.4 | -2.0 | 7.4 |
|  |  | (43.6) |  |  |
| MP2 g | -16.8 | 25.3 | 5.6 | 11.7 |
|  |  | (42.1) |  |  |
| Framework c | -6.4 | -4.9 | -7.6 | -4.3 |

a ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T:34T

b MP2/6-31G(d,p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T//5T:34T

c EONIOM – Ehigh level

d ONIOM(MP2/6-311+G(2df,2p):M06-2X/6-311+G(2df,2p))//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T:34T

e MP2/6-311+G(2df,2p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) model 5T//5T:34T

f ONIOM(MP2/6-311+G(2df,2p):M06-2X/6-311+G(2df,2p))//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) with charge model 5T:34T

g MP2/6-311+G(2df,2p)//ONIOM(MP2/6-31G(d,p):M06-2X/6-31G(d,p) with charge model 5T//5T:34T

Figure S12 Energy profiles for the stepwise mechanism of on the three zeolites H-[B]-ZSM-5, H-[Al]-ZSM-5 and H-[Ga]-ZSM-5 zeolites as calculated with the embedded ONIOM (MP2/6-311+G(2df,2p):M06-2X/6-311+G(2df,2p)) // ONIOM (MP2/6-31G(d,p):M06-2X/6-31G(d,p)).

Figure S13 Energy profiles for the concerted mechanism of on the three zeolites H-[B]-ZSM-5, H-[Al]-ZSM-5 and H-[Ga]-ZSM-5 zeolites as calculated with the embedded ONIOM (MP2/6-311+G(2df,2p):M06-2X/6-311+G(2df,2p)) // ONIOM (MP2/6-31G(d,p):M06-2X/6-31G(d,p)).