Parameters LCMCO

2θrange (degree) 20-90

Unit cell volume 230.4140

Step size (degree) 0.02

Reliability factor

Bragg R-factor 1.89

Rf factor 0.991

Crystal symmetry Orthorhombic

χ2 0.378

Space group Pbnm

Half-width parameters

U 4.062380

V -1.828204

W 0.151554

Cell parameters

a 5.4989

b 5.4265

c 7.7217

Table 1. Summary of refined crystallographic data for La0.7Ca0.3Mn0.6Co0.4O3

Atoms              x                  y                  z               Occupancy        Wyckoff pofition

La          -0.01970      -0.00100       0.25000            0.370                      4c

Ca          -0.01970      -0.00100       0.25000            0.204                      4c

Mn              0.5                0                   0                  0.218                     4b

Co               0.5                0                   0                  0.088                     4b

O(1)        0.03861       0.50314       0.25000             0.560                     4c

O(2)       -0.48250       0.13161       0.06321             1.000                     8d

Table 2. Refined atomic position of the atoms for La0.7Ca0.3Mn0.6Co0.4O3

2θ                  dobs                          dcal                              hkl

23.017         3.860895         3.860855              002

32.77           2.730686         2.730603              112

40.607         2.21993           2.219892              022

47.03           1.930629         1.930428              004

58.359         1.579949         1.579900              204

68.691         1.36534           1.365302              224

78.23           1.220995         1.220960              116

Table 3. Observed and calculated interplanar d-spacings for La0.7Ca0.3Mn0.6Co0.4O3

| Composition | Synthesis route | Sintering Temperature | MS (emu/gm) | HC (Oe) | Mr (emu/gm) | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| LaMnO3 | Sol gel | 850 | 1.69 | 82.95 | 0.1 | [24] |
| La0.7Ca0.3MnO3 | Sol gel | 1023 | 1.92 | 0.0267 | - | [54] |
| LaMn0.6Co0.4O3 | Hydrothermal | 850 | 36.52 | 2.625 | 18.69 | [59] |
| La0.7Ca0.3Mn0.6Co0.4O3 | Sol gel autocombustion | 1000 | 1.67 | 166.1 | 0.01 | Present work |

Table 4. Comparison table for magnetic parameters like Ms, HC and Mr of present sample with those reported in literature.