# Extended data figures

Extended Data Fig.1 | Nine step fabrication process used to realize HZO and HZO-SiO2 nanomechanical resonators. The fabrication process consists of successive deposition and patterning of SiO2, HZO-Al2O3, W, and Pt layers to realize two- or three-port nanomechanical resonators to operate in bulk acoustic wave modes. After deposition of HZO-Al2O3 and W layers, rapid thermal annealing is used for crystallization if ferroelectric transducer in polar orthorhombic phase. In HZO resonators, metal-ferroelectric-metal stack is sandwiched between HZO passivation layers that also serve to protect W electrodes from oxidation. In HZO-SiO2 resonators, HZO passivation layers are replaced by SiO2 layers. After deposition and patterning of different layers, the resonators are released from substrate by dry etching of silicon substrate.

Extended Data Fig.2 | Simulation of BAW HZO-SiO2 resonator operated in WE3 mode. a, Schematic cross-section of HZO-SiO2 resonator, used for COMSOL modeling. b, COMSOL-simulated vibration mode-shape of the WE3 mode. The color code represent in-plane longitudinal stress in width direction of the resonator.

Extended Data Fig.3 | Resonator and clock measurement setup. Resonators and clock s are measured using an RF probe station with temperature-controlled chuck. The measurement setup consists of a controller unit controlling chuck temperature with resistive heating and liquid nitrogen lines, a liquid nitrogen cannister, RF vector network analyzer, UHF lock-in amplifier, and ferroelectric tester.

Extended Data Fig.4 | Ab-initio calculated stiffness constants of HZO. a, Thermal expansion coefficient, b, Unit cell volume, and c, Young’s Modulus of orthorhombic and tetragonal phases of HZO with 50% Zr content.

Extended Data Fig.5 | Temperature dependence of remanent polarization. Temperature-dependent remanent polarization of HZO films with different Zr contents of a, 50%, b, 40%, and c, 67%, extracted from PUND tests on non-released capacitors.

Extended Data Fig.6 | HZO-SiO2 stable nanomechanical clock. a, Schematic diagram of clock system, consisting of two oscillators locked around HZO and HZO-SiO2 resonators that are placed on a common interposer. The HZO oscillator serves for real-time temperature sensing, enabling calculation of the required DC tuning voltage for compensation of residual frequency drifts in HZO-SiO2 oscillator. The temperature-to-voltage scaling function is created using LabOne interface in lock-in amplifier, based on the measured frequency-tuning characteristic. Measured b-c, spectrum and d, phase-noise of the HZO and HZO-SiO2 oscillators, at room temperature.

Extended data Table 1| Measured Characteristic of Resonator Groups.

| Composition | Number | f0 (MHz) | Q | IL (dB) | TCF1 (ppm/℃) | TCF2 (ppb/℃2) |
| --- | --- | --- | --- | --- | --- | --- |
| Hf0.5Zr0.5O2 | 1 | 238.92 | 844 | −45.39 | -73.87 | -3.13 |
|  | 2 | 239.15 | 794 | −46.16 | -73.46 | -3.69 |
|  | 3 | 239.91 | 738 | −45.81 | -74.71 | -6.79 |
|  | 4 | 239.49 | 736 | −46.40 | -73.14 | -2.14 |
|  | 5 | 239.76 | 742 | −45.91 | -74.22 | -3.53 |
|  | 6 | 238.57 | 798 | −45.66 | -72.68 | -2.81 |
|  | 7 | 238.91 | 788 | −45.77 | -73.32 | -6.23 |
|  | 8 | 239.22 | 801 | −45.92 | -73.33 | -4.50 |
|  | 9 | 239.26 | 802 | −45.75 | -71.88 | -3.50 |
|  | 10 | 238.83 | 767 | −45.94 | -74.38 | -4.68 |
| Hf0.33Zr0.67O2 | 1 | 239.69 | 708 | −41.00 | -75.23 | 21.40 |
|  | 2 | 239.15 | 679 | −42.67 | −75.99 | 21.86 |
|  | 3 | 239.51 | 787 | −42.67 | −74.81 | 21.92 |
|  | 4 | 239.07 | 715 | −42.69 | −75.08 | 21.60 |
|  | 5 | 238.37 | 810 | −42.67 | −76.77 | 22.46 |
|  | 6 | 239.29 | 724 | −42.67 | −74.48 | 23.51 |
|  | 7 | 238.68 | 732 | −42.66 | −74.82 | 20.91 |
|  | 8 | 239.11 | 792 | −42.68 | −74.98 | 22.23 |
|  | 9 | 239.6 | 748 | −42.67 | −76.32 | 21.50 |
|  | 10 | 239.52 | 695 | −42.66 | −75.52 | 22.61 |

Extended data Table 2| Key parameters used in COMSOL simulation.

| Material Property | Value |
| --- | --- |
| EW 53 | 430 Gpa |
| TCE1,W 53 | -77.6 ppm/℃ |
| TCE2,W 53 | -28.6 ppb/℃2 |
| νW 54 | 0.26 |
| α1,W 55 | 4.5 ppm/⁰C |
| ESiO2 56 | 60 GPa |
| νSiO2 56 | 0.25 |
| α1,SiO2 56 | 2.67 ppm/⁰C |
| TCE1,SiO2 57 | 163 ppm/⁰C |
| EHZO, Transducer 34 | 320 GPa |
| EHZO, Passivation 34 | 285.43 GPa |
| νHZO 58 | 0.29 |
| α1,HZO 59 | 4.5 ppm/⁰C |
| EHf0.54Zr0.46O2 58 | 264±8 Gpa |
| EHf0.21Zr0.79O2 58 | 259±7 Gpa |