Supplementary Material

Figure 1. Availability of soluble Cl-, HCO3-, NO3-, PO43-, and SO42-, anions (A), NH4+, K+, Mg2+ and Ca2+ cations (B) and Na+ (C) in bone and BoC pyrolyzed at different temperatures.

Figure 2. SEM image of BoC produced at 400 °C

Figure 3. EDS spectrum of BoC produced at 400 °C

Table 1. Semi quantification results of BoC produced at 400 °C

| Element | Wt% |
| --- | --- |
| O | 47.86 |
| P | 11.34 |
| Ca | 29.11 |
| C | 11.69 |
| Total | 100 |

Figure 4. SEM image of BoC produced at 1000 °C

Figure 5. EDS spectrum of BoC produced at 1000 °C

Table 2. Semi quantification results of BoC produced at 1000 °C

| Element | Wt% |
| --- | --- |
| O | 42.06 |
| Ca | 29.26 |
| P | 13.91 |
| Ca | 13.76 |
| Na | 1.01 |
| Total | 100 |