Table1. Test Data for Materials

| S. NO | Material | Property | Value |
| --- | --- | --- | --- |
| 1. | Cement conforming to IS: IS:279-2015 | Ordinary Portland Cement (OPC). | 43 grade |
| 2. |  | Specific Gravity | 3.15 |
| 3. |  | Fineness of Cement by sieving | 10% |
| 4. |  | Normal Consistency | 25-30% |
| 5. |  | Initial Setting time | 30 minutes |
| 6. |  | Final Setting time | 600 minutes |
| 7. |  | 7 days compressive strength | 33 N/mm² |
| 8. |  | 28 days compressive strength | 43N/mm² |
| 9. | Natural River Sand as a Fine Aggregate(These values are below the maximum permissible values specified by IS-383) | Grading of Sand | - Zone I |
| 10. |  | Specific Gravity | 2.57 |
| 11. |  | Density (compacted) | 1791 kg/m³ |
| 12. |  | Water Absorption | 2.26 % |
| 13. |  | Fineness Modulus | 2.75 |
| 14. |  | Fines | 6 % |
| 15. | Locally available crushed siliceous stone as a Coarse Aggregate (These values are below the maximum permissible values specified by IS-383) | Specific Gravity | 2.85 |
| 16. |  | Density | 1691 kg/m³ |
| 17. |  | Water Absorption | 0.90 % |
| 18. |  | Flakiness Index | 20% |
| 19. |  | Elongation Index | 20% |
| 20. |  | Crushing Value | 21.33 % |
| 21. |  | Impact Value | 15.40 % |
| 22. |  | Fineness Modulus | 6.65 |
| 23. | Super plasticizer as per IS 9103- 1999 | Appearance | Light brown colour |
| 24. |  | Specific gravity | 1.12 ± 0.01 |
| 25. |  | pH | Minimum 6 |
| 26. |  | Chloride ion content | 0.2% |
| 27. | Water | miming and curing of concrete | Potable water |

Table 2: Mix Design Proportions and Water-Cement Ratios

| Mix Proportions | 1:3:6 | 1:2:4 | 1:1.5:3 | 1:1:2 | 1:0.75:1.5 | 1:0.5:1 | 1:0.25:0.5 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Water-Cement Ratio (w/c) | 0.55 | 0.55 | 0.5 | 0.5 | 0.45 | 0.45 | 0.45 |
| Cement Content | - | - | - | 300 kg | 320 kg | 340 kg | 340 kg |
| Mix Grade | M10 | M15 | M20 | M25 | M30 | M35 | M40 |

Table 3: Quantity of Materials for Different Concrete Grades

| Grade | M10, M15, M20, M25 | M30 | M35 | M40 |
| --- | --- | --- | --- | --- |
| Cement (kg) | 280 | 290 | 430 | 430 |
| Fly Ash (kg) | 270 | 270 | 110 | 110 |
| Fine Aggregate (kg) | 799 | 836 | 814 | 814 |
| Coarse Aggregate (kg) | 834 | 858 | 814 | 814 |
| Water (kg) | 182 | 166 | 172 | 172 |
| Super Plasticizer (kg) | 3.3 | 4.48 | 3.48 | 3.48 |

Table 4:- Training and testing parameters of Linear and Nonlinear Models

| S.No | Linear and non-linear Model | SSE | R-square | DFE | Adj R-sq | RMSE | Goodness of Validation |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  | SSE | RMSE |
| 1. | Polynomial Curve Fit (poly1) f(x) = p1*x + p2 Value Lower Upper p1 1.0938 1.0692 1.1184 p2 -0.0146 -0.0262 -0.0031 | 0.51 | 0.96 | 236 | 0.97 | 0.05 | 0.29 | 0.05 |
| 2. | Polynomial Curve Fit (poly2) f(x) = p1*x^2 + p2*x + p3 Value Lower Upper p1 -0.1570 -0.2576 -0.0564 p2 1.2334 1.1407 1.3261 p3 -0.0362 -0.0541 -0.0183 | 0.49 | 0.97 | 235 | 0.97 | 0.04 | 0.27 | 0.04 |
| 3. | Polynomial Curve Fit (poly3) f(x) = p1*x^3 + p2*x^2 + p3*x + p4 Value Lower Upper p1 -0.5215 -0.9156 -0.1273 p2 0.5555 0.0079 1.1032 p3 0.9708 0.7521 1.1894 p4 -0.0141 -0.0384 0.0101 | 0.48 | 0.97 | 234 | 0.97 | 0.0453 | 0.262 | 0.0469 |
| 4. | Polynomial Curve Fit (poly4) f(x) = p1*x^4 + p2*x^3 + p3*x^2 + p4*x + p5 Value Lower Upper p1 -0.6880 -2.1755 0.7996 p2 0.7791 -2.0606 3.6189 p3 -0.2400 -2.0453 1.5653 p4 1.1426 0.7115 1.5737 p5 -0.0234 -0.0548 0.0081 | 0.478 | 0.972 | 233 | 0.971 | 0.0453 | 0.260 | 0.0468 |
| 5. | Polynomial Curve Fit (poly5) f(x) = p1*x^5 + p2*x^4 + p3*x^3 + p4*x^2 + p5*x + p6 Value Lower Upper p1 -4.1475 -9.7700 1.4750 p2 9.3277 -4.3308 22.9861 p3 -7.8367 -19.8553 4.1820 p4 2.9123 -1.7251 7.5498 p5 0.6906 -0.0580 1.4392 p6 -0.0065 -0.0453 0.0323 | 0.474 | 0.973 | 232 | 0.972 | 0.0452 | 0.2535 | 0.0462 |
| 6. | Polynomial Curve Fit (poly6) f(x) = p1*x^6 + p2*x^5 + p3*x^4 + p4*x^3 + p5*x^2 + p6*x + p7 Value Lower Upper p1 -7.2727 -30.2097 15.6643 p2 17.2977 -50.5711 85.1666 p3 -14.6497 -91.4973 62.1980 p4 4.7988 -36.8290 46.4266 p5 -0.2454 -11.2338 10.7430 p6 1.0167 -0.2560 2.2895 p7 -0.0155 -0.0636 0.0326 | 0.473 | 0.972 | 231 | 0.972 | 0.0453 | 0.2538 | 0.0462 |
| 7. | Polynomial Curve Fit (poly7) f(x) = p1*x^7 + p2*x^6 + p3*x^5 + p4*x^4 + p5*x^3 + p6*x^2 + p7*x + p8 Value Lower Upper p1 -82.7149 -173.9461 8.5163 p2 276.2005 -37.2913 589.6923 p3 -367.1013 -796.4254 62.2228 p4 247.4802 -51.5849 546.5453 p5 -89.5102 -201.4773 22.4568 p6 16.8570 -4.9475 38.6614 p7 -0.3169 -2.2581 1.6244 p8 0.0131 -0.0442 0.0705 | 0.467 | 0.973 | 230 | 0.972 | 0.045 | 0.2494 | 0.0458 |
| 8. | Polynomial Curve Fit (poly8) f(x) = p1*x^8 + p2*x^7 + p3*x^6 + p4*x^5 + p5*x^4 + p6*x^3 + p7*x^2 + p8*x + p9 Value Lower Upper p1 91.8999 -256.8712 440.6710 p2 -443.8682 -1.8175e+03 929.7940 p3 855.8697 -1.3663e+03 3.0781e+03 p4 -856.0839 -2.7610e+03 1.0488e+03 p5 479.7070 -451.1358 1.4105e+03 p6 -151.1918 -410.7582 108.3746 p7 25.3929 -13.6763 64.4621 p8 -0.8356 -3.6024 1.9313 p9 0.0220 -0.0446 0.0886 | 0.466 | 0.973 | 229 | 0.972 | 0.0451 | 0.2522 | 0.0460 |
| 9. | Exponential Curve Fit (exp1) f(x) = a*exp(b*x) Value Lower Upper a 0.1649 0.1530 0.1769 b 2.0830 1.9768 2.1892 | 1.943 | 0.887 | 236 | 0.886 | 0.0907 | 1.0801 | 0.0953 |
| 10. | Exponential Curve Fit (exp2) f(x) = a*exp(b*x) + c*exp(d*x) Value Lower Upper a 1.8421e+03 -1.7316e+10 1.7316e+10 b -0.1353 -3.1377e+03 3.1375e+03 c -1.8421e+03 -1.7316e+10 1.7316e+10 d -0.1360 -3.1386e+03 3.1383e+03 | 0.495 | 0.971 | 234 | 0.971 | 0.0460 | 0.2713 | 0.0478 |
| 11. | Gaussian Curve Fit (gauss1) f(x) = a1*exp(-((x-b1)/c1)^2) Value Lower Upper a1 0.8976 0.8679 0.9272 b1 0.9171 0.8797 0.9544 c1 0.5821 0.5512 0.6129 | 0.650 | 0.962 | 235 | 0.962 | 0.0526 | 0.3638 | 0.0553 |
| 12. | Gaussian Curve Fit (gauss2) f(x) = a1*exp(-((x-b1)/c1)^2) + a2*exp(-((x-b2)/c2)^2) Value Lower Upper a1 0.9352 0.8709 0.9995 b1 0.9527 0.8958 1.0096 c1 0.4482 0.0891 0.8073 a2 0.2323 -0.2630 0.7276 b2 0.4063 0.2419 0.5707 c2 0.2759 0.1236 0.4282 | 0.502 | 0.971 | 232 | 0.970 | 0.0465 | 0.2710 | 0.0477 |
| 13. | Sum of Sine Curve Fit (sin1) f(x) = a1*sin(b1*x+c1) Value Lower Upper a1 1.3982 1.0656 1.7307 b1 0.8454 0.6100 1.0808 c1 -0.0237 -0.0387 -0.0086 | 0.488 | 0.972 | 235 | 0.971 | 0.0456 | 0.2653 | 0.0472 |
| 14. | Sum of Sine Curve Fit (sin5) f(x) = a1*sin(b1*x+c1) + a2*sin(b2*x+c2) + a3*sin(b3*x+c3) + a4*sin(b4*x+c4) + a5*sin(b5*x+c5) Value Lower Upper a1 0.9743 -339.2205 341.1690 b1 2.9302 -598.4242 604.2845 c1 -0.3816 -158.6463 157.8832 a2 3.5489 -1.0216e+06 1.0216e+06 b2 6.5538 -2.4789e+04 2.4803e+04 c2 1.5104 -9.8327e+03 9.8357e+03 a3 3.2349 -1.0220e+06 1.0220e+06 b3 6.7149 -2.3953e+04 2.3966e+04 c3 4.5879 -9.5674e+03 9.5765e+03 a4 0.0033 -0.0049 0.0115 b4 273.4460 261.6435 285.2486 c4 -4.0128 -9.4024 1.3768 a5 0.0052 -0.0031 0.0136 b5 484.8741 477.9369 491.8113 c5 -3.0198 -6.1605 0.1210 | 0.470 | 0.973 | 223. | 0.971 | 0.0459 | 0.2607 | 0.0468 |
| 15. | Sum of Sine Curve Fit (sin8) f(x) = a1*sin(b1*x+c1) + a2*sin(b2*x+c2) + a3*sin(b3*x+c3) + a4*sin(b4*x+c4) + a5*sin(b5*x+c5) + a6*sin(b6*x+c6) + a7*sin(b7*x+c7) + a8*sin(b8*x+c8) Value Lower Upper a1 1.1542 -798.0175 800.3260 b1 3.3282 -818.2804 824.9368 c1 -0.4910 -235.9622 234.9803 a2 4.2823 -7.4091e+05 7.4092e+05 b2 6.3264 -1.9482e+04 1.9495e+04 c2 1.6060 -7.6253e+03 7.6285e+03 a3 3.7675 -7.4174e+05 7.4174e+05 b3 6.5304 -1.8438e+04 1.8451e+04 c3 4.6673 -7.2872e+03 7.2965e+03 a4 0.0045 -0.0047 0.0137 b4 269.7201 261.8513 277.5889 c4 -2.2803 -5.9217 1.3610 a5 0.0061 -0.0026 0.0148 b5 484.3686 478.2597 490.4775 c5 -2.6262 -5.3651 0.1127 a6 0.0099 0.0014 0.0183 b6 394.0583 390.4152 397.7013 c6 2.6594 0.9267 4.3921 a7 0.0061 -0.0024 0.0146 b7 172.2420 166.2443 178.2398 c7 4.6861 1.8588 7.5133 a8 0.0059 -0.0029 0.0147 b8 39.5767 33.0991 46.0544 c8 1.2596 -1.8376 4.3568 | 0.450 | 0.974 | 214 | 0.971 | 0.0459 | 0.2704 | 0.0477 |
| 16. | Sigmoidal Curve Fit (logistic) f(x) = a/(1 + exp(-b*(x-c))) Value Lower Upper a 0.9628 0.9226 1.0029 b 5.6338 5.2401 6.0276 c 0.4482 0.4279 0.4686 | 0.62 | 0.964 | 235. | 0.963 | 0.0516 | 0.3497 | 0.0542 |
| 17. | Sigmoidal Curve Fit (gompertz) f(x) = d + (a-d)*exp(-exp(-b*(x-c))) Coefficients and 95% Confidence Bounds Value Lower Upper a 1.4481 1.0946 1.8015 b 1.8374 1.0811 2.5937 c 0.3306 0.2437 0.4175 d -0.2898 -0.6009 0.0212 | 0.482 | 0.972 | 234. | 0.972 | 0.0454 | 0.2645 | 0.0471 |

Where

F(x)=Compressive strength by DT;X=Compressive strength by NDT; a1 to c8 = Variables based on Linear and non-linear Models

Table 5; Percentage difference between of error in higher orders in the various models.

| S.No | Models | SSE (%) | RSME(%) |
| --- | --- | --- | --- |
| 1 | Polynomial Models | 86 | 92 |
| 2 | Exponential | 25 | 50 |
| 3 | Gaussian | 74 | 86 |
| 4 | Sum of Sine | 81 | 91 |
| 5 | Sigmoidal | 75 | 86 |