Supplementary Information

Alloying–Realloying Enabled High Durability for Pt–Pd–3d-Transition Metal Nanoparticle Fuel Cell Catalysts

Zhi-Peng Wu,1,2 Dominic T. Caracciolo,1 Yazan Maswadeh,3 Jianguo Wen,4 Zhijie Kong,1 Shiyao Shan,1 Jorge A Vargas,3 Shan Yan,1 Emma Hopkins,1 Keonwoo Park,1 Anju Sharma,1 Yang Ren,4 Valeri Petkov,3,* Lichang Wang2,5,* and Chuan-Jian Zhong1,*

1 Department of Chemistry, State University of New York at Binghamton, Binghamton, NY 13902, USA.

2 Key Laboratory of Ministry of Education for Green Chemical Technology, Tianjin University, Tianjin 300072, China.

3 Department of Physics, Central Michigan University, Mt. Pleasant, MI 48859, USA.

4 Center for Nanoscale Materials and X-ray Science Division, Argonne National Laboratory, Lemont, IL 60439, USA.

5 Department of Chemistry and Biochemistry and the Materials Technology Center, Southern Illinois University, Carbondale, IL 62901, USA.

*Correspondence to: cjzhong@binghamton.edu, lwang@chem.siu.edu, petkolvg@cmich.edu.

Supplementary Tables 1–6

Supplementary Figures 1 –14

Supplementary Table 1. Comparisons of the structures, compositions, preparations, and catalytic properties of the relevant catalysts reported in the recent literature. The compositions of the catalysts show the results after acid etching or electrochemical treatment processes.

| Catalysts | Composition | Catalysts treatment | Mass Activity | Durability | Refs |
| --- | --- | --- | --- | --- | --- |
| PtPdCu NPs | Pt27Pd20Cu53 | Thermochemical annealing under 20% O2 at 260 ℃ and 15% H2 at 400 ℃ in sequence. | 1.08 A mgPt+Pd-1 | Negligible MA decay after 50,000 cycles | This work |
| PdCu2@Pt core-shell NPs | Pt13.0Pd41.9Cu45.1 | Synthesize PdCu2/C core first, then anneals it at 500 ℃ in 10% H2 (balanced by N2) for 2h. Deposit Pt as the shell. | 0.485 A mgPt+Pd-1 | Negligible MA decay after 10,000 cycles | 52 |
| Hollow PtPdCu NPs | Pt37Pd41Cu22 | NPs supported on carbon then acid treated (dealloying). | 0.61 A mg-1 | Negligible MA decay after 10,000 cycles | 53 |
| PtPdCu nanodendrite | Pt14Pd80Cu6 | Deposit Pt-shell on PdCu nanodendrites. Surfactants removed by washing. | 0.42 A mgPt+Pd-1 (at 0.85 V vs. RHE) | 64% MA remains after 5,000 cycles | 54 |
| PtPdCu nanoparticle nanotubes | Pt32.6Pd15.4Cu52 | PtPdCu nanoparticles on Cu nanowires. Catalysts treated by electrochemical dealloying. | 0.52 A mgPt-1; 0.33 A mgPt+Pd-1. | 88.3% MA remains after 30,000 cycles | 55 |
| PtPdCu nanoframe | Pt74.7Pd18.6Cu6.7 | Catalysts treated by acid etching. | 1.04 A mgPt-1 | Observable MA decay after 10,000 cycles | 56 |
| PtPdCo nanoparticles | Pt35.1Pd35.4Co29.5 | Catalysts treated by washing with DI water and drying in a vacuum oven at 70 ℃ | The ORR activity is comparable to commercial Pt/C | No RDE data | 57 |
| Pd@PtNi core-shell octahedra | Pt1Pd1Ni0.55 | Catalysts treated by acid washing, heat at 60 ℃, then wash with ethanol. | 2.5 A mgPt-1; 1.6 A mgPt+Pd-1. | 1.7% MA decays after 10,000 cycles | 58 |
| Pd@Pt octahedra | Pt1Pd3.73 | Catalysts treated by acid etching. | 1.05 A mgPt-1 | 35% MA decays after 20,000 cycles | 59 |
| Pt3Ni nanoframe | Pt3Ni | Surfactants of the catalysts were removed by thermal treatment, then further annealing catalysts in inert gas below 400 ℃ for 12h. | 5.7 A mgPt-1 | Negligible MA decay after 10,000 cycles | 5 |
| Mo-doped Pt3Ni octahedral | Pt73.9Ni24.5Mo1.6 | Wash the catalysts by ethanol/acetone mixture. | 6.9 A mgPt-1 | 5.5% MA decays after 8,000 cycles | 6 |
| PtPb@Pt nanoplate | Pt55.9Pb44.1 | After assembly, anneal the catalyst at 250 ℃ at atmosphere for 1h. | 4.3 A mgPt-1 | 7.7% MA decays after 50,000 cycles | 8 |
| PtNi nanocages | Pt81Ni19 | As-synthesized nanocages undergo acid washing and then assembly on carbon support | 3.52 A mgPt-1 | Negligible MA decay after 50,000 cycles | 3 |
| PtNiCu NPs | Pt82.6Cu11.9Ni5.5 | Two-step wet chemical synthesis without post-treatments | 3.7 A mgPt-1 | 30.7% MA decays after 30,000 cycles | 13 |

Supplementary Table 2. Comparisons of the atomic compositions and their changes before and after electrochemical durability tests of the catalysts studied in this work. (NM: noble metal. NNM: non-noble metal.)

| Sample name | Feeding ratio | ICP composition (As-prepared) | ICP composition (Cycled) | NM:NNM (As-prepared) | NM:NNM (Cycled) | NNM% change |
| --- | --- | --- | --- | --- | --- | --- |
| PtPdCu* | 20:20:60 | 19:19:62 | 27:20:53 | 38:62 | 47:53 | 9 |
| PtPdCu* | 20:40:40 | 19:39:42 | 20:43:37 | 58:42 | 63:37 | 5 |
| PtPdCu* | 22:5:75 | 23:4:73 | 37:4:59 | 27:73 | 41:59 | 14 |
| PtPd* | 20:80 | 20:80 | 19:81 | / | / | / |
| PtPdCo* | 20:40:40 | 22:43:35 | 28:45:27 | 65:35 | 73:27 | 8 |
| PtPdNi* | 20:40:40 | 17:42:41 | 31:42:27 | 59:41 | 73:27 | 14 |
| PtCu* | 20:80 | 22:78 | 58:42 | 22:78 | 58:42 | 36 |
| PtFeCu** | 20:40:40 | 24:17:59 | 63:16:21 | 24:76 | 63:37 | 39 |
| PtFeCo** | 20:40:40 | 37:17:46 | 76:2:22 | 37:63 | 76:24 | 39 |
| PtFeNi** | 20:40:40 | 31:23:46 | 78:9:13 | 31:69 | 78:22 | 47 |
| PtNiCo** | 20:40:40 | 19:39:42 | 55:23:22 | 19:81 | 55:45 | 36 |
| PtCuCo** | 20:40:40 | 18:43:39 | 84:9:7 | 18:82 | 84:16 | 66 |
| PtCuNi** | 20:40:40 | 17:41:42 | 74:15:11 | 17:83 | 74:26 | 57 |
| PtFe** | 20:80 | 30:70 | 55:45 | 30:70 | 55:45 | 25 |
| PtNi** | 20:80 | 20:80 | 44:56 | 20:80 | 44:56 | 24 |
| PtCo** | 20:80 | 25:75 | 74:26 | 25:75 | 74:26 | 49 |

Note: * Catalysts tested 20,000 potential cycles;

** Catalysts tested 10,000 potential cycles.

Supplementary Table 3. Comparisons of the structures, compositions, and catalytic properties of the relevant PtPd catalysts reported in the recent literature.

| Catalysts | Composition | Mass Activity | Durability | Refs |
| --- | --- | --- | --- | --- |
| PtPdCu NPs | Pt19Pd19Cu62 | 1.08 A mgPt+Pd-1 | Negligible MA decay after 50,000 cycles | This work |
| PtPd nanowire | Pt78Pd22 | 0.92 A mgPt+Pd-1 | 9% MA decays after 8,000 cycles | 60 |
| PtPd nanocubes | Pt32Pd68 | 0.38 A mgPt+Pd-1 | 46% MA decays after 15,000 cycles | 61 |
| PtPdCo nanorings | Pt47Pd41Co12 | 3.58 A mgPt-1 (0.1 M KOH) | 29% MA decay after 30,000 cycles | 24 |
| Pt~Pd nanowire | N/A | 0.55 A mgPGM-1 | 37% ECSA and 3 mV half wave potential loss after 30,000 cycles | 62 |
| Pt monolayer /PdCu/C | Pt:Pd~1:5 (mass) | 0.44 A mgPGM-1 | ~36% MA loss after 5,000 cycles | 63 |
| Pd@Pt/C | Pt:Pd~1:1.5 (mass) | 0.38 A mgPGM-1 | 18% MA loss after 10,000 cycles | 64 |
| Pd-Pt nanodentrites | Pt:Pd~5.6:1 (mass) | 0.20 A mgPGM-1 | 50% ECSA loss after 10,000 cycles | 65 |
| Pd@Pt octahedra | Pt1Pd3.73 | 0.35 A mgPGM-1 | 35% MA loss after 20,000 cycles | 66 |
| Pt-Pd nanocages | N/A | 0.75 A mgPt-1 | 36% MA loss after 10,000 cycles | 67 |
| PtPd NPs | Pt14Pd86 | 0.20 A mgPGM-1 | N/A | 68 |
| PtPd alloy | Pt1Pd1 | 0.49 A mgPt-1 | 3.5% MA loss after 10,000 cycles | 69 |

Supplementary Table 4 | The reaction barriers (unit: eV) of some key elementary steps involved in the ORR on Pt (111), Pd (111), and PtPdCu (111) surfaces.

|  | Pt (111) | Pd (111) | PtPdCu (111) |
| --- | --- | --- | --- |
| *O2 + *H → *OOH + * | 0.34 | 0.67 | 0.19 |
| *OOH + * → *OH + *O | 0.26 | 0.07 | 0.03 |
| *O + *H → *OH + * | 0.74 | 0.73 | 0.29 |
| *OH + *H → *H2O + * | 0.22 | 0.44 | 0.29 |
| *O2 + * → *O + *O | 0.69 | 0.72 | 0.26 |

Supplementary Table 5 | Binding energies (unit: eV) of some key intermediates on Pt (111), Pd (111), and PtPdCu (111) surfaces.

|  | Pt (111) | Pd (111) | PtPdCu (111) |
| --- | --- | --- | --- |
| O2 | 0.52 | 0.74 | 0.28 |
| OOH | 1.13 | 1.22 | 1.23 |
| O | 3.99 | 4.18 | 4.05a 3.76b |
| OH | 2.17 | 2.37 | 2.38 |
| H2O | 0.29 | 0.29 | 0.26 |
| H | 2.63 | 2.57 | 2.45 |

a. On PdCuCu fcc site;

b. On PtPtPd fcc site.

Supplementary Table 6 | XPS peak positions (unit: eV) for Pt20PdnCu80-n/C catalysts. The deconvoluted XPS peak positions for Pt20PdnCu80-n/C catalysts, including Pt 4f7/2, and 4f5/2, Pd 3d5/2, and Pd 3d3/2, Cu 2p3/2, and Cu 2p1/2.

| XPS peak | Pt20Cu80 | Pt20Pd5Cu75 | Pt20Pd20Cu60 | Pt20Pd40Cu40 | Pt20Pd60Cu20 |
| --- | --- | --- | --- | --- | --- |
| Pt0 4f7/2 | 71.35 | 71.25 | 71.13 | 71.23 | 71.11 |
| Pt2+ 4f7/2 | 72.00 | 71.84 | 71.85 | 72.25 | 72.35 |
| Pt0 4f5/2 | 74.56 | 74.55 | 74.43 | 74.44 | 74.50 |
| Pt2+ 4f5/2 | 76.50 | 76.50 | 76.17 | 76.50 | 76.36 |
| Pd0 3d5/2 | --- | 336.02 | 335.89 | 335.86 | 335.65 |
| Pd2+ 3d5/2 | --- | --- | 337.20 | 336.86 | 336.95 |
| Pd0 3d3/2 | --- | 341.28 | 341.15 | 341.12 | 340.91 |
| Pd2+ 3d3/2 | --- | --- | 342.46 | 342.12 | 342.21 |
| Cu0 2p3/2 | 933.16 | 933.19 | 932.98 | 932.90 | 932.65 |
| Cu2+ 2p3/2 | 935.53 | 935.24 | 935.30 | 935.34 | 935.12 |
| Cu0 2p1/2 | 952.96 | 953.09 | 952.78 | 952.70 | 952.78 |
| Cu2+ 2p1/2 | 955.33 | 955.45 | 955.10 | 955.14 | 954.80 |

Supplementary Fig. 1 | Chart illustration of the progress of Pt catalysts development and evolution. a, Pt catalysts development towards higher activity & durability with lower cost, by tuning composition of ternary alloy (Ptx(MM)y, M, M: other transition metals), in comparison with most of the state-of-the-art catalysts with higher Pt content (>50%), and the catalyst composition evolution in fuel cell durability test. b, Plots of the percentage of the number of atoms (e.g., Pt) in the outmost layers of metal nanoparticles in terms of the different number of layers (1, 2, …, and 6) as a function of the nanoparticle diameter. c, An illustration of the design of Pt(MM') ternary alloy catalysts with different levels of reduction of the amount of Pt (in Pt%). The points in the Pt% < 50% region (red-highlight) show two scenarios: (I) Varying M% and M'% at fixed Pt% (e.g., Pt% fixed at 10%, 20%, and 40%). (II) Varying M'% while letting M% equal to fixed Pt%. d, Plots of the fraction (n) in Pt20PdnCu80-n NPs of Pd and Cu determined by ICP–OES as a function of the feeding ratios.

Supplementary Fig. 2 | Morphology characterizations of Pt20PdnCu80-n NPs. a-e, TEM images of the as-synthesized NPs. TEM images of a, Pt20Cu80, b, Pt20Pd5Cu75, c, Pt20Pd20Cu60, d, Pt20Pd40Cu40, and e, Pt20Pd60Cu20 NPs. The corresponding size distributions are 6.6±0.7 nm for Pt20Cu80, 9.7±0.7 nm for Pt20Pd5Cu75, 4.6±0.4 nm for Pt20Pd20Cu60, 4.3±0.4 nm for Pt20Pd40Cu40, and 4.1±0.4 nm for Pt20Pd60Cu20. f, HR-TEM image of the as-synthesized Pt20Pd20Cu60 NPs.

Supplementary Fig. 3 | Physical characterizations of Pt20PdnCu80-n/C catalysts. a, Optimization of the lattice strain by a combination of alloying and thermochemical treatment, which was demonstrated for many different alloy catalysts30. Gray, blue, and red atoms represent noble metal, non-noble metal, and oxygen atoms, respectively. b, XRD patterns of Pt20PdnCu80-n/C catalysts. c, Experimental curves (black symbols) and phase structure model-derived atomic PDFs (red lines) for the as-prepared Pt20PdnCu80-n/C catalysts.

Supplementary Fig. 4 | Electrochemical properties of Pt20PdnCu80-n/C catalysts. a, CV curves of the activation process for the as-prepared Pt20Pd20Cu60/C catalyst at a scan rate of 100 mV/s. b, The integrated charges for the copper oxidation and reduction waves at ~0.6 V in a, expressed as the ratio of the reacted Cu to the total Cu in the catalyst on the electrode surface as a function of the potential cycle number. c, The peak potential positions for the Cu oxidation wave in a as a function of the potential cycle number. d, CV curves for Pt20PdnCu80-n/C catalysts with different compositions. e, f, Plots of the ECSA values based on e, Pt and f, platinum group metals (Pt and Pd) as a function of Pd% in NPs. g, The theoretically-estimated ECSA values for Pt, Pd, and PtPd alloy spherical nanoparticles as a function of particle size. h, SA values as a function of Pd% in NPs. Error bars represent s.d. based on three independent experiments in e, f, h. i, CV curves and j, the corresponding ECSA values of Pt20Pd20Cu60/C catalyst before cycling and after 10K, 20K, 30K, 40K, 50K, 60K, and 70K cycles. k, RDE polarization curves of Pt20Pd20Cu60/C catalyst after 50 K, 60 K, and 70 K cycles. l, The corresponding MA and SA values extracted from k at 0.900 V (vs RHE) of Pt20Pd20Cu60/C catalyst during potential cycling from 50 K to 70K cycles.

Supplementary Fig. 5 | ORR accelerated durability test of Pt20Pd40Cu40/C, Pd50Cu50/C, and the commercial E-tek Pt/C catalysts. a, RDE curves of Pt20Pd40Cu40/C catalyst before cycling and after 10K, 20K, 30K, and 40K cycles, respectively. b, The corresponding MA and SA at 0.900 V (vs RHE) for the ORR. c, RDE curves of Pd50Cu50/C catalyst before cycling and after 1K cycles27. d, The corresponding MA values at 0.900 V (vs RHE) for the ORR. e, RDE curves of E-tek Pt/C catalyst before cycling and after 20K cycles. f, The corresponding MA values at 0.900 V (vs RHE) for the ORR. (RDE scan rate: 10 mV; ADT scan rate: 100 mV/s; potential cycle window: 0.6 and 1.0 V; Electrolyte: 0.1 M HClO4 saturated with oxygen; RDE rotating speed: 1600 rpm.)

Supplementary Fig. 6 | The Design Concept of Low-Noble-Metal-Content Alloy Catalysts (PtPdM (M= Ni, Co)) and Their Activity and Durability for ORR. a, Triangle plots of Pt, Pd, Ni, and Co atomic percentages of Pt20PdnNi80-n/C and Pt20PdnCo80-n/C catalysts determined by ICP-OES as a function of the feeding ratios in terms of the atomic percentage. The data points in the graph are for Pt16Pd16Ni68, Pt17Pd42Ni41, Pt20Pd9Co71, and Pt22Pd43Co35. b, RDE curves of Pt20Pd40Ni40/C, c, RDE curves of Pt20Pd40Co40/C catalysts before cycling and after 10K, 20K, 30K, 40K, 50K, 60K, 70K, 80K, 90K, and 100K cycles, respectively. d, MA values at 0.900 V (vs RHE) of Pt20Pd40Ni40/C and Pt20Pd40Co40/C catalysts from 50K to 100 K potential cycles during accelerated durability test. e, RDE curves of Pt20Pd20Co60/C catalyst before cycling and after 10K, 20K, 30K, 40K, and 50K cycles, respectively. f, The corresponding MA and SA at 0.900 V (vs RHE) for the ORR. g, RDE curves of Pt20Pd20Ni60/C catalyst before cycling and after 10K, and 20K cycles, respectively. h, The corresponding MA and SA at 0.900 V (vs RHE) for the ORR. (RDE scan rate: 10 mV; ADT scan rate: 100 mV/s; potential cycle window: 0.6 and 1.0 V; Electrolyte: 0.1 M HClO4 saturated with oxygen; RDE rotating speed: 1600 rpm.)

Supplementary Fig. 7 | Metal Component Distributions in the as-synthesized Pt20Pd20Cu60 NPs and the 20,000-cycled Pt20Pd20Cu60/C catalysts. a, STEM-EELS elemental mapping of Pt (in red), Pd (in blue), Cu (in green), the integrated mapping of Pt and Cu, and the integrated mapping of Pt, Pd, and Cu for the as-synthesized Pt20Pd20Cu60 NPs. b, The corresponding EELS line-scan profiles and the highlighted Pt-shell regions. c, Additional representative STEM-EELS elemental mapping of Pt (in red), Pd (in blue), Cu (in green), the integrated mapping of Pt and Cu, and the integrated mapping of Pt, Pd, and Cu for the 20,000-cycled Pt20Pd20Cu60/C catalyst. d, The corresponding EELS line-scan profiles.

Supplementary Fig. 8 | HAADF images and the corresponding analyses of Pt20Pd20Cu60 NPs in different states. a, e, i, HAADF-STEM images; b, f, j, contrast profiles measured along with the yellow arrows; c, g, k, metallic particle size distribution plots; and d, h, l, EDX spectra for a-d the as-synthesized Pt20Pd20Cu60 NPs; e-h the as-prepared Pt20Pd20Cu60/C catalyst after thermochemical treatment; and i-l the 20,000-cycled Pt20Pd20Cu60/C catalyst.

Supplementary Fig. 9 | Physical characterizations of Pt20Pd20Cu60/C catalysts before and after 20,000 potential cycles. a, XRD patterns of the as-prepared and the 20,000-cycled Pt20Pd20Cu60/C catalysts. b, A magnified view of the major features in panel a for a better visual comparison. c-e, XPS spectra and deconvoluted peaks for the as-prepared and the 20,000-cycled Pt20Pd20Cu60/C catalysts in regions of c, Pt 4f, d, Pd 3d, and e, Cu 2p. f, Plot of the compositions of the 20,000-cycled Pt20Pd20Cu60/C catalysts during Ar ion sputtering as a function of the sputtering time. We also examined Pt20PdnCu80-n/C catalysts with different compositions by XPS (see Supplementary Table 6). g, Plots of Pt, Pd and Cu atomic percentages in Pt20PdnCu80-n NPs determined by ICP-OES before (solid symbols) and after 20,000 cycles ADT test (hollow symbols). The results gave Pt58Cu42, Pt37Pd4Cu59, Pt27Pd20Cu53, Pt20Pd43Cu37, and Pt19Pd81, respectively, corresponding to the initial ICP results of Pt22Cu78, Pt23Pd4Cu73, Pt19Pd19Cu62, Pt19Pd39Cu42, and Pt20Pd80, respectively.

Supplementary Fig. 10 | Schematic illustrations of the in-situ HE-XRD/PEMFC experimental set up, PDF analysis, and RMC simulation for the catalyst structural characterization. a, Experiment setup: synchrotron X-ray HE-XRD study of catalyst in PEMFC device and HE-XRD pattern collected. b, PDF analysis. c, RMC simulation: an example showing a best-fitted 3D RMC simulation model. d, A comparison of atomic PDFs generated from HE-XRD experiments (black symbols) and RMC simulations (red lines). The best-fitted 3D modeling provides the structure information of the catalyst.

As shown in Supplementary Fig. 10a, high-energy (> 100 keV) synchrotron X-rays penetrate through the catalyst MEA in a custom-designed PEMFC device.  The signals are collected by a panel detector and are transformed to HE-XRD patterns. The data are analyzed by PDFs technique (Supplementary Fig. 10b), in which the numbers of atom pairs in the first coordination shell constitute the first (σ) strong peak in the atomic PDF pattern (blue lines), that in the second coordination shell constitute the second peak in the atomic PDF pattern, and so on. Detailed structures of the catalysts are analyzed by 3D RMC models, revealing lattice parameters, atomic coordination numbers, nanophase contents and distributions, and atomic compositions and distributions, etc. (Supplementary Fig. 10c)70. The PDFs converted from experimental HE-XRD patterns (black symbols) and 3D RMC simulations (read lines) are depicted in Supplementary Fig. 10d. The best fitting between the experimental and the simulative PDFs produces the most accurate information extracted from the best-fitted 3D RMC models. The major PDF oscillations gradually calm down at a radial distance of ~30 Å in Supplementary Fig. 10d, corresponding to the NP size which is about 6 nm in the data as shown (Supplementary Fig. 10c).

Supplementary Fig. 11 | Ex situ experimental HE-XRD data and analyzed results of PtPdCu/C catalysts before and after potential cycling. a, Experimental curves (black symbols) and phase structure model-derived atomic PDFs (red lines) for other 20,000-cycled PtPdCu/C and PtPd/C catalysts. b, Lattice constants of Pt20PdnCu80-n/C catalysts before and after 20,000 potential cycles. c, Plot of the lattice parameters of the 20,000-cycled Pt20PdnCu80-n/C (n=0, 5, 20, 40, 80) catalysts. Error bars represent s.d. based on three independent experiments in b and c. d, e, HE-XRD experimental curves (black symbols) and reverse Monte Carlo model computed atomic PDFs (red lines) for d, the as-prepared and e, the 20,000-cycled Pt20Pd20Cu60/C catalyst

Supplementary Fig. 12 | Data collected from in situ/operando HE-XRD measurements of PtPdCu/C catalyst in MEA in an PEMFC cell under operating condition. a, A magnified view of the in operando HE-XRD patterns and b, the corresponding atomic PDFs obtained by Fourier transform for Pt20Pd20Cu60/C catalyst inside an operating PEMFC upon potential cycling. c, d, Simulations of the kinetics of the lattice constants (LC) extracted from the HE-XRD patterns for Pt20Pd20Cu60/C catalyst during potential cycling based on first-order reaction model. c, LC = 3.736 + 0.029(1-exp(-kt)), and d, LC = 3.736 + 0.034(1-exp(-kt)). Apparently, Model A with k= 4x10-5 s-1 fits all data points, whereas Model B does not. e, EDX spectra during in-situ potential cycling of the Pt20Pd20Cu60/C catalyst in MEA assembled in a custom-designed fuel cell. f, Normalized ECSA, MA, and SA values from in-house RDE measurements of Pt20Pd20Cu60/C catalyst, mimicking the in-situ experimental condition. g, Normalized ECSA values obtained from in-situ fuel cell measurements of Pt20Pd20Cu60/C catalyst.

Supplementary Fig. 13 | Data collected from testing PtPdCu/C and commercial Pt/C catalyst in MEA in an PEMFC. a, H2–O2 fuel cell polarization plots with the MEAs prepared using Pt20Pd20Cu60/C and commercial Pt/C as the cathode catalysts. b, Stability test: fuel cell voltage vs. time at 1.55 A/cm2/mgPt (0.232 A/cm2) for the MEA with Pt20Pd20Cu60/C as the cathode catalyst. (Anode: commercial Pt/C).

Supplementary Fig. 14 | The theoretical modeling of enhanced stability and activity of the ternary alloy catalyst. a, Plots of the dissociation energies of Cu vs. the Cu atomic percentage in PdCu, PtCu, and PtPdCu slab models with different compositions. b, Plot of the binding energies vs the compositions for PtPdCu, PtCu, PtPd and Pd clusters. A set of 1.5 nm cluster models with 116 atoms with different compositions was built. Pure Pt cluster shows the highest binding energy (4.48 eV) while pure Pd and Cu give the lowest binding energies (3.01 and 3.00 eV). By fixing Pt at 20% in Pt-alloys while varying the compositions of Pd and Cu, maximum binding energy was achieved for Pt20Pd20Cu60 cluster. The optimized metal binding energies may be an important factor for good durability. c, Free energy diagram comparing the energetics for the different ORR species and the reaction barriers for some key elementary steps in ORR. The calculations were conducted on Pt (111), Pd (111), and PtPdCu (111) surface models at 0 V with respect to computational hydrogen electrode. Insert in c is the slab surface model of Pt20Pd20Cu60. Note: the red, blue, and green balls denote the Pt, Pd, and Cu atoms, respectively. d, Plots of the mass activity vs. the d-band centers on the catalysts’ (111) surfaces. The mass activity is apparently maximized at Pt20Pd20Cu60 with a d-band center close to -2.2 eV.  According to the d-band theory71, Pt-based alloy can negatively tune the d-band center of Pt by around 0.2-0.3 eV, e.g., -2.8 eV. In comparison with Pt-skin alloy model, our full alloy model shows a reverse positively shift of the d-band center by 0.3 eV, e.g., -2.2 eV. Alloying with Pd apparently increases the d-band center of Pt.

Additional Methods, Experimental Details and Kinetic/Thermodynamic Considerations:

Control experiments. While it is possible that Pt migration of dissolved Pt from counter electrode during the durability testing could contribute to the initial activity enhancement, as noted in recent studies72, we can rule out the possibility by the fact that PdCu catalyst showed poor durability under the same testing condition (Supplementary Fig. 4c, d).

Atomic mobility (diffusion) in nanoparticles and thermodynamics at the nanoscale. The atomic diffusion, which is referred to the atom displacement induced by thermal energy, is governed by the Arrhenius-type equation:

D∞ = D0,∞ e-Q∞RT

where D0,∞ is the pre-exponential factor, Q∞ refers to the thermal activation energy regardless of size and shape effects, R is the ideal gas constant while T is the absolute temperature. The thermal activation energy Q∞ is proportional to the melting temperature Tm,  ∞ via a constant coefficient C in the following equation:

Q∞=CTm,  ∞

At the nanoscale, the diffusion is accelerated by the dramatically enhanced surface area to volume ratios and quantum effect at the interatomic distance range. The melting temperatures of nanoparticles are highly dependent on the particle size, which decreases at the nanoscale in comparison with the bulk counterparts. Therefore, the thermal activation energy is proportionally decreased while the atomic diffusion rate is exponentially enhanced with the particle size at the nanoscale73. The nanoscale effect contributes to the greatly-decreased melting temperature, thus leading to an enhanced atomic diffusion rate in nanoparticles.

The nanoscale atomic diffusion is driven by thermal energy, kT.  Considering ΔG = ΔH – TΔS, given the negative ΔH values for many nanoscale alloys and positive ΔS value for alloying (enthalpy change and entropy change, respectively), alloying could be favored even at moderate temperatures, e.g., room temperature, from the thermodynamic viewpoint.  On the other hand, the electrochemical potential of metals depends on the degree of alloying, as determined by ΔG = − nFE, where ΔG is the Gibbs free energy, n is number of electrons transferred, F is the Faraday constant, and E is the electrochemical potential.  A more negative ΔG means a more positive E.

Reverse Monte Carlo (RMC) simulation. RMC simulation was used to refine the MD generated models. In RMC simulation, positions of atoms in the MD models were adjusted as to minimize the difference between the model-computed and experimental-obtained atomic PDFs. During the simulations, Pt and TM atoms were constrained both to maintain as maximal (i.e., as close to 12) as possible coordination numbers. The distances were determined from the positions of the first peak in the experimental atomic PDFs. Simulations were done with the help of a new version of the program RMC++74. More details of modelling the 3D structure of metallic NPs by joint MD and RMC computations can be found in our previous works70.

References

52	Park, H. Y. et al. Hollow PdCu2@Pt core@shell nanoparticles with ordered intermetallic cores as efficient and durable oxygen reduction reaction electrocatalysts. Appl. Catal. B Environ. 225, 84–90 (2018).

53	Liu, X. J. et al. Hollow ternary PtPdCu nanoparticles: a superior and durable cathodic electrocatalyst. Chem. Sci. 6, 3038–3043 (2015).

54	Fu, S. et al. Low Pt-content ternary PdCuPt nanodendrites: an efficient electrocatalyst for oxygen reduction reaction. Nanoscale 9, 1279–1284 (2017).

55	Li, H. H. et al. Mixed-PtPd-Shell PtPdCu Nanoparticle Nanotubes Templated from Copper Nanowires as Efficient and Highly Durable Electrocatalysts. Adv. Energy Mater. 2, 1182–1187 (2012).

56	Ye, W. et al. Pt4PdCu0.4 alloy nanoframes as highly efficient and robust bifunctional electrocatalysts for oxygen reduction reaction and formic acid oxidation. Nano Energy 39, 532–538 (2017).

57	Cho, Y. H. et al. PtPdCo ternary electrocatalyst for methanol tolerant oxygen reduction reaction in direct methanol fuel cell. Appl. Catal. B Environ. 154-155, 309–315 (2014).

58	Choi, S. II et al. Synthesis and Characterization of Pd@Pt-Ni Core-Shell Octahedra with High Activity toward Oxygen Reduction. ACS nano 8, 10363–10371 (2014).

59	Zhou, M. et al. Quantitative Analysis of the Reduction Kinetics Responsible for the One-Pot Synthesis of Pd−Pt Bimetallic Nanocrystals with Different Structures. J. Am. Chem. Soc. 138, 12263–12270 (2016).

60	Chang, F. et al. Strain-Modulated Platinum−Palladium Nanowires for Oxygen Reduction Reaction. Nano Lett. 20, 2416–2422 (2020).

61	Wu, R. Tsiakaras, P. & Shen, P. K. Facile synthesis of bimetallic Pt-Pd symmetry-broken concave nanocubes and their enhanced activity toward oxygen reduction reaction. Appl. Catal. B Environ. 251, 49–56 (2019).

62	Koenigsmann, C. et al. Enhanced Electrocatalytic Performance of Processed, Ultrathin, Supported Pd–Pt Core–Shell Nanowire Catalysts for the Oxygen Reduction Reaction. J. Am. Chem. Soc. 133, 9783–9795 (2011).

63	Shao, M. et al. Pt Monolayer on Porous Pd–Cu Alloys as Oxygen Reduction Electrocatalysts. J. Am. Chem. Soc. 132, 9253–9255 (2010).

64	Zhang, L. et al. Palladium–Platinum Core–Shell Electrocatalysts for Oxygen Reduction Reaction Prepared with the Assistance of Citric Acid. ACS Catal. 6, 3428–3432 (2016).

65	Lim, B. et al. Pd–Pt Bimetallic Nanodendrites with High Activity for Oxygen Reduction. Science 324, 1302–1305 (2009).

66	Zhou, M. et al. Quantitative Analysis of the Reduction Kinetics Responsible for the One-Pot Synthesis of Pd–Pt Bimetallic Nanocrystals with Different Structures. J. Am. Chem. Soc. 138, 12263–12270 (2016).

67	Zhang, L. et al. Platinum-based nanocages with subnanometer-thick walls and well-defined, controllable facets. Science 349, 412–416 (2015).

68	Wu, J. et al. Understanding Composition-Dependent Synergy of PtPd Alloy Nanoparticles in Electrocatalytic Oxygen Reduction Reaction. J. Phys. Chem. C 121, 14128–14136 (2017).

69	Wang, W. et al. Highly Active and Stable Pt-Pd Alloy Catalysts Synthesized by Room-Temperature Electron Reduction for Oxygen Reduction Reaction. Adv. Sci. 4, 1600486 (2017).

70	Petkov, V. et al. Solving the nanostructure problem: exemplified on metallic alloy nanoparticles. Nanoscale 6, 10048-10061 (2014).

71	Stamenkovic, V. et al. Changing the activity of electrocatalysts for oxygen reduction by tuning the surface electronic structure. Angew. Chem. Int. Ed. 45, 2897-2901 (2006).

72	Chen, R. et al. Use of platinum as the counter electrode to study the activity of nonprecious metal catalysts for the hydrogen evolution reaction. ACS Energy Lett. 2, 1070–1075 (2017).

73	Guisbiers, G. & Buchaillot, L. Size and shape effects on creep and diffusion at the nanoscale. Nanotechnology 19, 435701 (2008).

74	Gereben, O. & Petkov, V. Reverse Monte Carlo study of spherical sample under non-periodic boundary conditions: the structure of Ru nanoparticles based on x-ray diffraction data. J. Phys. Condens. Matter 25, 454211 (2013).