Table 1. Thermal, optical and electrochemical properties of FPTC and CPTC.

| Acceptors | Td (oC) | λmaxsol. (nm) | ε sol. (M-1 cm-1) | λmaxfilm (nm) | Egopt (eV) | HOMO (eV) | LUMO (eV) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| FPTC | 212 | 498 | 6.64 × 104 | 515 | 2.09 | -5.75 | -4.05 |
| CPTC | 173 | 486 | 1.75 × 104 | 513 | 1.92 | -5.70 | -4.13 |

Table 3. Calculated properties of the target compounds in their ground state calculated by DFT methods atB3LYP/6-31G(d,p) level of theory.

| Torsion angle | Θ1 | Θ2 | Θ3 | Θ4 | HUMO | LUMO | Egap |
| --- | --- | --- | --- | --- | --- | --- | --- |
| FPTC | 91.2398 | 15.7572 | -15.2146 | 90.5868 | 4.434eV | 4.365eV | 0.762eV |
| CPTC | 91.4518 | 18.9607 | -18.1638 | 92.1319 | 3.672eV | 3.653eV | 0.712eV |

Table 3. Photovoltaic performances of the SM-OSCs based on PTB7-Th: FPTC and PTB7-Th: CPTC under the optimized device conditions.

| Blending layers | Voc (V) | Jsc (mA cm-2) | FF | PCE a (%) | μh (cm2 V-1 s-1) | μe (cm2 V-1 s-1) |
| --- | --- | --- | --- | --- | --- | --- |
| PTB7-Th: FPTC | 0.71 | 3.42 | 36.19 | 1.09 (0.87) | 1.69 × 10-4 | 2.28 × 10-6 |
| PTB7-Th: CPTC | 0.49 | 0.42 | 23.98 | 0.12 (0.05) | 0.54 × 10-4 | 0.62× 10-6 |
| a The average PCE values in brackets from 10 devices. |  |  |  |  |  |  |