Supplementary Materials for

Surface Functionalization of Nanoparticles for Enhanced Polymer-Nanoparticle Interactions in Nanocomposites

Mohamad Ali Sanjari Shahrezaei1, Fatemeh Goharpey1,*, Atefeh Alimadadi1

1 Department of Polymer Engineering and Color Technology, Amirkabir University of Technology, Tehran, Iran,

*Correspondence: goharpey@aut.ac.ir

This file includes:

Supplementary Text section1 (S1)

Figure S1

Table S1 to S4

Supplementary Text

S1. Derivation of Yziquel & coworker’s model

Yziquel & coworker proposed kinetic network model based on Marrucci et al [1] and Coussot et al [2] to describe the nonlinear behavior of concentrated suspensions composed of interactive particles. They assume that the flow properties are controlled by the simultaneous breakdown and the build-up of the suspension microstructure [3]. The stress was described by a modified upper convected Jeffrey’s model with a single relaxation time:

δδtσGξ+σηξ=1+η∞ηξγ.+η∞δδt(γ.Gξ)						(4)

With

Gξ= G0ξ+G∞									(5)

Where η∞ and G ∞ is the viscosity and the elastic modulus respectively for the destroyed structure and the solvent, and G0+G∞ is the equilibrium value of the elastic modulus of the structure [34]. ηξ is the structured viscosity defined by the following relation

ηξ=η0f(ξ)										(6)

Where η0 is a characteristic viscosity and f(ξ) is an empirical structural function. The evolution of the structural parameter, ξ, is described following three possible kinetic equations which depend on flow parameters. The first one assumes that structure changes are due to the rate of strain; the second one supposes that this evolution is associated with the stored elastic energy as in polymer systems; the third is related to the rate of energy dissipated.

The kinetic equation which assumes that the breakdown of the structure is controlled by the rate-of-strain given by the following equation:

λ0k1∂ξ∂t=1-ξ-k2k1ξλ0γ2								(7)

Where k1 and k2 are kinetic constants for the build-up of the suspension microstructure and for the shear induced breakdown respectively and λ0 is a characteristic relaxation time related to theparticle interactions. The characteristic relaxation time is assumed to be constant and is given by:

λ0=η0G0+G∞										(8)

A characteristic relaxation time is a function of the structural parameter. The relaxation time would become infinite when the suspension is completely structured (ξ= 1).The structural function is given by

fξ=1ξ-11-n2									(9)

The stored elastic energy is assumed to be proportional to the first invariant of the stress tensor which proposed by second kinetic equation:

λ0k1∂ξ∂t=1-ξ-k2k1ξσ112Gξ								(10)

As for the first kinetic equation, the characteristic time is assumed constant. The structural function is related to the structural parameter by:

fξ=1ξ-1k1k2G0G0+G∞ξ-1+11n-1					(11)

Another kinetic equation on the assumption that the breakdown of the suspension micro-structure is related to the double dot product of the stress and the rate-of-deformation tensors,

That is, the rate of energy dissipated by the flow process. The dissipation of energy is directly related to the micro mixing mechanism. The proposed kinetic equation is then:

λ0k1∂ξ∂t=1-ξ-λ02η0k2k1ξσ12γ							(12)

The structure breakdown is directly proportional to the dissipated power. The structural function is then given by the following relation:

fξ=1ξ-11-n1+n									(13)

Figure S1 . a) Loss tangent versus frequency. The neat polymer has no maximum in the frequency measurements range and it appears at very low frequency. The intensity of tan(δ) decrease and the maximum tan(δ) increase in sample R974, R805, R816 and A200 respectively. b) van Gurp–Palmen plots for samples containing 5 vol% of different nanoparticle. Cole-Cole plot, η" versus η', of the neat polystyrene and samples containing c)1 and d) 5 vol% NPs.

Table S1: Initial and final point and widths of glass transition temperature obtained by  DSC for neat Polystyrene and nanocomposites contain A200, R816, R805, R974 nanoparticle. The onset and end of glass transition increase respectively. These data is extracted from figure 3.

| Sample | PS/A200 | PS/R816 | PS/R805 | PS/R974 | Polystyrene |
| --- | --- | --- | --- | --- | --- |
| Tgi (˚C) | 84 | 81 | 78 | 75 | 75 |
| Tgf (˚C) | 119 | 117 | 111 | 106 | 105 |
| Transition width (˚C) | 35 | 36 | 33 | 31 | 30 |

Table S2: The [η] and Φm Obtained from Krieger-Dougherty Equation for nanocomposites contain A200, R816, R805, R974 nanoparticle.

| Sample | [η] | Φm |
| --- | --- | --- |
| A200 | 80 | 0.121 |
| R816 | 73 | 0.157 |
| R805 | 54 | 0.188 |
| R974 | 38 | 0.21 |

Table S3: Maximum loss tangent for PNCs containing 5 vol%  A200, R816, R805, R974 NPs.

| Sample | ωMax(tanδ)(1/sec) |
| --- | --- |
| A200 | 2.7 |
| R816 | 2.03 |
| R805 | 0.26 |
| R974 | 0.1 |

Table S4: k1 and k2 obtained parameters of different samples.

| Sample | k1 | k2 | n | k2/ k1 |
| --- | --- | --- | --- | --- |
| A200 | 0.02 | 0.012 | 0.3 | 0.6 |
| R816 | 0.015 | 0.01 | 0.5 | 0.66 |
| R805 | 0.012 | 0.009 | 0.55 | 0.75 |
| R974 | 0.01 | 0.008 | 0.6 | 0.8 |

1.           Acierno, D., et al., A non-linear viscoelastic model with structure-dependent relaxation times: I. Basic formulation. Journal of Non-Newtonian Fluid Mechanics, 1976. 1(2): p. 125-146.

2.	Coussot, P., A. Leonov, and J. Piau, Rheology of concentrated dispersed systems in a low molecular weight matrix. Journal of Non-Newtonian Fluid Mechanics, 1993. 46(2-3): p. 179-217.

3.	Leonov, A.I., On the rheology of filled polymers. Journal of rheology, 1990. 34(7): p. 1039-1068.