Precise modulation of electron spin states in metal-organic framework towards exceptional oxygen evolution reaction

Xianbiao Hou a, Tengjia Ni a, Zhaozheng Zhang a, Jian Zhou a, Shucong Zhang a, Shuixing Dai a, Lei Chu a, Huanlei Wang a, Bolong Huang b, *, Minghua Huang a, *

a School of Materials Science and Engineering, Ocean University of China, Qingdao 266100, China

b Department of Applied Biology and Chemical Technology, The Hong Kong Polytechnic University, Hung Hom, Kowloon, Hong Kong SAR, China

Corresponding author. E-mail: bhuang@polyu.edu.hk, huangminghua@ouc.edu.cn

Figure S1. HAADF-STEM and corresponding elemental mapping images of NiFe-MOF-D3

Figure S2. The XPS survey spectra of NiFe-MOF-D0 and NiFe-MOF-D3.

Figure S3. The XPS valence bands of these obtained catalysts.

Figure S4. The k3-weighted EXAFS fitting curves of Fe at R space. (a) NiFe-MOF-D0 and (b) NiFe-MOF-D3.

Figure S5. The k3-weighted EXAFS fitting curves of Ni at R space. (a) NiFe-MOF-D0 and (b) NiFe-MOF-D3.

Figure S6. The k3-weighted EXAFS fitting curves at k space. (a) Fe, (b) Ni.

Figure S7. Wavelet transform of Fe K-edge EXAFS spectra. (a) FeO, (b) Fe2O3, and (c) Fe foil.

Figure S8. Wavelet transform of Ni K-edge EXAFS spectra. (a) NiFe-MOF-D3, (b) NiFe-MOF-D0, (c) NiO, and (d) Ni foil.

Figure S9. The transitions of Fe 3d electron configuration in different spin states on the catalysts.

Figure S10. The NiO6-FeO4 model structure within NiFe-MOF, (a) side view, (b) top view.

Figure S11. The NiO6-FeO5 model structure within NiFe-MOF, (a) side view, (b) top view.

Figure S12. The NiO6-FeO6 model structure within NiFe-MOF, (a) side view, (b) top view.

Figure S13. The COHP analysis of (a, d) NiO6-FeO6, (b, e) NiO6-FeO5, and (c, f) NiO6-FeO4 models after the adsorption of OH* and OOH*.

Figure S14. The OER pathway for the NiO6-FeO6 model of NiFe-MOF at (a) Fe sites, and (b) Ni Sites.

Figure S15. The free energy diagrams at different metal sites within NiO6-FeO6 model of NiFe-MOF during the OER process: (a) U = 0V, (b) U=1.23 V.

Figure S16. The cyclic voltammetry curves of (a) NiFe-MOF-D0, (b) NiFe-MOF-D1, (c) NiFe-MOF-D2, and (d) NiFe-MOF-D3 with different scan rates from 20 to 120 mVs-1.

Figure S17. The LSV curves normalized by ECSA for these obtained catalysts.

Figure S18. Cyclic voltammetry curves of these obtained catalysts in PBS solution at a scan rate of 50 mV s-1.

Figure S19. Polarization curves of (a)NiFe-MOF-D0, (b) NiFe-MOF-D1, (c) NiFe-MOF-D2, and (d) NiFe-MOF-D3 in 1.0 M KOH solution with or without adding 1.0 M CH3OH.

Figure S20. (a) Nyquist plots and (b) Bode phase plots for NiFe-MOF-D0. (c) Nyquist plots for NiFe-MOF-D3. The voltage range tested is from 1.25 V to 1.50V.

Figure S21. The corresponded Rct values at different potentials for NiFe-MOF-D0 and NiFe-MOF-D3.

Figure S22. Polarization curves of (a)NiFe-MOF-D0, (b) NiFe-MOF-D3 in 1.0 M KOH dissolved in H2O and D2O.

Table S1. EXAFS fitting parameters at the Ni K-edge for the Ni foil, NiO, NiFe-MOF-D0, and NiFe-MOF-D3.

| Sample | Shell | CNa | R(Å)b | σ2(Å2)c | ΔE0(eV)d | R factor |
| --- | --- | --- | --- | --- | --- | --- |
| Ni foil | Ni-Ni | 12.0* | 2.48 | 0.0061 | 7.33 | 0.0018 |
| NiO | Ni-O | 6.0* | 2.09 | 0.0067 | -1.13 | 0.0043 |
|  | Ni-Ni | 12* | 2.95 | 0.0064 | -3.46 |  |
| NiFe-MOF-D0 | Ni- O | 6.3 | 2.04 | 0.0041 | -1.44 | 0.0094 |
| NiFe-MOF-D3 | Ni- O | 6.1 | 2.03 | 0.0077 | -3.86 | 0.0087 |

Table S2. EXAFS fitting parameters at the Fe K-edge for the Fe foil, Fe2O3, FeO, NiFe-MOF-D0, and NiFe-MOF-D3.

| Sample | Shell | CNa | R(Å)b | σ2(Å2)c | ΔE0(eV)d | R factor |
| --- | --- | --- | --- | --- | --- | --- |
| Fe foil | Fe- Fe | 8* | 2.46 | 0.0048 | 4.09 | 0.0037 |
|  | Fe- Fe | 6* | 2.86 | 0.0038 | 5.33 |  |
| Fe2O3 | Fe-O1 | 6.7 | 1.96 | 0.0081 | -5.78 | 0.0066 |
|  | Fe-O2 | 1.5 | 2.14 | 0.0029 | -5.34 |  |
|  | Fe-Fe1 | 7.9 | 2.98 | 0.0077 | -0.33 |  |
|  | Fe-Fe2 | 4.0 | 3.45 | 0.0037 | 14.71 |  |
| FeO | Fe-O1 | 3.8 | 2.17 | 0.0025 | 12.82 | 0.0049 |
|  | Fe-O2 | 5.8 | 2.36 | 0.0108 | 1.10 |  |
|  | Fe-Fe1 | 6.0 | 3.03 | 0.0108 | -1.57 |  |
| NiFe-MOF-D0 | Fe-O | 5.8 | 2.01 | 0.0096 | 0.24 | 0.0055 |
| NiFe-MOF-D3 | Fe-O | 4.4 | 1.99 | 0.0101 | -0.53 | 0.0040 |

Table S3. Comparisons of overpotential and Tafel slope for the as-synthesized NiFe-MOF-D3 in this work and related electrocatalysts in the literatures.

| Catalysts | j (A cm-2) |  | η (mV) | Stability | Reference |
| --- | --- | --- | --- | --- | --- |
| NiFe-MOF-D3 |  | 0.5 1.0 | 285 328 | 170 h @500 mA cm-2 | This work |
|  |  | 1.5 | 365 |  |  |
| NiMOF-Ni2P/IF |  | 1.0 | 330 | 100 h @500 mA cm-2 | Chem. Eng. J. 2024, 497, 154483 |
| Ru@Cr-FeMOF |  | 1.0 | 348 | 80000 s @20 mA cm-2 | Adv. Funct. Mater. 2024, 34, 2307917 |
| Fe-MOFs-SO3 |  | 1.0 | 330 | 100 h @1000 mA cm-2 | Adv. Energy Mater. 2020, 10, 2000184 |
| Er0.4Fe-MOF/NF |  | 1.0 | 326 | 25 h @500 mA cm-2 | Nanomaterials. 2021, 11, 1847 |
| NiCo(OH)x@Co-MOF/NF |  | 1.0 | 531 | 24 h @500 mA cm-2 | Int J Hydrogen Energy. 2022, 47, 31587-31595 |
| NiFe-MOF-74/NiFe-LDH |  | 1.0 | 284 | 10 h @1000 mA cm-2 | Adv. Funct. Mater. 2023, 33, 2211260 |
| CoFeP TPAs/Ni |  | 0.7 | 335 | 100 h @20 mA cm-2 | J. Mater. Chem. A. 2019, 7, 17529-17535 |
| NFN-MOF/NF |  | 0.5 | 360 | 30 h @500 mA cm-2 | Adv. Energy Mater. 2018, 8, 1801065 |
| FeOOH-NiBDC-NF |  | 0.5 | 316 | 100 h @500 mA cm-2 | Chem. Eng. J. 2022, 431, 134040 |
| Fe-doped-(Ni-MOFs)/FeOOH |  | 0.4 | 314 | 120 h @10 mA cm-2 | Angew. Chem. Int. Ed. 2022, 61, e202116934 |
| CoCe-MOF/CP |  | 0.2 | 539 | 70 h @100 mA cm-2 | Small 2024, 20, 2307685 |
| Er0.5Ni-BDC MOF |  | 0.1 | 420 | 14 h @20 mA cm-2 | Energy & Fuels, 2024, 38, 5397-5406. |

Table S4. Comparisons of cell voltages of AEMWE for the NiFe-MOF-D3 // Pt/C in this work and related electrocatalysts in the literatures.

| Catalysts | j (mA cm-2) | potential (V) | Reference |
| --- | --- | --- | --- |
| NiFe-MOF-D3 | 500 | 1.77 | This work |
| Ni-Co-Fe-P NBs | 800 | 1.98 | Appl. Catal. B Environ. 2022, 310, 121353 |
| CeO2-NiCoPx/NCF | 300 | 1.78 | Appl. Catal. B Environ. 2022, 316, 121678 |
| F-CDs/CoP/NF | 240 | 1.81 | Adv. Energy Mater. 2022, 12, 2102573 |
| FeOx@Co0.75Fe0.25P | 100 | 1.67 | Adv. Sci. 2024, 11, 2403206 |
| Pd-NiFeB/NF | 500 | 1.81 | Appl. Catal. B Environ. 2024, 342, 123343 |
| NiCo₂O₄-B-CC | 400 | 2.0 | Adv. Funct. Mater. 2024, 2410439 |
| NiCoP | 500 | 1.815 | Adv. Energy Mater. 2023, 13, 2300499 |
| Ru SAs-MoO3−x/NF | 100 | 1.759 | Adv. Sci. 2023, 10, 2300342 |
| NiSAFeSA-NixFe/CNT | 382 | 1.8 | ACS Catal. 2022, 12, 1167-1179 |
| 6%LS-CMMOFs | 500 | 1.85 | Appl. Catal. B Environ. 2022, 307, 121151 |
| Sn4P3/Co2P SCNAs | 80 | 1.72 | Appl. Catal. B Environ. 2022, 304, 120923 |

Calculations of AEM electrolyzer efficiency and H2 cost

H2 production rate @ 0.5 A cm-2

= (j A cm-2)(1 e-/1.602 ×10-19 C)(1 H2/2 e-)

= 0.5 A cm-2 / (1.602 × 10-19 C x 2)

= 2.59 × 10-6 mol H2 cm-2 s-1

LHV of H2

= 120 kJ g-1 H2 = 2.42 × 105 J mol-1 H2

H2 power out

= (2.59 × 10-6 mol cm-2 s-1) × (2.42 × 105 J mol-1)

= 0.627 W cm-2

Electrolyzer Power of NiFe-MOF-D3 // Pt/C @ 0.5 A cm-2

= (0.5 A cm-2) (1.61 V)

= 0.885 W cm-2

Efficiency of NiFe-MOF-D3 // Pt/C

= (H2 Power Out) / (Electrolyzer Power)

= 0.627 W cm-2/0.885 W cm-2

= 70.8 %

Efficiency of RuO2//Pt/C

= (H2 Power Out) / (Electrolyzer Power)

= 0.627 W cm-2/1.097 W cm-2

= 57.15%

Price per gasoline-gallon equivalent (GGE) H2

= 1GGE H2 / H2 production rate × Electrolyzer power × Electricity bill

= 0.997 kg / (2.59 × 10-6 mol H2.cm-2 s-1 × 2 kg/mol) × 0.885 W cm-2 × $ 0.02 / kW h

= $ 0.94 /GGE H2

<< $ 2 /GGE H2 of U.S. Department of Energy (DOE) by 2026