## Additional file 7: Preparation of the colloidal gold labeled McAbs

Colloidal gold particles with a mean particle diameter of 25.0 nm were produced under the following procedures. One hundred ml 0.01% (w/v) chloroauric acid (HAuCl4) (Aladdin, Shanghai, China) was boiled thoroughly for 3 min. Then 2.0 ml 1.0 % (w/v) sodium citrate (Aladdin, Shanghai, China) was added quickly into the solution on a magnetic stirring apparatus over 30 min. The color changed gradually from yellow to black–blue and finally brilliant red. After stirring for a few minutes at low speed, the colloidal gold suspension was rested to cool down and stored in the dark case at room temperature. Total volume was made up to the original volume (100.0 ml) by adding ultrapure water. To measure the size and size distribution of these gold nanoparticles, the colloidal gold solution was scanned under a transmission electron microscopy (Tecnai G2 spirit Biotwin, USA) at 120 KV. The OD value of the colloidal gold solution was measured at 400-680 nm using an ultraviolet spectrophotometer (Tecan Sunrise, Switzerland).

The optimal pH, dose and concentration of BSA for conjugation of gold colloids and H9E monoclonal antibodies were evaluated (Fig. S5 and Table S5). Briefly, 200.0 μl of H9E was incubated with 0.5 ml of colloidal gold (pH 9.0) for 30 min at room temperature with stirring gently. Then, 50.0 µl bovine serum albumin (BSA, Amresco, United States) of different final concentration were dripped into the colloidal gold as the blocking buffer to stabilize the gold-labeled antibody. After incubated for 15 min, the colloidal gold-antibody complex was collected in pellet and unmarked antibodies were remained in supernatant by a centrifugation at 8000 ×g at 4 °C for 20 min. Centrifugal process should be avoided the presence of black massive deposits on the wall of the tube. Then, the conjugated colloidal gold-antibody was finally resuspended to 50.0 μl dissolution buffer pH 9.0 PBS containing 10.0 % w/v sucrose (Sangon Biotech, Shanghai, China), 0.2 % (w/v) PVA-205 (Aladdin, Shanghai, China), 0.2 % (v/v) Tween-20 (Aladdin, Shanghai, China) and BSA (3.0 %, 2.5 %, 2.0 %, 1.5 %, 1.0 % and 0.5 %, w/v) respectively. The conjugation was confirmed by UV-vis spectroscopy using the same method as unlabeled gold particles. Ultimately, 50.0 μl of colloidal gold-antibody mixture was dispensed evenly on the 0.5 cm×2.5 cm conjugated pad and was dried for 3 h at room temperature.

# (A)

# (B)

# Additional file 7: Fig. S5 Selection of optimal conditions for gold labeled antibody complex. (A) Evaluation of the optimal pH. Five hundred μl of colloidal gold solution was added to eight sterile EP tubes, respectively. The pH values were modified to 6.5 to 9.5 by adding 0.2 M potassium carbonate (K2CO3) or 0.1 M hydrochloric acid (HCl). Two hundred µl of H9E (50.0 μg/ml) was added into each tube with gentle stirring for 30 min, and then 50.0 µl NaCl (10.0 % w/v) was added to the above tubes. The mixture was permitted to stand for 2 h at room temperature. The OD520 and OD580 values were measured in accordance with an ultraviolet spectrophotometer (Eppendorf Bio Spectrometer, Germany). The optimal pH and labeled antibody concentration conditions can be determined by measuring A520-A580, the differential absorbance. (B) Dose for conjugation of 1.0 ml gold colloids and H9E monoclonal antibodies (μg). Various amounts of H9E antibodies were mixed with 500.0 µl of colloid gold at pH 9.0 and 1.0 % BSA.

# Additional file 7: Table S5. Optimal BSA concentration for blocking

| BSA final concentration (%) | 3.0 | 2.5 | 2.0 | 1.5 | 1.0 | 0.5 |
| --- | --- | --- | --- | --- | --- | --- |
| Colloidal gold state | - | - | - | + | + | + |
| Background color effect | ND | ND | ND | * | ** | *** |
| ’-: coagulation +: normality ND: not detected * :color level |  |  |  |  |  |  |

Additional file 7: Table S6. Selection of conjugate pad and dilution multiple of gold labeled antibody

| Fiber | 1:1 | 1:2 | 1:4 | 1:8 |
| --- | --- | --- | --- | --- |
| Glass fiber (Ahlstrom 8964, Whatman USA) | * | ** | *** | *** |
| Polyester fiber (fusion 3, Whatman, USA) | * | * | ** | ** |

* Release effect

Note: Two conjugate pads were selected for comparison: the glass fiber Ahlstrom 8964 (Whatman, USA) and the polyester material fusion 3 (Whatman, USA). In addition, colloidal gold-antibody mixture was diluted with dissolution buffer in gradient of 1:1, 1:2, 1:4 and 1:8 to find the best spraying amount. S protein (0.3 μg/ml) was used to test the most suitable amount of spray. Glass fiber was finally selected for conjugate pad with a spraying amount of 1:4.

## Additional file 7: Table S7. (A) Selection of the Nitrocellulose Membrane. (B) Optimization of the capture antibody and control antibody concentration. (C) Optimal concentration of sucrose (w/v) for the immobilized antibody on NC membrane.

(A) Selection of the Nitrocellulose Membrane

|  | Flow time (s) | Fixation effect | Background color |
| --- | --- | --- | --- |
| CN 140 (Sartorius, Germany) | 212±2 | ** | * |
| CN 95 (Sartorius, Germany) | 143±4 | * | * |
| M 135 (Millipore, USA) | 203±3 | * | * |
| M 180 (Millipore, USA) | 256±2 | ** | ** |

Note: Quantity of * denoted the color intensity

(B) Optimization of the capture antibody and control antibody concentration

| Control line Ig G(mg/ml) Test line J5D (mg/ml) | 1.0 | 1.2 | 1.4 | 1.6 | 1.8 | 2.0 |
| --- | --- | --- | --- | --- | --- | --- |
| 0.5 | *＊ | *＊ | *＊ | *＊＊ | *＊＊ | *＊＊ |
| 1.0 | *＊ | *＊ | *＊ | *＊ | *＊＊ | *＊＊ |
| 1.5 | **＊ | **＊ | **＊＊ | **＊＊ | **＊＊＊ | **＊＊＊ |
| 2.0 | ***＊ | ***＊＊ | ***＊＊ | ***＊＊＊ | ***＊＊＊ | ***＊＊＊ |
| 2.5 | ***＊ | ***＊ | ***＊ | ***＊＊ | ***＊＊ | ***＊＊ |
| 3.0 | *** | *** | ***＊ | **＊ | ***＊ | ***＊＊ |
| *Test line ＊Control line Quantity of *and＊denoted the color intensity. |  |  |  |  |  |  |

# (C) Optimal concentration of sucrose (w/v) for the immobilized antibody on NC membrane.

| Sucrose Concentration (%) | 0.0 | 1.0 | 2.0 | 3.0 | 4.0 | 5.0 | 6.0 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Immobilized Antibody | * | * | ** | *** | ** | ** | ** |

Note: Quantity of * denoted the color intensity

# Four NC membranes were selected as candidates (Table S7): CN 140 (Sartorius, Germany), CN 95 (Sartorius, Germany), M 135 (Millipore, USA), M 180 (Millipore, USA). CN 140 was finally selected with the merits of slower flow rate, higher sensitivity and less background color (Table S7 A). Optimal concentration of capture antibody used in the Test line (J5E) and the Control line (goat-anti-mouse Ig G (Beyotime Biotech, Shanghai, China) were tested with a range of 0.5 to 3.0 mg/ml and 1.0 to 2.0 mg/ml, respectively (Table S7 B). Finally, 2.0 mg/ml J5E and 1.6 mg/ml goat-anti-mouse Ig G was selected to draw T and C lines by using the XYZ3010 instrument (Jiening Biotechnology, Shanghai). The distance between the two lines was 5 mm. To get better fixation and protection effect, 0, 1.0 %, 2.0 %, 3.0 %, 4.0 %, 5.0 % and 6.0 % (w/v) of sucrose were evaluated in the diluted McAb and Ig G for immobilized antibodies on NC membrane. The results indicated that 3.0 % sucrose was the best (Table S7 C).

# Additional file 7: Preparation of the sample pad and others and assembling of the ICA

The sample pad, absorbent pad and PVC board were provided by Jieyi Biotechnology Co., Ltd. (Shanghai, China).The sample pad was saturated with PBS solution (pH 9.0) containing 1.0% (w/v) BSA, 0.5% (w/v) PVA-205 and 0.5% (v/v) Tween-20 and dried before use. H5072 cellulose was used as the absorbent pad without treatment. The PVC board served as the bottom plate of the test strip.

The pre-treated conjugate pad, NC membrane, sample pad, and absorbent pad were assembled and immobilized on the PVC board as described in Fig. 3, overlapping 5 mm between each membrane. Then these strips were cut into 4 mm wide and stored in sealing bag with desiccant. The control line should always show a visible red line. The appearance of both two lines indicated a positive result.