Supplementary information

Novel fusion peptide-mediated siRNA delivery using self-assembled nanocomplex

Yeong Chae Ryu1, Kyungah Kim1, Byoung Choul Kim1,2, Hui-Min David Wang3, Byeong Hee Hwang1,2,*

1 Department of Bioengineering and Nano-bioengineering, Incheon National University, Incheon, 22012, Korea

2 Division of Bioengineering, Incheon National University, Incheon, 22012, Korea

3 Graduate Institute of Biomedical Engineering, National Chung Hsing University, Taichung 402, Taiwan

_____

* Corresponding author.

Address: Academy-ro 119, Yeonsu-gu, Incheon, South Korea, 22012

Phone: +82-32-835-8834

Fax: +82-32-835-2699

E-mail address: bhwang@inu.ac.kr

Table S1. List of peptides used in this study

| Name | Sequence | Origin | Reference |
| --- | --- | --- | --- |
| Skin permeating and cell entering (SPACE) | ACTGSTQHQCG | Artificial | [1] |
| Oligo-arginine (R11) | RRRRRRRRRRR | Artificial | [2] |
| TAT | RKKRRQRRR | HIV-1 | [3] |
| SPACE-R7 (S-R7) | ACTGSTQHQCGGCGRRRRRRR | Artificial | In this study |
| SPACE-R11 (S-R11) | ACTGSTQHQCGGCGRRRRRRRRRRR | Artificial | In this study |
| SPACE-R15 (S-R15) | ACTGSTQHQCGGCGRRRRRRRRRRRRRRR | Artificial | In this study |
| * The underlined sequence indicated a linker between two sequences. |  |  |  |

Table S2. Average size, polydispersity index (PdI), and zeta potential of complexes with siRNA and each peptide. The data represented mean ± standard deviation (n=3).

| Complex with siRNA | Size | PdI | Zeta potential |
| --- | --- | --- | --- |
| SPACE | 647.7 ± 295.18 | 0.889 ± 0.192 | -28.33 ± 1.079 |
| R11 | 413.73 ± 50.28 | 0.228 ± 0.009 | -11.77 ± 0.451 |
| S-R7 | 327.1 ± 42.63 | 0.217 ± 0.013 | 5.23 ± 2.796 |
| S-R11 | 456.97 ± 56.79 | 0.235 ± 0.013 | 6 ± 0.684 |
| S-R15 | 286.97 ± 11.42 | 0.04 ± 0.006 | 6.08 ± 1.618 |

Table S3. Primer sequences used in real-time PCR

| Gene | Sequence |
| --- | --- |
| GAPDH | Forward : 5’-GTCTCCTCTGACTTCAACAGCG-3’ Reverse : 5’-ACCACCCTGTTGCTGTAGCCAA-3’ |
| β-actin | Forward : 5’-CACCATTGGCAATGAGCGGTTC-3’ Reverse : 5’-AGGTCTTTGCGGATGTCCACGT-3’ |

Table S4. Absorbance measurement of released LDH. The data represented mean ± standard deviation (n=3).

| Concentration (mg/mL) | S-R7 | S-R11 | S-R15 |
| --- | --- | --- | --- |
| 0 | 1.000 ± 0.195 | 1.000 ± 0.195 | 1.000 ± 0.195 |
| 0.0125 | 1.020 ± 0.186 | 1.179 ± 0.145 | 0.836 ± 0.159 |
| 0.025 | 0.921 ± 0.122 | 1.157 ± 0.300 | 1.086 ± 0.243 |
| 0.05 | 1.185 ± 0.238 | 1.037 ± 0.089 | 0.879 ± 0.352 |
| 0.1 | 1.270 ± 0.243 | 1.007 ± 0.102 | 1.044 ± 0.273 |
| 0.2 | 1.071 ± 0.235 | 0.983 ± 0.216 | 1.167 ± 0.059 |

Table S5. Relative in vivo fluorescence values by normalized mean of intensity. The data represented mean ± standard deviation (n=4). The outliers were removed by Grubbs’ test.

| Group | 0 h | 1 h | 2 h | 3 h | 4 h |
| --- | --- | --- | --- | --- | --- |
| Free siRNA | 1 | 0.568 ± 0.047 | 0.459 ± 0.124 | 0.457 ± 0.166 | 0.421 ± 0.189 |
| S-R11 complex | 1 | 1.011 ± 0.196 | 0.938 ± 0.221 | 0.977 ± 0.228 | 0.972 ± 0.198 |

Table S6. Relative in vivo fluorescence values by normalized integrated density. The data represented mean ± standard deviation (n=4). The outliers were removed by Grubbs’ test.

| Group | 0 h | 1 h | 2 h | 3 h | 4 h |
| --- | --- | --- | --- | --- | --- |
| Free siRNA | 1 | 0.451 ± 0.147 | 0.148 ± 0.073 | 0.137 ± 0.123 | 0.089 ± 0.118 |
| S-R11 complex | 1 | 0.756 ± 0.05 | 0.482 ± 0.328 | 0.562 ± 0.175 | 0.544 ± 0.311 |

Figure S1. Cellular uptake evaluation of siRNA/peptide nanocomplexes into HeLa and HaCaT cells using a flow cytometry. Cy3-labeled IL10-siRNAs of final 200 nM concentration were delivered into each 3.0×105 cells in a 6-well plate via PC: LipofectamineTM 2000 as a commercialized positive control, SPACE, R11, S-R7, S-R11, and S-R15 (20:1 N/P ratio) for 4 hours. Fluorescent cells of free siRNA and each condition exhibited in red and green populations, respectively. The population of fluorescent-positive cells was expressed as a percentage.

References

[1] T. Hsu, S. Mitragotri, Delivery of siRNA and other macromolecules into skin and cells using a peptide enhancer, P Natl Acad Sci USA, 108 (2011) 15816-15821.

[2] D.J. Mitchell, D.T. Kim, L. Steinman, C.G. Fathman, J.B. Rothbard, Polyarginine enters cells more efficiently than other polycationic homopolymers, J Pept Res, 56 (2000) 318-325.

[3] E. Vives, P. Brodin, B. Lebleu, A truncated HIV-1 Tat protein basic domain rapidly translocates through the plasma membrane and accumulates in the cell nucleus, J Biol Chem, 272 (1997) 16010-16017.