Supplementary Information

Computational Investigation on the Mechanism of Electrocatalytic Water Oxidation by Copper(II) Porphyrin

Shanti Gopal Patra,a,* Aritra Saha,a Pratim Kumar Chattarajb,*

aDepartment of Chemistry, National Institute of Technology Silchar, Silchar, 788010, India

bDepartment of Chemistry, Birla Institute of Technology, Mesra, Ranchi, Jharkhand 835215, India

Table S1. Chemical formula, charge, spin multiplicity, bond length (Å), and bond angles (o) around the metal centers as obtained at the PBE0/H,C,N,O(6-31+G(d,p)); Cu (LanL2DZ) level of theory.

| Species | Charge, Spin Multiplicity | Electronic energy (au) | ΔE (kcal/mol)a | Bond length (Å) | Bond angle (o) |
| --- | --- | --- | --- | --- | --- |
| [LCuII-OH2] (1) | 0, 2 | -1259.775521 |  | Cu-N; 2.027, 2.027, 2.027, 2.027; O-H, 0.965; Cu-O, 2.573 | ∠NCuN, 90.1, 89.9, 89.9, 179.8, 179.9 90.1; ∠HOH, 103.8 |
| [LCuIII-OH2]+ (2) | 1, 3 | -1259.532179 | 17.5 | Cu-N; 2.034, 2.034, 2.034, 2.034, O-H, 0.962; Cu-O, 2.393 | ∠NCuN, 89.7, 89.9 89.7, 89.9, 173.9, 173.9; ∠HOH, 106.5 |
|  | 1, 1 | -1259.504226 |  | Cu-N; 2.028, 2.012, 2.028, 2.012, O-H, 0.962; Cu-O, 2.425 | ∠NCuN, 90.4, 90.4 90.5, 90.4, 170.1, 170.3; ∠HOH, 104.4 |
| [LCuIII-OH] (3) | 0, 3 | -1259.087456 | 23.0 | Cu-N, 2.024, 2.031, 2.032, 2.032; Cu-O, 2.147; O-H, 0.969 | ∠NCuN, 89.6, 89.6, 89.8, 89.8, 170.8, 172.6 |
|  | 0, 1 | -1259.050819 |  | Cu-N, 2.001, 2.001, 2.318, 2.027; Cu-O, 1.866; O-H, 0.964 | ∠NCuN, 90.6, 90.6, 84.2, 84.2, 156.74, 153.1 |
| [LCuIV-OH]+ (4) | 1, 4 | -1258.836413 | -0.4 | Cu-N, 2.028, 2.041, 2.025, 2.020; Cu-O, 2.322; O-H, 0.974 | ∠NCuN, 90.1, 90.1, 89.4, 89.8, 175.5, 174.6 |
|  | 1, 2 | -1258.837070 |  | Cu-N, 2.029, 2.025, 2.027, 2.025; Cu-O, 2.185; O-H, 0.969 | ∠NCuN, 89.5, 89.6, 89.6, 89.5, 169.4, 170.1 |
| [LCuIV=O] (5) | 0, 4 | -1258.412302 | 13.8 | Cu-N, 2.023, 2.023, 2.055, 2.055; Cu-O, 2.684 | ∠NCuN, 89.9, 89.9 89.5, 90.0, 178.6, 178.6; ∠NCuO, 90.7, 90.7, 90.7, 90.7 |
|  | 0, 2 | -1258.390293 |  | Cu-N, 2.048, 2.161, 2.159, 2.049; Cu-O, 1.883 | ∠NCuN, 87.8, 87.8 87.8, 87.8, 162.4, 162.4; ∠NCuO, 98.8, 98.8, 98.8, 98.8 |
| [LCuII=O-+OH2] (6) | 0, 2 | -1334.767060 | - | Cu-N, 2.034, 2.014, 2.020, 2.106; Cu-O 2.274; O-O, 1.478; O-H, 1.035, O-H, 0.969 | ∠NCuN, 88.1, 90.8, 90.7, 89.4, 173.7, 170.6 ∠HOO, 103.3; ∠HOO, 100.5; ∠HOH, 107.2 |
| TS1 | 0, 2 | -1334.746478 | - | Cu-N, 2.043, 2.031, 2.029, 2.017; Cu-O, 2.405; O-O, 1.558; O-H, 1.269, 1.092, 0.996 | ∠NCuN, 89.7, 89.6, 90.2, 90.4, 178.8, 179.1; ∠OOH, 43.99, 53.78, 102.97; ∠HOH, 107.17, 82.23 |
| [LCuII-OH-OH] (7) | 0, 2 | -1334.824826 | - | Cu-N, 2.039, 2.032, 2.031, 2.023; Cu-O 2.574; O-O, 1.428; O-H, 0.969, 0.979 | ∠NCuN, 89.7, 89.7, 90.1, 90.2, 178.3, 179.4; ∠HOO, 102.47, 102.54 |
| [LCuII-O•-OH] (8) | 0, 3 | -1334.188191 | 41.9 | Cu-N, 2.046, 2.031, 2.031, 2.020; Cu-O 2.585; O-O, 1.311; O-H, 0.997 | ∠NCuN, 89.6, 89.6, 90.3, 90.3, 177.7, 179.2; ∠HOO, 106.5 |
|  | 0, 1 | -1334.121426 |  | Cu-N, 1.938, 2.099, 1.993, 2.146; Cu-O, 2.065; O-H, 0.972 | ∠NCuN, 90.6, 89.2, 88.0, 89.8, 168.9, 168.8; ∠HOO, 104.0 |
| [LCuII-O=O] (9) | 0, 4 | -1333.594185 | 0.0 | Cu-N, 2.027, 2.027, 2.026, 2.025; Cu-O , 3.176; O-O, 1.201 | ∠NCuN, 89.9, 90.1, 90.1, 89.9, 179.9, 179.9 |
|  | 0, 2 | -1333.594127 | - | Cu-N, 2.020, 2.020, 2.020, 2.020; Cu-O 3.219; O-O, 1.203 | ∠NCuN, 90.0, 89.9, 90.1, 90.0, 179.9, 179.9 |
| [LCuII-O–-OH]– (10) | 0, 2 | -1334.242779 |  | Cu-N, 2.028, 2.032, 2.033, 2.030; Cu-O, 2.295, O-O, 1.472, O-H, 0.969 | ∠NCuN, 89.9, 89.9, 90.0, 89.9, 178.6, 178.1; ∠HOO, 102.5 |
| [LCuII-O•–O–]– (11) | 0, 3 | -1333.643286 | 30.3 | Cu-N,2.026, 2.028, 2.029, 2.029; Cu-O, 3.217; O-O, 1.328 | ∠NCuN, 90.1, 89.9, 89.8, 90.0, 179.4, 179.3 |
|  | 0, 1 | -1333.594969 |  | Cu-N,2.027, 2.048, 2.019, 2.019; Cu-O, 1.906; O-O, 1.194 | ∠NCuN, 81.9, 86.9, 86.9, 81.9, 141.0, 145.7 |
| aΔE = E (low spin) − E (high spin); E = electronic energy |  |  |  |  |  |

Table S2. Chemical formula, charge, spin multiplicity, bond length (Å), and bond angles (o) around the metal centres as obtained at the SMD/PBE0/H,C,N,O(6-31+G(d,p)); Cu (LanL2DZ) level of theory.

| Species | Charge, Spin Multiplicity | Electronic energy | ΔE (kcal/mol)a | Bond length (Å) | Bond angle (o) |
| --- | --- | --- | --- | --- | --- |
| [LCuII-OH2] (1) | 0, 2 | -1259.807612 |  | Cu-N; 2.027, 2.027, 2.027, 2.027; O-H, 0.965; Cu-O, 4.727 | ∠NCuN, 90.1, 89.9, 89.9, 179.8, 179.9, 90.1; ∠HOH, 103.8 |
| [LCuIII-OH2]+ (2) | 1, 3 | -1259.614355 | 16.9 | Cu-N; 2.036, 2.036, 2.036, 2.036, O-H, 0.964; Cu-O, 3.402 | ∠NCuN, 89.9, 89.9, 89.9, 89.9, 178.6, 178.6; ∠HOH, 104.4 |
|  | 1, 1 | -1259.587320 |  | Cu-N; 2.017, 2.017, 2.017, 2.017, O-H, 0.964; Cu-O, 3.618 | ∠NCuN, 90.4, 90.4, 90.4, 90.4, 170.1, 170.3; ∠HOH, 104.3 |
| [LCuIII-OH] (3) | 0, 3 | -1259.124434 | 20.5 | Cu-N, 2.045, 2.048, 2.053, 2.058; Cu-O, 2.163; O-H, 0.964 | ∠NCuN, 89.1, 89.1, 89.1, 89.1, 165.1, 166.2 |
|  | 0, 1 | -1259.091795 |  | Cu-N, 2.085, 1.993, 2.073, 1.993; Cu-O, 2.221; O-H, 0.964 | ∠NCuN, 89.4, 89.7, 89.4, 89.1, 164.6, 173.3 |
| [LCuIV-OH]+ (4) | 0, 4 | -1258.916037 | -5.7 | Cu-N, 2.029, 2.025, 2.025, 2.029; Cu-O, 2.186; O-H, 0.969 | ∠NCuN, 89.9, 89.8, 89.9, 89.8, 173.5, 175.6 |
|  | 0, 2 | -1258.925157 |  | Cu-N, 2.043, 2.043, 2.0, 2.039; Cu-O, 2.250; O-H, 0.972 | ∠NCuN, 89.5, 89.6, 89.6, 89.5, 169.4, 170.1 |
| [LCuIV=O] (5) | 0, 4 |  |  |  |  |
| [LCuIV=O] (5) | 0, 2 | -1258.441031 |  | Cu-N, 2.048, 2.048, 2.056, 2.056; Cu-O, 2.216 | ∠NCuN, 89.2, 89.2, 89.2, 89.2, 167.4, 165.8 |
| [LCuII=O-+OH2] (6) | 0, 2 | -1334.813621 |  | Cu-N, 2.026, 2.019, 2.056, 2.024; Cu-O 3.203; O-O, 1.462; O-H, 1.011, O-H, 0.974 | ∠NCuN, 90.4, 89.3, 90.4, 89.7, 178.4, 178.3, ∠HOO, 106.9; ∠HOO, 05.9; ∠HOH, 106.1 |
| TS1 | 0, 2 | -1334.781173 |  | Cu-N, 2.029, 2.043, 2.031, 2.017; Cu-O, 3.206; O-O, 1.558; O-H, 1.269, 1.092, 0.996 | ∠NCuN, 90.4, 89.7, 90.2, 90.4, 178.8, 179.1; ∠OOH, 53.7, 103.0, 44.7; ∠HOH, 103.0, 82.3 |
| [LCuII-OH-OH] (7) | 0, 2 | -1334.824826 |  | Cu-N,2.023, 2.030, 2.038, 2.032; Cu-O, 3.345; O-O, 1.428; O-H, 0.997 | ∠NCuN, 90.2, 89.8, 89.7, 90.1, 178.6, 179.5; ∠HOO, 102.5 |
| [LCuII-O•-OH] (8) | 0, 3 | -1334.216402 | 37.5 | Cu-N,2.046, 2.030, 2.030, 2.046; Cu-O, 3.276; O-O, 1.312; O-H, 0.994 | ∠NCuN, 89.6, 90.3, 90.3, 89.6, 179.2, 177.7; ∠HOO, 106.5 |
|  | 0, 1 | -1334.156615 |  | Cu-N,2.014, 2.081, 1.962, 2.070; Cu-O, 2.266; O-O, 1.421; O-H, 0.971 | ∠NCuN, 88.8, 90.6, 90.6, 89.3, 167.9, 177.2; ∠HOO, 103.0 |
| [LCuII-O=O] (9) | 0, 4 | -1333.616931 | 10.5 | Cu-N, 2.026, 2.027, 2.026, 2.027; Cu-O, 4.051; O-O, 1.202 | ∠NCuN, 89.9, 90.1, 90.1, 89.9, 179.9, 179.9 |
|  | 0, 2 | -1333.600226 |  | Cu-N, 2.026, 2.027, 2.026, 2.027; Cu-O, 3.887; O-O, 1.202 | ∠NCuN, 89.9, 90.1, 90.1, 89.9, 179.9, 179.9 |
| [LCuII-O–-OH]– (10) | -1, 2 | -1334.371467 |  | Cu-N, 2.028, 2.032, 2.033, 2.030; Cu-O, 3.340, O-O, 1.472, O-H, 0.969 | ∠NCuN, 89.9, 89.9, 90.0, 89.9, 178.6, 178.1; ∠HOO, 102.5 |
| [LCuII-O•–O–]– (11) | -1, 3 | -1333.755183 | 43.2 | Cu-N,2.027, 2.028, 2.029, 2.029; Cu-O, 3.437; O-O, 1.328 | ∠NCuN, 90.1, 89.9, 89.8, 90.0, 179.4, 179.3 |
|  | -1, 1 | -1333.686382 |  |  |  |
| aΔE = E (low spin) − E (high spin); E = electronic energy |  |  |  |  |  |

Fig. S1. The optimized geometries of intermediates 2 (S=0), 3 (S=0), 4 (S=1/2), 8 (S=1/2), 9 (S=0), and 11 (S=1/2) are shown in a, b, c, d, e, and f, respectively at the PBE0/H,C,N,O (6-31+G(d,p)); Cu (LanL2DZ) level of theory. Color code: H, white; C, grey; N, blue; O, red; Cu, orange.

Fig. S2. The optimized geometries of intermediates 1 (S=1/2), 2 (S=1), 3 (S=1), 4 (S=3/2), 6 (S=1), 7 (S=1/2), 8 (S=1), 9 (S=3/2), 10 (S=1/2) and 11 (S=1) are shown in a, b, c, d, e, f, g, h, i, and j, respectively at the SMD/PBE0/H,C,N,O (6-31+G(d,p)); Cu (LanL2DZ) level of theory. Color code: H, white; C, grey; N, blue; O, red; Cu, orange.

Fig. S3. The optimized geometries of intermediates 2 (S=0), 3 (S=0), 4 (S=1/2), 5 (S=1/2), 8 (S=0), 9 (S=1/2), and 11 (S=0) are shown in a, b, c, d, e, f, and g, respectively at the SMD/PBE0/H,C,N,O (6-31+G(d,p)); Cu (LanL2DZ) level of theory. Color code: H, white; C, grey; N, blue; O, red; Cu, orange.

XYZ coordinates of the optimized geometries

40

[LCuII-OH2] (1) doublet

Cu       0.033488000     -0.000158000     -0.061937000

N       -1.383952000      1.458050000     -0.128166000

N       -1.433544000     -1.408745000     -0.129070000

N        1.480309000      1.407726000     -0.114567000

N        1.430726000     -1.457539000     -0.114091000

C        3.447590000     -2.565081000     -0.108973000

H        4.520888000     -2.706524000     -0.103037000

C       -3.400445000      2.565678000     -0.199352000

H       -4.473129000      2.708857000     -0.231766000

C        1.308933000      2.761246000     -0.128353000

C       -3.394977000      0.058976000     -0.169261000

C        2.783632000     -1.284980000     -0.102684000

C        0.083879000      3.418241000     -0.144447000

C        3.439073000     -0.059188000     -0.094139000

C        2.469970000     -3.510749000     -0.125506000

H        2.575568000     -4.588156000     -0.135755000

C       -0.034281000     -3.418548000     -0.145419000

C       -1.261450000     -2.764223000     -0.154139000

C       -2.540763000     -3.425169000     -0.196707000

H       -2.683461000     -4.498036000     -0.224068000

C       -3.487034000     -2.446003000     -0.202211000

H       -4.564009000     -2.551987000     -0.235319000

C        3.534210000      2.444905000     -0.110512000

H        4.611762000      2.549133000     -0.105159000

C        2.589858000      3.423819000     -0.126718000

H        2.732657000      4.496925000     -0.137217000

C        1.212724000     -2.804287000     -0.127896000

C       -2.782594000     -1.189861000     -0.163622000

C       -1.165168000      2.806713000     -0.152240000

C       -2.739755000      1.285892000     -0.162237000

C        2.826435000      1.188536000     -0.103561000

C       -2.420903000      3.511530000     -0.193484000

H       -2.526426000      4.588717000     -0.219792000

H        4.524775000     -0.077986000     -0.084855000

H       -0.051884000     -4.504232000     -0.161410000

H       -4.480441000      0.077779000     -0.197837000

H        0.103842000      4.503893000     -0.159981000

O       -0.356746000      0.000137000      2.481004000

H       -0.952667000     -0.752909000      2.400417000

H       -0.923057000      0.776896000      2.413953000

40

[LCuII-OH2] (1) doublet SMD

Cu      -0.177943000      0.001299000     -0.154585000

N        0.846739000     -1.744555000     -0.257059000

N        1.556517000      1.033944000     -0.334682000

N       -1.912996000     -1.031853000      0.024146000

N       -1.203323000      1.746487000     -0.045935000

C       -2.901559000      3.292278000      0.122837000

H       -3.909480000      3.676531000      0.221490000

C        2.544292000     -3.291199000     -0.427235000

H        3.551558000     -3.676019000     -0.530287000

C       -2.060791000     -2.391149000      0.043497000

C        3.117660000     -0.850456000     -0.496566000

C       -2.556541000      1.893482000      0.085933000

C       -1.025544000     -3.314841000     -0.057917000

C       -3.475268000      0.852127000      0.175281000

C       -1.734105000      3.986404000      0.011420000

H       -1.583903000      5.059053000     -0.000391000

C        0.670492000      3.317063000     -0.224166000

C        1.705433000      2.393534000     -0.333779000

C        3.098334000      2.739179000     -0.464818000

H        3.482745000      3.751504000     -0.490980000

C        3.787187000      1.565577000     -0.545118000

H        4.854501000      1.413801000     -0.650903000

C       -4.142716000     -1.563066000      0.246681000

H       -5.210048000     -1.411173000      0.351835000

C       -3.452967000     -2.736571000      0.183644000

H       -3.836055000     -3.748855000      0.225835000

C       -0.680135000      3.009186000     -0.093474000

C        2.812103000      0.507544000     -0.462127000

C        0.323931000     -3.006913000     -0.197629000

C        2.199443000     -1.892085000     -0.396682000

C       -3.169284000     -0.504968000      0.147209000

C        1.377654000     -3.984573000     -0.302934000

H        1.227767000     -5.057144000     -0.282789000

H       -4.522401000      1.122204000      0.277509000

H        0.940032000      4.369129000     -0.243063000

H        4.164460000     -1.120449000     -0.602667000

H       -1.293877000     -4.366913000     -0.026581000

O        3.374548000     -0.020216000      2.963258000

H        3.617812000      0.683545000      2.349431000

H        3.046571000     -0.722629000      2.388843000

40

[LCuIII-OH2]+ (2) triplet

Cu       0.000009000      0.000023000     -0.021539000

N       -1.433501000      1.439099000     -0.129426000

N       -1.442522000     -1.429969000     -0.128856000

N        1.442641000      1.430005000     -0.128627000

N        1.433629000     -1.439041000     -0.129293000

C        3.466415000     -2.521994000     -0.178853000

H        4.540337000     -2.652145000     -0.208513000

C       -3.466302000      2.522025000     -0.178891000

H       -4.540221000      2.652190000     -0.208576000

C        1.256911000      2.779009000     -0.127544000

C       -3.415192000      0.010809000     -0.174850000

C        2.783066000     -1.256393000     -0.160434000

C        0.010766000      3.410113000     -0.118953000

C        3.415307000     -0.010763000     -0.174644000

C        2.498785000     -3.481258000     -0.156698000

H        2.619348000     -4.556667000     -0.165044000

C       -0.010635000     -3.410063000     -0.119026000

C       -1.256808000     -2.778966000     -0.127669000

C       -2.520474000     -3.465421000     -0.156634000

H       -2.647839000     -4.540044000     -0.165185000

C       -3.482074000     -2.500049000     -0.178780000

H       -4.556786000     -2.623465000     -0.208663000

C        3.482182000      2.500104000     -0.178651000

H        4.556896000      2.623503000     -0.208527000

C        2.520591000      3.465471000     -0.156465000

H        2.647944000      4.540096000     -0.164996000

C        1.239433000     -2.786808000     -0.127934000

C       -2.790826000     -1.238806000     -0.160259000

C       -1.239328000      2.786862000     -0.127931000

C       -2.782961000      1.256435000     -0.160563000

C        2.790923000      1.238854000     -0.160055000

C       -2.498668000      3.481300000     -0.156707000

H       -2.619247000      4.556707000     -0.165030000

H        4.501491000     -0.014173000     -0.203031000

H       -0.014055000     -4.496607000     -0.120464000

H       -4.501376000      0.014226000     -0.203300000

H        0.014193000      4.496657000     -0.120373000

O       -0.000673000     -0.000464000      2.371847000

H        0.768990000      0.012081000      2.948846000

H       -0.772949000     -0.012750000      2.945352000

40

[LCuIII-OH2]+ (2) triplet SMD

Cu      -0.000574000      0.000499000     -0.153138000

N        0.547478000     -1.960061000     -0.179583000

N        1.959576000      0.548441000     -0.176989000

N       -1.961007000     -0.547713000     -0.176218000

N       -0.548833000      1.960802000     -0.177670000

C       -1.794857000      3.895836000     -0.185635000

H       -2.673573000      4.528098000     -0.189025000

C        1.793585000     -3.895082000     -0.189497000

H        2.672306000     -4.527340000     -0.193713000

C       -2.458354000     -1.815558000     -0.179771000

C        2.975544000     -1.678064000     -0.182037000

C       -1.816605000      2.458183000     -0.179838000

C       -1.679011000     -2.975882000     -0.181908000

C       -2.976932000      1.678823000     -0.178915000

C       -0.479770000      4.261346000     -0.186394000

H       -0.052697000      5.256160000     -0.190592000

C        1.677646000      2.976622000     -0.180960000

C        2.456953000      1.816256000     -0.180286000

C        3.894567000      1.794536000     -0.185920000

H        4.526822000      2.673254000     -0.189622000

C        4.260118000      0.479432000     -0.186522000

H        5.254958000      0.052410000     -0.190786000

C       -4.261528000     -0.478724000     -0.183398000

H       -5.256349000     -0.051662000     -0.186430000

C       -3.895989000     -1.793831000     -0.184695000

H       -4.528223000     -2.672566000     -0.188908000

C        0.281202000      3.041641000     -0.180832000

C        3.040470000     -0.281567000     -0.180609000

C       -0.282496000     -3.040885000     -0.182947000

C        1.815276000     -2.457437000     -0.182876000

C       -3.041858000      0.282310000     -0.178363000

C        0.478496000     -4.260591000     -0.189643000

H        0.051441000     -5.255413000     -0.194063000

H       -3.923410000      2.212192000     -0.180813000

H        2.211102000      3.923049000     -0.183613000

H        3.922034000     -2.211412000     -0.184967000

H       -2.212419000     -3.922332000     -0.184798000

O       -0.005992000      0.012100000      3.248675000

H       -0.666031000     -0.112464000      3.940751000

H        0.839384000     -0.057701000      3.707677000

40

[LCuIII-OH2]+ (2) singlet

Cu       0.000315000      0.000076000     -0.046495000

N       -0.033119000     -1.999855000     -0.266926000

N        2.027586000     -0.033642000      0.014903000

N       -2.027168000      0.033861000      0.014556000

N        0.033622000      2.000041000     -0.266744000

C       -0.632011000      4.204819000     -0.038344000

H       -1.297209000      5.054910000      0.038543000

C        0.632468000     -4.204642000     -0.038648000

H        1.297657000     -5.054733000      0.038300000

C       -2.858095000     -1.059115000     -0.103985000

C        2.378338000     -2.442428000     -0.181976000

C       -1.059819000      2.838324000     -0.176433000

C       -2.447440000     -2.372810000     -0.104878000

C       -2.377880000      2.442663000     -0.182282000

C        0.724191000      4.180718000      0.025751000

H        1.409171000      5.010713000      0.140304000

C        2.447918000      2.372999000     -0.104174000

C        2.858546000      1.059308000     -0.103272000

C        4.221096000      0.633529000     -0.285056000

H        5.066970000      1.299146000     -0.397216000

C        4.195807000     -0.723606000     -0.350565000

H        5.021254000     -1.407056000     -0.501309000

C       -4.195283000      0.723821000     -0.351610000

H       -5.020693000      1.407249000     -0.502655000

C       -4.220576000     -0.633333000     -0.286131000

H       -5.066408000     -1.298944000     -0.398647000

C        1.117181000      2.801695000     -0.103399000

C        2.821470000     -1.116355000     -0.178130000

C       -1.116714000     -2.801521000     -0.103876000

C        1.060282000     -2.838122000     -0.176514000

C       -2.821038000      1.116589000     -0.178670000

C       -0.723747000     -4.180559000      0.025172000

H       -1.408740000     -5.010572000      0.139523000

H       -3.133898000      3.221631000     -0.205467000

H        3.216945000      3.139469000     -0.110182000

H        3.134381000     -3.221375000     -0.205006000

H       -3.216465000     -3.139282000     -0.111134000

O       -0.003849000     -0.002087000      2.378608000

H       -0.778969000      0.035211000      2.947405000

H        0.763031000     -0.036566000      2.958633000

40

[LCuIII-OH2]+ (2) singlet SMD

Cu       0.005706000      0.000572000     -0.186114000

N        0.097799000     -2.007147000     -0.360995000

N        2.013217000      0.092456000     -0.008758000

N       -2.004455000     -0.091845000     -0.021541000

N       -0.086026000      2.008223000     -0.360493000

C       -0.850913000      4.163711000     -0.061287000

H       -1.566832000      4.966828000      0.058698000

C        0.860247000     -4.163050000     -0.058192000

H        1.575189000     -4.966361000      0.066207000

C       -2.773295000     -1.207301000     -0.193129000

C        2.519876000     -2.303100000     -0.145900000

C       -1.202364000      2.777691000     -0.196360000

C       -2.298522000     -2.514211000     -0.231135000

C       -2.509719000      2.303766000     -0.162370000

C        0.508259000      4.225224000     -0.098090000

H        1.155308000      5.087898000     -0.003053000

C        2.309127000      2.515161000     -0.212707000

C        2.783445000      1.208116000     -0.172827000

C        4.170057000      0.856124000     -0.300655000

H        4.973854000      1.571530000     -0.419170000

C        4.231196000     -0.502963000     -0.259199000

H        5.094253000     -1.150382000     -0.348077000

C       -4.220263000      0.503868000     -0.290287000

H       -5.082461000      1.151397000     -0.386397000

C       -4.158811000     -0.855197000     -0.332270000

H       -4.961550000     -1.570463000     -0.458502000

C        0.975179000      2.874972000     -0.240947000

C        2.880156000     -0.969218000     -0.120913000

C       -0.964362000     -2.873873000     -0.249846000

C        1.212803000     -2.776988000     -0.189677000

C       -2.870374000      0.969908000     -0.140400000

C       -0.498630000     -4.224340000     -0.105073000

H       -1.146448000     -5.087046000     -0.015704000

H       -3.308292000      3.039728000     -0.155012000

H        3.044632000      3.314150000     -0.220029000

H        3.318466000     -3.038945000     -0.132488000

H       -3.033855000     -3.313264000     -0.245423000

O       -0.084970000      0.002528000      3.431655000

H       -0.910803000     -0.011195000      3.929615000

H        0.600532000     -0.092296000      4.103484000

39

[LCuIII-OH] (3) triplet

Cu      -0.022492000      0.000156000      0.015594000

N       -0.007722000      2.024411000     -0.146996000

N       -2.043199000      0.012186000     -0.099604000

N        2.004862000     -0.011894000     -0.129262000

N       -0.031991000     -2.024135000     -0.147074000

C        0.633908000     -4.227892000     -0.138423000

H        1.302087000     -5.079622000     -0.141384000

C       -0.675502000      4.227643000     -0.125363000

H       -1.344285000      5.078824000     -0.115296000

C        2.830878000      1.079033000     -0.135753000

C       -2.418836000      2.428658000     -0.099844000

C        1.053898000     -2.848590000     -0.143949000

C        2.408908000      2.402378000     -0.142621000

C        2.379954000     -2.430865000     -0.143811000

C       -0.726026000     -4.219227000     -0.125010000

H       -1.404966000     -5.062326000     -0.114495000

C       -2.447719000     -2.399598000     -0.098551000

C       -2.867228000     -1.074261000     -0.089602000

C       -4.246029000     -0.654805000     -0.077530000

H       -5.097517000     -1.323216000     -0.070500000

C       -4.237859000      0.705587000     -0.078102000

H       -5.081229000      1.384220000     -0.071669000

C        4.198678000     -0.705913000     -0.150181000

H        5.043185000     -1.383115000     -0.164129000

C        4.206881000      0.655679000     -0.149741000

H        5.059510000      1.322633000     -0.163296000

C       -1.128661000     -2.834933000     -0.123562000

C       -2.854126000      1.108444000     -0.090429000

C        1.087929000      2.835836000     -0.143119000

C       -1.094656000      2.848248000     -0.124204000

C        2.817683000     -1.112682000     -0.136402000

C        0.684448000      4.220050000     -0.137773000

H        1.362811000      5.063694000     -0.140196000

H        3.142370000     -3.204291000     -0.147601000

H       -3.220293000     -3.162745000     -0.083832000

H       -3.182228000      3.201003000     -0.085806000

H        3.180522000      3.166629000     -0.145880000

O        0.315715000     -0.002436000      2.136330000

H        1.273799000     -0.007428000      2.285565000

39

[LCuIII-OH] (3) triplet SMD

Cu       0.002100000     -0.009589000      0.109802000

N       -1.959635000     -0.552804000     -0.158927000

N        0.544333000     -1.970411000     -0.102470000

N       -0.536192000      1.949232000     -0.154379000

N        1.968784000      0.528452000     -0.151658000

C        3.908098000      1.770604000     -0.181862000

H        4.542107000      2.648220000     -0.200334000

C       -3.900007000     -1.793748000     -0.174109000

H       -4.534766000     -2.670990000     -0.180958000

C       -1.804402000      2.449572000     -0.149582000

C       -1.684296000     -2.981050000     -0.128394000

C        2.468128000      1.796336000     -0.163526000

C       -2.966674000      1.675357000     -0.158810000

C        1.692421000      2.957861000     -0.158291000

C        4.270855000      0.456209000     -0.171472000

H        5.265253000      0.027949000     -0.179619000

C        2.975983000     -1.698113000     -0.123702000

C        1.812405000     -2.470955000     -0.108329000

C        1.785408000     -3.910186000     -0.120648000

H        2.662719000     -4.544744000     -0.132246000

C        0.470446000     -4.272020000     -0.122015000

H        0.041520000     -5.266058000     -0.134982000

C       -0.462340000      4.251169000     -0.152057000

H       -0.033440000      5.245320000     -0.155876000

C       -1.777068000      3.889551000     -0.151643000

H       -2.654284000      4.524377000     -0.155028000

C        3.047832000     -0.303931000     -0.146923000

C       -0.289119000     -3.049297000     -0.110623000

C       -3.037895000      0.280560000     -0.166862000

C       -2.460159000     -1.820390000     -0.152438000

C        0.297728000      3.027866000     -0.149898000

C       -4.261512000     -0.478991000     -0.182183000

H       -5.255521000     -0.050016000     -0.197397000

H        2.228645000      3.902900000     -0.162054000

H        3.919492000     -2.236996000     -0.125113000

H       -2.219354000     -3.926733000     -0.129659000

H       -3.910927000      2.212969000     -0.160515000

O       -0.048322000      0.129876000      2.268223000

H       -0.361794000      1.033151000      2.395984000

39

[LCuIII-OH] (3) singlet

Cu      -0.138768000      0.000015000      0.291146000

N       -0.037056000      1.960119000     -0.099197000

N       -2.125236000      0.000283000     -0.115880000

N        2.098149000     -0.000204000     -0.318349000

N       -0.037673000     -1.960087000     -0.099169000

C        0.672194000     -4.140167000      0.113176000

H        1.354298000     -4.978863000      0.174328000

C       -0.686750000      4.160034000      0.128159000

H       -1.345064000      5.015518000      0.209978000

C        2.903793000      1.082416000     -0.360642000

C       -2.453752000      2.400012000     -0.121564000

C        1.074812000     -2.762870000     -0.033725000

C        2.407977000      2.377901000     -0.200736000

C        2.407263000     -2.378450000     -0.200745000

C       -0.687907000     -4.159846000      0.127990000

H       -1.346431000     -5.015177000      0.209712000

C       -2.454473000     -2.399340000     -0.121493000

C       -2.922505000     -1.092512000     -0.241858000

C       -4.290369000     -0.681066000     -0.452908000

H       -5.132313000     -1.348920000     -0.584085000

C       -4.290162000      0.682285000     -0.452942000

H       -5.131899000      1.350390000     -0.584161000

C        4.293969000     -0.681746000     -0.483082000

H        5.144834000     -1.348991000     -0.544337000

C        4.294194000      0.680604000     -0.483088000

H        5.145277000      1.347569000     -0.544358000

C       -1.121775000     -2.792789000     -0.003543000

C       -2.922167000      1.093315000     -0.241921000

C        1.075629000      2.762640000     -0.033684000

C       -1.120952000      2.793099000     -0.003543000

C        2.903437000     -1.083114000     -0.360624000

C        0.673345000      4.140028000      0.113278000

H        1.355655000      4.978553000      0.174477000

H        3.133210000     -3.187961000     -0.188417000

H       -3.195080000     -3.194379000     -0.135625000

H       -3.194138000      3.195258000     -0.135707000

H        3.134130000      3.187227000     -0.188394000

O        0.590952000     -0.000439000      2.009321000

H        1.552086000     -0.000543000      1.927918000

39

[LCuIII-OH] (3) singlet SMD

Cu       0.002100000     -0.009589000      0.109802000

N       -1.959635000     -0.552804000     -0.158927000

N        0.544333000     -1.970411000     -0.102470000

N       -0.536192000      1.949232000     -0.154379000

N        1.968784000      0.528452000     -0.151658000

C        3.908098000      1.770604000     -0.181862000

H        4.542107000      2.648220000     -0.200334000

C       -3.900007000     -1.793748000     -0.174109000

H       -4.534766000     -2.670990000     -0.180958000

C       -1.804402000      2.449572000     -0.149582000

C       -1.684296000     -2.981050000     -0.128394000

C        2.468128000      1.796336000     -0.163526000

C       -2.966674000      1.675357000     -0.158810000

C        1.692421000      2.957861000     -0.158291000

C        4.270855000      0.456209000     -0.171472000

H        5.265253000      0.027949000     -0.179619000

C        2.975983000     -1.698113000     -0.123702000

C        1.812405000     -2.470955000     -0.108329000

C        1.785408000     -3.910186000     -0.120648000

H        2.662719000     -4.544744000     -0.132246000

C        0.470446000     -4.272020000     -0.122015000

H        0.041520000     -5.266058000     -0.134982000

C       -0.462340000      4.251169000     -0.152057000

H       -0.033440000      5.245320000     -0.155876000

C       -1.777068000      3.889551000     -0.151643000

H       -2.654284000      4.524377000     -0.155028000

C        3.047832000     -0.303931000     -0.146923000

C       -0.289119000     -3.049297000     -0.110623000

C       -3.037895000      0.280560000     -0.166862000

C       -2.460159000     -1.820390000     -0.152438000

C        0.297728000      3.027866000     -0.149898000

C       -4.261512000     -0.478991000     -0.182183000

H       -5.255521000     -0.050016000     -0.197397000

H        2.228645000      3.902900000     -0.162054000

H        3.919492000     -2.236996000     -0.125113000

H       -2.219354000     -3.926733000     -0.129659000

H       -3.910927000      2.212969000     -0.160515000

O       -0.048322000      0.129876000      2.268223000

H       -0.361794000      1.033151000      2.395984000

39

[LCuIV-OH]+ (4) quartet

Cu       0.048519000      0.000491000     -0.017407000

N       -0.140458000     -2.012590000     -0.133831000

N        2.059920000     -0.182774000     -0.063151000

N       -1.978981000      0.196555000     -0.130294000

N        0.226089000      2.019721000     -0.090475000

C       -0.233184000      4.275683000     -0.147044000

H       -0.825129000      5.180601000     -0.189531000

C        0.317956000     -4.268732000     -0.145127000

H        0.912569000     -5.172750000     -0.155200000

C       -2.891376000     -0.804980000     -0.128960000

C        2.229775000     -2.619022000     -0.126151000

C       -0.765157000      2.933713000     -0.145491000

C       -2.579367000     -2.182983000     -0.107784000

C       -2.144156000      2.632260000     -0.194148000

C        1.118481000      4.153317000     -0.088414000

H        1.864660000      4.937019000     -0.073936000

C        2.663370000      2.187861000     -0.021724000

C        2.970423000      0.808106000     -0.032941000

C        4.314736000      0.279290000     -0.032643000

H        5.218357000      0.874266000     -0.011751000

C        4.195049000     -1.072652000     -0.069154000

H        4.980056000     -1.817443000     -0.082740000

C       -4.109067000      1.077603000     -0.232449000

H       -4.896502000      1.817701000     -0.294558000

C       -4.227677000     -0.279332000     -0.193929000

H       -5.131542000     -0.873817000     -0.216604000

C        1.401825000      2.737507000     -0.057553000

C        2.778683000     -1.359666000     -0.087815000

C       -1.318673000     -2.729078000     -0.119236000

C        0.847541000     -2.923815000     -0.140394000

C       -2.697326000      1.370934000     -0.185918000

C       -1.033550000     -4.147088000     -0.128208000

H       -1.779914000     -4.930692000     -0.123471000

H       -2.827054000      3.475351000     -0.241607000

H        3.504318000      2.874565000      0.001907000

H        2.915336000     -3.461082000     -0.140718000

H       -3.419419000     -2.871030000     -0.098043000

O       -0.861105000     -0.159737000      2.112758000

H       -1.229778000      0.671038000      2.463729000

39

[LCuIV-OH]+ (4) quartet SMD

Cu       0.007113000     -0.000003000      0.104907000

N        0.008620000     -2.052350000     -0.148909000

N        2.050765000      0.000206000     -0.114467000

N       -2.035933000     -0.000209000     -0.140442000

N        0.008201000      2.052342000     -0.148920000

C       -0.686595000      4.233608000     -0.197659000

H       -1.358477000      5.083136000     -0.221152000

C        0.702816000     -4.233966000     -0.191553000

H        1.374510000     -5.083778000     -0.209167000

C       -2.856889000     -1.097379000     -0.141476000

C        2.445816000     -2.414220000     -0.134006000

C       -1.085231000      2.873697000     -0.166315000

C       -2.429288000     -2.414507000     -0.153660000

C       -2.429775000      2.414012000     -0.153638000

C        0.701964000      4.234097000     -0.191567000

H        1.373491000      5.084041000     -0.209185000

C        2.445328000      2.414705000     -0.134032000

C        2.871982000      1.097197000     -0.117561000

C        4.257825000      0.679901000     -0.122546000

H        5.104658000      1.355443000     -0.129936000

C        4.257960000     -0.679052000     -0.122486000

H        5.104926000     -1.354427000     -0.129828000

C       -4.243156000      0.679026000     -0.148721000

H       -5.090220000      1.354292000     -0.156977000

C       -4.243020000     -0.679886000     -0.148712000

H       -5.089950000     -1.355321000     -0.156964000

C        1.101078000      2.874426000     -0.156982000

C        2.872200000     -1.096623000     -0.117548000

C       -1.084650000     -2.873921000     -0.166322000

C        1.101659000     -2.874215000     -0.156959000

C       -2.857109000      1.096797000     -0.141458000

C       -0.685743000     -4.233753000     -0.197649000

H       -1.357457000     -5.083414000     -0.221143000

H       -3.202348000      3.178645000     -0.160379000

H        3.218275000      3.178961000     -0.138058000

H        3.218920000     -3.178316000     -0.138010000

H       -3.201705000     -3.179297000     -0.160406000

O       -0.056565000      0.000013000      2.344566000

H       -1.013013000      0.000425000      2.466648000

39

[LCuIV-OH]+ (4) doublet

Cu       0.041535000     -0.001009000     -0.006063000

N        2.056956000      0.033878000     -0.068272000

N        0.000130000      2.012511000     -0.138853000

N        0.072391000     -2.021799000     -0.108150000

N       -1.986715000     -0.043930000     -0.127618000

C       -4.186143000     -0.770223000     -0.188872000

H       -5.022703000     -1.456154000     -0.221107000

C        4.257213000      0.762175000     -0.060487000

H        5.092412000      1.450370000     -0.062261000

C        1.194809000     -2.822684000     -0.090377000

C        2.408854000      2.453078000     -0.094557000

C       -2.788873000     -1.167658000     -0.152447000

C        2.492619000     -2.376045000     -0.059375000

C       -2.338005000     -2.464620000     -0.157986000

C       -4.206084000      0.582464000     -0.184110000

H       -5.063101000      1.242645000     -0.213137000

C       -2.421606000      2.366145000     -0.149521000

C       -1.119034000      2.810377000     -0.143236000

C       -0.729188000      4.211908000     -0.144469000

H       -1.419304000      5.045457000     -0.151952000

C        0.622142000      4.235853000     -0.129834000

H        1.282362000      5.093195000     -0.123786000

C       -0.547855000     -4.245080000     -0.146073000

H       -1.207855000     -5.102238000     -0.173759000

C        0.803643000     -4.222524000     -0.115126000

H        1.492601000     -5.057120000     -0.110846000

C       -2.822776000      1.020342000     -0.145912000

C        1.057231000      2.849455000     -0.121026000

C        2.892233000     -1.023029000     -0.055809000

C        2.857426000      1.154141000     -0.073779000

C       -0.983475000     -2.859018000     -0.137959000

C        4.278614000     -0.589905000     -0.049738000

H        5.135226000     -1.251052000     -0.040873000

H       -3.081329000     -3.254989000     -0.184063000

H       -3.206841000      3.115160000     -0.159849000

H        3.154148000      3.242056000     -0.090648000

H        3.280476000     -3.122428000     -0.046927000

O       -0.717408000      0.172747000      2.105613000

H       -1.231142000     -0.593178000      2.414532000

39

[LCuIV-OH]+ (4) doublet SMD

Cu       0.007280000     -0.003391000      0.106871000

N        1.063393000     -1.731411000     -0.127694000

N        1.739678000      1.052705000     -0.132463000

N       -1.723539000     -1.058055000     -0.156858000

N       -1.046923000      1.727395000     -0.153339000

C       -2.778016000      3.264954000     -0.158223000

H       -3.798519000      3.625211000     -0.164741000

C        2.794240000     -3.268944000     -0.136763000

H        3.814742000     -3.629194000     -0.140896000

C       -1.855066000     -2.411694000     -0.153739000

C        3.328340000     -0.805161000     -0.117496000

C       -2.400673000      1.858966000     -0.150365000

C       -0.795518000     -3.321198000     -0.144745000

C       -3.311687000      0.800688000     -0.149729000

C       -1.624771000      3.969768000     -0.158226000

H       -1.479981000      5.042072000     -0.164597000

C        0.811530000      3.316671000     -0.146597000

C        1.870608000      2.405876000     -0.141913000

C        3.276107000      2.784112000     -0.154858000

H        3.635588000      3.804795000     -0.170273000

C        3.981645000      1.631136000     -0.144333000

H        5.053987000      1.486549000     -0.149180000

C       -3.965665000     -1.635679000     -0.164804000

H       -5.037928000     -1.490528000     -0.172230000

C       -3.260982000     -2.789077000     -0.164378000

H       -3.621011000     -3.809663000     -0.171004000

C       -0.546204000      2.992253000     -0.150473000

C        3.004248000      0.552881000     -0.127951000

C        0.562718000     -2.995658000     -0.137071000

C        2.416858000     -1.863405000     -0.123736000

C       -2.987722000     -0.557211000     -0.154368000

C        1.640645000     -3.973467000     -0.145164000

H        1.495339000     -5.045640000     -0.157684000

H       -4.366793000      1.056839000     -0.147993000

H        1.067797000      4.371744000     -0.150048000

H        4.383346000     -1.061659000     -0.111845000

H       -1.050316000     -4.376647000     -0.146424000

O       -0.065866000      0.019692000      2.234474000

H       -0.972531000      0.297612000      2.413948000

38

[LCuIV=O] (5) quartet

Cu       0.000025000      0.000002000     -0.082607000

N       -2.023483000     -0.000719000     -0.106676000

N        0.000732000     -2.023443000     -0.107238000

N       -0.000708000      2.023442000     -0.107201000

N        2.023497000      0.000721000     -0.107043000

C        4.221784000      0.681960000     -0.121261000

H        5.069500000      1.355296000     -0.128103000

C       -4.221771000     -0.681960000     -0.120425000

H       -5.069486000     -1.355298000     -0.127073000

C       -1.094552000      2.841350000     -0.112741000

C       -2.415842000     -2.417554000     -0.112239000

C        2.841380000      1.094555000     -0.112563000

C       -2.417563000      2.415836000     -0.112197000

C        2.415865000      2.417559000     -0.112668000

C        4.222268000     -0.678955000     -0.121177000

H        5.070463000     -1.351689000     -0.127955000

C        2.417583000     -2.415838000     -0.112706000

C        1.094569000     -2.841350000     -0.113007000

C        0.681974000     -4.221726000     -0.121958000

H        1.355263000     -5.069477000     -0.129024000

C       -0.678955000     -4.222209000     -0.121862000

H       -1.351643000     -5.070436000     -0.128827000

C        0.678970000      4.222210000     -0.121940000

H        1.351654000      5.070440000     -0.129034000

C       -0.681960000      4.221724000     -0.121753000

H       -1.355252000      5.069473000     -0.128673000

C        2.842158000     -1.092532000     -0.112585000

C       -1.092528000     -2.842126000     -0.112789000

C       -2.842140000      1.092529000     -0.112032000

C       -2.841361000     -1.094550000     -0.112051000

C        1.092549000      2.842130000     -0.112957000

C       -4.222256000      0.678955000     -0.120408000

H       -5.070452000      1.351687000     -0.127042000

H        3.183420000      3.185651000     -0.117152000

H        3.185684000     -3.183384000     -0.117169000

H       -3.183398000     -3.185647000     -0.116567000

H       -3.185666000      3.183382000     -0.116503000

O       -0.000263000     -0.000012000      2.601719000

38

[LCuIV=O] (5) doublet

Cu       0.000580000      0.000025000      0.266057000

N        2.091774000     -0.000025000     -0.273100000

N        0.000183000      2.024887000     -0.047492000

N        0.000198000     -2.024905000     -0.047407000

N       -2.091510000     -0.000039000     -0.274578000

C       -4.287946000     -0.680955000     -0.145765000

H       -5.138411000     -1.349103000     -0.093402000

C        4.288190000      0.680933000     -0.145542000

H        5.138691000      1.349072000     -0.093703000

C        1.091680000     -2.834402000     -0.105852000

C        2.425343000      2.401595000     -0.147726000

C       -2.898599000     -1.086696000     -0.203488000

C        2.425364000     -2.401627000     -0.147671000

C       -2.425022000     -2.401538000     -0.148259000

C       -4.287949000      0.680879000     -0.145787000

H       -5.138414000      1.349027000     -0.093441000

C       -2.425039000      2.401470000     -0.148278000

C       -1.091325000      2.834273000     -0.106187000

C       -0.681480000      4.216414000     -0.171721000

H       -1.350857000      5.065438000     -0.227938000

C        0.681713000      4.216487000     -0.171604000

H        1.351019000      5.065573000     -0.227697000

C       -0.681443000     -4.216446000     -0.171717000

H       -1.350819000     -5.065467000     -0.227975000

C        0.681741000     -4.216508000     -0.171569000

H        1.351061000     -5.065583000     -0.227675000

C       -2.898603000      1.086623000     -0.203496000

C        1.091658000      2.834392000     -0.105916000

C        2.898910000     -1.086721000     -0.202599000

C        2.898895000      1.086689000     -0.202628000

C       -1.091304000     -2.834301000     -0.106145000

C        4.288198000     -0.680944000     -0.145496000

H        5.138709000     -1.349068000     -0.093615000

H       -3.177650000     -3.186537000     -0.136258000

H       -3.177682000      3.186455000     -0.136259000

H        3.178017000      3.186552000     -0.135970000

H        3.178033000     -3.186588000     -0.135908000

O       -0.005116000      0.000298000      2.149612000

38

[LCuIV=O] (5) doublet SMD

Cu      -0.000024000      0.000001000      0.121905000

N       -2.040370000     -0.000365000     -0.131972000

N        0.000380000     -2.036535000     -0.102761000

N       -0.000356000      2.036537000     -0.102743000

N        2.040351000      0.000368000     -0.132243000

C        4.239066000      0.682895000     -0.167589000

H        5.083749000      1.360122000     -0.184388000

C       -4.239087000     -0.682892000     -0.166777000

H       -5.083778000     -1.360114000     -0.183352000

C       -1.089424000      2.853885000     -0.119837000

C       -2.416253000     -2.415501000     -0.131018000

C        2.857686000      1.088913000     -0.141391000

C       -2.417122000      2.414637000     -0.130985000

C        2.416257000      2.415507000     -0.131435000

C        4.239311000     -0.681371000     -0.167594000

H        5.084236000     -1.358296000     -0.184398000

C        2.417126000     -2.414638000     -0.131466000

C        1.089431000     -2.853895000     -0.120081000

C        0.683015000     -4.234503000     -0.147788000

H        1.360192000     -5.079094000     -0.169458000

C       -0.681505000     -4.234740000     -0.147642000

H       -1.358394000     -5.079566000     -0.169169000

C        0.681494000      4.234750000     -0.147724000

H        1.358371000      5.079583000     -0.169375000

C       -0.683025000      4.234499000     -0.147586000

H       -1.360215000      5.079084000     -0.169100000

C        2.858077000     -1.087885000     -0.141405000

C       -1.088397000     -2.854272000     -0.119872000

C       -2.858094000      1.087891000     -0.140906000

C       -2.857703000     -1.088913000     -0.140921000

C        1.088404000      2.854287000     -0.120046000

C       -4.239332000      0.681374000     -0.166786000

H       -5.084265000      1.358294000     -0.183364000

H        3.183515000      3.185205000     -0.143118000

H        3.184662000     -3.184058000     -0.143162000

H       -3.183500000     -3.185212000     -0.142519000

H       -3.184647000      3.184071000     -0.142478000

O        0.000147000     -0.000031000      2.33872000041

[LCuII=O-+OH2] (6) doublet

Cu      -0.112648000     -0.000276000     -0.037126000

N        0.351641000      1.972732000     -0.206020000

N       -2.077322000      0.421455000     -0.178732000

N        1.949057000     -0.421284000     -0.118752000

N       -0.500065000     -1.977192000     -0.190146000

C       -0.290973000     -4.268110000     -0.172274000

H        0.192244000     -5.236873000     -0.168810000

C        0.137583000      4.264074000     -0.220583000

H       -0.345996000      5.232692000     -0.214758000

C        2.964030000      0.483146000     -0.374607000

C       -1.934491000      2.858907000     -0.157721000

C        0.399186000     -2.999081000     -0.183415000

C        2.801836000      1.863336000     -0.366071000

C        1.785937000     -2.868720000     -0.239838000

C       -1.620746000     -3.986891000     -0.169908000

H       -2.454690000     -4.677140000     -0.163559000

C       -2.946471000     -1.859590000     -0.186623000

C       -3.099017000     -0.475945000     -0.189994000

C       -4.365513000      0.217386000     -0.195389000

H       -5.336330000     -0.261541000     -0.206356000

C       -4.079827000      1.547587000     -0.180503000

H       -4.768445000      2.382934000     -0.177761000

C        3.896216000     -1.556470000     -0.580553000

H        4.566461000     -2.389181000     -0.752687000

C        4.184036000     -0.220938000     -0.634643000

H        5.134548000      0.247363000     -0.857230000

C       -1.737767000     -2.547696000     -0.180132000

C       -2.640280000      1.659573000     -0.168978000

C        1.587396000      2.545941000     -0.272121000

C       -0.550133000      2.996547000     -0.181237000

C        2.497968000     -1.677109000     -0.291946000

C        1.467619000      3.984510000     -0.280913000

H        2.298857000      4.676235000     -0.334513000

H        2.361689000     -3.787205000     -0.307524000

H       -3.853434000     -2.457023000     -0.185323000

H       -2.518373000      3.774664000     -0.145967000

H        3.696011000      2.466744000     -0.493268000

O        0.017646000     -0.020617000      2.233112000

O        1.483156000     -0.026804000      2.421902000

H        1.796837000     -0.219190000      1.454292000

H        1.688285000      0.902186000      2.610249000

41

[LCuII=O-+OH2] (6) doublet SMD

Cu       0.121504000     -0.006044000     -0.223472000

N       -0.196094000     -2.006789000     -0.256298000

N        2.116010000     -0.305718000     -0.133258000

N       -1.913167000      0.293894000     -0.258760000

N        0.407649000      1.998161000     -0.236134000

C        0.060182000      4.273392000     -0.242500000

H       -0.482794000      5.210301000     -0.262992000

C        0.150273000     -4.282707000     -0.223450000

H        0.692189000     -5.219951000     -0.192132000

C       -2.884684000     -0.673394000     -0.415150000

C        2.136455000     -2.755796000     -0.136074000

C       -0.553556000      2.968914000     -0.270461000

C       -2.649086000     -2.042815000     -0.397642000

C       -1.927274000      2.749220000     -0.345601000

C        1.406346000      4.071691000     -0.187049000

H        2.199570000      4.808488000     -0.152875000

C        2.857945000      2.028528000     -0.128683000

C        3.086626000      0.655361000     -0.110230000

C        4.389202000      0.039740000     -0.066312000

H        5.326871000      0.581224000     -0.040978000

C        4.185490000     -1.307934000     -0.066678000

H        4.921089000     -2.102615000     -0.041672000

C       -3.960518000      1.299227000     -0.570987000

H       -4.690843000      2.090939000     -0.684941000

C       -4.165228000     -0.051506000     -0.592460000

H       -5.096844000     -0.587366000     -0.726689000

C        1.611491000      2.644827000     -0.181571000

C        2.759279000     -1.510930000     -0.111989000

C       -1.399495000     -2.653526000     -0.311261000

C        0.764431000     -2.978881000     -0.199932000

C       -2.553788000      1.508974000     -0.382036000

C       -1.195142000     -4.080514000     -0.294118000

H       -1.988645000     -4.816816000     -0.332185000

H       -2.565253000      3.626084000     -0.407240000

H        3.729205000      2.676457000     -0.098832000

H        2.778827000     -3.631205000     -0.106996000

H       -3.513663000     -2.695097000     -0.479178000

O       -0.346833000      0.125155000      2.941228000

O       -1.737620000      0.077574000      2.489860000

H       -1.724601000      0.173163000      1.482979000

H       -2.047571000     -0.828230000      2.671954000

41

TS1 doublet

Cu       0.094396000      0.004264000     -0.108518000

N       -1.960363000      0.225226000     -0.172393000

N       -0.157965000     -2.007604000     -0.217184000

N        0.299042000      2.011154000     -0.213146000

N        2.095353000     -0.225319000     -0.170072000

C        4.353710000      0.203634000     -0.154290000

H        5.272155000      0.776683000     -0.150516000

C       -4.191620000     -0.201830000     -0.548820000

H       -5.101111000     -0.768330000     -0.703735000

C       -0.694472000      2.943902000     -0.228663000

C       -2.604371000     -2.135005000     -0.348437000

C        3.026383000      0.768792000     -0.166914000

C       -2.059204000      2.675394000     -0.282453000

C        2.744568000      2.130800000     -0.171857000

C        4.200789000     -1.148266000     -0.147082000

H        4.968047000     -1.911923000     -0.136740000

C        2.201870000     -2.667107000     -0.158240000

C        0.838653000     -2.940180000     -0.191311000

C        0.276953000     -4.267655000     -0.227286000

H        0.852498000     -5.184567000     -0.218896000

C       -1.074235000     -4.118459000     -0.282686000

H       -1.835035000     -4.887376000     -0.327951000

C        1.220916000      4.119572000     -0.194279000

H        1.984760000      4.886568000     -0.181019000

C       -0.129830000      4.272051000     -0.219104000

H       -0.703900000      5.189797000     -0.230032000

C        2.780648000     -1.402541000     -0.156789000

C       -1.333116000     -2.699635000     -0.275922000

C       -2.642016000      1.414524000     -0.312715000

C       -2.891426000     -0.775348000     -0.353528000

C        1.475977000      2.699359000     -0.189872000

C       -4.037189000      1.154418000     -0.522122000

H       -4.795657000      1.915969000     -0.651872000

H        3.590694000      2.811392000     -0.160061000

H        2.875068000     -3.519151000     -0.143705000

H       -3.443666000     -2.817709000     -0.442091000

H       -2.728003000      3.528743000     -0.343685000

O        0.045551000      0.003200000      2.296385000

O       -1.503637000      0.045732000      2.553777000

H       -0.905134000     -0.829259000      2.635107000

H       -1.813913000      0.111336000      1.604713000

41

TS1 doublet SMD

Cu       0.222243000      0.002597000     -0.241789000

N       -1.805656000     -0.168864000     -0.417092000

N        0.381194000     -2.021683000     -0.212681000

N        0.038965000      2.024118000     -0.252886000

N        2.220909000      0.170968000     -0.028216000

C        4.340981000      1.036503000      0.201013000

H        5.122608000      1.781474000      0.286711000

C       -3.900162000     -1.035130000     -0.821813000

H       -4.674147000     -1.777528000     -0.973074000

C       -1.115048000      2.746662000     -0.374067000

C       -1.982547000     -2.617087000     -0.492881000

C        2.938580000      1.332188000      0.050924000

C       -2.390341000      2.212372000     -0.540775000

C        2.403329000      2.616396000      0.003375000

C        4.455965000     -0.321461000      0.213528000

H        5.351601000     -0.922701000      0.310934000

C        2.810821000     -2.207529000      0.048539000

C        1.534000000     -2.744936000     -0.080836000

C        1.237403000     -4.155399000     -0.101404000

H        1.976405000     -4.942472000     -0.013876000

C       -0.112112000     -4.269472000     -0.251150000

H       -0.711594000     -5.169528000     -0.311448000

C        0.528005000      4.272101000     -0.179860000

H        1.125591000      5.172612000     -0.108309000

C       -0.821483000      4.157422000     -0.329807000

H       -1.562160000      4.944050000     -0.406394000

C        3.123401000     -0.851284000      0.071325000

C       -0.636183000     -2.928200000     -0.319787000

C       -2.704375000      0.858885000     -0.591858000

C       -2.518864000     -1.336390000     -0.567815000

C        1.055125000      2.931292000     -0.134756000

C       -4.015071000      0.324957000     -0.836951000

H       -4.902381000      0.923336000     -1.003416000

H        3.099899000      3.446042000      0.083063000

H        3.636117000     -2.907545000      0.141755000

H       -2.673608000     -3.448647000     -0.596017000

H       -3.210262000      2.914827000     -0.658984000

O       -3.028768000     -0.040606000      2.895458000

O       -1.540001000     -0.076246000      2.435525000

H       -2.096278000      0.807910000      2.756897000

H       -1.613111000     -0.125431000      1.442662000

41

[LCuII-OH-OH] (7) doublet

Cu       0.079304000      0.019105000     -0.176600000

N       -1.953261000      0.149169000     -0.251855000

N       -0.062605000     -2.004637000     -0.235407000

N        0.204122000      2.032255000     -0.216926000

N        2.093461000     -0.122312000     -0.168868000

C        4.330554000      0.412046000     -0.116296000

H        5.220490000      1.028003000     -0.093072000

C       -4.180637000     -0.383589000     -0.486624000

H       -5.068257000     -0.996108000     -0.580855000

C       -0.830595000      2.921251000     -0.245861000

C       -2.499700000     -2.238004000     -0.358456000

C        2.979617000      0.914575000     -0.141635000

C       -2.179167000      2.589039000     -0.304834000

C        2.640194000      2.262426000     -0.139835000

C        4.241876000     -0.945515000     -0.128423000

H        5.043950000     -1.672526000     -0.117311000

C        2.323374000     -2.558528000     -0.180920000

C        0.974707000     -2.894831000     -0.221933000

C        0.471085000     -4.243830000     -0.267510000

H        1.085811000     -5.134986000     -0.267799000

C       -0.886117000     -4.152734000     -0.316795000

H       -1.612713000     -4.953837000     -0.364749000

C        1.029765000      4.180201000     -0.178077000

H        1.758188000      4.980505000     -0.149830000

C       -0.326236000      4.271999000     -0.223186000

H       -0.940789000      5.163034000     -0.238939000

C        2.836819000     -1.266772000     -0.160803000

C       -1.207548000     -2.748509000     -0.298874000

C       -2.695975000      1.299375000     -0.335093000

C       -2.841106000     -0.890995000     -0.362542000

C        1.348511000      2.773922000     -0.174548000

C       -4.090603000      0.976223000     -0.468791000

H       -4.889507000      1.702658000     -0.545940000

H        3.455807000      2.978693000     -0.111201000

H        3.037625000     -3.376441000     -0.172741000

H       -3.312569000     -2.954691000     -0.426236000

H       -2.890361000      3.408389000     -0.347348000

O       -0.061365000     -0.160077000      2.387649000

O       -1.444025000     -0.057280000      2.736929000

H        0.089775000     -1.113850000      2.463047000

H       -1.839070000      0.078151000      1.855362000

41

[LCuII-OH-OH] (7) doublet SMD

Cu       0.099664000      0.005593000     -0.270577000

N       -1.935246000      0.091696000     -0.345542000

N        0.005508000     -2.024461000     -0.278910000

N        0.178947000      2.034318000     -0.259333000

N        2.117175000     -0.081789000     -0.148115000

C        4.340662000      0.505194000     -0.068019000

H        5.215033000      1.143791000     -0.037481000

C       -4.154498000     -0.495634000     -0.510492000

H       -5.028284000     -1.132460000     -0.574962000

C       -0.880318000      2.897360000     -0.299943000

C       -2.427326000     -2.311871000     -0.402723000

C        2.980190000      0.978217000     -0.118590000

C       -2.221303000      2.528683000     -0.367686000

C        2.610450000      2.320246000     -0.139188000

C        4.282515000     -0.856507000     -0.072347000

H        5.099436000     -1.567330000     -0.045896000

C        2.403943000     -2.517030000     -0.157285000

C        1.064212000     -2.888011000     -0.225752000

C        0.591906000     -4.249614000     -0.251784000

H        1.229726000     -5.124602000     -0.222142000

C       -0.767985000     -4.191279000     -0.320109000

H       -1.478000000     -5.008492000     -0.357228000

C        0.951656000      4.201334000     -0.208318000

H        1.661321000      5.018799000     -0.170325000

C       -0.408474000      4.259210000     -0.270241000

H       -1.047112000      5.133804000     -0.292894000

C        2.886727000     -1.211652000     -0.125900000

C       -1.122820000     -2.794099000     -0.334594000

C       -2.706555000      1.225238000     -0.400768000

C       -2.799948000     -0.971515000     -0.418840000

C        1.307082000      2.804355000     -0.200489000

C       -4.096588000      0.867418000     -0.498398000

H       -4.913326000      1.576903000     -0.551703000

H        3.410402000      3.054342000     -0.104680000

H        3.138065000     -3.317204000     -0.128595000

H       -3.225280000     -3.047204000     -0.452562000

H       -2.953744000      3.330020000     -0.403862000

O       -0.297686000     -0.008625000      3.051670000

O       -1.678536000      0.002829000      2.685660000

H       -0.115285000     -0.955540000      3.154696000

H       -1.639293000      0.040749000      1.707820000

40

[LCuII-O•-OH] (8) triplet

Cu       0.090335000     -0.000002000     -0.148382000

N       -1.960783000     -0.002254000     -0.197099000

N        0.076407000     -2.020247000     -0.209158000

N        0.072087000      2.020135000     -0.209801000

N        2.105220000      0.002106000     -0.159171000

C        4.301324000      0.684695000     -0.117295000

H        5.148304000      1.358669000     -0.100823000

C       -4.137871000     -0.686806000     -0.502912000

H       -4.979650000     -1.357265000     -0.620618000

C       -1.020409000      2.837709000     -0.247517000

C       -2.339563000     -2.422741000     -0.311900000

C        2.919464000      1.095664000     -0.142447000

C       -2.344745000      2.417412000     -0.312496000

C        2.488322000      2.417063000     -0.146458000

C        4.302797000     -0.675715000     -0.117133000

H        5.151232000     -1.347852000     -0.100484000

C        2.493507000     -2.411999000     -0.146022000

C        1.170415000     -2.836256000     -0.177273000

C        0.760233000     -4.218115000     -0.193141000

H        1.434832000     -5.064558000     -0.174861000

C       -0.599045000     -4.220765000     -0.238188000

H       -1.270398000     -5.069604000     -0.263656000

C        0.751166000      4.219469000     -0.193458000

H        1.423919000      5.067377000     -0.175065000

C       -0.608119000      4.219190000     -0.238527000

H       -1.281289000      5.066593000     -0.263884000

C        2.921832000     -1.089678000     -0.142211000

C       -1.014316000     -2.840162000     -0.246992000

C       -2.777474000      1.097550000     -0.332142000

C       -2.775132000     -1.103815000     -0.331764000

C        1.164331000      2.838511000     -0.177742000

C       -4.139328000      0.677583000     -0.503115000

H       -4.982538000      1.346205000     -0.621016000

H        3.252655000      3.188093000     -0.126277000

H        3.259469000     -3.181408000     -0.125766000

H       -3.099410000     -3.195525000     -0.378519000

H       -3.106265000      3.188537000     -0.379230000

O       -0.155959000      0.000942000      2.425665000

O       -1.455941000      0.000379000      2.609828000

H       -1.830218000     -0.000699000      1.688328000

40

[LCuII-O•-OH] (8) triplet SMD

Cu      -0.110236000      0.000046000     -0.249230000

N        1.936153000      0.001638000     -0.294249000

N       -0.099929000      2.030809000     -0.242667000

N       -0.096758000     -2.030770000     -0.242750000

N       -2.126895000     -0.001606000     -0.123868000

C       -4.322317000     -0.684810000     -0.045708000

H       -5.168203000     -1.360742000     -0.016349000

C        4.122385000      0.685954000     -0.513595000

H        4.966691000      1.359439000     -0.595677000

C        0.998966000     -2.846528000     -0.288842000

C        2.319569000      2.425139000     -0.361488000

C       -2.942501000     -1.098179000     -0.097942000

C        2.323358000     -2.421255000     -0.361853000

C       -2.513593000     -2.422532000     -0.122238000

C       -4.323386000      0.678161000     -0.045717000

H       -5.170333000      1.352762000     -0.016372000

C       -2.517396000      2.418718000     -0.122217000

C       -1.194832000      2.847510000     -0.185215000

C       -0.781264000      4.228434000     -0.198978000

H       -1.456072000      5.074993000     -0.163719000

C        0.579894000      4.229028000     -0.263378000

H        1.254424000      5.076095000     -0.290868000

C       -0.774600000     -4.229485000     -0.199467000

H       -1.448060000     -5.077121000     -0.164324000

C        0.586550000     -4.227906000     -0.264023000

H        1.262421000     -5.073894000     -0.291794000

C       -2.944220000      1.093692000     -0.097977000

C        0.994506000      2.848315000     -0.288471000

C        2.754879000     -1.099229000     -0.386919000

C        2.753154000      1.103790000     -0.386753000

C       -1.190355000     -2.849221000     -0.185367000

C        4.123454000     -0.679230000     -0.513703000

H        4.968812000     -1.351380000     -0.595892000

H       -3.280320000     -3.191360000     -0.089798000

H       -3.285336000      3.186334000     -0.089764000

H        3.082750000      3.196215000     -0.414910000

H        3.087739000     -3.191128000     -0.415467000

O        0.440459000     -0.000154000      2.980763000

O        1.695569000     -0.000502000      2.603099000

H        1.692617000      0.001009000      1.605553000

40

[LCuII-O•-OH] (8) singlet

Cu       0.077277000      0.008707000     -0.024171000

N       -2.035529000      0.272891000     -0.291288000

N       -0.132691000     -1.900581000     -0.284781000

N        0.270002000      1.989352000     -0.141548000

N        2.161812000     -0.176272000     -0.190369000

C        4.409204000      0.284023000     -0.323026000

H        5.321869000      0.865652000     -0.355920000

C       -4.262131000     -0.171988000     -0.636380000

H       -5.168887000     -0.747209000     -0.775672000

C       -0.739331000      2.918756000     -0.094744000

C       -2.602936000     -2.068888000     -0.307089000

C        3.073596000      0.826396000     -0.201977000

C       -2.102621000      2.685301000     -0.264043000

C        2.733630000      2.167261000     -0.066060000

C        4.269422000     -1.069310000     -0.382936000

H        5.044585000     -1.819902000     -0.472430000

C        2.241963000     -2.588169000     -0.256315000

C        0.874108000     -2.830573000     -0.197346000

C        0.305628000     -4.148251000     -0.089205000

H        0.881914000     -5.062189000     -0.023065000

C       -1.045774000     -3.999452000     -0.086518000

H       -1.806498000     -4.766945000     -0.022399000

C        1.165074000      4.092886000      0.139742000

H        1.919170000      4.860835000      0.256377000

C       -0.185711000      4.236993000      0.077868000

H       -0.768572000      5.147510000      0.135617000

C        2.850323000     -1.335832000     -0.294361000

C       -1.315710000     -2.590101000     -0.203186000

C       -2.711462000      1.441610000     -0.408094000

C       -2.942051000     -0.721493000     -0.422521000

C        1.441070000      2.686583000     -0.000430000

C       -4.116997000      1.184208000     -0.629600000

H       -4.881330000      1.939497000     -0.763555000

H        3.545934000      2.886737000     -0.013776000

H        2.888272000     -3.461140000     -0.260725000

H       -3.413264000     -2.792530000     -0.319564000

H       -2.742514000      3.563027000     -0.289026000

O       -0.100436000     -0.230193000      2.018904000

O       -1.277392000     -0.782800000      2.419796000

H       -1.920007000     -0.059384000      2.328749000

40

[LCuII-O•-OH] (8) singlet SMD

Cu       0.064731000      0.014986000     -0.090410000

N       -1.981734000      0.380623000     -0.193951000

N       -0.242479000     -1.903638000     -0.367974000

N        0.385401000      1.999450000     -0.229201000

N        2.112577000     -0.292356000     -0.070248000

C        4.377888000      0.048659000     -0.304822000

H        5.313069000      0.589909000     -0.375917000

C       -4.219291000      0.061771000     -0.628820000

H       -5.145812000     -0.470828000     -0.803300000

C       -0.567655000      2.984361000     -0.136067000

C       -2.709411000     -1.931833000     -0.324539000

C        3.084059000      0.661911000     -0.140195000

C       -1.941790000      2.811757000     -0.256737000

C        2.844357000      2.026672000     -0.058727000

C        4.162757000     -1.295369000     -0.371126000

H        4.884243000     -2.091657000     -0.505083000

C        2.085467000     -2.714336000     -0.262347000

C        0.709165000     -2.890426000     -0.246752000

C        0.074073000     -4.173826000     -0.126703000

H        0.608014000     -5.111996000     -0.042943000

C       -1.268625000     -3.952407000     -0.124936000

H       -2.075332000     -4.670129000     -0.044146000

C        1.395796000      4.043756000      0.125037000

H        2.196165000      4.758277000      0.271135000

C        0.053951000      4.264775000      0.064472000

H       -0.485658000      5.199374000      0.152701000

C        2.740504000     -1.487663000     -0.241047000

C       -1.458272000     -2.533651000     -0.255587000

C       -2.593975000      1.589349000     -0.353192000

C       -2.945652000     -0.562740000     -0.384127000

C        1.590105000      2.629288000     -0.042265000

C       -3.998784000      1.407600000     -0.611062000

H       -4.706643000      2.211764000     -0.768653000

H        3.706410000      2.686223000     -0.017387000

H        2.696513000     -3.611844000     -0.285379000

H       -3.570430000     -2.593273000     -0.354643000

H       -2.551446000      3.710238000     -0.282764000

O       -0.041981000     -0.368132000      2.140984000

O       -1.363943000     -0.660305000      2.573237000

H       -1.903273000     -0.027612000      2.071355000

39

[LCuII-O=O] (9) quartet

Cu       0.120940000      0.000130000     -0.244393000

N       -1.310982000     -1.421380000     -0.353304000

N        1.538600000     -1.435451000     -0.142352000

N       -1.297056000      1.435743000     -0.351867000

N        1.552566000      1.421702000     -0.141254000

C        2.633736000      3.452657000     -0.062258000

H        2.761811000      4.527593000     -0.052511000

C       -2.392403000     -3.452465000     -0.426741000

H       -2.520592000     -4.527409000     -0.433831000

C       -2.646965000      1.248891000     -0.448631000

C        0.103914000     -3.416602000     -0.245605000

C        1.365985000      2.775078000     -0.154016000

C       -3.287097000      0.016921000     -0.494168000

C        0.137301000      3.416904000     -0.242590000

C        3.588723000      2.485835000      0.005908000

H        4.662081000      2.603771000      0.083202000

C        3.528679000     -0.016617000      0.001088000

C        2.888525000     -1.248441000     -0.045048000

C        3.564268000     -2.519540000      0.003883000

H        4.636421000     -2.648032000      0.081088000

C        2.599885000     -3.476929000     -0.065113000

H        2.717454000     -4.553073000     -0.056281000

C       -2.358570000      3.477354000     -0.423543000

H       -2.476264000      4.553503000     -0.429675000

C       -3.322901000      2.519997000     -0.494206000

H       -4.395133000      2.648402000     -0.570371000

C        2.900592000      1.221445000     -0.044092000

C        1.338818000     -2.786921000     -0.156325000

C       -2.659003000     -1.221271000     -0.449860000

C       -1.124560000     -2.774880000     -0.336654000

C       -1.097409000      2.787321000     -0.334062000

C       -3.347330000     -2.485668000     -0.496522000

H       -4.420771000     -2.603481000     -0.572780000

H        0.142495000      4.502714000     -0.240319000

H        4.611664000     -0.021940000      0.079350000

H        0.098453000     -4.502413000     -0.244287000

H       -4.370260000      0.022232000     -0.569909000

O       -0.836086000     -0.004972000      2.784002000

O       -2.016619000      0.001429000      3.014309000

39

[LCuII-O=O] (9) quartet SMD

Cu       0.222035000      0.002081000     -0.250429000

N       -1.180310000     -1.450612000     -0.430327000

N        1.661008000     -1.413988000     -0.069142000

N       -1.216771000      1.417086000     -0.433296000

N        1.624004000      1.453463000     -0.070289000

C        2.662731000      3.503305000      0.081340000

H        2.769269000      4.581044000      0.101858000

C       -2.219084000     -3.500576000     -0.580884000

H       -2.325848000     -4.578315000     -0.600086000

C       -2.555473000      1.204615000     -0.614834000

C        0.264641000     -3.421843000     -0.245553000

C        1.413974000      2.804826000     -0.090813000

C       -3.168641000     -0.041481000     -0.701914000

C        0.178422000      3.424922000     -0.249655000

C        3.629292000      2.550988000      0.208912000

H        4.694146000      2.684513000      0.356198000

C        3.612891000      0.044362000      0.199138000

C        2.999538000     -1.201827000      0.115626000

C        3.692005000     -2.461668000      0.216461000

H        4.759592000     -2.568997000      0.365180000

C        2.748874000     -3.437404000      0.090603000

H        2.881432000     -4.512223000      0.114226000

C       -2.306883000      3.440416000     -0.578879000

H       -2.440574000      4.515206000     -0.596095000

C       -3.249356000      2.464344000     -0.707696000

H       -4.317504000      2.571206000     -0.852757000

C        2.967686000      1.274247000      0.113056000

C        1.483632000     -2.770078000     -0.085356000

C       -2.523583000     -1.271405000     -0.615199000

C       -0.970450000     -2.802100000     -0.408098000

C       -1.040622000      2.773415000     -0.409749000

C       -3.185352000     -2.548170000     -0.710473000

H       -4.250109000     -2.681677000     -0.858414000

H        0.164147000      4.511059000     -0.248796000

H        4.688608000      0.058237000      0.348778000

H        0.279011000     -4.507979000     -0.243435000

H       -4.244525000     -0.054978000     -0.850737000

O       -2.045696000     -0.089001000      3.106271000

O       -3.194008000      0.052449000      2.780193000

39

[LCuII-O=O] (9) doublet

Cu       0.125394000      0.000188000     -0.245770000

N       -1.314987000     -1.412519000     -0.358337000

N        1.533947000     -1.443929000     -0.140275000

N       -1.283684000      1.444320000     -0.355418000

N        1.565230000      1.412985000     -0.137603000

C        2.658417000      3.437328000     -0.054234000

H        2.792935000      4.511464000     -0.043236000

C       -2.408471000     -3.437013000     -0.435444000

H       -2.543177000     -4.511155000     -0.443083000

C       -2.634424000      1.265728000     -0.456488000

C        0.087485000     -3.416325000     -0.247340000

C        1.386839000      2.767483000     -0.149703000

C       -3.281912000      0.037734000     -0.504865000

C        0.162282000      3.416760000     -0.240887000

C        3.607387000      2.464717000      0.015528000

H        4.681238000      2.576121000      0.095629000

C        3.532277000     -0.037316000      0.008734000

C        2.884745000     -1.265198000     -0.039424000

C        3.552569000     -2.540402000      0.011132000

H        4.623713000     -2.675451000      0.091100000

C        2.582527000     -3.491870000     -0.060369000

H        2.693477000     -4.568714000     -0.051249000

C       -2.332637000      3.492381000     -0.428740000

H       -2.443793000      4.569227000     -0.434385000

C       -3.302517000      2.540927000     -0.503104000

H       -4.373722000      2.675852000     -0.582385000

C        2.911788000      1.204536000     -0.037249000

C        1.325945000     -2.794165000     -0.154826000

C       -2.661476000     -1.204249000     -0.459012000

C       -1.136823000     -2.767133000     -0.341518000

C       -1.075947000      2.794674000     -0.336107000

C       -3.357307000     -2.464433000     -0.507995000

H       -4.431208000     -2.575750000     -0.587460000

H        0.173993000      4.502515000     -0.237764000

H        4.615007000     -0.049246000      0.089726000

H        0.075442000     -4.502081000     -0.246202000

H       -4.364780000      0.049688000     -0.583974000

O       -0.884542000     -0.008772000      2.809606000

O       -2.070906000      0.003910000      3.007084000

39

[LCuII-O=O] (9) doublet SMD

Cu       0.187977000      0.002879000     -0.256190000

N       -1.072835000     -1.574561000     -0.418069000

N        1.757407000     -1.269637000     -0.084547000

N       -1.378221000      1.276626000     -0.439965000

N        1.452020000      1.579608000     -0.106181000

C        2.296537000      3.719106000      0.002082000

H        2.301416000      4.802302000      0.010393000

C       -1.920742000     -3.713672000     -0.501525000

H       -1.927765000     -4.796863000     -0.494268000

C       -2.693300000      0.938490000     -0.598270000

C        0.549770000     -3.399953000     -0.209675000

C        1.115314000      2.904951000     -0.133755000

C       -3.188791000     -0.360225000     -0.663356000

C       -0.174874000      3.406009000     -0.277762000

C        3.351296000      2.863266000      0.112181000

H        4.402434000      3.097340000      0.229272000

C        3.570593000      0.366410000      0.123414000

C        3.073984000     -0.932106000      0.066635000

C        3.881768000     -2.121124000      0.168208000

H        4.957641000     -2.126872000      0.293836000

C        3.030504000     -3.181449000      0.077289000

H        3.261969000     -4.239063000      0.112822000

C       -2.654950000      3.187941000     -0.574203000

H       -2.888634000      4.245484000     -0.593170000

C       -3.503355000      2.127364000     -0.685901000

H       -4.578640000      2.132590000     -0.816473000

C        2.810762000      1.529329000      0.043183000

C        1.705744000     -2.636331000     -0.079250000

C       -2.430238000     -1.523508000     -0.575678000

C       -0.738972000     -2.899850000     -0.367188000

C       -1.329615000      2.643189000     -0.420443000

C       -2.972694000     -2.857429000     -0.632755000

H       -4.023231000     -3.091045000     -0.756039000

H       -0.290136000      4.486039000     -0.280757000

H        4.643689000      0.482541000      0.245114000

H        0.663562000     -4.479885000     -0.185563000

H       -4.261302000     -0.476135000     -0.790732000

O       -1.651372000     -0.127637000      3.165887000

O       -2.810302000      0.056810000      2.903741000

40

[LCuII-O–-OH]– (10) doublet

Cu       0.073838000     -0.000079000     -0.067936000

N       -1.989313000     -0.010630000     -0.237949000

N        0.074639000     -2.028722000     -0.205081000

N        0.053819000      2.028433000     -0.206311000

N        2.111233000      0.010288000     -0.180639000

C        4.294351000      0.708089000     -0.174964000

H        5.140593000      1.384707000     -0.172080000

C       -4.154729000     -0.710597000     -0.517618000

H       -4.995713000     -1.385122000     -0.625350000

C       -1.047553000      2.836484000     -0.228778000

C       -2.340745000     -2.440781000     -0.298818000

C        2.918935000      1.109075000     -0.176800000

C       -2.365726000      2.415731000     -0.298914000

C        2.468590000      2.438027000     -0.176788000

C        4.301415000     -0.664959000     -0.174136000

H        5.154584000     -1.332814000     -0.170496000

C        2.493483000     -2.413608000     -0.174544000

C        1.176352000     -2.838050000     -0.182270000

C        0.764766000     -4.225974000     -0.180049000

H        1.442412000     -5.071326000     -0.160157000

C       -0.593480000     -4.232704000     -0.206977000

H       -1.263210000     -5.084515000     -0.213928000

C        0.721419000      4.232654000     -0.182488000

H        1.390367000      5.084922000     -0.163321000

C       -0.636841000      4.225453000     -0.208486000

H       -1.315301000      5.070329000     -0.215253000

C        2.930187000     -1.080083000     -0.175703000

C       -1.018405000     -2.848038000     -0.227964000

C       -2.807036000      1.084310000     -0.350516000

C       -2.795647000     -1.113955000     -0.350502000

C        1.147204000      2.849025000     -0.184380000

C       -4.161878000      0.666905000     -0.517609000

H       -5.009815000      1.332669000     -0.625325000

H        3.228765000      3.214736000     -0.164982000

H        3.261555000     -3.182490000     -0.161933000

H       -3.096349000     -3.220656000     -0.343728000

H       -3.129288000      3.187830000     -0.343526000

O       -0.015780000      0.002851000      2.225844000

O       -1.314030000      0.000888000      2.676843000

H       -1.832026000     -0.003497000      1.848435000

40

[LCuII-O–-OH]– (10) doublet SMD

Cu      -0.092864000     -0.000313000     -0.229609000

N        1.929820000     -0.014667000     -0.375030000

N       -0.080318000      2.031523000     -0.263309000

N       -0.108795000     -2.032585000     -0.261394000

N       -2.120821000      0.013760000     -0.132403000

C       -4.322520000     -0.652171000     -0.056405000

H       -5.173695000     -1.321531000     -0.028070000

C        4.129489000      0.651751000     -0.503361000

H        4.980294000      1.320403000     -0.551495000

C        0.978988000     -2.857690000     -0.319826000

C        2.338715000      2.404604000     -0.396668000

C       -2.945576000     -1.076027000     -0.106216000

C        2.304884000     -2.439459000     -0.393877000

C       -2.528352000     -2.403980000     -0.131396000

C       -4.312943000      0.710706000     -0.057402000

H       -5.154633000      1.392026000     -0.030210000

C       -2.494436000      2.437013000     -0.135280000

C       -1.168981000      2.856150000     -0.205201000

C       -0.746255000      4.234225000     -0.231186000

H       -1.414897000      5.085762000     -0.197228000

C        0.614639000      4.225035000     -0.303855000

H        1.294662000      5.067358000     -0.341601000

C       -0.805501000     -4.225641000     -0.225153000

H       -1.486001000     -5.067672000     -0.189349000

C        0.555390000     -4.235602000     -0.298276000

H        1.223513000     -5.087435000     -0.334801000

C       -2.930196000      1.115070000     -0.108341000

C        1.018852000      2.841294000     -0.322887000

C        2.740909000     -1.118226000     -0.422057000

C        2.756161000      1.077440000     -0.423649000

C       -1.208901000     -2.841730000     -0.201414000

C        4.120031000     -0.711845000     -0.502413000

H        4.961449000     -1.392368000     -0.549486000

H       -3.301619000     -3.166185000     -0.097021000

H       -3.256965000      3.210039000     -0.102649000

H        3.111477000      3.166893000     -0.438030000

H        3.066953000     -3.212515000     -0.433772000

O        0.284532000      0.013430000      3.089245000

O        1.735367000     -0.001151000      2.833467000

H        1.777726000     -0.015646000      1.864795000

39

[LCuII-O•–O–]– (11) triplet

Cu      -0.027591000     -0.000591000     -0.239648000

N       -2.058116000      0.018163000     -0.175526000

N       -0.049160000     -2.040622000     -0.259056000

N       -0.011294000      2.039381000     -0.261183000

N        1.998493000     -0.019443000     -0.362640000

C        4.207450000      0.639195000     -0.311167000

H        5.062056000      1.305151000     -0.286864000

C       -4.265927000     -0.640604000     -0.228763000

H       -5.120856000     -1.306321000     -0.248927000

C       -1.098767000      2.868628000     -0.242478000

C       -2.482860000     -2.395168000     -0.217157000

C        2.826261000      1.072118000     -0.332490000

C       -2.437999000      2.438950000     -0.219692000

C        2.422701000      2.392914000     -0.310427000

C        4.194826000     -0.719015000     -0.310439000

H        5.036902000     -1.400728000     -0.285482000

C        2.377881000     -2.439223000     -0.307839000

C        1.040580000     -2.869496000     -0.275073000

C        0.621312000     -4.233105000     -0.263313000

H        1.285713000     -5.088881000     -0.277787000

C       -0.756383000     -4.220396000     -0.246443000

H       -1.435996000     -5.064109000     -0.226907000

C        0.699629000      4.219058000     -0.268106000

H        1.379796000      5.062337000     -0.283602000

C       -0.678059000      4.231893000     -0.251231000

H       -1.341905000      5.088092000     -0.232747000

C        2.805872000     -1.126214000     -0.331314000

C       -1.151764000     -2.849529000     -0.239400000

C       -2.864801000      1.125776000     -0.205356000

C       -2.885220000     -1.074236000     -0.204212000

C        1.093557000      2.847858000     -0.278223000

C       -4.253291000      0.717880000     -0.229452000

H       -5.095683000      1.399378000     -0.250239000

H        3.201772000      3.150662000     -0.300315000

H        3.142786000     -3.211267000     -0.296863000

H       -3.261809000     -3.152975000     -0.223000000

H       -3.202781000      3.211055000     -0.226341000

O        0.817913000      0.003878000      2.683917000

O       -0.130326000      0.010957000      3.457729000

39

[LCuII-O•–O–]– (11) triplet SMD

Cu      -0.061397000      0.001311000     -0.280120000

N        1.390702000      1.413256000     -0.358809000

N       -1.477104000      1.453410000     -0.230996000

N        1.352595000     -1.453158000     -0.352733000

N       -1.514593000     -1.413315000     -0.221245000

C       -2.613973000     -3.435648000     -0.173996000

H       -2.749313000     -4.510349000     -0.167653000

C        2.489997000      3.435654000     -0.402381000

H        2.625414000      4.510356000     -0.404833000

C        2.706819000     -1.276790000     -0.416060000

C       -0.015273000      3.421019000     -0.290191000

C       -1.337126000     -2.769122000     -0.228772000

C        3.358313000     -0.047171000     -0.445498000

C       -0.108534000     -3.421027000     -0.283726000

C       -3.563783000     -2.459060000     -0.133436000

H       -4.640815000     -2.565114000     -0.087136000

C       -3.482613000      0.047199000     -0.137882000

C       -2.831369000      1.276950000     -0.166912000

C       -3.495712000      2.555635000     -0.132628000

H       -4.569103000      2.692098000     -0.081792000

C       -2.519104000      3.505393000     -0.175574000

H       -2.623814000      4.583507000     -0.167178000

C        2.395016000     -3.505200000     -0.400945000

H        2.499869000     -4.583328000     -0.404245000

C        3.371443000     -2.555496000     -0.447131000

H        4.444925000     -2.691857000     -0.496211000

C       -2.864055000     -1.199378000     -0.163620000

C       -1.261565000      2.803672000     -0.235387000

C        2.740017000      1.199440000     -0.417877000

C        1.213165000      2.769027000     -0.347396000

C        1.137419000     -2.803319000     -0.341882000

C        3.439664000      2.459180000     -0.447515000

H        4.516679000      2.565163000     -0.494115000

H       -0.123597000     -4.507188000     -0.281771000

H       -4.567653000      0.061563000     -0.088940000

H        0.000351000      4.507171000     -0.286485000

H        4.443400000     -0.061724000     -0.492893000

O        0.118262000     -0.033525000      3.151891000

O        1.345551000      0.027849000      3.655119000

39

[LCuII-O•–O–]– (11) singlet

Cu       0.000479000     -0.099227000      0.467733000

N        0.006516000     -2.034367000     -0.204907000

N        2.089720000      0.004557000     -0.169231000

N       -2.089818000     -0.008130000     -0.168293000

N       -0.006397000      2.033748000     -0.298759000

C       -0.694320000      4.228542000     -0.425945000

H       -1.367961000      5.076334000     -0.481535000

C        0.695276000     -4.207865000     -0.447322000

H        1.367855000     -5.051210000     -0.553368000

C       -2.889929000     -1.097230000     -0.240718000

C        2.439736000     -2.401646000     -0.277392000

C       -1.098626000      2.836457000     -0.337809000

C       -2.424475000     -2.416491000     -0.278323000

C       -2.430397000      2.404079000     -0.307645000

C        0.667984000      4.232711000     -0.426528000

H        1.336382000      5.084603000     -0.482722000

C        2.415262000      2.418899000     -0.308919000

C        2.880378000      1.100676000     -0.254247000

C        4.272899000      0.700817000     -0.351636000

H        5.117429000      1.375603000     -0.435166000

C        4.283349000     -0.662950000     -0.345108000

H        5.137720000     -1.326250000     -0.419276000

C       -4.277238000      0.674334000     -0.351810000

H       -5.126010000      1.343764000     -0.435440000

C       -4.278990000     -0.689490000     -0.346224000

H       -5.129087000     -1.358139000     -0.421476000

C        1.080852000      2.843132000     -0.338561000

C        2.896840000     -1.079473000     -0.240314000

C       -1.089234000     -2.836409000     -0.295698000

C        1.107108000     -2.829778000     -0.295135000

C       -2.887372000      1.082971000     -0.253312000

C       -0.668982000     -4.211992000     -0.447636000

H       -1.336391000     -5.059388000     -0.554052000

H       -3.191415000      3.180067000     -0.361719000

H        3.171508000      3.199512000     -0.363345000

H        3.195585000     -3.180792000     -0.347681000

H       -3.175427000     -3.200277000     -0.349512000

O       -0.003322000      0.773179000      2.162857000

O        0.001454000     -0.487262000      2.456022000