A Label-free Optical Sensing Platform for beta-glucosidase Activity Using Protein-inorganic Hybrid Nanoflowers

Ziping Liua,b, Shasha Liua, Decai Gaoa,*, Yanan Lic, Ye Tiand and Edith Baia,*

a Key Laboratory of Geographical Processes and Ecological Security of Changbai Mountains, Ministry of Education, School of Geographical Sciences, Northeast Normal University, Changchun 130024, China

b School of Geographical Sciences, Northeast Normal University, People’s Street 5268, Changchun 130024, Jilin, China

c Key Laboratory for Vegetation Ecology, Ministry of Education, Institute of Grassland Science, Northeast Normal University,Changchun, Jilin Province 130024, China

d Jilin Province Product Quality Supervision Testing Institute, Changchun 130012, People’s Republic of China

*Corresponding author

Tel.: +86-431-85099550

E-mail address: gaodc493@nenu.edu.cn; baie612@nenu.edu.cn

Fig. S1 Effect of temperature on the catalytic activities of nanoflowers (red curve) and free HRP (black curve)

Fig. S2 Effect of storage time on the catalytic activities of nanoflowers (red curve) and free HRP (black curve) at room temperature for a month

Table S1 A comparison of analytical parameters of the proposed sensor with other methods

| Receptor | Method | Linear range | Detection limit | Media | References |
| --- | --- | --- | --- | --- | --- |
| Flavonol a CuInS2 QDs RDE-PAP b MCH-GCNCs c Au-Cellobiose-NCs d Glc-Lip-AuNPs SPCE-MWCNT e FMGlc f BSA-Cu3(PO4)2·3H2O Hybrid NFs h | Fluorimetry Fluorimetry Electrochemistry Colorimetry Colorimetry Colorimetry Electrochemistry CE-LIF g Colorimetry and Fluorimetry | Not Given 0.5-700.0 U·L-1 Not Given 3.0-100.0 U·L-1 3.0-100.0 U·L-1 0.01-2.5 μM 2.7-11.3 mmol·L-1 6.4×10−6-0.01 mg·mL-1 0.5-1500.0 U·L-1 | Not Given 0.2 U·L-1 Not Given 1.0 U·L-1 1.0 U·L-1 22.3 nmol·L-1 Not Given 1.3×10−7 mg·mL-1 0.35 U·L-1 | PBS buffer Soil Not Given Compost Extracts Compost Extracts PBS buffer Soil Soil Soil and Serum | [S1] [S2] [S3] [S4] [S5] [S6] [S7] [S8] This work |

a 4’-Fluoroflavonol β-D-glucopyranoside; b Rotating disk electrode in a microliter droplet-substrate conjugated p-nitro-phenol; c 6-Mercapto-1-hexanol-Gold-cellobiose nanocomposites; d Gold-cellobiose nanocomposites; e Screen-printed carbon electrodes modified with multiwalled carbon nanotubes; f Fluorescein mono-β-D-glucopyranoside; g  Capillary electrophoresis-laser induced fluorescence; h nanoflowers

Table S2 Results of β-Glu determination in real samples

| Samples | Found (U·L-1) | Added (U·L-1) | Total Found (U·L-1) | Recovery (%) | RSD (%, n=3) |
| --- | --- | --- | --- | --- | --- |
| Serum Water Soil | 0 0 0 0 0 0 84.5 83.9 84.9 | 50.0 100.0 500.0 50.0 100.0 500.0 50.0 100.0 500.0 | 48.2 97.1 518.9 49.0 101.6 517.4 131.7 187.2 581.7 | 96.4 97.1 103. 8 98.0 101.6 103.5 96.7 103.9 96.2 | 4.3 2.5 3.8 1.1 3.4 2.3 4.2 3.5 4.2 |

References

1. Serdiuk IE, Reszka M, Myszka H, Krzyminski K, Liberek B, Roshal AD (2016) Flavonol-based fluorescent indicator for determination of β-glucosidase activity. RSC Adv 6: 42532-42536.

2. Liu ZP, Tian Y, Han Y, Bai E, Li YN, Xu ZW, Liu SS (2019) A “turn off-on” fluorescent nanoprobe consisting of CuInS2 quantum dots for determination of the activity of β-glucosidase and for inhibitor screening. Microchim Acta 186: 806.

3. Sazawa K, Kuramitz H (2015) Hydrodynamic voltammetry as a rapid and simple method for evaluating soil enzyme activities. Sensors 15: 5331-5343.

4. Lai C, Zeng GM, Huang DL, Zhao MH, Wei Z, Huang C, Xu P, Li NJ, Zhang C, Chen M, Li X, Lai MY, He YB (2014) Synthesis of gold-cellobiose nanocomposites for colorimetric measurement of cellobiase activity. Spectrochimica Acta Part A: Molecular and Biomolecular Spectroscopy 132: 369-374.

5. Lai C, Zeng GM, Huang DL, Zhao MH, Chen M, Wei Z, Huang C, Xu P, Li NJ, Li X, Zhang C (2014) Colorimetric screening of β-glucosidase inhibition based on gold nanocomposites. Anal Methods 6: 312-315.

6. Zeng ZH, Mizukami S, Kikuchi K (2012) Simple and real-time colorimetric assay for glycosidases activity using functionalized gold nanoparticles and its application for inhibitor screening. Anal Chem 84: 9089-9095.

7. Stege PW, Messina GA, Bianchi G, Olsina RA, Raba J (2010) Determination of β-glucosidase activity in soils with a bioanalytical sensor modified with multiwalled carbon nanotubes. Anal Bioanal Chem 397: 1347-1353.

8. Stege PW, Messina GA, Bianchi G, Olsina RA (2010) Determination of the β-Glucosidase activity in different soils by pre capillary enzyme assay using capillary electrophoresis with laser-induced fluorescence detection. J Fluoresc 20: 517-523.