SUPPORTING INFORMATION

Phase-Transition-Driven Reconfigurable Thermoelectric Logic in Correlated Electron Systems

Xin Sun1,2, Kening Xiao3, Yingdong Wei1,4, Libo Zhang3*, Li Han1, Kaixuan Zhang3, Yage Yang1, Fang Wang1*, Xiaoshuang Chen1,2,3,4,Lin Wang1*, Weida Hu1,2*

1 State Key Laboratory for Infrared Physics, Shanghai Institute of Technical Physics, Chinese Academy of Sciences, 500 Yu-tian Road, Shanghai 200083, China.

2 School of Microelectronics Shanghai University, 20 Chengzhong Road, Shanghai 201899, China.

3College of Physics and Optoelectronic Engineering, Hangzhou Institute for Advanced Study, University of Chinese Academy of Sciences, No. 1, Sub-Lane Xiangshan, Xihu District, Hangzhou 310024, China.

4School of Physical Science and Technology, ShanghaiTech University, Shanghai 201210, China.

These authors contributed equally: Xin Sun, Kening Xiao, Yingdong Wei

Figure S1. Material Structure and Characterization Diagrams. (A) Raman spectroscopy on 1T-TaS2. (B) Elemental spectrum of 1T-TaS2. (C) Electron image of surface morphology. (D) TEM image of 1T-TaS2

Figure S2. THz Detection Performance of 1T-TaS2 Device. (A) The test process diagram of the PD. (B) FDTD modeling of the butterfly antenna structure, simulating the electric field distribution at 0.3 THz. (C) The effect of different power illumination on the phase transition at room temperature. (D) Photocurrent response of the device under different bias voltages with illumination conditions at 0.04 , 0.12 , and 0.30 THz. (E) Comparison of photoresponse before and after the abrupt change at 0.3 THz.

Figure S3. Noise testing and performance comparison. (A) Noise spectrum measured under different bias voltages. (B) Current responsivity and equivalent noise power of the TaS2 device under different bias voltages. (C) Comparison of responsivity with the reported typical 2D material THz PDs. (D) Comparison of NEP with the reported typical 2D material THz PDs.

Figure S4. THz imaging at room temperature. Schematic of the scanning imaging optical path, along with the optical image and transmission image of the pin under 0.12 THz.

Figure S5. The optical heterodyne detection experiments under 21 and 24 GHz microwave irradiation. (A) The corresponding spectrum of the mixing process is shown in the frequency spectrum diagram. (B) By changing the power of the RF signal, the corresponding amplitude of the IF signal is obtained. (C) By changing the power of the LO signal, the corresponding amplitude of the IF signal is obtained. (D) By changing the RF signal, the corresponding amplitude of the IF signal is obtained. (E) The spectrum diagram obtained by changing the power of the RF signal. (F) The spectrum diagram obtained by changing the power of the LO signal.