Table. 1. The Optimization of the model reaction conditions.

| Entry | Catalyst (mol%) | Temperature (oC) | Solvent | Time (h) | Yield (%( |
| --- | --- | --- | --- | --- | --- |
| 1 | 0 | 110 | DMF | 10 | Trace |
| 2 | 3 | 80 | DMF | 18 | 10 |
| 3 | 3 | 100 | DMF | 18 | 21 |
| 4 | 5 | 100 | DMF | 15 | 48 |
| 5 | 8 | 120 | DMSO | 16 | 70 |
| 6 | 8 | 100 | H2O | 12 | 68 |
| 7 | 8 | 80 | H2O | 15 | 55 |
| 8 | 10 | 120 | DMSO | 10 | 83 |
| 9 | 10 | 100 | Toluene | 12 | 80 |
| 10 | 10 | 100 | DMF | 12 | 94 |
| 11 | 10 | 100 | H2O | 12 | 96 |

| Table. 2. C-N reaction cross-coupling derivatives of Arylhalides and ArylAmines using Fe3O4@Agar-Cu NPs |  |  |  |  |
| --- | --- | --- | --- | --- |
| Entry | Arylhalides | ArylAmines | Product | Yield (%) |
| 1a |  |  |  | 94 |
| 2a |  |  |  | 88 |
| 3a |  |  |  | 90 |
| 4a |  |  |  | 93 |
| 5a |  |  |  | 90 |
| 6b |  |  |  | 96 |
| 7b |  |  |  | 90 |
| 8b |  |  |  | 85 |
| 9b |  |  |  | 83 |
| 10b |  |  |  | 80 |
| 11b |  |  |  | 82 |
| 12b |  |  |  | 80 |
| 13b |  |  |  | 89 |
| 14b |  |  |  | 91 |
| 15b |  |  |  | 90 |
| 16b |  |  |  | 88 |

a Reaction conditions for secondary amines: H2O (4 ml), K2CO3 (2 mmol), catalyst (10 mol%), temperature (100 ºC), reaction time (12 h).

b Reaction conditions for primary conditions: H2O (0.5 ml), K2CO3 (1 mmol), catalyst (10 mol%), temperature (100 ºC), reaction time (12 h).

Table. 3. Comparison of catalytic activity of the Fe3O4@Agar-Cu NPs C-N cross-coupling of amines with aryl halides.

| Entry | Condition | Time(h) | Yield(%) | Ref. |
| --- | --- | --- | --- | --- |
| 1 | Fe3O4@PDA/Pd(II) -Cs2CO3-DMF at 100 °C | 10 | 80 | [24] |
| 2 | Pd(IPr*me)(acac)Cl- LiHMDS,1,4-dioxane 110℃ | 3 | 75-90 | [47] |
| 3 | Toluene, ,NaOtBu, Pd/ligand 1:2, phosphonium salt: EtFluPCy2·HBF4, 120 °C | 12 | 48-95 | [48] |
| 4 | Pd2(dba)3,XhantPhos, DBU, DMF, 100 °C | 18 | 70 | [49] |
| 5 | Fe3O4@Agar-Cu NPs-K2CO3,H2O,100 °C | 12 | 80-96 | current work |