Supplementary Information

Unlocking Ultra-stable Li5FeO4 in Air: Key Advances and Practical Demonstrations

Canshang Liu1,2, Hao Zhang1,2, Weiwei Zhou2,3*, Xu Tian2,3, Tiantian Zhang1,2, Sicheng Niu2,3, Minglei Cao4,5, Qin Wang4, Fei Lv4, Tangping Peng4, Lijuan Tao4, Xiaodong Rang4, Zhicheng Chen4, Xin Su1,2*

1School of Marine Science and Technology, Harbin Institute of Technology, Weihai 264209, P. R. China.

2Advanced Battery Technology Center, Harbin Institute of Technology, Weihai 264209, P. R. China.

3School of Materials Science and Engineering, Harbin Institute of Technology, Weihai 264209, P. R. China.

4Hubei WanRun New Energy Technology Co., Ltd, Shiyan 442000, P. R. China.

5Hubei Key Laboratory of Energy Storage and Power Battery, School of Mathematics, Physics and Optoelectronic Engineering, Hubei University of Automotive Technology, Shiyan 442002, P. R. China.

*Corresponding authors: sux@hit.edu.cn; zhouweiwei@hit.edu.cn.

Supplementary Figure 1│ XRD refinement pattern of LFO

Supplementary Figure 2│SEM images of LFO@C (a) and LFO (b). Scale bars, 500 nm.

Supplementary Figure 3│TEM images of LFO@C. a, b TEM images of localized of LFO@C. c, d High-Resolution TEM images of LFO@C.

Supplementary Figure 4│XPS spectra of C 1s for LFO@C (top) and LFO (bottom).

Supplementary Figure 5│Optical images of LFO and LFO@C exposed to air. Images of LFO (a) and LFO@C (b) exposed to air (25 °C, 20% RH) for 0-8 mins.

Supplementary Figure 6│Raman spectrum of LFO after 6 mins in air exposure (25 °C, 20% RH).

Supplementary Figure 7│XRD patterns of LFO after being placed in air. The XRD patterns of LFO after exposure to air (25 °C, 20% RH) for 6 h (a), 8 h (b), and 12 h (c).

Supplementary Figure 8│Initial charge curves of half-cells with LFO and LFO@C cathodes assembled in air (25 °C, 20% RH).

Supplementary Figure 9│Initial charge curves of LFO. Initial charge curves of LFO after being placed in air (25 °C, 20% RH) for 0 h (a), 1 h (b), 4 h (c).

Supplementary Figure 10│Optical images of LFO@C and LFO before and after exposure to air (25 °C, 20% RH). a. LFO@C before and after 72 h of placement. b. LFO before and after 8 h of placement.

Supplementary Figure 11│Initial charge curves of LFO@C after exposure to air (25 °C, 20% RH). Initial charge curves of LFO@C after 8 h (a), 16 h (b), 24 h (c), 32 h (d), 40 h (e), 48 h (f), 56 h (g), 64 h (h), and 72 h (i) of air exposure.

Supplementary Figure 12│The capacity retention curves of LFO@C after exposure to air for 8 h (25°C, 20%, 30%, and 60% RH), 16 h (25°C, 20%, and 30% RH), and 24 h (25°C, 20%, and 30% RH).

Supplementary Figure 13│Initial charge curves of LFO@C after exposure to air (25 °C, 30% RH). Initial charge curves of LFO@C after 8 h (a), 16 h (b), 24 h (c) of air exposure.

Supplementary Figure 14│Initial charge curve of LFO@C after exposure to air (25 °C, 60% RH) after 8 h.

Supplementary Figure 15│The rate performance of LFO@C and LFO. Initial charge curves of LFO@C (a) and LFO (b) at different rates (0.05C, 0.1C, 0.2C, 0.5C, 1C).

Supplementary Figure 16│XPS survey spectrum of the Li foil. a. XPS spectra of Fe 2p for Li foil in LFO@C||Li (top) and LFO||Li (bottom) half-cells. XPS survey spectrum of the Li foil in half-cells with LFO@C (b) and LFO (c).

Supplementary Figure 17│Half-cell tests for NCM+LFO@C. a. GCD curves of NCM+LFO@C and NCM. b. dQ/dV curves of NCM+LFO@C and NCM. c. Magnified view of dQ/dV curves between 4.12 V and 4.22 V.

Supplementary Figure 18│Rate and cycle performance of half cells with NCM+LFO@C and NCM cathodes.

Supplementary Figure 19│In situ XRD patterns for NCM+LFO@C and NCM. Selected (101) counter plot of in situ XRD patterns for NCM+LFO@C (a) and NCM (b).

Supplementary Figure 20│GCD curve of Gr+SiOx.

Supplementary Figure 21│dQ/dV curves for NCM||Gr+SiOx and NCM+LFO@C||Gr+SiOx full cells.

Supplementary Figure 22│Cycling performances of coin-type full cells with NCM+LFO@C and NCM cathodes under 2.8–4.25 V

Supplementary Figure 23│EIS plots of NCM||Gr+SiOx and NCM+LFO@C||Gr+SiOx full cells at 3.8 V.

Supplementary Figure 24│Optical images of the prepared NCM+LFO@C and NCM+LFO electrodes. Electrode slurry of NCM+LFO@C (a) and NCM+LFO (b). Electrode sheets of NCM+LFO@C (c) and NCM+LFO (d).

Supplementary Figure 25│Energy retention for NCM||Gr+SiOx and NCM+LFO@C||Gr+SiOx pouch cells.

Supplementary Figure 26│Optical images of the front (top) and side (bottom) views of the NCM+LFO@C||Gr+SiOx pouch cell before and after 100 cycles. a. Before cycling. b. After cycling.

Supplementary Figure 27│Optical images of the disassembled NCM+LFO@C||Gr+SiOx pouch cell.

Supplementary Figure 28│SEM images of the cathode sheet of the NCM||Gr+SiOx pouch cell after 100 cycles.

Supplementary Figure 29│SEM images of the cathode sheet of the NCM+LFO@C||Gr+SiOx pouch cell after 100 cycles.

Supplementary Figure 30│XPS spectra of F 1s for Gr+SiOx anode in NCM+LFO@C||Gr+SiOx (top) and NCM||Gr+SiOx (bottom) pouch cells after 100 cycles under 0.5C discharge rate.

Supplementary Table 1│Carbon and sulfur content for LFO@C.

|  | C element content | S element content |
| --- | --- | --- |
| LFO@C | 2.68% | 0.13% |

Supplementary Table 2│The lithium-ion diffusion coefficients of LFO and LFO@C were determined using GITT technology.

|  | Voltage (V) | t (s) | r (cm) | ΔEs (v) | ΔEt (v) | D (cm2/s) |
| --- | --- | --- | --- | --- | --- | --- |
| LFO | 3.70 - 3.75 | 600 | 5.0 × 10-4 | 0.0129 | 0.3569 | 6.93×10-13 |
| LFO@C | 3.70 - 3.75 | 600 | 5.3 × 10-4 | 0.1050 | 0.3244 | 6.24×10-11 |
| LFO | 4.05 - 4.10 | 600 | 5.0 × 10-4 | 0.0067 | 0.1435 | 1.16×10-12 |
| LFO@C | 4.05 - 4.10 | 600 | 5.3 × 10-4 | 0.0113 | 0.1056 | 6.83×10-12 |

Determination of Li ion diffusion coefficient: The lithium diffusion coefficients for LFO and LFO@C were determined via the GITT technique as shown in the following equation. Since the pulse time, τ, is short and the pulse current is small, the Li+ ion diffusion coefficient, D, can be described by Equation:

(1)

where r is the particle size of the cathode materials, ΔEs is the change of the steady-state voltage of cell for this step, and ΔEt is the total transient voltage change of the cell for applied current for time τ.

Supplementary Table 3│The Fe content in the pure Li foil and Li foil used in the LFO/LFO@C||Li half-cell determined by ICP-OES.

|  | Li | Li¦¦LFO | Li¦¦LFO@C |
| --- | --- | --- | --- |
| Fe Elemental content (ppm) | 78.15 | 115.24 | 76.74 |

Supplementary Table 4│Full-cell specifications. (CC: constant current. CV: constant voltage.)

| Full-cell specifications |  |  |
| --- | --- | --- |
|  | Cathode | Anode |
| Sample | NCM/NCM+LFO@C | Graphite+SiOx |
| Cell dimension | 57 mm × 75 mm | 60 mm × 78 mm |
| Composition | NCM811: SP: PVDF = 93: 3.5 :3.5/Active material (AM): LFO@C: SP: PVDF = 90.8: 2.2: 3.5: 3.5/ | Graphite: SiOx: SP: CMC: SBR = 83.2: 10.4: 2.4: 1.8: 2.2 (CMC: carboxymethyl cellulose, SBR: styrene butadiene rubber) |
| One-side Loading level (mg cm-2) | 13.0 ± 0.1 | 7.1 ± 0.1 |
| Two-side Loading level (mg cm-2) | 26.0 ± 0.2 | 14.2 ± 0.2 |
| Electrode density (g cm-3) | 3.0 ± 0.02 | 1.5 ± 0.02 |
| Negative/positive (N/P) ratio | 1.06 ± 0.01 |  |
| Amount of electrolyte | 4.5 g Ah-1 |  |
| Cycling test condition | Voltage range: 2.8 - 4.25 V Charge: 0.5 C (CC) – 0.05C (CV) / Discharge: 0.5C (CC) |  |

Supplementary Table 5│DC impedances of NCM+LFO@C||Gr+SiOx and NCM||Gr+SiOx pouch cells.

|  | NCM¦¦Gr+SiOx | NCM-LFO@C¦¦Gr+SiOx |
| --- | --- | --- |
| DC internal resistance (mΩ) | 25.89 | 18.42 |

Supplementary Table 6│The Fe content in the Gr+SiOx anode of NCM+LFO@C||Gr+SiOx and NCM||Gr+SiOx pouch cells determined by ICP-OES.

|  | NCM | NCM-LFO@C |
| --- | --- | --- |
| Gr+SiOx-Fe Elemental content (ppm) | 32.64 | 32.47 |